Supplementary material for

Effects of CsSnxPb1-xI3 quantum dots as interfacial layer on photovoltaic performance of carbon-based perovskite solar cells

Chi Zhang, Zhiyuan He, Xuanhui Luo, Rangwei Meng, Mengwei Chen, Haifei Lu and  Yingping Yang*

*correspondence: ypyang@whut.edu.cn

Department of Physics, School of Science, Wuhan University of Technology, Wuhan 430070, P. R. China

Fig. S1 EDS mappings of different tin-doped PQDs under HAADF STEM patterns. a CsSn0.1Pb0.9I3 QDs, b CsSn0.2Pb0.8I3 QDs, c CsSn0.3Pb0.7I3 QDs.

Table S1 EDS chemical composition analysis for CsSn0.1Pb0.9I3 QDs.

| Element | Atomic fraction (%) | Atomic error (%) | Mass fraction (%) | Mass error (%) | Fit error (%) |
| --- | --- | --- | --- | --- | --- |
| Cs | 14.08 | 2.31 | 12.89 | 1.68 | 2.15 |
| Sn | 3.31 | 0.50 | 2.71 | 0.30 | 7.37 |
| Pb | 22.09 | 3.68 | 31.52 | 4.21 | 1.38 |
| I | 60.52 | 9.85 | 52.89 | 6.80 | 0.81 |

Table S2 EDS chemical composition analysis for CsSn0.2Pb0.8I3 QDs

| Element | Atomic fraction (%) | Atomic error (%) | Mass fraction (%) | Mass error (%) | Fit error (%) |
| --- | --- | --- | --- | --- | --- |
| Cs | 17.44 | 2.79 | 16.16 | 2.08 | 1.95 |
| Sn | 5.65 | 0.77 | 4.68 | 0.46 | 5.24 |
| Pb | 19.89 | 3.25 | 28.73 | 3.81 | 1.88 |
| I | 57.02 | 9.05 | 50.44 | 6.40 | 0.62 |

Table S3 EDS chemical composition analysis for CsSn0.3Pb0.7I3 QDs.

| Element | Atomic fraction (%) | Atomic error (%) | Mass fraction (%) | Mass error (%) | Fit error (%) |
| --- | --- | --- | --- | --- | --- |
| Cs | 17.37 | 2.79 | 16.47 | 2.12 | 2.09 |
| Sn | 7.72 | 1.02 | 6.54 | 0.59 | 3.65 |
| Pb | 15.98 | 2.63 | 23.62 | 3.15 | 2.28 |
| I | 58.94 | 9.40 | 53.37 | 6.79 | 0.86 |

Fig. S2 UPS data and Tauc plots for a CsSn0.1Pb0.9I3 QDs, b CsSn0.2Pb0.8I3 QDs, c CsSn0.3Pb0.7I3 QDs and d MAPbI3. The valence band (VB) edges were calculated by EVB = − (21.21 eV − ECut-off + ELow-binding). Then, the conduction band (CB) edges were calculated by ECB = EVB + Eg.

Table S4 Photovoltaic parameters of different PSCs

| Device | Voc (V) | Jsc (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| Control | 0.98 | 22.58 ± 0.11 | 55.44 ± 1.14 | 12.29 ± 0.09 |
| With CsSn0.1Pb0.9I3 QDs | 1.01 | 23.28 ± 0.13 | 54.96 ± 3.63 | 12.91 ± 0.13 |
| With CsSn0.2Pb0.8I3 QDs | 1.04 | 23.46 ± 0.15 | 55.86 ± 1.48 | 13.58 ± 0.16 |
| With CsSn0.3Pb0.7I3 QDs | 0.96 | 14.80 ± 3.22 | 45.63 ± 11.53 | 6.48 ± 0.82 |

Table S5 Photovoltaic parameters of CsSn0.2Pb0.8I3 QDs-added PSCs under different concentrations of the PQD solution.

| Concentration (mg mL-1) | Voc (V) | Jsc (mA cm-2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| 5 | 1.00 | 23.58 ± 0.15 | 56.28 ± 2.75 | 13.29 ± 0.25 |
| 10 | 1.04 | 23.46 ± 0.15 | 55.86 ± 1.48 | 13.58 ± 0.16 |
| 15 | 1.01 | 22.86 ± 0.78 | 49.25 ± 6.37 | 11.38 ± 0.73 |
| 20 | 0.99 | 22.48 ± 0.21 | 49.06 ± 2.60 | 10.97 ± 0.20 |

The variance values of the open circuit voltage of different devices were so small that could be negligible.

Fig. S3 Bar charts indicating photovoltaic parameters of ten CsSn0.2Pb0.8I3 QDs-added devices at the PQD concentration of 10 mg mL-1.

Fig. S4 Error bars of photovoltaic parameters for different PSCs.