Supplementary information

The First Polymer Weaire-Phelan Structure: Space-filling polyhedrons of polymer cubic cells created by polymerization induced phase separation

Naofumi Naga, Masumi Jinno, Yuting Wang, Tamaki Nakano

Correspondence to: nnaga@sic.shibaura-it.ac.jp, tamaki.nakano@cat.hokudai.ac.jp

Fig. S1. FT-IR spectra of (a) PEMP-HDI/toluene mixture before the reaction at a monomer concentration of 25 wt%, and (b) the resulting PEMP-HDI network polymer (sample 1).

Table S1. Coordinate points of Pentagon I (Fig. 4 (c)).

| m | A1 | B1 | B2 | C1 | C2 |
| --- | --- | --- | --- | --- | --- |
| x | 5.87 | 6.66 | 5.61 | 6.82 | 6.00 |
| y | 3.33 | 3.28 | 2.75 | 2.75 | 2.33 |
| z | 0.749 | 0.740 | 0.751 | 0.761 | 0.748 |

Table S2. Coordinate points of Hexagon II (Fig. 4 (d)).

| m | D1 | D2 | D3 | D4 | E1 | E2 |
| --- | --- | --- | --- | --- | --- | --- |
| x | 18.9 | 19.0 | 19.7 | 19.8 | 18.7 | 20.2 |
| y | 17.7 | 18.7 | 17.6 | 18.7 | 18.2 | 18.2 |
| z | 1.30 | 1.27 | 1.17 | 1.19 | 1.36 | 1.15 |

Table S3. Coordinate points of Pentagon III (Fig. 4 (e)).

| m | B3 | B4 | F1 | F2 | G1 |
| --- | --- | --- | --- | --- | --- |
| x | 5.05 | 5.72 | 5.42 | 5.75 | 5.22 |
| y | 11.5 | 11.9 | 11.3 | 11.4 | 12.0 |
| z | 1.26 | 1.21 | 1.16 | 1.11 | 1.35 |