Tailoring of performance characteristics of green tyre tread formulation using thermally exfoliated graphite/ carbon black binary filler system via scalable and competent method

Supplementary Information

Table S1 shows various formulations adopted in this work to study the effects of various blend formulations of NR/BR, (NR/BR ratio varied from 100/0 to 10/90) to understand the effect of blending NR with hard segmented BR polymer components.

Table S1: Details of the various NR/BR blend formulations prepared

| Composition | 100 | 90 | 80 | 70 | 60 | 50 | 40 | 30 | 20 | 10 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NR | 100 | 90 | 80 | 70 | 60 | 50 | 40 | 30 | 20 | 10 |
| BR | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 |
| Zinc Oxide | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| Stearic Acid | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 |
| HAF (N330) | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 |
| Aromatic Oil | 8.5 | 8.5 | 8.5 | 8.5 | 8.5 | 8.5 | 8.5 | 8.5 | 8.5 | 8.5 |
| 6PPD | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 |
| TQ | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 |
| CBS | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 |
| Sulphur | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 |

The order of addition of chemicals during the compounding was done as per ASTM D 3182 in a brabender plasticoder and it is depicted in the table S2.

Table S2: Process conditions for the preparation of various green tyre tread formulations

| Time (min) | Master batch preparation (Brabender plasticoder 50 rpm,70˚C) | Temperature (˚C) |
| --- | --- | --- |
| 0:00 | Addition of NR | 28 |
| 1:00 | Addition of BR | 30 |
| 2:00 | Addition of master batch of Graphite | 31 |
| 3:00 | ZnO and Stearic acid added | 33 |
| 3:30 | Anti-degradants are added | 37 |
| 4:30 | Add half HAF and oil | 45 |
| 6:00 | Add remaining black and oil | 65 |
| 8:00 | Dumb | 78 |
| Time (min) | Final batch preparation in two roll mill |  |
| 0:00 | Add master batch compound | 28 |
| 1:00 | Add sulfur and accelerators | 45 |
| 3:00 | dumb | 48 |

Table S3: Details of the Various tyre tread formulations prepared

| Composition | Reference with 50 phr HAF and Ar. Oil 8.5 (B) | Formulation with 32 phr HAF and 3phr Ar. Oil (B1) | Formulation with 24 HAF, 8 phr Graphite and 3 phr Ar. Oil (B2) | Formulation with 22 HAF, 10 phr Graphite and 3 phr Ar. Oil (B3) | Formulation with 20 HAF, 12 phr Graphite and 3 phr Ar. Oil (B4) | Formulation with 24 HAF, 8 phr exfoliated Graphite@500˚C and 3 phr Ar. Oil (E1) | Formulation with 22 HAF, 10 phr exfoliated Graphite@500˚C and 3 phr Ar. Oil (E2) | Formulation with 20 HAF, 12 phr exfoliated Graphite@500˚C and 3 phr Ar. Oil (E3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NR | 60 | 60 | 60 | 60 | 60 | 60 | 60 | 60 |
| BR | 40 | 40 | 40 | 40 | 40 | 40 | 40 | 40 |
| Zinc Oxide | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 |
| Stearic Acid | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 |
| HAF (N330) | 50 | 32 | 24 | 22 | 20 | 24 | 22 | 20 |
| Graphite | 0 | 0 | 8 | 10 | 12 | 8 | 10 | 12 |
| Aromatic Oil | 8.5 | 3 | 3 | 3 | 3 | 3 | 3 | 3 |
| 6PPD | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 |
| TQ | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 |
| CBS | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 |
| Sulphur | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 | 2.1 |

Table S4: Mechanical properties of the various NR/BR blend formulations prepared

| Formulation | Tensile strength (N/mm2) | Tear strength (N/mm) | Elongation at break, Eb (%) | M100 (MPa) | M300 (MPa) |
| --- | --- | --- | --- | --- | --- |
| NR 100 | 30.63±1.31 | 117.75±1.43 | 825±29 | 2.02±0.04 | 7.39±0.11 |
| NR 90 | 28.88±0.97 | 106.45±2.08 | 762±27 | 2.26±0.1 | 8.09±0.4 |
| NR 80 | 26.75±0.37 | 94.87±4.03 | 719±8 | 2.39±0.07 | 8.47±0.23 |
| NR 70 | 23.61±1.03 | 79.88±2.11 | 743±31 | 1.96±0.07 | 6.98±0.17 |
| NR 60 | 24.01±1.15 | 83.71±0.86 | 756±22 | 2.05±0.09 | 7.12±0.33 |
| NR 50 | 21.31±1.44 | 76.87±1.62 | 709±32 | 1.88±0.03 | 6.59±0.05 |
| NR 40 | 19.11±1.03 | 72.16±1.71 | 667±30 | 2.04±0.05 | 6.92±0.06 |
| NR 30 | 17.09±0.07 | 73.54±1.55 | 639±6 | 1.91±0.005 | 6.52±0.02 |
| NR 20 | 16.11±0.97 | 65.12±2.08 | 638±13 | 2.2±0.02 | 6.98±0.25 |
| NR 10 | 14.88±1.02 | 64.28±2.54 | 629±18 | 2±0.04 | 6.48±0.12 |

Table S5: Rheological characterization parameters via rubber process analyzer

| Temperature | Formulation | Scorch time (min.dec) | Cure time (min.dec) | Cure rate index CRI = 100t90-t10 |
| --- | --- | --- | --- | --- |
| 350 ˚C | EG 8 | 3.65 | 8.90 | 19.0476 |
|  | EG 10 | 3.93 | 8.47 | 22.0264 |
|  | EG 12 | 4.17 | 9.05 | 20.4918 |
| 400˚C | EG 8 | 2.91 | 7.93 | 19.9203 |
|  | EG 10 | 3.65 | 8.39 | 21.0970 |
|  | EG 12 | 3.77 | 8.60 | 20.7039 |
| 450˚C | EG 8 | 3.43 | 8.57 | 19.4552 |
|  | EG 10 | 3.48 | 8.24 | 21.0084 |
|  | EG 12 | 2.96 | 8.32 | 18.6567 |
| 500˚C | EG 8 | 3.29 | 8.80 | 18.1488 |
|  | EG 10 | 3.89 | 9.31 | 18.4501 |
|  | EG 12 | 3.83 | 8.22 | 22.7790 |
| 550˚C | EG 8 | 3.67 | 8.98 | 18.8323 |
|  | EG 10 | 3.74 | 8.65 | 20.3665 |
|  | EG 12 | 3.95 | 9.01 | 19.7628 |
| 600˚C | EG 8 | 3.35 | 8.12 | 20.9643 |
|  | EG 10 | 3.45 | 8.25 | 20.8333 |
|  | EG 12 | 3.86 | 9.10 | 19.0839 |

Table S6: Specific gravity and hardness of various tyre tread formulation

| Temperature | Formulation | Specific gravity | Hardness (Shore A) |
| --- | --- | --- | --- |
| 350 ˚C | EG 8 | 0.94 | 60 |
|  | EG 10 | 0.94 | 59 |
|  | EG 12 | 0.95 | 58 |
| 400˚C | EG 8 | 0.95 | 57 |
|  | EG 10 | 0.95 | 60 |
|  | EG 12 | 0.94 | 59 |
| 450˚C | EG 8 | 0.95 | 58 |
|  | EG 10 | 0.96 | 57 |
|  | EG 12 | 0.96 | 59 |
| 500˚C | EG 8 | 0.96 | 58 |
|  | EG 10 | 0.96 | 57 |
|  | EG 12 | 0.96 | 58 |
| 550˚C | EG 8 | 0.96 | 60 |
|  | EG 10 | 0.94 | 60 |
|  | EG 12 | 0.94 | 59 |
| 600˚C | EG 8 | 0.96 | 59 |
|  | EG 10 | 0.95 | 58 |
|  | EG 12 | 0.94 | 59 |

Table S7: Performance evaluation of Tyre tread compound via heat build-up and abrasion testing

| Temperature | Formulation | Heat build up(˚C) | Abrasion loss (cm3) | Abrasion resistance index(%) (ARI) |
| --- | --- | --- | --- | --- |
| 450 | EG 8 | 19 | 0.093 | 171 |
|  | EG 10 | 21 | 0.109 | 145 |
|  | EG 12 | 23 | 0.108 | 147 |
| 500 | EG 8 | 19 | 0.104 | 152 |
|  | EG 10 | 20 | 0.103 | 154 |
|  | EG 12 | 18 | 0.134 | 118 |
| 550 | EG 8 | 19 | 0.106 | 149 |
|  | EG 10 | 19 | 0.108 | 147 |
|  | EG 12 | 20 | 0.112 | 142 |

Table S8: Mechanical properties of thermally exfoliated graphite incorporated rubber composites at different temperatures

|  | Formulation | Tensile strength (N/mm2) | Tear strength (N/mm) | Elongation at break, Eb (%) | M100 (MPa) | M300 (MPa) |
| --- | --- | --- | --- | --- | --- | --- |
| 350 ˚C | EG 8 | 22.71±1.50 | 65.86±25 | 830±50 | 1.90±0.02 | 5.04±0.02 |
|  | EG 10 | 21.37±2.12 | 65.88±2.14 | 880±66 | 1.90±0.02 | 4.81±0.14 |
|  | EG 12 | 21.38±0.68 | 67.95±1.56 | 811±20 | 2.07±0.03 | 5.13±0.14 |
| 400˚C | EG 8 | 21.44±1.75 | 67.41±2.13 | 779±64 | 1.39±0.24 | 4.88±0.40 |
|  | EG 10 | 20.01±2.65 | 64.23±1.78 | 770±43 | 2.10±0.02 | 5.12±0.08 |
|  | EG 12 | 21.79±1.90 | 60.42±2.98 | 827±77 | 2.12±0.04 | 5.17±0.04 |
| 450˚C | EG 8 | 23.84±1.59 | 65.11±1.54 | 881±39 | 1.84±0.01 | 4.86±0.05 |
|  | EG 10 | 21.08±1.58 | 65.02±1.65 | 881±39 | 2.07±0.03 | 5.13±0.01 |
|  | EG 12 | 22.43±0.18 | 66.23±2.22 | 861±3 | 1.79±0.10 | 4.93±0.21 |
| 500˚C | EG 8 | 23.72±1.50 | 64.50±1.12 | 915±49 | 1.88±0.05 | 4.84±0.24 |
|  | EG 10 | 24.37±2.12 | 70.84±0.76 | 880±66 | 2.30±0.02 | 5.81±0.12 |
|  | EG 12 | 21.38±0.68 | 68.59±2.08 | 811±20 | 2.07±0.03 | 5.93±0.01 |
| 550˚C | EG 8 | 23.20±0.14 | 57.55±3.43 | 921±20 | 1.87±0.04 | 5.00±0.16 |
|  | EG 10 | 23.77±1.03 | 58.28±1.33 | 880±38 | 1.96±0.01 | 5.02±0.10 |
|  | EG 12 | 20.95±1.65 | 61.66±1.76 | 804±72 | 2.10±0.03 | 5.29±0.16 |
| 600˚C | EG 8 | 23.52±1.20 | 53.96±2.44 | 824±42 | 1.71±0.03 | 5.17±0.14 |
|  | EG 10 | 20.86±2.65 | 59.12±1.76 | 820±51 | 1.57±0.05 | 4.83±0.11 |
|  | EG 12 | 23.97±2.98 | 61.25±1.09 | 841±50 | 1.84±0.14 | 5.48±0.46 |

Table S9: TGA of bulk graphite incorporated rubber composites

| Formulation | Initial degradation temp.(˚C)Id | Maximum degradation temp. (˚C)Md1 | Maximum degradation temp. (˚C)Md2 | Final degradation temp. (˚C )Fd | Residue % |
| --- | --- | --- | --- | --- | --- |
| B | 301 | 375 | 453 | 486 | 11.13 |
| B1 | 303 | 374 | 452 | 490 | 27.53 |
| B2 | 316 | 373 | 454 | 491 | 17.29 |
| B3 | 328 | 377 | 457 | 488 | 24.89 |
| B4 | 325 | 378 | 451 | 493 | 27.53 |