Supporting Information

Reversible Flowering of CuO Nanoclusters via Conversion Reactions for Dual-Ion Li Metal Batteries

Siying Li1,2, Jung-Hun Lee2, Soo Min Hwang2, *, and Young-Jun Kim 2,3 *

1 School of Mechanical and Automotive Engineering, Guangxi University of Science and Technology, Liuzhou 545616, China

2 SKKU Advanced Institute of Nanotechnology (SAINT), Sungkyunkwan University, Suwon 16419, Republic of Korea

3 Department of Nano Engineering, Sungkyunkwan University, Suwon, 16419, Republic of Korea

Natural activation reactions

Main reaction:

3CuO+2LiAlCl4→3CuCl2+2LiCl+Al2O3

∆G°=-342.48 kJ mol-1	(S1)

Side reactions:

CuO+LiAlCl4+12SO2 → CuCl+12Li2SO4+AlCl3

∆G°=-61.22 kJ mol-1	(S2)

3Li2SO4+2AlCl3→6LiCl+Al2(SO4)3

∆G°=-562.2 kJ mol-1 	(S3)

3CuO+2AlCl3→3CuCl2+Al2O3.

∆G°=-570.86 kJ mol-1	(S4)

CuCl2+13Al2O3+12SO2 → CuCl+13AlCl3+16Al2(SO4)3

∆G°=-60.8 kJ mol-1	(S5)

Figure S1 Schematic of conversion reaction for the cathode active materials during resting and cycling. Crystal structure and parameters of CuO, CuCl, and CuCl2 are illustrated.

Figure S2 FE-SEM images of as-prepared (a) MYS-CuO and (b) CuO hollow nanocubes (HNCs). (c-h) FE-SEM images for electrodes after immersion in electrolyte, including no carbon electrodes with (c) MYS-CuO and (d) CuO HNCs, KB containing electrodes (CuO : KB : PTFE = 6 : 2 : 2) with (e) MYS-CuO (MYS-CuO+KB) and (f) CuO HNCs (CuO HNCs+KB), and cyclized PAN containing electrodes (CuO : KB : PAN : PTFE = 6 : 2 : 1 : 1) with (g) MYS-CuO (MYS-CuO+KB+PAN) and (h) CuO HNCs (CuO HNCs+KB+PAN)

Figure S3 XRD patterns of as-prepared MYS-CuO, and electrodes with different compositions after immersion in electrolyte.

As shown in Figure. S2c-f and Figure. S3, after immersion in the electrolyte, more, thicker and longer CuCl2 nanorods or nanowires were observed on CuO cathodes containing 0-D KB compared to carbon-free CuO cathodes, indicating that KB promoted the conversion of CuO to CuCl2. In the absence of KB, well-dispersed nano-sized CuO HNCs were converted to needle-like CuCl2 more rapidly compared to 1-μm MYS-CuO.

Figure S4 N 1s XPS profiles for MYS-CuO electrode with PAN cyclized at different temperatures.

Figure S5 Differential scanning calorimetry thermograms of PAN powder, PAN-coated MYS-CuO, and bare MYS-CuO (a) before and (b) after heat treatment at 280 ℃ from 25 to 500℃ with air flowing at a heating rate of 2 ℃ min-1。

Figure S6 (a) FE-SEM images of bare P-280-MYS electrode and P-280-MYS electrodes after resting and 1st discharge and charge. (b) FE-SEM images of P-280-MYS electrode after 50th discharge.

Figure S7 (a) XRD patterns for raw, rested, discharged, and charged P-280-MYS electrodes. FE-SEM and EDS mapping images of (b) rested, (c) fully discharged, and (d) fully charged P-280-MYS electrodes.