Supplementary material

Article title: Effect on the thermal conductivity inhomogeneity of clay-bearing sandstone subjected to drying-wetting process

Journal name: Environmental Earth Sciences

Authors: Mohua Bu, Pingye Guo, Meng Wang, Manchao He, Yanwei Wang

Corresponding author: Pingye Guo, State Key Laboratory for Geo-Mechanics and Deep Underground Engineering, 100083 Beijing, China; School of Mechanics, Architecture and Civil Engineering, China University of Mining and Technology, 100083 Beijing, China;

E-mail: guopingye@foxmail.com

S1. Experimental results of thermal conductivity of samples (Fig. 3 and Fig. 4)

| Sample NO. | Dry Ⅰ (W/mK) | Saturation Ⅰ (W/mK) | Dry Ⅱ (W/mK) | Saturation Ⅱ (W/mK) | Dry Ⅲ (W/mK) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.2358 | 2.6288 | 2.0609 | 2.5625 | 2.0112 |
|  | 2.4478 | 2.4575 | 2.1005 | 2.2329 | 1.9548 |
|  | 2.2606 | 2.5990 | 2.1299 | 2.2984 | 1.7957 |
|  | 2.0610 | 2.5000 | 1.8969 | 2.2084 | 1.7534 |
|  | 2.1043 | 2.5482 | 2.0003 | 2.4926 | 1.9229 |
|  | 2.4363 | 2.6413 | 2.3734 | 2.5018 | 2.2789 |
|  | 2.5252 | 2.6439 | 2.4567 | 2.6803 | 2.4379 |
|  | 2.1719 | 2.4974 | 2.1426 | 2.4208 | 1.9579 |
|  | 2.0329 | 2.5769 | 2.0149 | 2.1381 | 1.7660 |
|  | 2.3466 | 2.6671 | 2.3210 | 2.6862 | 2.3201 |
|  | 2.3875 | 2.5582 | 1.9438 | 2.3249 | 1.9311 |
|  | 2.1933 | 2.6923 | 2.1379 | 2.5591 | 1.9847 |
|  | 2.2136 | 2.7362 | 2.0195 | 2.6892 | 2.0078 |
|  | 2.3931 | 2.5514 | 2.3335 | 2.4895 | 2.267 |
|  | 2.3954 | 2.5084 | 2.1217 | 2.3029 | 1.8924 |
|  | 2.1263 | 2.7015 | 2.0072 | 2.2243 | 1.7418 |
|  | 2.4020 | 2.5732 | 2.1967 | 2.0924 | 1.7061 |
|  | 2.5124 | 2.5229 | 2.5014 | 2.5112 | 2.4998 |
|  | 2.2796 | 2.3002 | 2.2573 | 2.2568 | 2.0592 |
|  | 2.2823 | 2.6374 | 2.0441 | 2.1573 | 1.7037 |
| 2 | 2.5572 | 2.5733 | 2.4961 | 2.4530 | 2.1271 |
|  | 2.3986 | 2.3623 | 2.0616 | 2.1407 | 1.8846 |
|  | 2.5173 | 2.5564 | 2.3471 | 2.1133 | 1.7606 |
|  | 2.4543 | 2.4318 | 2.4616 | 2.4151 | 2.4571 |
|  | 2.1776 | 2.6923 | 2.0371 | 2.372 | 1.8778 |
|  | 2.0935 | 2.6722 | 1.9147 | 2.4927 | 1.7299 |
|  | 2.0097 | 2.5317 | 1.9140 | 2.3341 | 1.7734 |
|  | 2.1484 | 2.6932 | 1.9832 | 2.3230 | 1.9344 |
|  | 2.1637 | 2.5473 | 2.0648 | 2.3659 | 1.9455 |
|  | 2.6399 | 2.7703 | 2.6228 | 2.7061 | 2.5978 |
|  | 2.4361 | 2.4863 | 2.1236 | 2.0951 | 1.7637 |
|  | 2.4061 | 2.5946 | 2.2107 | 2.4047 | 2.1432 |
|  | 2.4098 | 2.7212 | 1.9559 | 2.1099 | 1.8809 |
|  | 2.2217 | 2.5243 | 2.1313 | 2.4182 | 2.1164 |
|  | 2.2412 | 2.7336 | 2.1867 | 2.4134 | 1.8395 |
|  | 2.1183 | 2.6308 | 2.0098 | 2.4516 | 1.9008 |
|  | 2.4907 | 2.4842 | 2.2228 | 2.1596 | 1.6707 |
|  | 2.5318 | 2.6055 | 2.0365 | 2.2405 | 1.9135 |
|  | 2.0645 | 2.420 | 2.0638 | 2.4455 | 2.0538 |
|  | 2.4753 | 2.5342 | 2.2587 | 2.1965 | 1.8011 |
| 3 | 2.0228 | 2.3255 | 2.0169 | 2.1268 | 1.9934 |
|  | 2.349 | 2.5079 | 2.1879 | 2.2696 | 1.7017 |
|  | 2.4082 | 2.6619 | 1.9629 | 2.3811 | 1.8783 |
|  | 2.5817 | 2.5329 | 2.5595 | 2.5743 | 2.5473 |
|  | 2.176 | 2.3897 | 2.1329 | 2.1618 | 2.088 |
|  | 2.3772 | 2.7197 | 2.3362 | 2.576 | 2.1987 |
|  | 2.3371 | 2.4375 | 1.9102 | 2.2681 | 1.8381 |
|  | 2.0603 | 2.4833 | 1.8706 | 2.3723 | 1.7179 |
|  | 2.1912 | 2.3386 | 1.9036 | 2.1953 | 1.8823 |
|  | 2.6093 | 2.6560 | 2.6042 | 2.6772 | 2.6034 |
|  | 2.4706 | 2.3133 | 2.4187 | 2.3411 | 2.1664 |
|  | 2.5221 | 2.4390 | 2.3531 | 2.2596 | 2.0398 |
|  | 2.5954 | 2.6226 | 2.5917 | 2.6236 | 2.5672 |
|  | 2.1812 | 2.2880 | 2.0410 | 2.1299 | 2.0216 |
|  | 2.471 | 2.6756 | 1.9032 | 2.3277 | 1.7551 |
|  | 2.4725 | 2.6834 | 1.9133 | 2.2061 | 1.7083 |
|  | 2.3462 | 2.6097 | 2.2801 | 2.3622 | 1.9410 |
|  | 2.1912 | 2.4419 | 2.0885 | 2.1268 | 2.0125 |
|  | 2.6163 | 2.5924 | 2.4191 | 2.4243 | 2.0961 |
|  | 2.0487 | 2.6791 | 1.8651 | 2.2435 | 1.7229 |
| 4 | 2.5191 | 2.4705 | 2.2836 | 2.3778 | 2.2585 |
|  | 2.6317 | 2.6908 | 2.6191 | 2.6981 | 2.6165 |
|  | 2.4163 | 2.6397 | 2.1767 | 2.3492 | 2.0011 |
|  | 2.5007 | 2.6983 | 2.4638 | 2.1012 | 2.3824 |
|  | 2.1622 | 2.5211 | 2.1236 | 2.2637 | 1.9640 |
|  | 2.3186 | 2.7398 | 2.3015 | 2.7097 | 2.2944 |
|  | 2.3464 | 2.4471 | 2.1569 | 2.1539 | 1.8836 |
|  | 2.1440 | 2.5999 | 2.0034 | 2.2042 | 1.9567 |
|  | 2.1779 | 2.4379 | 2.0542 | 2.2864 | 1.7334 |
|  | 2.3180 | 2.3461 | 2.2381 | 2.1406 | 1.8098 |
|  | 2.1264 | 2.4271 | 2.0694 | 2.4039 | 2.0509 |
|  | 2.5871 | 2.5697 | 2.3132 | 2.3956 | 2.1003 |
|  | 2.5673 | 2.7234 | 2.5507 | 2.7298 | 2.5280 |
|  | 2.1467 | 2.4938 | 2.0950 | 2.1079 | 1.7721 |
|  | 2.4676 | 2.6698 | 1.9444 | 2.4267 | 1.7584 |
|  | 2.0672 | 2.3817 | 2.0219 | 2.3293 | 2.0026 |
|  | 2.3464 | 2.5292 | 2.1329 | 2.4816 | 2.1258 |
|  | 2.3487 | 2.6448 | 2.2258 | 2.4491 | 2.2196 |
|  | 2.5606 | 2.6326 | 2.3443 | 2.5361 | 2.0215 |
|  | 2.5967 | 2.7275 | 2.2704 | 2.5115 | 2.2688 |
| 5 | 2.2608 | 2.4539 | 2.2245 | 2.3986 | 1.9845 |
|  | 2.0109 | 2.4593 | 1.8767 | 2.1567 | 1.6865 |
|  | 2.2964 | 2.5730 | 2.1158 | 2.3397 | 2.0595 |
|  | 2.5449 | 2.5860 | 2.5185 | 2.5704 | 2.5001 |
|  | 2.5312 | 2.3796 | 2.4568 | 2.1222 | 2.2400 |
|  | 2.5435 | 2.4960 | 2.4214 | 2.4844 | 2.3986 |
|  | 2.0108 | 2.7269 | 2.0096 | 2.5056 | 1.9521 |
|  | 2.1465 | 2.3553 | 2.0089 | 2.3253 | 1.9978 |
|  | 2.3575 | 2.4865 | 2.2172 | 2.3648 | 2.0208 |
|  | 2.3760 | 2.4470 | 2.3528 | 2.4335 | 2.3147 |
|  | 2.0211 | 2.3607 | 2.0089 | 2.1092 | 1.7287 |
|  | 2.1783 | 2.5320 | 2.0392 | 2.3884 | 1.8988 |
|  | 2.1183 | 2.6850 | 2.0794 | 2.3445 | 2.0403 |
|  | 2.5810 | 2.6756 | 2.5393 | 2.6819 | 2.5348 |
|  | 2.6401 | 2.6448 | 1.9873 | 2.4925 | 1.9517 |
|  | 2.1739 | 2.6950 | 2.1236 | 2.5377 | 2.0098 |
|  | 2.4176 | 2.7315 | 2.3482 | 2.6188 | 2.0698 |
|  | 2.3848 | 2.7055 | 2.3038 | 2.4871 | 1.965 |
|  | 2.6348 | 2.5640 | 2.3054 | 2.4058 | 1.7333 |
|  | 2.3492 | 2.4988 | 2.3464 | 2.2193 | 1.8049 |
| 6 | 2.3585 | 2.4548 | 2.1680 | 2.2728 | 1.8345 |
|  | 2.0251 | 2.3577 | 1.9781 | 2.1663 | 1.8236 |
|  | 2.0152 | 2.4590 | 1.9064 | 2.2878 | 1.8235 |
|  | 2.1663 | 2.3687 | 2.0038 | 2.2125 | 1.7899 |
|  | 2.6055 | 2.6814 | 2.4697 | 2.5895 | 2.3372 |
|  | 2.2547 | 2.2919 | 2.2100 | 2.2101 | 2.0529 |
|  | 2.0144 | 2.3393 | 1.9801 | 2.2929 | 1.8219 |
|  | 2.1647 | 2.4752 | 2.0217 | 2.3779 | 1.8154 |
|  | 2.4180 | 2.5304 | 2.4087 | 2.4753 | 2.3895 |
|  | 2.1373 | 2.4679 | 2.1298 | 2.4650 | 2.1130 |
|  | 2.1630 | 2.6068 | 2.0339 | 2.3734 | 1.8714 |
|  | 2.0385 | 2.5198 | 2.0221 | 2.4873 | 2.0177 |
|  | 2.1065 | 2.7389 | 2.0361 | 2.5444 | 1.9861 |
|  | 2.3110 | 2.4356 | 2.1044 | 2.1713 | 1.7018 |
|  | 2.1989 | 2.7395 | 2.0427 | 2.3399 | 2.0234 |
|  | 2.0679 | 2.3672 | 2.0071 | 2.0255 | 1.6955 |
|  | 2.1167 | 2.3906 | 1.9111 | 2.1826 | 1.7689 |
|  | 2.0598 | 2.4213 | 1.8459 | 2.1385 | 1.7050 |
|  | 2.6066 | 2.7274 | 2.5954 | 2.7152 | 2.5642 |
|  | 2.0578 | 2.3917 | 1.8301 | 1.9865 | 1.6999 |
| 7 | 2.1119 | 2.5307 | 2.0376 | 2.0246 | 1.8993 |
|  | 2.0978 | 2.3431 | 2.0157 | 2.2498 | 1.9863 |
|  | 2.2631 | 2.6543 | 1.8962 | 2.2766 | 1.8321 |
|  | 2.0695 | 2.4909 | 2.0587 | 2.2429 | 2.0126 |
|  | 2.2089 | 2.5969 | 2.1371 | 2.2023 | 1.8073 |
|  | 2.0506 | 2.3909 | 2.0485 | 2.3422 | 2.0372 |
|  | 2.2551 | 2.3108 | 2.1327 | 2.2509 | 2.0289 |
|  | 2.2065 | 2.5864 | 2.204 | 2.2273 | 2.1674 |
|  | 2.5033 | 2.5172 | 2.4957 | 2.5136 | 2.4917 |
|  | 2.5248 | 2.4184 | 2.0264 | 2.1329 | 1.8098 |
|  | 2.6066 | 2.4048 | 2.2306 | 2.3315 | 1.8135 |
|  | 2.1133 | 2.6172 | 2.0734 | 2.5803 | 2.0887 |
|  | 2.4676 | 2.6256 | 2.4656 | 2.6115 | 2.4546 |
|  | 2.0781 | 2.3893 | 1.8456 | 2.0993 | 1.7432 |
|  | 2.2192 | 2.3658 | 2.0262 | 2.1610 | 1.8238 |
|  | 2.2309 | 2.5856 | 2.2026 | 2.3727 | 2.0037 |
|  | 2.0358 | 2.4106 | 1.9895 | 2.1858 | 1.9382 |
|  | 2.2165 | 2.4866 | 2.0410 | 2.1315 | 1.8953 |
|  | 2.5686 | 2.6129 | 2.5395 | 2.5733 | 2.5084 |
|  | 2.3526 | 2.5118 | 2.1318 | 2.4949 | 2.1071 |
| 8 | 2.1728 | 2.5434 | 2.0894 | 2.2306 | 1.9195 |
|  | 2.5689 | 2.425 | 2.4493 | 2.1157 | 1.6748 |
|  | 2.5720 | 2.5301 | 2.0682 | 2.2932 | 1.7837 |
|  | 2.4625 | 2.6499 | 2.3515 | 2.4809 | 2.1644 |
|  | 2.5040 | 2.6712 | 2.2937 | 2.3312 | 1.9957 |
|  | 2.0281 | 2.5967 | 1.9158 | 2.4832 | 1.8367 |
|  | 2.4326 | 2.6002 | 2.4289 | 2.5769 | 2.4261 |
|  | 2.1383 | 2.6093 | 1.9724 | 2.2847 | 1.7146 |
|  | 2.5464 | 2.7182 | 2.2562 | 2.3758 | 1.9130 |
|  | 2.0090 | 2.5451 | 1.9538 | 2.2184 | 1.8946 |
|  | 2.3875 | 2.2714 | 2.1843 | 2.2415 | 2.0511 |
|  | 2.0383 | 2.6763 | 2.0076 | 2.6152 | 1.9843 |
|  | 2.3334 | 2.5441 | 2.2657 | 2.3726 | 2.0145 |
|  | 2.6200 | 2.7804 | 2.6191 | 2.7626 | 2.6137 |
|  | 2.5045 | 2.5060 | 2.0215 | 2.2693 | 1.8188 |
|  | 2.1764 | 2.7171 | 2.1181 | 2.6782 | 2.1179 |
|  | 2.0659 | 2.3880 | 1.9666 | 2.2163 | 1.8846 |
|  | 2.4560 | 2.5142 | 2.2257 | 2.4773 | 2.1529 |
|  | 2.4510 | 2.4599 | 2.1813 | 2.2356 | 1.7303 |
|  | 2.6148 | 2.6423 | 2.6074 | 2.2332 | 2.5685 |
| 9 | 2.1723 | 2.2684 | 2.1348 | 2.2324 | 2.0423 |
|  | 2.0203 | 2.3808 | 2.0089 | 1.9863 | 1.6894 |
|  | 2.4337 | 2.4368 | 2.3943 | 2.3427 | 2.0123 |
|  | 2.2572 | 2.7152 | 2.2503 | 2.5587 | 2.0806 |
|  | 2.6389 | 2.6658 | 2.5850 | 2.5892 | 2.3746 |
|  | 2.1842 | 2.4901 | 2.1075 | 2.2748 | 1.9552 |
|  | 2.4699 | 2.6401 | 2.2583 | 2.5007 | 1.8140 |
|  | 2.3506 | 2.4040 | 2.0662 | 2.1468 | 1.6900 |
|  | 2.3488 | 2.4995 | 2.3476 | 2.4611 | 2.3353 |
|  | 2.0703 | 2.6646 | 1.9503 | 2.1263 | 1.7465 |
|  | 2.3317 | 2.5396 | 2.1057 | 2.3161 | 1.993 |
|  | 2.2800 | 2.7058 | 2.0934 | 2.3094 | 1.9084 |
|  | 2.0533 | 2.5004 | 1.9031 | 2.4536 | 1.9012 |
|  | 2.2382 | 2.5039 | 2.2147 | 2.3965 | 1.9312 |
|  | 2.4693 | 2.5762 | 2.2137 | 2.2491 | 1.7990 |
|  | 2.1739 | 2.3479 | 1.9772 | 2.2304 | 1.8732 |
|  | 2.0402 | 2.4905 | 1.9239 | 2.0362 | 1.6815 |
|  | 2.3128 | 2.5298 | 2.2481 | 2.3175 | 2.1254 |
|  | 2.0594 | 2.5777 | 1.9312 | 2.0681 | 1.8879 |
|  | 2.0122 | 2.6673 | 2.0117 | 2.5445 | 1.8764 |
| 10 | 2.1818 | 2.7402 | 1.9851 | 2.2844 | 1.9801 |
|  | 2.2992 | 2.2757 | 2.1899 | 2.1235 | 1.8952 |
|  | 2.6189 | 2.7935 | 2.5681 | 2.6219 | 2.4886 |
|  | 2.1048 | 2.4484 | 1.9537 | 2.4084 | 1.9159 |
|  | 2.0327 | 2.4699 | 1.9215 | 2.365 | 1.9038 |
|  | 2.0610 | 2.2887 | 1.8516 | 2.1328 | 1.7219 |
|  | 2.0459 | 2.6924 | 1.9824 | 2.5081 | 1.8120 |
|  | 2.1848 | 2.7293 | 1.8254 | 2.3802 | 1.7844 |
|  | 2.5407 | 2.5857 | 2.2097 | 2.4940 | 2.1985 |
|  | 2.3569 | 2.6929 | 2.0503 | 2.3941 | 1.9634 |
|  | 2.2440 | 2.4350 | 2.1036 | 2.3918 | 2.0834 |
|  | 2.5156 | 2.7743 | 2.1231 | 2.2821 | 1.8168 |
|  | 2.1393 | 2.4385 | 1.9946 | 2.3505 | 1.9943 |
|  | 2.2317 | 2.6846 | 2.1205 | 2.3557 | 1.9094 |
|  | 2.4480 | 2.5529 | 2.3529 | 2.3377 | 1.9303 |
|  | 2.0955 | 2.6276 | 2.0891 | 2.6107 | 2.0431 |
|  | 2.2941 | 2.4344 | 2.1368 | 2.3461 | 2.0969 |
|  | 2.1303 | 2.7258 | 2.1029 | 2.6948 | 2.0288 |
|  | 2.1655 | 2.3585 | 2.0986 | 2.2088 | 1.7813 |
|  | 2.3560 | 2.3964 | 1.9345 | 2.2216 | 1.8841 |
| Maximum value | 2.640 | 2.794 | 2.623 | 2.763 | 2.617 |
| Minimum value | 2.009 | 2.268 | 1.825 | 1.986 | 1.671 |
| Average value | 2.297 | 2.544 | 2.154 | 2.351 | 1.999 |
| 1/4 quartile | 2.465 | 2.655 | 2.275 | 2.484 | 2.096 |
| 3/4 quartile | 2.138 | 2.440 | 2.009 | 2.219 | 1.816 |
| Median | 2.281 | 2.542 | 2.117 | 2.342 | 1.956 |

S2. Thermal inhomogeneity factor calculated by Eq. (3) (Fig.6)

| Sample NO. | Dry Ⅰ | Saturation Ⅰ | Dry Ⅱ | Saturation Ⅱ | Dry Ⅲ |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.21494 | 0.16918 | 0.28077 | 0.24955 | 0.39813 |
| 2 | 0.27073 | 0.15825 | 0.32889 | 0.26195 | 0.47335 |
| 3 | 0.25240 | 0.17132 | 0.34092 | 0.23598 | 0.44550 |
| 4 | 0.23844 | 0.15322 | 0.30399 | 0.26381 | 0.42306 |
| 5 | 0.27022 | 0.14737 | 0.29925 | 0.23869 | 0.41490 |
| 6 | 0.26988 | 0.17989 | 0.36701 | 0.31467 | 0.44738 |
| 7 | 0.25268 | 0.13781 | 0.32579 | 0.25515 | 0.37835 |
| 8 | 0.25954 | 0.19810 | 0.32309 | 0.27242 | 0.47363 |
| 9 | 0.27905 | 0.17659 | 0.32515 | 0.26133 | 0.45015 |
| 10 | 0.26026 | 0.20248 | 0.35712 | 0.24049 | 0.39085 |

S3. Standard deviation of measuring surface height (Fig. 7)

| Sample NO. | Measuring surface | Dry Ⅰ | Dry Ⅱ | Dry Ⅲ |
| --- | --- | --- | --- | --- |
| 1 | 1 | 0.0294 | 0.1141 | 0.4580 |
|  | 2 | 0.0446 | 0.0784 | 0.0893 |
|  | 3 | 0.0325 | 0.0653 | 0.0956 |
|  | 4 | 0.0417 | 0.0833 | 0.5674 |
| 2 | 1 | 0.0375 | 0.1025 | 0.1823 |
|  | 2 | 0.0366 | 0.1606 | 0.2902 |
|  | 3 | 0.0444 | 0.1869 | 0.5060 |
|  | 4 | 0.0284 | 0.1467 | 0.1842 |
| 3 | 1 | 0.0435 | 0.0893 | 0.1222 |
|  | 2 | 0.0414 | 0.2023 | 0.3231 |
|  | 3 | 0.0370 | 0.0488 | 0.0727 |
|  | 4 | 0.0418 | 0.1324 | 0.2715 |
| 4 | 1 | 0.0252 | 0.2758 | 0.5100 |
|  | 2 | 0.0319 | 0.0417 | 0.0748 |
|  | 3 | 0.0423 | 0.2345 | 0.4812 |
|  | 4 | 0.0348 | 0.0524 | 0.0718 |
| 5 | 1 | 0.0411 | 0.1398 | 0.1584 |
|  | 2 | 0.0428 | 0.1082 | 0.2635 |
|  | 3 | 0.0435 | 0.1351 | 0.3917 |
|  | 4 | 0.0316 | 0.3300 | 0.5778 |
| 6 | 1 | 0.0274 | 0.0665 | 0.2026 |
|  | 2 | 0.0428 | 0.2961 | 0.3687 |
|  | 3 | 0.0423 | 0.1713 | 0.2616 |
|  | 4 | 0.0317 | 0.2568 | 0.5666 |
| 7 | 1 | 0.0267 | 0.0602 | 0.0644 |
|  | 2 | 0.0370 | 0.3296 | 0.4787 |
|  | 3 | 0.0375 | 0.2142 | 0.2840 |
|  | 4 | 0.0270 | 0.0826 | 0.0925 |
| 8 | 1 | 0.0322 | 0.2043 | 0.3145 |
|  | 2 | 0.0425 | 0.1635 | 0.2064 |
|  | 3 | 0.0315 | 0.0766 | 0.1903 |
|  | 4 | 0.0445 | 0.3416 | 0.4082 |
| 9 | 1 | 0.0280 | 0.0338 | 0.0886 |
|  | 2 | 0.0392 | 0.1035 | 0.2131 |
|  | 3 | 0.0441 | 0.0828 | 0.1184 |
|  | 4 | 0.0446 | 0.2573 | 0.4138 |
| 10 | 1 | 0.0265 | 0.3116 | 0.5172 |
|  | 2 | 0.0272 | 0.1781 | 0.4984 |
|  | 3 | 0.0408 | 0.0888 | 0.1608 |
|  | 4 | 0.0256 | 0.2876 | 0.4009 |

S4. Porosity of the measured position calculated by Eq. (5) (Fig.12)

| Sample NO. | Dry Ⅰ (%) | Dry Ⅱ (%) | Dry Ⅲ (%) |
| --- | --- | --- | --- |
| 1 | 5.16 | 7.75 | 8.53 |
|  | 0.13 | 5.00 | 7.29 |
|  | 4.44 | 6.34 | 11.78 |
|  | 6.15 | 8.80 | 11.30 |
|  | 6.10 | 7.71 | 8.97 |
|  | 2.57 | 3.41 | 4.70 |
|  | 1.46 | 2.34 | 2.58 |
|  | 4.45 | 4.88 | 7.75 |
|  | 7.55 | 7.84 | 12.04 |
|  | 4.08 | 4.43 | 4.44 |
|  | 2.20 | 8.75 | 8.96 |
|  | 6.53 | 7.35 | 9.71 |
|  | 6.75 | 9.68 | 9.86 |
|  | 2.04 | 2.84 | 3.77 |
|  | 1.47 | 5.33 | 8.98 |
|  | 7.63 | 9.46 | 13.98 |
|  | 2.19 | 5.04 | 13.09 |
|  | 0.13 | 0.27 | 0.29 |
|  | 0.29 | 0.60 | 3.53 |
|  | 4.61 | 8.12 | 13.92 |
| 2 | 0.20 | 0.97 | 6.07 |
|  | 0.49 | 4.34 | 7.20 |
|  | 0.49 | 2.72 | 11.88 |
|  | 0.29 | 0.39 | 0.33 |
|  | 6.76 | 8.88 | 11.48 |
|  | 7.78 | 10.62 | 13.85 |
|  | 7.36 | 8.91 | 11.34 |
|  | 7.20 | 9.75 | 10.54 |
|  | 5.20 | 6.69 | 8.59 |
|  | 1.54 | 1.74 | 2.05 |
|  | 0.65 | 5.02 | 10.94 |
|  | 2.40 | 5.10 | 6.09 |
|  | 3.87 | 10.52 | 11.77 |
|  | 4.07 | 5.39 | 5.62 |
|  | 6.33 | 7.11 | 12.62 |
|  | 6.90 | 8.58 | 10.35 |
|  | 0.08 | 3.54 | 12.64 |
|  | 0.91 | 7.85 | 9.83 |
|  | 5.06 | 5.07 | 5.23 |
|  | 0.75 | 3.67 | 10.88 |
| 3 | 4.44 | 4.54 | 4.91 |
|  | 2.09 | 4.35 | 12.36 |
|  | 3.19 | 9.70 | 11.11 |
|  | 0.61 | 0.33 | 0.18 |
|  | 2.98 | 3.62 | 4.30 |
|  | 4.29 | 4.84 | 6.77 |
|  | 1.34 | 7.77 | 8.99 |
|  | 5.95 | 9.03 | 11.74 |
|  | 2.07 | 6.56 | 6.92 |
|  | 0.57 | 0.63 | 0.64 |
|  | 2.10 | 1.42 | 2.09 |
|  | 1.07 | 1.14 | 5.69 |
|  | 0.33 | 0.38 | 0.68 |
|  | 1.52 | 3.64 | 3.94 |
|  | 2.53 | 10.85 | 13.43 |
|  | 2.61 | 10.78 | 14.39 |
|  | 3.39 | 4.30 | 9.43 |
|  | 3.45 | 4.98 | 6.16 |
|  | 0.29 | 2.20 | 6.77 |
|  | 8.55 | 11.54 | 14.06 |
| 4 | 0.62 | 2.51 | 2.86 |
|  | 0.71 | 0.86 | 0.89 |
|  | 2.82 | 6.14 | 8.82 |
|  | 2.42 | 2.90 | 3.97 |
|  | 4.89 | 5.47 | 7.96 |
|  | 5.32 | 5.55 | 5.65 |
|  | 1.34 | 4.02 | 8.34 |
|  | 6.14 | 8.30 | 9.05 |
|  | 3.59 | 5.46 | 10.87 |
|  | 0.38 | 1.50 | 8.27 |
|  | 4.21 | 5.08 | 5.37 |
|  | 0.22 | 3.35 | 6.43 |
|  | 1.88 | 2.09 | 2.37 |
|  | 4.77 | 5.55 | 10.88 |
|  | 2.51 | 10.10 | 13.30 |
|  | 4.51 | 5.22 | 5.52 |
|  | 2.39 | 5.43 | 5.54 |
|  | 3.78 | 5.50 | 5.58 |
|  | 0.88 | 3.69 | 8.41 |
|  | 1.57 | 5.84 | 5.87 |
| 5 | 2.61 | 3.13 | 6.76 |
|  | 6.41 | 8.61 | 12.02 |
|  | 3.62 | 6.23 | 7.09 |
|  | 0.51 | 0.84 | 1.08 |
|  | 1.97 | 1.02 | 1.93 |
|  | 0.60 | 0.97 | 1.27 |
|  | 9.71 | 9.72 | 10.65 |
|  | 2.96 | 5.07 | 5.24 |
|  | 1.70 | 3.65 | 6.61 |
|  | 0.94 | 1.25 | 1.77 |
|  | 4.95 | 5.14 | 9.93 |
|  | 4.79 | 6.90 | 9.17 |
|  | 7.55 | 8.14 | 8.75 |
|  | 1.15 | 1.67 | 1.72 |
|  | 0.06 | 9.11 | 9.68 |
|  | 6.85 | 7.59 | 9.35 |
|  | 3.89 | 4.82 | 8.84 |
|  | 4.02 | 5.12 | 10.19 |
|  | 0.87 | 3.39 | 12.47 |
|  | 1.97 | 2.00 | 10.36 |
| 6 | 1.27 | 3.96 | 9.28 |
|  | 4.84 | 5.59 | 8.18 |
|  | 6.34 | 8.11 | 9.53 |
|  | 2.85 | 5.33 | 8.93 |
|  | 0.91 | 2.62 | 4.38 |
|  | 0.52 | 1.16 | 3.51 |
|  | 4.76 | 5.31 | 7.96 |
|  | 4.27 | 6.45 | 9.88 |
|  | 1.45 | 1.57 | 1.83 |
|  | 4.58 | 4.69 | 4.95 |
|  | 5.95 | 7.91 | 10.56 |
|  | 6.75 | 7.01 | 7.08 |
|  | 8.36 | 9.45 | 10.24 |
|  | 1.67 | 4.66 | 11.42 |
|  | 7.00 | 9.35 | 9.65 |
|  | 4.31 | 5.26 | 10.63 |
|  | 3.88 | 7.13 | 9.60 |
|  | 5.15 | 8.64 | 11.17 |
|  | 1.44 | 1.58 | 1.97 |
|  | 4.79 | 8.53 | 10.88 |
| 7 | 5.76 | 6.90 | 9.14 |
|  | 3.52 | 4.80 | 5.26 |
|  | 5.08 | 10.72 | 11.81 |
|  | 5.90 | 6.07 | 6.79 |
|  | 5.16 | 6.21 | 11.55 |
|  | 4.89 | 4.92 | 5.10 |
|  | 0.78 | 2.56 | 4.14 |
|  | 5.06 | 5.10 | 5.63 |
|  | 0.18 | 0.27 | 0.32 |
|  | 1.37 | 5.63 | 9.24 |
|  | 2.57 | 2.40 | 8.99 |
|  | 6.81 | 7.42 | 7.19 |
|  | 1.98 | 2.00 | 2.15 |
|  | 4.45 | 8.23 | 10.04 |
|  | 2.04 | 4.94 | 8.29 |
|  | 4.70 | 5.11 | 8.12 |
|  | 5.38 | 6.12 | 6.95 |
|  | 3.66 | 6.29 | 8.65 |
|  | 0.54 | 0.91 | 1.30 |
|  | 2.09 | 5.23 | 5.60 |
| 8 | 5.02 | 6.26 | 8.97 |
|  | 1.84 | 0.32 | 11.79 |
|  | 0.52 | 6.42 | 11.14 |
|  | 2.34 | 3.81 | 6.45 |
|  | 2.06 | 4.85 | 9.29 |
|  | 7.87 | 9.69 | 11.03 |
|  | 2.12 | 2.17 | 2.21 |
|  | 6.34 | 8.92 | 13.38 |
|  | 2.08 | 5.93 | 11.19 |
|  | 7.54 | 8.42 | 9.40 |
|  | 1.59 | 1.25 | 3.25 |
|  | 8.68 | 9.16 | 9.53 |
|  | 2.75 | 3.69 | 7.44 |
|  | 1.89 | 1.90 | 1.97 |
|  | 0.02 | 6.84 | 10.21 |
|  | 7.07 | 7.93 | 7.94 |
|  | 4.62 | 6.19 | 7.54 |
|  | 0.75 | 3.88 | 4.94 |
|  | 0.12 | 3.83 | 11.21 |
|  | 0.33 | 0.42 | 0.90 |
| 9 | 1.38 | 1.93 | 3.35 |
|  | 5.23 | 5.41 | 10.93 |
|  | 0.04 | 0.56 | 6.10 |
|  | 5.89 | 5.98 | 8.48 |
|  | 0.32 | 0.98 | 3.69 |
|  | 4.18 | 5.31 | 7.70 |
|  | 2.12 | 4.98 | 11.96 |
|  | 0.72 | 4.82 | 11.23 |
|  | 1.98 | 2.00 | 2.16 |
|  | 8.04 | 9.94 | 13.46 |
|  | 2.72 | 5.97 | 7.72 |
|  | 5.45 | 8.18 | 11.12 |
|  | 6.28 | 8.70 | 8.73 |
|  | 3.57 | 3.91 | 8.27 |
|  | 1.35 | 4.83 | 11.44 |
|  | 2.45 | 5.47 | 7.20 |
|  | 6.35 | 8.22 | 12.51 |
|  | 2.86 | 3.76 | 5.55 |
|  | 7.15 | 9.20 | 9.92 |
|  | 8.98 | 8.99 | 11.21 |
| 10 | 7.26 | 10.27 | 10.35 |
|  | 0.33 | 1.22 | 5.83 |
|  | 2.06 | 2.68 | 3.68 |
|  | 4.82 | 7.19 | 7.81 |
|  | 6.21 | 8.00 | 8.29 |
|  | 3.34 | 6.75 | 9.07 |
|  | 8.75 | 9.75 | 12.62 |
|  | 7.09 | 12.82 | 13.54 |
|  | 0.56 | 5.01 | 5.17 |
|  | 4.25 | 8.69 | 10.07 |
|  | 2.60 | 4.66 | 4.97 |
|  | 3.12 | 8.52 | 13.49 |
|  | 4.17 | 6.40 | 6.41 |
|  | 5.89 | 7.51 | 10.86 |
|  | 1.34 | 2.60 | 8.91 |
|  | 7.21 | 7.31 | 8.02 |
|  | 1.89 | 4.15 | 4.75 |
|  | 7.85 | 8.27 | 9.41 |
|  | 2.72 | 3.72 | 8.94 |
|  | 0.54 | 6.82 | 7.66 |