Table 1 Lattice constant (a), Ge-Ge bond length (dGe-Ge), Ge-X bond length (dGe-X), Ge-Ge-Ge bond angle (θGe-Ge-Ge), Ge-Ge-X bond angle (θGe-Ge-X), band gap energy (Eg), binding energy (Eb) and bulk modulus (B) of germanane, hydrofluorinated germanene and fluorogermanene, where X= H for germanane and F for fluorogermanene.

| Parameters | Germanane |  | Hydrofluorinated germanene (GeH0.5F0.5) | Fluorogermanene |  |
| --- | --- | --- | --- | --- | --- |
|  | This work | Reported | This work | This work | Reported |
| a (Å) | 4.059 | 3.880a, 3.93e, 3.908g, 3.95d, 4.082c | 4.114 | 5.238 |  |
| dGe-Ge (Å) | 2.454 | 2.390g, 2.401e, 2.338f, 2.469c | 2.467 | 2.770 | 2.40d, 2.49i |
| dGe-X (Å) | 1.557 | 1.529d, 1.56g, 1.563c | dGe-H= 1.541, dGe-F= 1.785 | 1.754 | 1.70d, 1.780i |
| θGe-Ge-Ge (degrees) | 111.487 | 108.95g | 112.985 | 118.074 |  |
| θGe-Ge-X (degrees) | 107.372 | 109.99g | θGe-Ge-H=105.676, θGe-Ge-F=105.676 | 98.047 |  |
| Eg (eV) | 1.010 | 1.59a, 0.5b, 1.38e , 3.6j , 3.5h , 1.812g, 1.5f, 1.38d, 2.81i | 0.466 | 0.159 | 0.19d |
| Eb (eV) | 3.95 | 4.069g, 2.575d | 1.722 | -1.076 |  |
| B (GPa) | 103.037 |  | 110.674 | 118.074 |  |

Experimental values a Ref [16] and b Ref [17] , reported LDA c Ref. [18], d Ref. [23], e Ref. [13] and f Ref. [14], reported GGA g Ref. [24], reported GW h Ref. [13] and i Ref. [23], reported HSE  j Ref. [13]

Table 2

The calculated atomic populations, atomic charges and bond populations of germanane and fluorogermanene.

| Atom | s | p | d | f | Total | Charge (e) | Bond populations |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Germanane |  |  |  |  |  |  |  |  |
| Ge | 1.32 | 2.55 | 0.00 | 0.00 | 3.87 | 0.13 | Ge-H | 0.77 |
| H | 1.13 | 0.00 | 0.00 | 0.00 | 1.13 | -0.13 |  |  |
| Fluorogermanene |  |  |  |  |  |  |  |  |
| Ge | 1.75 | 1.68 | 10.00 | 0.00 | 13.43 | 0.57 | Ge-F | 0.30 |
| F | 1.97 | 5.60 | 0.00 | 0.00 | 7.57 | -0.57 |  |  |

Table 3

The calculated energy bandgap (Eg), binding energy (Eb), static dielectric constant ε(0), static refractive index n(0) and plasmon energy (ћωp) for different occupancy ratio of hydrogen and fluorine in hydrofluorinated germanene.

| Parameter | GeH | GeH0.875F0.125 | GeH0.75F0.25 | GeH0.625F0.375 | GeH0.5F0.5 | GeH0.375F0.625 | GeH0.25F0.75 | GeH0.125F0.875 | GeF |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Eg (eV) | 1.010 | 0.874 | 0.835 | 0.728 | 0.466 | 0.415 | 0.396 | 0.254 | 0.159 |
| Eb (eV) | 3.95 | 3.278 | 3.161 | 2.407 | 1.722 | 1.118 | 0.429 | 0.280 | -1.076 |
| ε(0) | 3.600 | 3.435 | 3.420 | 3.316 | 3.152 | 3.055 | 2.957 | 2.822 | 2.778 |
| n(0) | 1.898 | 1.854 | 1.849 | 1.821 | 1.775 | 1.748 | 1.720 | 1.680 | 1.667 |
| ћωp (eV) | 15.404 | 15.295 | 15.290 | 15.285 | 15.139 | 15.088 | 14.931 | 14.563 | 14.200 |