Design a new strategy for evaluating biodegradation mechanisms between plant tape and industrial tapes

Dongping Tang a, Houyong Yu a,, Somia Yassin Hussain Abdalkarim a, Mingxin Wang a, Xiang Chen a, , Jingli Zhu b,c,d, Meijin Jin b,c,d

a The Key Laboratory of Advanced Textile Materials and Manufacturing Technology of Ministry of Education, Zhejiang Provincial Key Laboratory of Fiber Materials and Manufacturing Technology, Zhejiang Sci-Tech University, Xiasha Higher Education Park Avenue 2 No.928, Hangzhou 310018, China

b Zhejiang Huafon Environmental Protection Material Co., Ltd, Kaifa Road 1688, Ruian Economic Development Zone, Wenzhou 325000, China

c Shanghai Huafon Material Technology Co., Ltd

d HUAFON GROUP CO., LTD

Results and discussion

The stress and strain curve of the plant tape during the process of immersing water for a different duration as Fig.S1a The breaking strength and elongation of plant tape showed a trend with the time of soaking in water which decreased at first and increased, especially when soaked in water for 5 minutes and 10 minutes. As shown in Fig. S1b after drying, the breaking strength of plant tape after soaking water can be recovered. The breaking strength of plant tape after water immersion was also higher than that of the unimmersed BOPP and BOPP/CaCO3 tapes. The highest tensile strength of plant tape can be ascribed to the enhanced intermolecular force, while it was difficult for intermolecular slippage (Xu et al. 2021; Roy et al. 2022).

Fig. S1 (a) Stress-strain curve of plant tape under different immersion time (b) Stress-strain curve of plant tape before and after being immersed in water for 30 min (the illustration was the plant tape that has dried naturally after being immersed in water for 30 min)

The infrared spectrum of the maximum degradation temperature of BOPP tape at 476 °C, as shown in Fig.S2a The stretching vibration peak near 3081 cm-1 and -C=C- stretching and bending vibration (1674 cm-1) indicate the formation of olefins. C-H stretching vibrations (2964 cm-1 and 1382 cm-1) and -CH2 scissor vibration (1450 and 2985 cm-1) reflect the formation of alkanes(Al-Salem et al. 2017). Fig. S2b shows the infrared spectrum of BOPP/CaCO3 tape with two maximum degradation temperatures of 482 and 782 °C.

Fig. S2 (a), (b) and (c) are the infrared peaks of the maximum degradation peaks of BOPP tape, BOPP/CaCO3 tape and Plant tape

At 478 °C, the degradation product of BOPP/CaCO3 tape was almost the same as BOPP tape degradation, While the difference was calcium oxide in the product after BOPP/CaCO3 tape degradation. The characteristic peaks near 2358 and 666cm-1, due to the formation of CO2 which was the decomposition of CaCO3(dos Santos Araújo et al. 2019). When the maximum degradation temperature of plant tape was 350°C, the infrared spectrum was shown in Fig. S2c The -OH characteristics peaks at 3730 cm-1, 2380-2278 cm-1,666 cm-1,2173 cm-1 and 2105 cm-1 were due to the formed of CO2 and CO, respectively. The peak at 1746 cm-1 was attributed to the C=O group of carbonyl compounds (including aldehydes, ketones, and acids) and the position 3000-2770 cm-1 and 1500-1300 cm-1 indicates the formation aliphatic alkanes (Zhu et al. 2018)

Reference

Al-Salem SM, Sharma BK, Khan AR, et al (2017) Thermal degradation kinetics of virgin polypropylene (PP) and PP with starch blends exposed to natural weathering. Ind Eng Chem Res 56:5210–5220. https://doi.org/10.1021/acs.iecr.7b00754

Dos Santos Araújo P, Belini GB, Mambrini GP, et al (2019) Thermal degradation of calcium and sodium alginate: A greener synthesis towards calcium oxide micro/nanoparticles. Int J Biol Macromol 140:749–760. https://doi.org/10.1016/j.ijbiomac.2019.08.103

Roy S, Ghosh BD, Goh KL, et al (2022) Modulation of interfacial interactions toward strong and tough cellulose nanofiber-based transparent thin films with antifogging feature. Compos Sci Technol 278:118974. https://doi.org/10.1016/j.compscitech.2020.108613

Xu L, Zhao J, Qian S, et al (2021) Green-plasticized poly(lactic acid)/nanofibrillated cellulose biocomposites with high strength, good toughness and excellent heat resistance. Compos Sci Technol 203:108613. https://doi.org/10.1016/j.compscitech.2020.108613

Zhu X, He Q, Hu Y, et al (2018) A comparative study of structure, thermal degradation, and combustion behavior of starch from different plant sources. J Therm Anal Calorim 132:927–935. https://doi.org/10.1007/s10973-018-7030-4

Corresponding authors. Tel: +86-571-86843618; Fax: +86-571-86843619.

E-mail addresses: phdyu@zstu.edu.cn (Houyong Yu), cx9528@zstu.edu.cn (Xiang Chen)