Supporting Information

Electrochemical Reduction of Carbon Dioxide to Methanol on Defective Graphene Supported Cu Based Single-Atom Catalysts: A First Principles Approach

Liu Jing1, Jun Zhao1*, Yang Li1, Chuangwei Liu2, Mohamed E. Zayed1,3

( 1 Tianjin University, Key Laboratory of Efficient Utilization of Low and Medium Grade Energy

, Ministry of Education, China, Tianjin 300350).

( 2 Department of Energy Conversion and Storage, Technical University of Denmark, 2800 Kgs. Lyngby, Denmark).

(3 Mechanical Power Engineering Department, Faculty of Engineering, Tanta University, Tanta 31521, Egypt).

Table S1 DFT electronic energy (𝐸DFT), zero point energy correction (ZPE), and entropy contribution (–TS) of Cu-G3/4 surface systems. All data are given in eV.

(S1-t)

|  | E（ev） | ZPE（ev） | TS（ev）- |
| --- | --- | --- | --- |
| CO2 | -23 | 0.8 | 0.67 |
| H2 | -6.77 | 0.3 | 0.4 |
| H2O | -14.23 | 1.34 | 0.67 |
| CH4 | -24.07 | 1.91 | 0.6 |
| CH3OH | -30.44 | 1.89 | 0.79 |
| Cu-G3 | -153.77 | 2.66 | 0.37 |

(S1-a)

| Cu-G3-HCOO | E (ev) | ZPE (ev) | T (ev) | Free energy G | ΔG |
| --- | --- | --- | --- | --- | --- |
| *+CO2+6(H++e-） | -193.55 | 1.7 | 1.87 | -193.72 | 0 |
| *HCOO+5(H++e-） | -196.81 | 4.09 | 1.52 | -194.24 | -0.52 |
| *HCOOH+4(H++e-） | -197.36 | 4.29 | 1.32 | -194.39 | -0.15 |
| *CHO+3(H++e-） | -197.35 | 4.39 | 1.17 | -194.13 | 0.26 |
| CH2O*+2(H++e-）+H2O | -198.19 | 5.27 | 1.46 | -194.38 | -0.25 |
| CH3O*+1(H++e-）+H2O | -198.9 | 5.29 | 1.4 | -195.01 | -0.63 |
| *+CH3OH+H2O | -198.42 | 3.23 | 1.46 | -196.65 | -1.64 |

(S1-b)

| Cu-G3-COOH | E (ev) | ZPE (ev) | T (ev) | Free energy G | ΔG |
| --- | --- | --- | --- | --- | --- |
| *+CO2+6(H++e-） | -193.55 | 1.7 | 1.87 | -193.72 | 0 |
| *COOH+5(H++e-） | -196.12 | 4.09 | 1.54 | -193.57 | 0.15 |
| *CO+4(H++e-)+H2O | -196.85 | 4.85 | 1.97 | -193.97 | -0.4 |
| *CHO+3(H++e-)+H2O | -196.39 | 4.97 | 1.85 | -193.27 | 0.7 |
| *CH2O+2(H++e-）+H2O | -197.21 | 4.82 | 1.56 | -193.95 | -0.68 |
| *CH3O+1(H++e-）+H2O | -198.94 | 5.29 | 1.4 | -195.05 | -1.1 |
| *+CH3OH+H2O | -198.46 | 3.23 | 1.46 | -196.69 | -1.64 |

(S1-c)

| Cu-G4-HCOO | E（ev） | ZPE（ev） | TS（ev） | G=E+ZPE-TS | ΔG |
| --- | --- | --- | --- | --- | --- |
| *+CO2+6(H++e-） | -184.13 | 1.7 | 1.87 | -184.3 | 0 |
| *HCOO+5(H++e-） | -186.17 | 3.94 | 1.57 | -183.8 | 0.5 |
| *HCOOH+4(H++e-） | -185.68 | 4.01 | 1.33 | -183 | 0.8 |
| *CHO+3(H++e-） | -184.5 | 3.74 | 1.29 | -182.05 | 0.95 |
| *CH2O+2(H++e-）+H2O | -185.81 | 4.97 | 1.51 | -182.35 | -0.3 |
| *CH3O+1(H++e-）+H2O | -187.1 | 5.15 | 1.4 | -183.35 | -1 |
| *+CH3OH+H2O | -186.76 | 3.23 | 1.46 | -184.99 | -1.64 |

(S1-d)

| Cu-G4-COOH | E（ev） | ZPE（ev） | TS（ev） | G=E+ZPE-TS | ΔG |
| --- | --- | --- | --- | --- | --- |
| *+CO2+6(H++e-） | -184.13 | 1.7 | 1.87 | -184.3 | 0 |
| *COOH+5(H++e-） | -185.77 | 3.95 | 1.46 | -183.28 | 1.02 |
| *CO+4(H++e-)+H2O | -186.53 | 4.71 | 2.09 | -183.91 | -0.63 |
| *CHO+3(H++e-)+H2O | -186.74 | 4.92 | 1.69 | -183.51 | 0.4 |
| *OCH2+2(H++e-）+H2O | -187.68 | 4.98 | 1.31 | -184.01 | -0.5 |
| *OCH3+1(H++e-）+H2O | -188.6 | 5.08 | 1.49 | -185.01 | -1 |
| *+CH3OH+H2O | -188.42 | 3.23 | 1.46 | -186.65 | -1.64 |

Table S2 Charge per atom of Cu-G3. MIN DIST = Minimum distance from nucleus to basin boundary

|  | X | Y | Z | CHARGE | MIN DIST | ATOMIC VOL |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 3.689066 | 6.449756 | 1.272905 | 3.851373 | 0.578938 | 28.417112 | 0.148627 |
| 2 | 1.183737 | 0.680924 | 1.352342 | 4.077504 | 0.601546 | 23.496492 | -0.0775 |
| 3 | 6.177465 | 2.130504 | 1.28145 | 3.819937 | 0.550823 | 28.388627 | 0.180063 |
| 4 | -0.071675 | 2.857742 | 1.34751 | 4.047599 | 0.510561 | 23.28571 | -0.0476 |
| 5 | 4.949696 | 4.299452 | 1.30352 | 3.979063 | 0.523316 | 25.494648 | 0.020937 |
| 6 | 1.295424 | 5.010578 | 1.29465 | 3.847781 | 0.585258 | 28.180694 | 0.152219 |
| 7 | 1.296555 | 6.440083 | 1.310588 | 4.116217 | 0.519216 | 27.421594 | -0.11622 |
| 8 | 3.683077 | 0.687624 | 1.327333 | 3.844417 | 0.563642 | 22.275951 | 0.155583 |
| 9 | 1.072796 | 2.067442 | 1.53085 | 4.201467 | 0.518736 | 24.605946 | -0.20147 |
| 10 | 0.059024 | 4.292682 | 1.316491 | 4.072258 | 0.542902 | 27.135329 | -0.07226 |
| 11 | 1.18957 | 5.015504 | 1.318227 | 3.827346 | 0.56113 | 22.344312 | 0.172654 |
| 12 | 1.204137 | 6.4497 | 1.271702 | 4.061655 | 0.554341 | 29.305814 | -0.06166 |
| 13 | 6.174343 | 0.696825 | 1.289191 | 4.061405 | 0.554914 | 29.469597 | -0.0614 |
| 14 | 3.79102 | 2.080771 | 1.448615 | 4.207745 | 0.610291 | 28.109484 | -0.20775 |
| 15 | 4.94999 | 2.862237 | 1.317689 | 4.137945 | 0.578167 | 22.904024 | 0.13795 |
| 16 | 2.44919 | 4.410884 | 1.441962 | 4.1126 | 0.532154 | 25.253958 | -0.1126 |
| 17 | 3.706421 | 5.021557 | 1.312905 | 4.246681 | 0.612587 | 23.114806 | -0.24668 |
| 18 | 2.454531 | 2.867108 | 2.51091 | 10.486979 | 0.768158 | 144.149227 | 0.513021 |

The valence of carbon atoms is positive 4. We can see that the valence of carbon atoms from 1 to 17 is about 4. The change of valence is caused by copper atoms. The atomic serial number is identified in Figure S1. No. 17 is a copper atom

Fig. S1 The atomic serial number of Cu-G3

Table S3 Charge per atom of Cu-G4. MIN DIST = Minimum distance from nucleus to basin boundary

|  | X | Y | Z | CHARGE | MIN DIST | ATOMIC VOL |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 3.846754 | 6.218992 | 2.299594 | 4.127713 | 0.56325 | 24.955536 | -0.12771 |
| 2 | 1.257219 | 0.737307 | 2.299392 | 3.927144 | 0.615299 | 24.632589 | 0.072856 |
| 3 | 6.390755 | 2.024589 | 2.299266 | 4.053457 | 0.552077 | 23.97812 | -0.05346 |
| 4 | 0.075506 | 2.760596 | 2.30072 | 4.276621 | 0.523468 | 24.278204 | -0.27662 |
| 5 | 2.496358 | 4.196488 | 2.301916 | 3.905929 | 0.537056 | 22.31337 | 0.094071 |
| 6 | 1.285876 | 4.931259 | 2.300048 | 3.785293 | 0.499931 | 22.324802 | 0.214707 |
| 7 | 2.551784 | 0.065314 | 2.300056 | 4.033009 | 0.527623 | 23.933822 | FALSE |
| 8 | 3.847229 | 0.736691 | 2.30011 | 3.94453 | 0.554003 | 24.574001 | 0.05547 |
| 9 | 1.182927 | 2.142609 | 2.298709 | 4.273949 | 0.458805 | 29.385344 | -0.27395 |
| 10 | 0.075224 | 4.196808 | 2.298042 | 4.008803 | 0.493751 | 22.176189 | -0.0088 |
| 11 | 1.183395 | 4.815475 | 2.300178 | 4.118183 | 0.55702 | 28.4608 | -0.11818 |
| 12 | 1.256797 | 6.218542 | 2.299915 | 3.777037 | 0.573012 | 23.305075 | 0.222963 |
| 13 | 6.390822 | 0.616429 | 2.299603 | 3.964879 | 0.534357 | 23.760917 | 0.035121 |
| 14 | 3.921039 | 2.141063 | 2.300959 | 4.264234 | 0.654637 | 29.040962 | -0.26423 |
| 15 | 5.179919 | 2.759404 | 2.29842 | 4.107765 | 0.542563 | 23.060721 | -0.10777 |
| 16 | 3.921902 | 4.815002 | 2.299502 | 4.064047 | 0.507448 | 28.323619 | -0.06405 |
| 17 | 2.55285 | 3.477905 | 2.299839 | 10.367425 | 0.771276 | 40.475581 | 0.632575 |

Fig. S2 The atomic serial number of Cu-G4