Supplementary Information for

Spectral evidence of Wigner crystallisation over a one-dimensional moiré superlattice under magnetic fields

Jufeng Wang1,3, Lingyun Wan1,3, Hongjian Du1,3, Chuanxu Ma1,2✉, Mingyang Tian1, Junyao Li1, Wei Hu1,2✉, Shijing Tan1,2, Yi Luo1,2, Jinlong Yang1,2, Bing Wang1,2✉, and J. G. Hou1

1Hefei National Research Center for Physical Sciences at the Microscale and Synergetic Innovation Center of Quantum Information & Quantum Physics, University of Science and Technology of China, Hefei, Anhui 230026, China

2Hefei National Laboratory, University of Science and Technology of China, Hefei 230088, China

3These authors contributed equally to this work: Jufeng Wang, Lingyun Wan, Hongjian Du.

✉Email: cxma85@ustc.edu.cn; whuustc@ustc.edu.cn; bwang@ustc.edu.cn

S1. Surface potential variation

S2. Efros-Shlovshi Coulomb gap

S3. Estimated upper limit of the effective Bohr radius aB

S4. Fitting of the splitting ELLs

Supplementary References

S1. Surface potential variation

Due to the bending region is induced by a monoatomic Cu(111) step, there may exist potential difference when crossing the bending region. This behavior is indeed observed in Fig. 2c. However, the potential change can only shift the Landau levels (LLs), but not create a gap-like feature. On the other hand, the potential change works both for the electron-like LLs (ELLs) and hole-like LLs (HLLs). However, only the ELL (Ne = 11) splitting is observed near site iii, while the HLLs do not show this feature, even no broadening. Therefore, we can safely exclude the origin due to surface potential change.

Supplementary Fig. 1 | Schematic drawing of the B-dependent double-peak gap induced by the continuous surface potential variation (dashed green curve), following the mechanism reported in Ref. 111111. Here, for simplification, the wave function of the 1st LL (N = 1) is considered.

Secondly, we exclude the possibility of B-dependent double-peak gap induced by the continuous surface potential variation. Following the mechanism reported in ref. 111111, we also consider the possibility of the continuous surface potential variation induced double-peak gap feature. As illustrated in Supplementary Fig. 1, for B2 > B1, the smaller ring radius (r2 < r1) will give a smaller double-peak gap (2 < 1) in the local density of states (LDOS), which is in contrary to our observation. Therefore, this mechanism can also be safely excluded in our experiment.

S2. Efros-Shlovshi Coulomb gap

In the partial filling scenario, the Coulomb interaction should play an important role. A possible reason for the splitting of the ELLs could be the Coulomb pseudogap2,3. However, in a two-dimensional electron gas (2DEG) system, the Coulomb pseudogap has a linear relation with the LDOSs at the EF, i.e., . In addition, more pronounced and wider splitting gaps for the HLLs should be simultaneously observed accompanying the appearance of the ELL splitting, because the hole pockets have the LDOSs higher than that of the electron pocket by six folds. Our observations are obviously different from these features. Therefore, we may rule out this possibility.

S3. Estimated upper limit of the effective Bohr radius aB

The effective Bohr radius  ≈ 3 nm, by adopting the effective mass of electron me* ~ 0.17m0 (Extended Data Fig. 2), with m0 the rest mass of electron, e the electron charge,  the vacuum permittivity, and  the relative dielectric constant of the bismuth film at zero field4,5. Here, the estimated value of  should be the upper limit of the Bohr radius since the effective mass me* is expected to increase, and the effective dielectric function  could decrease, both leading to the decrease of , due to the electron localization induced by the moiré potential and the increase of magnetic field.

S4. Fitting the splitting ELLs

We firstly summarize the full width at half maximum (FWHM) of the non-splitting ELLs at the normal regions away from the bending area, such as site i in Extended Data Fig. 7. The result is shown in Supplementary Fig. 2a. One can see that the peak widths are barely dependent on the magnetic field B, and show slight variation between 0.5 and 0.8 meV with an average value of about 0.6 meV. In order to obtain the splitting gap, the ELLs are fitted with two peaks with the similar area and the peak widths according to those acquired at site i (Supplementary Fig. 2a). For those ELLs close to the strong HLL peaks, the two split peaks together with one HLL peak are fitted together. Representative fitting examples are shown in Supplementary Fig. 2b. Typically, the ELL peak shows a width of around 0.6 meV at B = 8.3 T, suggesting a zero gap. By doing this, we obtain the splitting gaps of the ELLs at different B as shown in Fig. 3e and Extended Data Fig. 7j.

Supplementary Fig. 2 | Fitting of the splitting ELLs. a, Summary of the full width at half maximum (FWHM) of the non-splitting ELL peaks at normal regions (site i in Extended Data Fig. 7) away from the bending region. An average peak width (red line) of about 0.6 meV is obtained. b−f, Representative examples of the double-peak fitting of the splitting ELLs of site ii (Extended Data Fig. 7) at B = 8.3, 8.7, 9.6, 10.15, and 10.9 T, respectively. At B = 8.3 T, the ELL peak shows a width of around 0.6 meV, suggesting a zero gap.

Supplementary reference:

1.	Bindel, J. R., Ulrich, J., Liebmann, M. & Morgenstern, M. Probing the Nodal Structure of Landau Level Wave Functions in Real Space. Phys. Rev. Lett. 118, 016803, doi:10.1103/PhysRevLett.118.016803 (2017).

2.	Efros, A. L. & Shklovskii, B. I. Coulomb gap and low temperature conductivity of disordered systems. J. Phys. C: Solid State Phys. 8, L49–L51, doi:10.1088/0022-3719/8/4/003 (1975).

3.	Baranovskii, S. D., Efros, A. L., Gelmont, B. L. & Shklovskii, B. I. Coulomb gap in disordered systems: computer simulation. J. Phys. C: Solid State Phys. 12, 1023–1034, doi:10.1088/0022-3719/12/6/015 (1979).

4.	Harrison, M. J. Magneto-Attenuation of Sound in Semimetals: Longitudinal Waves. Phys. Rev. 119, 1260–1269, doi:10.1103/PhysRev.119.1260 (1960).

5.	Wu, C.-C. & Tsai, J. The effect of energy bands on the amplification of surface phonons in thin bismuth films. J. Phys.: Condens. Matter 1, 2851–2855, doi:10.1088/0953-8984/1/17/007 (1989).