Supporting　Information

# Effect of hydrophobic species on the oxygen reduction reaction on the high index planes of Pt3Fe

Akane Suzuki, Masashi Nakamura, Nagahiro Hoshi*

Department of Applied Chemistry and Biotechnology, Graduate School of Engineering, Chiba University, Yayoi–cho–1–33, Inage–ku, Chiba, 263–8522, Japan

Corresponding author

Nagahiro Hoshi

hoshi@faculty.chiba–u.jp

Fig. S1 CVs before and after THA+ modification in 0.1 M HClO4 saturated with Ar.

Scanning rate: 0.010 V s-1. (a) Pt3Fe(111), (b) Pt3Fe(775) = 7(111)–(111), (c) Pt3Fe(544) = 9(111)–(100). Black line: without THA+, blue line: after THA+ modification.

Fig. S2 CVs before and after IL modification in 0.1 M HClO4 saturated with Ar.

Scanning rate: 0.010 V s-1. (a) Pt3Fe(111), (b) Pt3Fe(775) = 7(111)–(111), (c) Pt3Fe(544) = 9(111)–(100). Black line: without IL, green line: after IL modification.

Table S1. Values of the charge of adsorbed hydrogen region QH and the coverage of hydrophobic species θ of the low index planes of Pt3Fe(111), Pt3Fe(775) = 7(111)–(111), Pt3Fe(544) = 9(111)–(100) before and after the modification with THA+, IL and melamine.

|  |  | QH/μCcm-2 | θ |
| --- | --- | --- | --- |
| Pt3Fe(111) | bare | 111 | － |
|  | THA+ | 85.0 | 0.23 |
|  | IL | 78.2 | 0.30 |
|  | melamine– adsorbed | 86.7 | 0.22 |
|  | melamine–added | 100 | 0.10 |
| Pt3Fe(775) | bare | 122 | － |
|  | THA+ | 74.9 | 0.38 |
|  | IL | 84.2 | 0.31 |
|  | melamine– adsorbed | 83.3 | 0.32 |
|  | melamine–added | 90.4 | 0.26 |
| Pt3Fe(544) | bare | 116 | － |
|  | THA+ | 102 | 0.12 |
|  | IL | 98.6 | 0.15 |
|  | melamine– adsorbed | 105 | 0.095 |
|  | melamine–added | 106 | 0.086 |

Fig. S3. LSVs before and after THA+ modification in 0.1 M HClO4 saturated with O2.

Scanning rate: 0.010 V s-1. (a) Pt3Fe(111), (b) Pt3Fe(775) = 7(111)–(111), (c) Pt3Fe(544) = 9(111)–(100). Black line : without THA+, blue line : after THA+ modification.

Fig. S4. LSVs before and after IL([MTBD][beti]) modification in 0.1 M HClO4 saturated with O2.

Scanning rate: 0.010 V s-1. (a) Pt3Fe(111), (b) Pt3Fe(775) = 7(111)–(111), (c) Pt3Fe(544) = 9(111)–(100). Black line: without IL, green line: after IL modification.