Supplementary Information

For

Extraction of non-noble metal columbite-tantalite as a highly efficient electrocatalyst for water splitting

Patrick M. Bacirhonde et al.

Calculation of Turnover frequencies of Gas adsorption using BET surface area

The BET = 42.8963 m2g−1 for WOCT. For HER,  = 190.2 mV (V vs RHE) at 10 mA cm-2. On the surface of WOCT (200), A(m2) = 1226.4 pm  8430.9 pm = 1.03  10-18m2 and we have 70 visibles atoms on the crystal structure (orthorhombic).

The total number of surface atoms = [70/ (1.03 × 10-18m2)]  (0.005g  42.8963 m2g−1) = 3.16 1019 atoms.

Turnover frequency of H2 production = [(10 mA/cm2  0.001  0.87cm2  6.022  1023 atoms/mol)] / [(96485.3 C/mol) (2) (3.16 1019 atoms)] = 0.87 sites s-1.

For oxygen, TOF was calculated at  = 284.84 mV (current density at 10 mA cm-2) = [(10 mA cm-2 × (0.001) × (0.89 cm2) × 6.022 × 1023 atoms/mol)] / [(96485.3 C/mol) (4)(3.16 × 1019 atoms)] = 0.44 sites s-1.

SUPLLEMETARY TABLES

Supplementary Table 1: Representative compositions of the coltan ore using X-ray fluorescence spectroscopy measurements.

| Major elements | Contents (%) |
| --- | --- |
| F | 0.939 |
| Na2O | 0.546 |
| MgO | 1.46 |
| Al2O3 | 6.71 |
| SiO2 | 15.7 |
| P2O5 | 0.238 |
| SO3 | 0.0206 |
| K2O | 2.22 |
| CaO | 5.46 |
| TiO2 | 3.21 |
| MnO | 0.546 |
| Fe2O3 | 8.44 |
| Rb2O | 0.275 |
| SrO | 0.274 |
| ZrO2 | 0.514 |
| Nb2O5 | 5.80 |
| SnO2 | 7.44 |
| BaO | 0.296 |
| HfO2 | 0.141 |
| Ta2O5 | 38.7 |
| PbO | 1.19 |
| U3O8 | 0.683 |
| Mass % | 100 |

| Oxide form | Peaks positions and miller indices |
| --- | --- |
| Ta2O5 | 15 (110), 24 (020), 29 (220), 30 (202), 35 (022), 49 (422), 53 (004), 60 (242). |
| Nb2O5 | 22 (001), 29 (100), 46 (002) and 55 (102) |
| MnO | 20 (100), 22 (110), 43 (050), 53 (201), 74 (321) |
| Fe2O3 | 25 (012), 34 (104), 37 (110), 51 (024), 56 (116) |
| Mn2Ta | 24 (101), 37 (110), 44 (112), 56 (203) |
| Fe0.24Mn0.76Nb2O6 | 24 (310), 30 (311), 35 (002), 51 (330), 53 (621), 60 (313), 63 (332) |

Supplementary Table 2: Oxides forms and their peaks positions (hkl indices)

Supplementary Table 3: Calculated peaks, FWHM and d(spacing)

| Peak position | FWHM | Miller indice | Theta () | d (Spacing) |
| --- | --- | --- | --- | --- |
| 18.26331 | 0.37014 | 110 | 9.131655 | 4.853703 |
| 23.10498 | 4.86425 | 111 | 11.55249 | 3.846392 |
| 30.05942 | 0.62724 | 180 | 15.02971 | 2.970463 |
| 32.61318 | 0.30074 | 200 | 16.30659 | 2.743457 |
| 36.90606 | 0.60884 | 201 | 18.45303 | 2.433599 |
| 36.90606 | 2346.54001 | 202 | 18.45303 | 2.433599 |
| 56.95608 | 206544.3749 | 002 | 28.47804 | 1.615488 |
| 56.95608 | 0.39071 | 422 | 28.47804 | 1.615488 |
| 58.21814 | 0.35541 | 440 | 29.10907 | 1.583436 |
| 70.88718 | 58.32215 | 531 | 35.44359 | 1.32833 |
| 77.84268 | 0.39841 | 321 | 38.92134 | 1.226099 |
| 77.84268 | 136.11545 | 128 | 38.92134 | 1.226099 |

SUPPLEMETARY FIGURES

Supplementary Figure 1: Field emission scanning electron microscopy (FESEM) and mapping of coltan.

Supplementary Figure 2: SEM images of WOCT-135, WOCT-1050, WOCTs and WOCT

Supplementary Figure 3: SEM image, element mapping and Energy dispersive x-ray spectroscopy (EDS) analysis of WOCTs (hydrothermal synthesis)

Supplementary Figure 4 Different HRTEM image taken from 20, 10, 5 and 2nm of WOCT

Supplementary Figure 5: (a) HER onset, b Cdl investigation c HER, d OER after IR correction

Supplementary Figure 6: SEM image of WOCT after 32 hours electrolysis

Supplementary Figure 7: XRD after electrolysis experiment

Supplementary Figure 8: Optimized bulk structure of (a) FeTa2O6 and (b) Fe0.75Mn0.25Ta1.875Nb0.125O6 with their corresponding relaxed unit cell parameters.

Supplementary Figure 9: Optimized structure of (a) FeTa2O6(100) and (b) Fe0.75Mn0.25Ta1.875Nb0.125O6(100) with surface used to model the HER and OER processes

Supplementary Figure 10: illustration of extraction process