# Supplementary Material

In-situ inorganic nano-hybrid strategy to facilely fabricate high flame-safety epoxy resin by inorganic phosphorus/boron-layered double hydroxide complexes

Zhu-Bao Shaoa, Tian-Ci Wanga, Xue-Bao Linb*, Xiang Songa, Jing Cuia, Longxiang Zhua*

aInstitute of Functional Textiles and Advanced Materials, National Engineering Research Center for Advanced Fire-Safety Materials D & A (Shandong), College of Textiles and Clothing, State Key Laboratory of Bio-Fibers and Eco-Textiles, Qingdao University, Ningxia Road, 308, Qingdao 266071, China

bIMDEA Materials Institu te, C/Eric Kandel, 2, Getafe, Madrid, 28906, Spain

Corresponding authors:

*Xue-Bao Lin, Email: xuebao.lin@imdea.org;

*Longxiang Zhu, Email: lxzhu@qdu.edu.cn;

Fig. S1. The morphology of B-LDH@APP (a) and corresponding elements mapping of full (b), P (c), Ni (d), Co (e), and B (f)

Fig. S2. The heat release rate (a), total heat release (b), and mass loss (c) curves of corresponding B-LDH@APP/EPs.

Fig. S3. The smoke production rate (a) and total smoke production (b) curves of corresponding B-LDH@APP/EPs.

Table S1. CC data of corresponding B-LDH@APP/EPs

| Sample | 1B-LDH@APP/EP | 2B-LDH@APP/EP | 3B-LDH@APP/EP | 4B-LDH@APP/EP |
| --- | --- | --- | --- | --- |
| TTI (s) | 65 | 65 | 64 | 63 |
| Peak HRR (kW/m2) | 742 | 641 | 505 | 482 |
| Time to PHRR (s) | 140 | 142 | 200 | 201 |
| FGR (kW/m2.s) | 5.3 | 4.5 | 2.5 | 2.4 |
| THR (MJ/m2) | 64.1 | 67.5 | 68.4 | 71.0 |
| Peak SPR (m2/s) | 0.22 | 0.21 | 0.21 | 0.18 |
| TSP (m2) | 22.5 | 20.8 | 24.8 | 25.4 |
| Residue (%) | 18.9 | 19.7 | 21.0 | 25.3 |