SUPPLEMENTARY INFORMATION

Piezo-phototronic Effect in Centro-symmetric BiVO4 Epitaxial Films

Pao-Wen Shao1,2, Heng-Jui Liu3, Yuanwei Sun4,5, Mei Wu4,5, Ren-Ci Peng6, Meng Wang7, Fei Xue8, Xiaoxing Cheng8, Lei Su11, Hsiao-Wen Chen15, Meng-Chin Lin16, Qian Zhuang18,19, Jiawei Huang18,19, Yachin Ivry9,10, Hsiang-Lin Liu15, Yu-Jung Lu2, Shi Liu18,19,20, Pu Yu7, Long-Qing Chen8, Peng Gao4,5, Xiaoqing Pan11,12,13, Yung-Jung Hsu1, Jyh-Ming Wu16,17, Yi-Chun Chen14, and Ying-Hao Chu1,21*

*Correspondence to: yhc@nctu.edu.tw

This file includes:

Materials and Methods

Supplementary Text S1 to S5

Figure S1 to S24

References (35-47)

Materials and Methods

Sample preparation

BVO epitaxial film was deposited on YSZ substrate via pulsed laser deposition.35 YSZ substrates were pre-annealed at 1300℃ for 8 hrs. The atomic step surface of substrate could be obtained and is shown in Figs. 1. The KrF excimer laser (λ = 248 nm, COMPex 102, Coherent) was operated at laser fluence of 1 J/cm2 using commercial BVO target. The deposition temperatrue was kept at 550℃ and an oxygen pressure was maintained at 60 mTorr. After the deposition, the cooling rate was 25℃/min.

Figure S1. Three dimensional topography of pre-treated YSZ substrate. The scanning size is 5 μm × 5 μm.

X-ray diffraction

XRD investigation was performed at Bruker D2 Discover XRD System with Cu Kα x-ray (λ = 1.5406 Å) to obtain the 2θ-θ scan along normal direction at room temperature. The temperature dependent RSMs were conducted by synchronism based high-resolution 8 circle diffractometer at beamline 17B at the National Synchrotron Radiation Research Center in Hsinchu, Taiwan. The incident beam with energy of 10 keV and size 0.3 × 0.7 mm2 was adopted. These RSMs were recorded in reciprocal lattice unit that is normalized by referencing (001)-oriented YSZ substrate.

Electron microscopy characterization and analysis

The cross-sectional TEM specimen was thinned to less than 30 μm first by mechanical polishing. The subsequent argon ion-beam milling was carried out using PIPSTM (Model 691, Gatan Inc.) with the accelerating voltage of 3.5 kV until a hole was made. Low voltage milling was performed with accelerating voltage of 0.3 kV to remove the surface amorphous layer. Part of HAADF–STEM images were recorded at an aberration corrected FEI (Titan Cubed Themis G2) operated at 300 kV. The convergence semi-angle for imaging is 30 mrad, the collection semi-angles snap is 39 to 200 mrad. GPA are based on the STEM image using Gatan Microscopy Suite software. The TEM specimens used for plane-view were prepared by focused ion beam equipment (GAIA3 GMH SEM-FIB, Tescan). HAADF and ABF images were collected by a double aberration­corrected STEM (JEM ARM300CF, JEOL) operated at 300 kV. All high-resolution ABF images were raw data without any post filtering. The in-situ evolution of the twin domains was recorded with a TEM (JEM-2100F, JEOL), operating at temperatures ranging from room temperature to 300℃.

Piezoresponse force microscopy and conductive atomic force microscopy

PFM was carried out on a commercial SPM system (Asylum Research MPF-3D) using commercial Platinum coating tips (mikromasch HQ:NSC36/PT, cantilever C, resonance frequency = 65kHz) for room temperature and diamond tips (Adama AD-2.8-AS, resonance frequency = 65kHz) for high temperature analysis, because single crystal diamond conducting probe display superior durability and stable resolution. Fig. 2b and Figs. 10 and Figs. 11 were collected at the in-plane contact resonance frequency (about 680 kHz) at DART mode with AC tip bias of 1.5 V. Fig. 3d, e, f and Figs. 18 were performed by vector PFM with out-of-plane contact resonance ~300 kHz and lateral resonance ~680 kHz at 1.5V ac tip bias. CAFM was performed on a commercial SPM system (Bruker MultiMode 8 SPM system) and the light source was 405 nm laser pointer. Gold commercial tips (Rocky Mountain 25PT400B) were used for photo-current detection.

Photodeposition

HAuCl4 was chosen for the precursor because the reduction potential of HAuCl4 to Au is lower than the conduction band of BVO.36 40 μM HAuCl4 was prepared for precursor, and the stirring speed was kept at 300 rpm. 20 μl ethanol was added as hole scavenger. BVO/YSZ sample was immersed in the precursor, perpendicular to the simulated light incident direction. The energy intensity of simulated light was 50 mW/cm2 while the reaction time was 15 mins. After the reaction, the sample was rinsed with deionized water and ultrasonic cleaner for 1 sec.

Photodegradation

The BiVO4 were mixed with the Rhodamine B (RhB) solution (10 ppm) to evaluate their degradation activity. Before the degradation test, the absorption effect was evaluated by placing BVO sample in the dye solution under a dark environment for 15 min. Thereafter, the experiments were carried out under the three different conditions of light illumination (with a 150 W Xe lamp), ultrasonic vibration (at 300 W with 40 kHz) and applied light irradiation with simultaneous ultrasonic vibration to simulate photo-catalysis, piezo-catalysis, and piezo-photo-catalysis, respectively. Degradation activity (i.e., concentration of RhB) was measured by absorption spectrum using an UV-vis photospectrometer (Hitachi, U3900).

Electron Paramagnetic Resonance Spectroscopy

The reactive species created by the piezocatalyst were detected by the electron paramagnetic resonance (EPR) technique with BRUKER E-580 spectrometer. First, a 0.5*0.5 cm2 sample was placed in a bottle with 10 mL DI water and 1.2 mL 5,5-dimethyl-1-pyrroline N-oxide (DMPO) solution. After ultrasounds of 3, 10, 20 min, the piezoelectrically generated •OH radicals were trapped by DMPO to form DMPO•-OH.

Phase-field modeling

In the phase-field simulations, four order parameters of 1, 2, 3, and 4, for four variants of M-phase were used. The total energy of the BVO film consists of bulk energy, gradient energy, and elastic energy is expressed as,

where fbulk consists of polynomial of ,  and (i ,j =1,2,3,4, but ij), fgradient consists of the gradient of i (i =1,2,3,4), and felastic can be expressed by (i.e., eij is elastic strain). The simulated 3D grids of 256 x  256 y  36 z with x =y =z=1 nm are used to describe a 3D constrained system consisting of the bottom substrate layer (=12z), BVO thin film (=20z) and the top air layer (=4z). Thin film boundary conditions were utilized. A spectral iteration method for heterogeneous system was used obtain the elastic solution. 37,38

DFT calculations

First-principles DFT calculations were carried out using QUANTUM-ESPRESSO package 39 with PBEsol ultrasoft pseudopotentials taken from the Garrity, Bennet, Rabe, Vanderbilt high-throughput pseudopotential set40. The supercell containing two twin domain walls has 288 atoms. The cell dimensions are fixed to values determined based on optimized lattice constants of orthorhombic unit cell of BVO, following the same protocol in Ref. 41.  Given the large supercell size, the structure was optimized using a plane-wave cutoff of 40 Ry, a charge density cutoff of 200 Ry, a Marzari–Vanderbilt smearing of 1 mRy, and the Gamma-point algorithm. The atoms are fully relaxed until the force is below 1.0 × 10−4 Ry/Bohr.

Supplementary Text and Figures

S1. First-principles density functional theory (DFT) calculations with quantified polarization.

The presence of strain gradient at twin domain walls hinting at the emergence of spontaneous polarization is confirmed by our first-principles density functional theory (DFT) calculations. We found that Bi and V atoms at the interfaces between A/B domains are displaced appositively with respect to their surrounding oxygen cages along the domain walls, respectively. To quantify the net polarization, we calculated the dipoles (𝜇) centered at Bi and V atoms as 𝜇 =dZ where d is the atomic displacement and Z is the Born effective charge. As shown in Figs. 2, the polarization arising mainly from Bi displacements emerges only at domain walls. Interestingly, neighboring domain walls have antiparallel polarization orientations. However, this model assumes the γ angle is 90°, and therefore, the polarization direction is parallel to domain wall direction.

Figure S2. Local electrical dipoles centered at V and Bi atoms across the supercell containing two domain walls. The red arrows represent the net polarization.

S2: Calculated strain gradient at the center of domain wall:

The deformation between A and B domains at domain walls is plotted from top view in Figs. 3. From the phase transition, the strain gradient concentrates at domain wall. In this calculation, we consider the strain from transition of lattice constant and γ angle, whereas the deviation angle φ of BVO from [100]YSZ was ignored.

Figure S3. Schematics for the estimated strain gradients at ferroelastic domain walls and the induced piezoresponse. The green box represents the structure transition across domain wall.

In order to calculate the strain tensor perpendicular and parallel to domain wall, the three-dimensional Cartesian coordinate system was rotated respect to the x axis for -35°. The transformed matrix ε’ was obtained by manipulating rotation matrix listed below.42

,

On the other hand, the strain from phase transition could be listed by the lattice deformation from tetragonal to monoclinic one. λ and ν represent normal strain while μ represents shear strain.

,  ,

Figure S4. Strain tensors of A1 and Bii monoclinic unit cells with the reference of tetragonal unit cell (gray cube).

Thus, the strain tensor across domain wall could be obtained by matrix addition. In addition, from PFM signal in Fig. 2b, the piezoresponse appears between each domain wall along four directions. Based on Figs. 8, the adjacent domains match each other if B domain is rotated by 90.37° (1.07°+89.3°) counterclockwise. Thus, we assume the piezoelectric domain wall is created between A1 to Bii domain, A3 to Biv domain, A2 to Bi domain, and A4 to Biii domain. Due to the ignorance of deviation angle φ of BVO from [100]YSZ, the strain tensor equals to , and equals to . The 35° domain wall refers to the strain tensor. Manipulated by rotation matrix, the resulted normal strain and shear strain are listed below.

,

In consequence, the calculated normal and shear strain gradient are obtained over the domain wall length (~ 5nm from Fig. 2i).

,

The shear strain gradient is comparable with the observed one (~5×106 m-1 in Fig. 2g,), while the normal strain gradient is below the noise level.

S3: substrate clamping effect.

Note that instead of substrate clamping effect, YSZ substrate provides a compatible platform for the systematic distribution of multidomain because twin domains in BVO also appear stably without substrate during the preparation of TEM specimens and in bulk form.43

S4: piezoelectrically induced open-circuit voltage across twin domain walls (Vx):

To model the open-circuit voltage across twin domain walls, we assume ultrasonic vibration stimuli create in-plane stress field in aqueous solution. Thus, combined with in-plane piezoresponse at domain wall, the open-circuit voltage across domain walls is calculated by piezoelectric model with electrode/piezoelectric material/electrode structure, and the induced polarization Pj from stress and the open circuit voltage Vj are:

,

,

where dij, σij, εr, ε0, A, and w represents piezoelectric constant, stress tensor, relative dielectric constant, vacuum permittivity, effective area, and the distance between parallel electrodes. Thus, the piezo-voltage could be concluded as .

For BVO, the relative dielectric constant is 6844. On the other hand, we assume the w equal to the twin domain wall width ~5 nm from Fig. 2i. The measured effective d31~15 pm/V and the stress during the vibration could be as high as 2 MPa from collapsing bubbles in water. 45 Thus the induced open-circuit voltage across each domain wall is ~0.25 mV.

S5: generating continuous radicals by ultrasonic vibration.

For normal piezoelectric materials, polarization decreases under compressive strain because the displacement of ion reduces. However, for flexoelectric BVO, the compressive strain increases the strain gradient () as well as flexo-polarity () at BVO domain wall region, and thus it further attracts more screen charges (i.e., electrons and holes) accumulating at surface respectively to reach charge neutrality. During the strain relaxation process, the polarization reduced to P2, and thus the excess charges released from surface and react with oxygen and water, resulting in superoxide anions (•O2-) and hydroxyl radicals (•OH). Likewise, after reaching maximum tensile strain with minimum polarization P3, when applying compressing strain again, the polarization increases to P4 and the screen charges is produced with the outcome of radicals as well. Therefore, the persistent reactive radicals generate with continuous mechanical vibration.

Figure S5. Piezo-catalytic radicals generated by cycling mechanical vibration. The schematic diagrams of screen charges distribution with different instant polarization are at a, P1, b, P2, c, P3, d, P4.

Figure S6. cross-sectional HAADF-STEM image, the corresponding FFT patterns of heteroepitaxial BVO/YSZ taken along [010]YSZ zone axis and the schematic diagram of epitaxial relationship of multidomain.

Figure S7. a, Illustration of in-plane deviation angles of monoclinic BVO (φ and 2φ, φ=0.4°) from [100]YSZ. (Intensity from low to high: blue-green-yellow-red). b, schematic image of 8 in-plane structural BVO domains configuration according to RSM result (monoclinic I2/a, a=5.204 Å, b=5.101 Å, c=11.69 Å, γ=89.6°, and I2/b, a=5.204 Å, b=5.101 Å, c=11.69 Å, γ=90.4°). The dash line represents the lattice of YSZ substrate (cubic, a=5.153Å).

Figure S8. Plane-view STEM. a, High angle annular dark field (HAADF)-STEM image and the FFT pattern of each domain. b, The corresponding fast Fourier transform (FFT) image of two adjacent domains.

Figure S9. Rate constant of piezo-photo-degradation by linear fitting. Degradation reaction of RhB follows first order kinetics. Thus, the reaction rate equation is  ,  and the integration form is: , where A is constant of integration. Table S1 shows the rate constant with different condition. The piezo-phototronic effect (i.e., with vibration under illumination) shows superior degradation activity, whose rate constant is 10 folds higher than that of photo-catalytic property. In addition, piezo-degradation dominates the degradation effect compare to photo-degradation in thin film structure.

| Reaction condition | First order kinetics equation | Rate constant (min-1) |
| --- | --- | --- |
| Dark |  | 3.239E-4 |
| Light |  | 1.170E-3 |
| Dark with vibration |  | 8.580E-3 |
| Light with vibration |  | 1.252E-2 |

Table S1. First order kinetics equation and the rate constant of piezo-photo-degradation under different reaction condition.

Figure S10. Angular-resolved lateral PFM was carried out at different angles between the [010]YSZ axis and AFM cantilever. In-plane PFM phase and at different sample rotation angles of a, 20°, b, 70°, c, 110° and d, 160°. The scanning size is 1.2 μm × 1,2 μm. e, The distribution of piezoresponse direction. f, The according angle between piezoresponse (dotted line) and twin domain (solid line) direction. The lateral piezoresponse is resulted from the torsion of cantilever, thus the piezoresponse and the contrast of phase signal reach their minimum when the direction of piezoresponse is parallel to the cantilever long axis. As a result, the distribution of piezoresponse direction could be summarized in e and f. The angle between piezoresponse and twin domain direction is 35°. Moreover, the magenta circles in a and d display the reverse of contrast, which expresses the signal is attributed from piezoresponse rather than other artifacts.

Figure S11. Out-of-plane and in-plane of PFM signals. a, Surface of BVO/YSZ. b, Out-of-plane phase. c, Out of plane amplitude at resonance ~300 kHz. d, In-plane phase. e, In-plane amplitude at lateral resonance ~680 kHz. These results were performed by vector PFM. Note that the out-of-plane amplitude is weaker than in-plane one at the same tip bias.

Figure S12. GPA of plane view STEM along [001]YSZ zone axis. a, STEM image. b, FFT of the area. (220) and (220) were selected as g1 and g2 for analysis. The according c, ɛxx, d, ɛyy, e, ɛxy and f, ωxy. ɛxy and ωxy both express the strain gradient across the domain walls. In previous simulation study, the remaining shear strain46 is responsible for the formation of W’ twin domain walls in BVO. g. Shear strain, rotational strain, and h shear strain gradient distribution along the direction perpendicular to the twin domain walls marked by yellow arrow in e and f.

Figure S13. a, HAADF image of the BVO/YSZ along [010]YSZ zone axis. From left to right: surface, BVO, and YSZ substrate. b, FFT image. (004) and (200) facets of BVO were selected as g1 and g2 for analysis. GPA of BVO/YSZ along c, out of plane direction εxx and d, in-plane εyy. The strain gradient at domain walls is a universal characteristic through the film. It demonstrates again that the lattice misfit is along in-plane direction throughout the film rather than surface effect or substrate clamping effect, and the in-plane lattice misfit across the domain is about 2%. This result is comparable with the misfit calculated () based on the lattice parameters of monoclinic phase of BVO.

Figure S14. Surface morphology and twin domain width dependence on film thickness. The thickness is a, ~29.5nm. b, ~98.5nm. c, ~172nm. d, ~246nm. The thickness was obtained from the cross-sectional image of BVO/YSZ thin film. The contrast scale bar is 6 nm. The dependence of thickness is summarized in e.

Figure S15. High temperature RSM analysis of BVO (400) with YSZ (400) reference at a, 130℃, b, 225℃ and c, back to room temperature.

Figure S16. Plane-view TEM with temperature variation. a, 25℃. b, 100℃. c, 150℃. d, 200℃. e, 250℃. f, 275℃. g, 300℃. h, 25℃. The domain structure was captured at fixed temperature and the red dot is a reference point. The strain releasing process was observed at 250℃.

Figure S17. As-grown surface signal with temperature variation. a, 25℃. b, 100℃. c, 200℃. d, 230℃. e, 260℃. f, 275℃. g, 25℃.

Figure S18. In-plane PFM signal with temperature variation. a, 25℃. b, 100℃. c, 200℃. d, 230℃. e, 260℃. f, 275℃. g, 25℃. Evidently, the domains remain stable until 100℃. At 200 ℃, the circled area shows a 90o rotation. This phenomenon becomes more obviously with an increase of temperature. The temperature dependence results were performed at vector PFM mode. Few days after the experiment, in-plane phase signal is still identical to g, representing that the rotation of domain after phase transition is stable.

Figure S19. Phase field simulation. To understand the evolution of ferroelastic twin domains in BVO/YSZ heterostructure, the phase-field simulation was employed. There are two conclusions: (i) variant 1 (red color) and variant 2 (blue color) form a striped-like twin-domain configuration, while variant 3 (yellow color) and variant 4 (green color) form the other one; (ii) every variant reveals two perpendicular orientations, arising from mechanically compatible ferroelastic domain walls. (e.g., each of them belongs to non-crystallographic S-type wall 47). Ferroelastic twin domains from phase-field simulations results are consistent with those of the experimental results from Fig. 2b. The spontaneous strain during phase transition from tetragonal BVO to monoclinic BVO induced the formation of four orientations of ferroelastic twin domains. 48 Also, the orientation angles of twin domain walls for variant 1 and 2, and for variant 3 and 4 are about 35 and 55 from phase-field simulations.

Figure S20. EPR of a, vibration and b, vibration under illumination. The intensity of peaks represents the intensity of hydroxyl radicals (‧OH) captured by 5,5-dimethyl-1-pyrroline N-oxide (DMPO) scavenger. The piezo-catalytic effect is demonstrated in a, revealing increasing intensity of radicals with time. In comparison, piezo-phototronics effect with higher intensity at 10 mins further promotes the catalytic property. However, not much difference could be observed at 20 mins. We think it is because the light absorption depth (i.e., thickness) of BVO thin film is only 200 nm, thus the piezo-catalytic effect dominates the generation of radicals in this study. And the same conclusion could be addressed in table S1.

Figure S21. a, YSZ surface and b, BVO/YSZ surface after piezo-reduction. c, BVO/YSZ surface after photo-reduction with 20 mins. Obviously, there is no gold nanoparticles reduction on YSZ surface in comparison to BVO/YSZ at same contrast of scale, showing that the piezo-reduction only appears at BVO/YSZ with piezoresponse. In addition, the deposition of gold nanoparticles on BVO/YSZ shows low dependence on twin domains in comparison to photo-reduction one at c. The main reason is because both superoxide anions (O2-) and hydroxyl radicals (•OH) participate the photoreduction process and the continuous production of reactive radicals from screen charges occurs on both domains described at supplementary text S5.

Figure S22. The optical property of BVO samples with twin domains and without twin domains. The bandgap is almost identical, revealing the absorption activity is also identical.

Figure S23. The periodicity of a, the surface after photoreduction; b, clean surface; c, in-plane PFM phase signal at DART mode with 1.5Vac; d, periodicity calculated by FFT. AFM surface after photoreduction was collected by tapping mode scanning while the clean surface was obtained by contact mode, which could effectively remove Au nanoparticles.

Figure S24. Conducting AFM. a, Schematic diagram of the experimental setup and the in-plane photo-current flow generated by 405 nm point laser. b, Topography, and c, dark current acquired at 8 V sample bias. d, Photo-current acquired at 8V sample bias. e, The corresponding PFM in-plane phase signal at 1.5 Vac. A platinum electrode was constructed on the BVO/YSZ surface, and the photoconductivity dependence on twin domains is demonstrated in d. The photocurrent result displays highest current at the boundary from topography, but it also shows the specific domain displays higher current with periodicity. This result is attributed to the photoconductivity related with piezoresponse effect, demonstrating upper domain wall area (B domain) reveals higher conductivity. This result implies that the flexoelectric effect inside domain walls enhances conductivity at B domain area.

References

35	Huang, Y.-L. et al. Pulsed laser deposition of complex oxide heteroepitaxy. Chin. J. Phys. 60, 481-501, doi:https://doi.org/10.1016/j.cjph.2019.05.030 (2019).

36	Chen, Y., Ma, X., Li, D., Wang, H. & Huang, C. Mechanism of enhancing visible-light photocatalytic activity of BiVO4 via hybridization of graphene based on a first-principles study. RSC Advances 7, 4395-4401, doi:10.1039/C6RA25721F (2017).

37	Hu, S. Y. & Chen, L. Q. A phase-field model for evolving microstructures with strong elastic inhomogeneity. Acta Mater. 49, 1879-1890, doi:https://doi.org/10.1016/S1359-6454(01)00118-5 (2001).

38	Chen, L. Q. & Shen, J. Applications of semi-implicit Fourier-spectral method to phase field equations. Comput. Phys. Commun 108, 147-158, doi:https://doi.org/10.1016/S0010-4655(97)00115-X (1998).

39	Giannozzi, P. et al. QUANTUM ESPRESSO: a modular and open-source software project for quantum simulations of materials. J. Phys.: Condens. Matter 21, 395502, doi:10.1088/0953-8984/21/39/395502 (2009).

40	Garrity, K. F., Bennett, J. W., Rabe, K. M. & Vanderbilt, D. Pseudopotentials for high-throughput DFT calculations. Comput. Mater. Sci. 81, 446-452, doi:https://doi.org/10.1016/j.commatsci.2013.08.053 (2014).

41	Meyer, B. & Vanderbilt, D. Ab initio study of ferroelectric domain walls in PbTiO3. Phys. Rev. B 65, 104111, doi:10.1103/PhysRevB.65.104111 (2002).

42	Yun, S. et al. Flexopiezoelectricity at ferroelastic domain walls in WO3 films. Nat. Commun. 11, 4898, doi:10.1038/s41467-020-18644-w (2020).

43	Yokota, H., Hasegawa, N., Glazer, M., Salje, E. K. H. & Uesu, Y. Direct evidence of polar ferroelastic domain boundaries in semiconductor BiVO4. Appl. Phys. Lett. 116, 232901, doi:10.1063/5.0010414 (2020).

44	Wee, S.-H., Kim, D.-W. & Yoo, S.-I. Microwave Dielectric Properties of Low-Fired ZnNb2O6 Ceramics with BiVO4 Addition. J. Am. Ceram. Soc. 87, 871-874, doi:https://doi.org/10.1111/j.1551-2916.2004.00871.x (2004).

45	Mattox, D. M. in Handbook of Physical Vapor Deposition (PVD) Processing (Second Edition)   (ed Donald M. Mattox)  475-527 (William Andrew Publishing, 2010).

46	Massad, J. E. & Smith, R. C. A Domain Wall Model for Hysteresis in Ferroelastic Materials. J. Intell. Mater. Syst. Struct. 14, 455-471, doi:10.1177/1045389x03035235 (2003).

47	Marton, P., Rychetsky, I. & Hlinka, J. Domain walls of ferroelectric BaTiO3 within the Ginzburg-Landau-Devonshire phenomenological model. Phys. Rev. B 81, 144125, doi:10.1103/PhysRevB.81.144125 (2010).

48	Fan, D. & Chen, L. Q. Computer simulation of grain growth using a continuum field model. Acta Mater. 45, 611-622, doi:https://doi.org/10.1016/S1359-6454(96)00200-5 (1997).