Supporting Information

Combined polyhexamethylene guanidine and nanocellulose for the conservation and enhancement of ancient paper

Xiaochun Maa, Shenglong Tiana, Xiaohong Lib, Huiming Fana, Shiyu Fu a,*

Contact information: State Key Laboratory of Pulp and Paper Engineering, South China University of Technology, Guangzhou 510640, China; *Corresponding author: shyfu@scut.edu.cn

aState Key Laboratory of Pulp and Paper Engineering, South China University of Technology, Guangzhou 510640, 18742057146@163.com (X.M.); slonet623@163.com (S.T.); hmfan@scut.edu.cn.

bGuangzhou Paper Co., Ltd, Guangzhou 510280, lixiaohong@gzpaper.cn.

*Corresponding author. Tel.: +13570017263. Email address: shyfu@scut.edu.cn

Supporting Table and Figure Captions

Fig. S1. The crystallinity (CrI) of treated and untreated paper fiber after accelerated aging.

Fig. S2. The photo of treated and untreated paper samples.

Table S1. The brightness and Chromatic aberration(ΔE) of treated and untreated paper samples after aging

Fig. S1.

Fig. S2.

Table S1. The brightness and Chromatic aberration(ΔE) of treated and untreated paper samples after aging

| Paper sample | Treatment conditions | L* | a* | b* | Brightness (%) | Chromatic aberration(ΔE) |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | UT | 77.46 | 0.88 | 15.78 | 39.420 | --- |
| 03 | 0# aged 3 days | 76.39 | 1.44 | 16.18 | 38.27 | 0.929 |
| 05 | 0# aged 5 days | 76.06 | 1.42 | 16.03 | 37.35 | 1.517 |
| 07 | 0# aged 7 days | 75.63 | 1.56 | 15.9 | 36.75 | 1.951 |
| 09 | 0# aged 9 days | 75.49 | 2.88 | 17.84 | 35.11 | 3.479 |
| 1 | T | 77.51 | 0.79 | 16.24 | 39.15 | 0.472 |
| 13 | 1# aged 3 days | 76.17 | 1.87 | 17.94 | 35.52 | 2.701 |
| 15 | 1# aged 5 days | 76.0 | 2.26 | 18.53 | 35.29 | 3.404 |
| 17 | 1# aged 7 days | 75.80 | 2.21 | 18.3 | 35.20 | 3.296 |
| 19 | 1# aged 9 days | 75.87 | 2.28 | 18.76 | 34.94 | 3.654 |