In silico investigation of a series of D-A-D structured chain thiophene photosensitizers for photodynamic therapy

Zheng-Kun Qin,a Xu-Hui Liu,a Hai-Han Zhang,a Xin Pu,b Ye Ji,a Jia-Yu Yang,a Xi-Lian Guo,a Jia Wang,a Ming-Xing Song,a* Fu-Quan Bai,b**

a College of Information Technology, Jilin Normal University, Siping 136000, People’s Republic of China.

b International Joint Research Laboratory of Nano-Micro Architecture, Chemistry, Laboratory of Theoretical and Computational Chemistry, Institute of Theoretical Chemistry, Jilin University, Changchun, 130023, People's Republic of China

*Correspondence author: Ming-Xing Song (E-mail: mxsong@jlnu.edu.cn) Tel.: +86-434-3292050; Fax: +86-434-3292050.

** Also for correspondence: Fu-Quan Bai (E-mail: baifq@jlu.edu.cn)

| Table of contents | Page no |
| --- | --- |
| Fig. S1 The obtained electron and hole diagrams for the work from (hcb)2TD to (ppx)2TDH in T1 state | S3-S6 |
| Fig. S2 The obtained electron and hole diagrams for the work from (hcb)2TD to (ppt)2TDH in T3 state | S7-S9 |
| Table S1 Bond parameters of all the researched molecules in water solution | S10 |
| Table S2 The lowest Vertical Singlet Excitation Energies (ΔE), Oscillator Strengths (f), Main Transitions, and Molecular Orbital Contribution (%) for all the Studied Complexes, Calculated in Water Solvent | S11 |
| Table S3 The triple excited state energies and properties of (hcb)2TD to (ppx)2TDH PSs | S12 |
| Table S4 The holes and electrons contribution more than 1% of the orbital output | S13-S14 |
| Table S5 Molecular coordinates after geometric coordinate optimization | S15-S43 |

Fig. S1 The obtained electron and hole diagrams for the work from (hcb)2TD to (ppx)2TDH in T1 state. (Green represents the electron distribution and blue represents the hole distribution)

(hcb)2TDH

(npc)2TDH

(dpl)2TDH

(ndipl)2TDH

(pt)2TDH

(ppt)2TDH

(px)2TDH

(ppx)2TDH

Fig. S2 The obtained electron and hole diagrams for the work from (hcb)2TD to (ppt)2TDH in T3 state (Green represents the electron distribution and blue represents the hole distribution)

(hcb)2TDH

(npc)2TDH

(dpl)2TDH

(ndipl)2TDH

(pt)2TDH

(ppt)2TDH

Table S1 Bond parameters of all the researched molecules in water solution

| Molecules | Bond length A1(Å) | Bond length A2 (Å) | Dihedral Angle θ1(°) | Dihedral Angle θ2 (°) |
| --- | --- | --- | --- | --- |
| (hcb)2TDH | 1.387 |  | -65.2/-64.3 |  |
| (npc)2TDH | 1.454 | 1.415 | -20.5/21.4 | 51.9/51.8 |
| (dpl)2TDH | 1.391 |  | -58.1/-58.2 |  |
| (ndipl)2TDH | 1.452 | 1.415/1.416 | 20.9/-21.8 | -37.2/-38.0 |
| (pt)2TDH | 1.399 |  | 86.3/86.5 |  |
| (ppt)2TDH | 1.454 | 1.436 | 18.4/18.9 | -83.9/-83.4 |
| (px)2TDH | 1.389 |  | -87.2/-86.5 |  |
| (ppx)2TDH | 1.454 | 1.428/1.419 | 22.3/-20.5 | -80.0/86.7 |

The bond length between the substituted linker and the attached acceptor part is A1 and the dihedral angle is θ1° The bond length between the original substituent and the benzene ring at the addition of the benzene ring is A2 and the dihedral angle is θ2°

Table S2 The lowest Vertical Singlet Excitation Energies (ΔE), Oscillator Strengths (f), Main Transitions, and Molecular Orbital Contribution (%) for all the Studied Complexes calculated in Water Solvent condition

| Molecules | Excitation energy (eV) | Wavelength (nm) | f | Main configuration |
| --- | --- | --- | --- | --- |
| (hcb)2TDH | 2.393 eV | 518.1 nm | f=1.7796 | H→L(69%) |
| (npc)2TDH | 2.211 eV | 560.7 nm | f=2.5231 | H→L(69%) |
| (dpl)2TDH | 2.253 eV | 550.1 nm | f=1.8527 | H→L(69%) |
| (ndipl)2TDH | 2.136 eV | 580.3 nm | f=2.7058 | H→L(68%) |
| (pt)2TDH | 2.148 eV | 577.0 nm | f=1.7698 | H→L(70%) |
| (ppt)2TDH | 2.235 eV | 554.7 nm | f=2.3616 | H→ L(69%) |
| (px)2TDH | 2.444 eV | 507.3 nm | f=1.6830 | H→L(70%) |
| (ppx)2TDH | 2.235 eV | 554.5 nm | f=2.3310 | H→L(63%) |

H = HOMO L = LUMO

Table S3 The triple excited state energies and properties of (hcb)2TD to (ppx)2TDH PSs

| Molecules | States | Excitation energy (eV) | λ (nm) | Main configuration |
| --- | --- | --- | --- | --- |
| (hcb)2TDH | T1 | 1.569 eV | 790.1 nm | H→L(71%) |
|  | T2 | 2.395 eV | 517.4 nm | H-1→L(69%) |
|  | T3 | 2.641 eV | 469.4 nm | H-2→L(70%) |
| (npc)2TDH | T1 | 1.400 eV | 885.6 nm | H→L(71%) |
|  | T2 | 2.134 eV | 579.8 nm | H-1→L(54%) |
|  | T3 | 2.416 eV | 513.0 nm | H→L+1(49%) |
| (dpl)2TDH | T1 | 1.455 eV | 851.9 nm | H→L(71%) |
|  | T2 | 2.197 eV | 564.1 nm | H-1→L(64%) |
|  | T3 | 2.558 eV | 484.5 nm | H-1→L+1(61%) |
| (ndipl)2TDH | T1 | 1.338 eV | 926.3 nm | H→L(70%) |
|  | T2 | 1.969 eV | 629.4 nm | H-1→L(64%) |
|  | T3 | 2.287 eV | 542.0 nm | H-2→L(69%) |
| (pt)2TDH | T1 | 1.615 eV | 767.9 nm | H→L(71%) |
|  | T2 | 2.250 eV | 550.9 nm | H-1→L(70%) |
|  | T3 | 2.250 eV | 550.8 nm | H-2→L(70%) |
| (ppt)2TDH | T1 | 1.431 eV | 866.2 nm | H→L(71%) |
|  | T2 | 2.050 eV | 654.9 nm | H-1→L(70%) |
|  | T3 | 2.050 eV | 657.7 nm | H-2→L(69%) |
| (px)2TDH | T1 | 1.617 eV | 766.5 nm | H→L(71%) |
|  | T2 | 1.881 eV | 658.9 nm | H-1→L(69%) |
|  | T3 | 1.882 eV | 658.7 nm | H-2→L(69%) |
| (ppx)2TDH | T1 | 1.431 eV | 866.2 nm | H→L(71%) |
|  | T2 | 1.679 eV | 738.2 nm | H-1→L(70%) |
|  | T3 | 1.680 eV | 737.9 nm | H-2→L(69%) |

Table S4 The holes and electrons contribution more than 1% of the orbital output

| Molecules | States | Tracks |  | Excitation |
| --- | --- | --- | --- | --- |
| (hcb)2TDH | T1 | HOMO | Hole:93.034 % | LE |
|  |  | LUMO | Electron:93.172 % |  |
|  | T3 | HOMO | Hole:93.529 % | LE |
|  |  | LUMO | Electron:93.352 % |  |
| (npc)2TDH | T1 | HOMO | Hole:89.828 % | LE |
|  |  | LUMO | Electron:90.118 % |  |
|  | T3 | HOMO-1 | Hole:41.309 % | LE |
|  |  | HOMO | Hole:32.170 % |  |
|  |  | LUMO | Electron:52.471 % |  |
|  |  | LUMO+1 | Electron:39.088 % |  |
| (dpl)2TDH | T1 | HOMO | Hole:89.845 % | LE |
|  |  | LUMO | Electron:91.418 % |  |
|  | T3 | HOMO-1 | Hole:57.184 % | LE |
|  |  | HOMO | Hole:24.983 % |  |
|  |  | LUMO | Electron:56.439 % |  |
|  |  | LUMO+1 | Electron:24.931 % |  |
| (ndipl)2TDH | T1 | HOMO | Hole:86.527 % | LE |
|  |  | LUMO | Electron:89.266 % |  |
|  | T3 | HOMO-1 | Hole:42.267 % | LE |
|  |  | HOMO | Hole:30.425 % |  |
|  |  | LUMO | Electron:42.089 |  |
|  |  | LUMO+1 | Electron:27.663 % |  |
| (pt)2TDH | T1 | HOMO | Hole:93.526 % | LE |
|  |  | LUMO | Electron:93.306 % |  |
|  | T3 | HOMO-1 | Hole:92.526 % | CT |
|  |  | LUMO | Electron:63.185 % |  |
|  |  | LUMO+1 | Electron:23.423 % |  |
| (ppt)2TDH | T1 | HOMO | Hole:91.48 % | LE |
|  |  | LUMO | Electron:90.543 % |  |
|  | T3 | HOMO-1 | Hole:96.263 % | CT |
|  |  | LUMO | Electron:52.805 % |  |
|  |  | LUMO+1 | Electron:26.964 % |  |
| (px)2TDH | T1 | HOMO | Hole:93.529 % | LE |
|  |  | LUMO | Electron:93.352 % |  |
|  | T3 | HOMO-2 | Hole:96.595 % | CT |
|  |  | LUMO | Electron:67.431 % |  |
|  |  | LUMO+1 | Electron:22.276 % |  |
| (ppx)2TDH | T1 | HOMO | Hole:91.329 % | LE |
|  |  | LUMO | Electron:90.608 % |  |
|  | T3 | HOMO-1 | Hole:43.441 % | CT+LE |
|  |  | HOMO | Hole:54.371 % |  |
|  |  | LUMO | Electron:54.862 % |  |
|  |  | LUMO+1 | Electron:26.922 % |  |

Table S5 Molecular coordinates after geometric coordinate optimization

| Molecules | geometric coordinate |
| --- | --- |
| (hcb)2TDH | C 8.01159500 0.01837400 1.06360700 C 5.51797700 0.02919100 0.59084900 C 7.26131900 0.09936700 2.20409200 C 5.87206500 0.11622700 1.93419000 C 3.40093100 0.10176000 1.53036900 C 4.12885400 0.01742600 0.35671900 C 3.20123300 -0.06477500 -0.85357100 C 1.84512800 -0.01809400 -0.15042900 C 2.00554700 0.08940700 1.22108600 C 0.49083400 -0.03444000 -0.52561300 C -0.40616500 0.05976600 0.54438500 C -1.91871000 -0.15711800 -1.19488300 C -1.76033300 -0.00826100 0.17299100 C -3.11814300 0.06636900 0.87065200 C -4.04399900 -0.07917000 -0.33581900 C -3.31281000 -0.21037400 -1.50315500 C -5.78140700 -0.28363900 -1.91005600 C -5.43255900 -0.11716100 -0.57283300 C -7.16916800 -0.35684900 -2.17774800 C -7.92478700 -0.22609100 -1.04549900 C 3.04181900 -3.75716400 -1.88551600 C 4.08645900 -3.85462400 -2.80978500 C 4.81390400 -2.69676900 -3.10992100 C 4.50766100 -1.48118600 -2.50509100 C 3.45994500 -1.38857700 -1.57906800 C 2.73289200 -2.54340900 -1.27371000 H 2.46262400 -4.64649200 -1.64170700 H 5.63093800 -2.75228800 -3.82764300 H 5.07900500 -0.59125100 -2.76224200 H 1.92214600 -2.49537500 -0.55062400 C 3.34746200 3.43316800 -3.44762700 C 3.91421800 3.46951300 -2.17018200 C 3.89611300 2.34842700 -1.34205700 C 3.31032500 1.15487800 -1.77484000 C 2.73741300 1.11473800 -3.05328000 C 2.75573800 2.23821600 -3.87431500 H 4.37999400 4.38964500 -1.82080500 H 4.34278900 2.40374700 -0.35235700 H 2.28971400 0.19062300 -3.41458900 H 2.30733800 2.19036500 -4.86545200 C -3.37335000 -1.10270400 1.82601700 C -2.62318300 -2.27790200 1.76874000 C -2.92734600 -3.36135200 2.59649000 C -3.99173100 -3.30286600 3.49862400 C -4.74535300 -2.12017900 3.54740300 C -4.44427900 -1.03833200 2.73011100 H -1.79225200 -2.35463100 1.07146200 H -2.31879200 -4.25905600 2.53005900 H -5.58089400 -2.05252600 4.24257000 H -5.03573900 -0.12742800 2.80129400 C -2.67568400 1.62203700 2.82620600 C -3.23618800 1.43174300 1.55606100 C -3.81575500 2.52758200 0.90946900 C -3.83882400 3.77967200 1.52158500 C -3.27974600 3.97494300 2.78800000 C -2.69851700 2.87534200 3.43078100 H -2.23056800 0.77813600 3.35029700 H -4.24930800 2.40417900 -0.07996900 H -4.29861600 4.62224200 1.00741000 H -2.25858600 3.00719100 4.41809800 C -11.46636100 -0.67146500 -0.34876200 C -10.11963000 -1.09034500 -0.24289600 C -9.75089600 -2.23781300 0.45221500 C -10.76787700 -2.97170700 1.06022300 C -12.11065200 -2.57159200 0.97152700 C -12.46738600 -1.42446900 0.26726300 C -11.47641700 0.53931200 -1.14533400 C -10.13516600 0.82074700 -1.49441400 C -9.78262100 1.93205400 -2.25272600 C -10.81125400 2.77336400 -2.67295000 C -12.15036600 2.50900700 -2.34432000 C -12.48980400 1.39529400 -1.58045200 H -8.71209900 -2.54885000 0.51519500 H -10.51473800 -3.87299200 1.61127400 H -12.87848000 -3.16681900 1.45703000 H -13.50859000 -1.11978700 0.19665700 H -8.74525400 2.13595700 -2.50223000 H -10.57025200 3.65115400 -3.26584000 H -12.92832400 3.18345100 -2.68990500 H -13.52726800 1.19568000 -1.32395800 C 11.54960900 -0.56183500 0.45485900 C 10.20183000 -0.99016900 0.43929900 C 9.82783500 -2.25197000 -0.01201900 C 10.84096400 -3.09537100 -0.46437700 C 12.18490800 -2.68934300 -0.46135800 C 12.54673000 -1.42561000 -0.00167500 C 11.56434200 0.78361200 0.99399700 C 10.22468000 1.13183800 1.28455900 C 9.87618500 2.37259500 1.80735600 C 10.90744800 3.27863900 2.04820200 C 12.24501900 2.95133800 1.77457500 C 12.58039300 1.70718700 1.24674700 H 8.78800600 -2.56600900 -0.00930700 H 10.58382400 -4.08762500 -0.82399200 H 12.94973200 -3.37163100 -0.82068200 H 13.58885000 -1.11592900 0.00327100 H 8.83988200 2.62408900 2.01430800 H 10.66972400 4.25749600 2.45495500 H 13.02506900 3.67957600 1.97635800 H 13.61674800 1.45845000 1.03210800 N -9.30766700 -0.18008000 -0.94613300 N 9.39395600 0.04355100 0.95005700 S 6.97073000 -0.03335900 -0.45251300 S 4.41455700 0.18841600 3.00629400 S 0.45837500 0.18876300 2.12548900 S -0.37185300 -0.20874100 -2.10284900 S -4.32061400 -0.40583500 -2.97238400 S -6.89077300 0.01076800 0.45764400 H 7.71438600 0.13182100 3.18866800 H -7.61721200 -0.51107000 -3.15304800 C 2.04630300 5.48871600 -4.06763000 C 3.31474900 4.66333000 -4.31588400 H 2.01994300 6.38372900 -4.69988100 H 1.15063400 4.89082600 -4.27822200 H 1.99300800 5.80552300 -3.01845200 H 3.36250600 4.37268700 -5.37466800 H 4.20093500 5.28208800 -4.11736100 C 3.57370100 -5.27688700 -4.81588100 C 4.37693800 -5.15305600 -3.51546600 H 3.81680500 -4.45266100 -5.49835700 H 3.78430600 -6.22212100 -5.32927900 H 2.49712300 -5.22931900 -4.60892800 H 4.13679300 -5.99686900 -2.85366300 H 5.45072800 -5.22171200 -3.73922200 C -4.36061700 -4.44507200 4.41802300 C -3.51047600 -5.70242100 4.28212600 H -4.31314900 -4.08536900 5.45773300 H -5.41788700 -4.70064700 4.24685000 H -3.56868600 -6.11665700 3.26783300 H -2.45542300 -5.49854200 4.50361200 H -3.85260200 -6.47589900 4.97809300 C -4.63701400 5.43740100 4.31417000 C -3.36130300 5.31410400 3.47214000 H -4.69689100 6.41222800 4.81172100 H -5.52710300 5.31673200 3.68388500 H -4.66751100 4.65553200 5.08357300 H -3.33778300 6.11614300 2.72132100 H -2.48142600 5.45662200 4.11499200 |
| (npc)2TDH | C -8.04988000 0.31234500 0.93263900 C -5.53902200 0.23359500 0.49350600 C -7.29726600 0.60259500 2.04478100 C -5.90717900 0.55766400 1.79619800 C -3.43214100 0.42383300 1.43680500 C -4.14976600 0.15329300 0.28366800 C -3.20895700 -0.13917800 -0.88387500 C -1.86024400 0.00772300 -0.18049200 C -2.03539500 0.32923500 1.15593400 C -0.50294400 -0.11717400 -0.52148800 C 0.38222000 0.10822000 0.53932400 C 1.91632600 -0.25117100 -1.15744000 C 1.74035000 0.03621600 0.18669800 C 3.08873700 0.17212800 0.89311300 C 4.03008200 -0.08089500 -0.28275800 C 3.31364800 -0.31529600 -1.44452900 C 5.79010200 -0.39014100 -1.81443500 C 5.41962500 -0.11996100 -0.50022200 C 7.18069800 -0.44753500 -2.05709800 C 7.93142300 -0.22999600 -0.92704800 C -2.95598900 3.06592900 -2.98096600 C -4.01123700 2.91429100 -3.88516800 C -4.77636600 1.74357100 -3.81817700 C -4.49641500 0.75804600 -2.87653900 C -3.43873800 0.91551400 -1.97068900 C -2.67333700 2.08384100 -2.03263800 H -2.34760800 3.96820600 -3.02012400 H -5.60242400 1.60703600 -4.51436800 H -5.09577500 -0.15021300 -2.85096500 H -1.85325400 2.22988300 -1.33382300 C -3.38392600 -4.24103000 -2.34040800 C -3.94579600 -3.89856300 -1.10680500 C -3.91924300 -2.58418000 -0.64335200 C -3.32956100 -1.57336500 -1.40856900 C -2.76149600 -1.91229700 -2.64392200 C -2.78828400 -3.22698900 -3.09989600 H -4.41354400 -4.67370000 -0.50174600 H -4.36132000 -2.34367100 0.32052400 H -2.31082100 -1.13646000 -3.26031400 H -2.34339400 -3.47434100 -4.06252700 C 3.34917500 1.58382800 1.42758100 C 2.62135800 2.68615200 0.96906600 C 2.92838500 3.97152500 1.41268700 C 3.96852800 4.19304400 2.32019600 C 4.70010100 3.08734100 2.76996300 C 4.39640500 1.80135700 2.33294100 H 1.80795900 2.53988200 0.26237600 H 2.34791000 4.81923400 1.05185400 H 5.51516900 3.23987900 3.47582500 H 4.96558500 0.95402900 2.71086000 C 2.59198600 -0.67911800 3.23136000 C 3.17932300 -0.90452400 1.97907000 C 3.75748200 -2.15215500 1.72613000 C 3.75111600 -3.14634200 2.70319000 C 3.16329000 -2.92755600 3.95264400 C 2.58527400 -1.67687200 4.20144500 H 2.14799400 0.29006300 3.45178300 H 4.21217700 -2.35084300 0.75869300 H 4.20912900 -4.11150500 2.49241100 H 2.12343000 -1.48681500 5.16908400 C 15.74176000 0.66053900 -0.21084200 C 14.37691000 1.03633600 -0.25930400 C 13.98070200 2.36957500 -0.16250200 C 14.97660600 3.32829000 0.00876900 C 16.33303800 2.97128400 0.07620400 C 16.72170200 1.63992900 -0.03760200 C 15.79321200 -0.77510600 -0.38096700 C 14.45810400 -1.22464500 -0.52953100 C 14.15317400 -2.57725000 -0.67625100 C 15.21389100 -3.47992500 -0.69650000 C 16.54438100 -3.04939700 -0.56828200 C 16.83947500 -1.69915200 -0.40557900 H 12.93466700 2.65437600 -0.22759200 H 14.69567600 4.37479400 0.08804400 H 17.08364300 3.74424200 0.21269800 H 17.77280500 1.36453000 0.00206400 H 13.12570100 -2.91883300 -0.76119500 H 15.00460300 -4.53995900 -0.81016200 H 17.34771500 -3.77991200 -0.59044800 H 17.86865600 -1.36684900 -0.29343000 C -15.92082100 0.70909700 0.39275800 C -14.59155600 1.18652300 0.50212200 C -14.30434500 2.54997200 0.55085700 C -15.37710100 3.43759800 0.51220900 C -16.70199400 2.98109800 0.42143600 C -16.97939200 1.61881700 0.35674200 C -15.84941300 -0.73453400 0.32540300 C -14.47903900 -1.08623000 0.39346200 C -14.06285500 -2.41686200 0.39020300 C -15.04453100 -3.40014900 0.29324300 C -16.40643100 -3.06885300 0.20771800 C -16.81491200 -1.73856600 0.22796800 H -13.28119900 2.91014700 0.60626100 H -15.18196200 4.50573000 0.54922200 H -17.51523900 3.70045600 0.39559100 H -18.00449100 1.26594100 0.27382600 H -13.01223800 -2.68024300 0.46992100 H -14.74810100 -4.44536500 0.28750700 H -17.14592500 -3.86055300 0.13100400 H -17.87031900 -1.48270700 0.17425500 N 13.59902600 -0.11646300 -0.45456600 N -13.71702400 0.08816100 0.50184900 S -6.99144200 -0.03147400 -0.51757700 S -4.45933800 0.79997300 2.85770900 S -0.49919900 0.48710500 2.07016400 S 0.37921600 -0.45780000 -2.06103000 S 4.34353600 -0.59689200 -2.88548700 S 6.86942000 0.06718700 0.53130800 H -7.73757500 0.80879700 3.01408600 H 7.62289800 -0.61291300 -3.03330000 C -2.09228100 -6.39417900 -2.33996100 C -3.36057200 -5.67172700 -2.81048600 H -2.07335300 -7.43533400 -2.68216300 H -1.19680900 -5.88869200 -2.72285600 H -2.03126600 -6.38967300 -1.24442500 H -3.41574600 -5.70376100 -3.90765400 H -4.24656100 -6.20138600 -2.43349500 C -3.49776700 3.64732200 -6.23264500 C -4.27655400 3.94924900 -4.94659300 H -3.77969600 2.66472200 -6.63173200 H -3.69098600 4.40057100 -7.00508300 H -2.41891600 3.62691700 -6.03314000 H -3.99681300 4.94398900 -4.57272400 H -5.35226800 3.98574200 -5.16852900 C 4.33488400 5.58832100 2.75314500 C 5.38470000 6.20597800 1.82141000 H 3.43668900 6.22131300 2.76563800 H 4.72239000 5.56894800 3.78139800 H 6.29656800 5.59564500 1.81067700 H 5.00595400 6.25250900 0.79264200 H 5.65304600 7.22102100 2.13625400 C 4.46615300 -3.84884500 5.89345700 C 3.20923700 -3.98360700 5.02534200 H 4.49938800 -4.61800000 6.67365200 H 5.37015800 -3.94234700 5.27849300 H 4.49548000 -2.86489400 6.37851000 H 3.18631200 -4.98104200 4.56470100 H 2.31488900 -3.90741900 5.65942200 C 11.38965000 0.45150400 0.41416000 C 10.00595800 0.43263700 0.29569700 C 9.37805100 -0.20758700 -0.78687800 C 10.19477100 -0.83126300 -1.74879700 C 11.57868200 -0.79141500 -1.64869500 C 12.18838100 -0.15195800 -0.56285000 H 11.86281600 0.92729000 1.26864300 H 9.40181900 0.92780200 1.05194900 H 9.73584600 -1.35730700 -2.58142500 H 12.19991200 -1.24981900 -2.41324300 C -10.31715300 0.94249600 1.72098700 C -11.70090500 0.87601900 1.63231200 C -12.30652500 0.15085200 0.59931800 C -11.50408500 -0.51107600 -0.33608300 C -10.12024400 -0.46431200 -0.22749400 C -9.49671800 0.26186900 0.80204300 H -9.86083100 1.53483400 2.50938300 H -12.32485500 1.38031600 2.36505800 H -11.97471000 -1.05462400 -1.15063300 H -9.51219000 -1.00481600 -0.94885600 |
| (dpl)2TDH | C 8.04655800 -0.12940600 -1.05209600 C 5.54760800 -0.13244100 -0.56515600 C 7.29103200 -0.40692500 -2.15968600 C 5.90424100 -0.42167900 -1.87908300 C 3.43146100 -0.37614300 -1.48020800 C 4.15813300 -0.09805800 -0.33535400 C 3.22577300 0.17258900 0.84476100 C 1.87150800 -0.02137900 0.16355300 C 2.03647400 -0.33693600 -1.17498100 C 0.51630600 0.03603100 0.53173400 C -0.37780100 -0.22561200 -0.51257100 C -1.89850800 0.22911000 1.17394400 C -1.73315000 -0.11407000 -0.15782300 C -3.08726800 -0.27251800 -0.84811100 C -4.01969000 0.03278300 0.32335700 C -3.29387600 0.32670800 1.46458100 C -5.76773200 0.46852400 1.83692100 C -5.40924200 0.10704400 0.54166100 C -7.15495000 0.61779100 2.07381600 C -7.90791500 0.34655700 0.96301300 C 2.96723000 3.98559100 1.20875700 C 4.01710200 4.27391700 2.08571400 C 4.78181300 3.20801000 2.57457500 C 4.50617900 1.89678200 2.19840300 C 3.45289000 1.61241500 1.31891900 C 2.68877300 2.67458600 0.82547300 H 2.35913900 4.80129100 0.82038100 H 5.60505800 3.41205100 3.25748900 H 5.10785600 1.08315300 2.59868900 H 1.87222100 2.47709800 0.13510100 C 3.44215900 -2.78632100 4.03368000 C 4.00659500 -3.04672500 2.78151000 C 3.96640900 -2.09719400 1.76158200 C 3.36010000 -0.85500600 1.97155000 C 2.78991400 -0.59074500 3.22411300 C 2.82984200 -1.54384100 4.23729000 H 4.48749700 -4.00757800 2.60441200 H 4.41093700 -2.32415800 0.79564200 H 2.32792200 0.37695000 3.41128700 H 2.38294800 -1.32272700 5.20539300 C -3.33068400 0.77797800 -1.93724800 C -2.58230200 1.95764300 -1.99652700 C -2.88320500 2.94096400 -2.93796900 C -3.93786800 2.77731300 -3.84079000 C -4.68640400 1.59599400 -3.77606500 C -4.38838700 0.60945200 -2.84114000 H -1.75958300 2.11052000 -1.30221400 H -2.28795600 3.85209500 -2.97440700 H -5.51357200 1.45063200 -4.46919200 H -4.97509100 -0.30670700 -2.81895900 C -2.65070900 -2.05754100 -2.59796900 C -3.21141100 -1.70906900 -1.36185600 C -3.79520200 -2.71430200 -0.58490100 C -3.82215500 -4.03264000 -1.03681900 C -3.26347100 -4.38531500 -2.26895700 C -2.67804400 -3.37602700 -3.04264900 H -2.20109300 -1.28668900 -3.22140200 H -4.22819400 -2.46585900 0.38105700 H -4.28389600 -4.80380900 -0.42202200 H -2.23766100 -3.63105600 -4.00538500 N -9.29391000 0.30382600 0.85483300 N 9.43251800 -0.12615000 -0.93853000 S 7.00321500 0.12222200 0.44884800 S 4.44867600 -0.67945400 -2.92521200 S 0.49178000 -0.58715900 -2.05481600 S -0.35377200 0.42893700 2.06619000 S -4.31300500 0.73331600 2.88292600 S -6.86218100 -0.14024700 -0.47706500 H 7.73944800 -0.58704100 -3.13025400 H -7.60508900 0.91650300 3.01384700 C 2.17568800 -4.70915100 5.03586700 C 3.43426200 -3.83636900 5.11344400 H 2.16805700 -5.47335400 5.82168600 H 1.27353300 -4.09395500 5.14389600 H 2.11703200 -5.21339900 4.06309900 H 3.48736800 -3.35556800 6.10032600 H 4.32738700 -4.47013900 5.02190600 C 3.48492700 6.01282600 3.81885000 C 4.27596100 5.68412100 2.54692800 H 3.76020300 5.32767500 4.63066200 H 3.67343600 7.03883900 4.15552800 H 2.40788100 5.90041700 3.64140700 H 4.00220300 6.39106600 1.75127200 H 5.34979600 5.82109000 2.73674900 C -4.30654500 3.86900300 -4.81071500 C -5.36123400 4.81042700 -4.21598900 H -3.41059100 4.44466000 -5.08177300 H -4.69210100 3.42691800 -5.74014500 H -6.26955000 4.25302700 -3.95320400 H -4.98341900 5.27903100 -3.29852200 H -5.63502400 5.60373900 -4.92124500 C -4.62072700 -6.02004100 -3.60936500 C -3.34867800 -5.79872400 -2.78202600 H -4.68307600 -7.04867100 -3.98299200 H -5.51321800 -5.81826900 -3.00361500 H -4.64354700 -5.33907300 -4.46964400 H -3.33281200 -6.50158600 -1.93739600 H -2.46642200 -6.02381500 -3.39749000 C -11.24930700 -0.10632200 2.28023800 C -10.03103500 -0.53885600 1.74134400 C -9.52256400 -1.79416900 2.09658600 C -10.22753000 -2.60491000 2.98225700 C -11.44664000 -2.18112400 3.51339500 C -11.95292500 -0.93077200 3.15503600 H -11.63502300 0.87361000 2.01332700 H -8.57713300 -2.12500600 1.67463300 H -9.82510400 -3.57762100 3.25084200 H -11.99564800 -2.81763400 4.20084100 H -12.89633400 -0.58619900 3.56937800 C -11.16786800 2.56309000 -2.18638500 C -10.01618100 3.03897700 -1.55862000 C -9.40780800 2.30308500 -0.54528000 C -9.94323500 1.06804800 -0.15738200 C -11.09310900 0.58233400 -0.79428900 C -11.70186400 1.33390200 -1.79582800 H -11.64278800 3.14164800 -2.97306500 H -9.58991400 3.99422500 -1.85230500 H -8.51585200 2.67645700 -0.04962400 H -11.49992100 -0.38281200 -0.50667000 H -12.59229700 0.94754100 -2.28399700 C 10.16333200 -1.28521100 -1.34099500 C 11.37371900 -1.15188500 -2.03300000 C 12.07357600 -2.28777500 -2.43269400 C 11.57100600 -3.56169200 -2.16329700 C 10.35942100 -3.69092700 -1.48250800 C 9.65821200 -2.56192300 -1.06697700 H 11.75624900 -0.15987500 -2.25620700 H 13.01090500 -2.17464100 -2.97034000 H 12.11699300 -4.44446900 -2.48231300 H 9.96017600 -4.67734900 -1.26377700 H 8.71881800 -2.65911200 -0.52891900 C 10.20131600 3.41609200 -0.10744000 C 11.35118300 3.27813700 0.67073100 C 11.86622700 2.00319300 0.91141600 C 11.24095300 0.87558300 0.38635100 C 10.09346700 1.01805600 -0.40542300 C 9.57589100 2.29645200 -0.64958600 H 9.79024900 4.40251400 -0.30279700 H 11.83945400 4.15384600 1.08773900 H 12.75477100 1.88193400 1.52481100 H 11.63315100 -0.11662300 0.59019100 H 8.68548000 2.40252300 -1.26333700 |
| (ndipl)2TDH | C -8.05738100 -0.79790500 0.55014300 C -5.54292400 -0.42772000 0.31124800 C -7.30549000 -1.76342300 1.17548900 C -5.91453800 -1.55653000 1.03524100 C -3.43707100 -1.26020600 0.80250000 C -4.15297900 -0.25671300 0.17125500 C -3.20940800 0.75198400 -0.48195800 C -1.86195500 0.12679600 -0.12248700 C -2.03973000 -1.02818500 0.62174500 C -0.50383500 0.41316200 -0.34100200 C 0.38072000 -0.50419900 0.23798000 C 1.91688400 0.98326700 -0.65168800 C 1.73886100 -0.18477000 0.07196100 C 3.08624600 -0.78231600 0.47501400 C 4.03003000 0.23811700 -0.15945100 C 3.31435600 1.24149500 -0.79100300 C 5.79241700 1.58189300 -0.95182500 C 5.41996200 0.43976500 -0.24945000 C 7.18327600 1.78621300 -1.09563700 C 7.93465000 0.80227200 -0.49876700 C -2.91691900 3.73682400 1.91370800 C -3.96251000 4.56324900 1.49209500 C -4.73640800 4.14598100 0.40250700 C -4.47430300 2.94150500 -0.24382600 C -3.42506400 2.11619800 0.18259100 C -2.65170800 2.52789500 1.27254500 H -2.30188600 4.04559300 2.75765100 H -5.55535000 4.77627800 0.05899800 H -5.08204500 2.64302900 -1.09603900 H -1.83812500 1.89879100 1.62541800 C -3.40614100 0.84666100 -4.83203600 C -3.98020500 -0.20782200 -4.11583100 C -3.94692100 -0.23449400 -2.72255800 C -3.33807200 0.80103100 -2.00677400 C -2.75901100 1.85881400 -2.72035300 C -2.79212400 1.87811900 -4.11159300 H -4.46330400 -1.01887900 -4.65861600 H -4.39927900 -1.06654200 -2.18849200 H -2.29424700 2.68192800 -2.18056900 H -2.33784500 2.70754800 -4.65149200 C 3.31468500 -0.77108100 1.99036300 C 2.55146600 0.03375800 2.84175500 C 2.83240400 0.08716100 4.20616500 C 3.88117100 -0.65492400 4.75726400 C 4.64698600 -1.45416800 3.90012400 C 4.36892400 -1.51434600 2.53784800 H 1.73132700 0.62204300 2.43739100 H 2.22475000 0.71385400 4.85725100 H 5.46969800 -2.03804500 4.31005900 H 4.96459900 -2.15749400 1.89266400 C 2.63380400 -3.27823800 0.51811600 C 3.20882000 -2.18054200 -0.13625600 C 3.80515500 -2.38295400 -1.38455600 C 3.82976200 -3.65265800 -1.95950800 C 3.25585200 -4.75043700 -1.31136000 C 2.65823600 -4.54279500 -0.06242800 H 2.17561300 -3.14223200 1.49608800 H 4.25023900 -1.54292800 -1.91246200 H 4.30168300 -3.79514500 -2.93049000 H 2.20607600 -5.38551700 0.45837600 N 13.61157500 0.36068600 -0.25745800 N -13.73606600 -0.40070200 0.24918600 S -6.99439800 0.45194100 -0.25878800 S -4.46870300 -2.48139000 1.61604000 S -0.50334400 -1.82825200 1.09310100 S 0.38040500 1.75375100 -1.16998800 S 4.34685600 2.50265000 -1.54038000 S 6.87111900 -0.45652200 0.29504400 H -7.74831000 -2.57759400 1.73840300 H 7.62583000 2.61017300 -1.64428700 C -2.13967300 0.13949500 -6.88156400 C -3.39025800 0.84127500 -6.33809500 H -2.12574600 0.13574700 -7.97766100 H -1.23134300 0.64229100 -6.52639300 H -2.09989900 -0.89990000 -6.53218300 H -3.42495400 1.87337600 -6.71422600 H -4.28941500 0.33583300 -6.71731100 C -3.41259000 7.01423400 1.45799800 C -4.20746200 5.89771900 2.14585900 H -3.69429700 7.09154700 0.40017000 H -3.59066200 7.98573700 1.93345100 H -2.33679900 6.80186600 1.49957600 H -3.92746600 5.84792800 3.20737100 H -5.27983100 6.13609000 2.11233300 C 4.22033400 -0.54731000 6.22078000 C 5.23074200 0.57698100 6.47936300 H 3.30618000 -0.36064400 6.80148900 H 4.63293200 -1.50119600 6.57822500 H 6.15762600 0.39738500 5.92018300 H 4.82600300 1.54122100 6.14697400 H 5.47974300 0.65605200 7.54397300 C 4.60081900 -6.86811500 -1.44458800 C 3.33785900 -6.13136800 -1.90685600 H 4.66074000 -7.87337200 -1.87753300 H 5.49971500 -6.31169400 -1.73891000 H 4.61269200 -6.96261200 -0.35128500 H 3.33295200 -6.06332500 -3.00365100 H 2.44909600 -6.71166200 -1.62188500 C 11.38978500 -0.66007700 -0.10738800 C 10.00749100 -0.55195800 -0.15973100 C 9.37904300 0.67743200 -0.42574300 C 10.20315000 1.80144400 -0.62447500 C 11.58493800 1.70094300 -0.57086900 C 12.20117900 0.46568100 -0.31339900 H 11.85368000 -1.62376500 0.08280100 H 9.40310600 -1.44617100 -0.02419900 H 9.74861100 2.77545700 -0.78685400 H 12.20149000 2.58449000 -0.71041700 C -10.31991600 -1.81247300 0.65739300 C -11.70235000 -1.72001000 0.60092100 C -12.32446500 -0.49282100 0.32267800 C -11.51953700 0.63661700 0.11319400 C -10.13735500 0.54199600 0.19255700 C -9.50282900 -0.68241200 0.46570600 H -9.86018300 -2.77946100 0.84431000 H -12.31427500 -2.60307800 0.76183500 H -11.98807000 1.59115400 -0.10902600 H -9.53715500 1.43694600 0.04505500 C -15.73272100 3.00595300 1.75863500 C -14.65565400 2.45475600 2.45485100 C -14.00034300 1.32757300 1.96613800 C -14.40661100 0.74668800 0.75684200 C -15.48365600 1.30441600 0.05440800 C -16.14438200 2.42114100 0.55992400 H -16.24578300 3.88105400 2.14615400 H -14.33050800 2.89609800 3.39294500 H -13.17193800 0.88910600 2.51586100 H -15.79439300 0.85720600 -0.88585000 H -16.97778100 2.84423200 0.00585100 C -14.48868700 -1.45751600 -0.33662200 C -15.67800300 -1.89540100 0.26158900 C -16.41455900 -2.92435200 -0.32009200 C -15.96985200 -3.53936600 -1.49179400 C -14.78205600 -3.10740900 -2.08437700 C -14.04808900 -2.06777100 -1.51907600 H -16.01546300 -1.42452600 1.18091800 H -17.33480800 -3.25571200 0.15308000 H -16.54325300 -4.34607300 -1.93866800 H -14.42996700 -3.57290900 -3.00081800 H -13.13107600 -1.72043200 -1.98730700 C 14.06266200 1.24333100 -2.49890000 C 14.85634400 1.98958800 -3.36637300 C 16.02324800 2.60341800 -2.90788200 C 16.38613700 2.46984500 -1.56650900 C 15.58945300 1.73984500 -0.68795700 C 14.42151000 1.11779200 -1.14966800 H 13.16278000 0.75150100 -2.85821100 H 14.56788600 2.07942400 -4.41009500 H 16.64349900 3.17876100 -3.58873700 H 17.28919800 2.94761600 -1.19673500 H 15.86359500 1.64587100 0.35932700 C 14.22737200 -0.50384100 0.69139000 C 15.31591700 -1.30312900 0.31652400 C 15.92277500 -2.13926600 1.25057700 C 15.44530700 -2.20216300 2.56086000 C 14.35673900 -1.41115600 2.93253900 C 13.75442200 -0.55957000 2.00977900 H 15.67775900 -1.26247700 -0.70732500 H 16.76571700 -2.75458300 0.94832300 H 15.91683300 -2.86010300 3.28482600 H 13.98125500 -1.44586700 3.95155500 H 12.91613900 0.06751800 2.30114100 |
| (pt)2TDH | C 8.02681700 0.04263300 1.04420100 C 5.50796100 -0.05162900 0.57241700 C 7.26285300 0.01278100 2.18468700 C 5.88027600 -0.03853900 1.92390400 C 3.38265800 -0.05534800 1.52502200 C 4.13135500 -0.05859800 0.33546100 C 3.19743000 -0.08496200 -0.87638100 C 1.83667200 -0.07476600 -0.17154700 C 2.01266300 -0.05741800 1.22809700 C 0.50439600 -0.06553100 -0.54636300 C -0.42589700 -0.04264800 0.52670000 C -1.93257800 -0.12256600 -1.24735400 C -1.75819000 -0.07442800 0.15194800 C -3.12050000 -0.05994300 0.85441200 C -4.05252200 -0.09652300 -0.35871200 C -3.30188700 -0.14373700 -1.54597200 C -5.79851200 -0.16377100 -1.94902500 C -5.42871500 -0.11005600 -0.59784300 C -7.18089500 -0.13622000 -2.21410300 C -7.94706900 -0.05609200 -1.07761900 C 3.02674000 -3.73239800 -2.06671400 C 4.08063100 -3.79992200 -2.98435800 C 4.81746900 -2.63413300 -3.23020000 C 4.51127100 -1.44171500 -2.57869200 C 3.45511400 -1.37754600 -1.65832600 C 2.71851900 -2.54101000 -1.40989900 H 2.43923900 -4.62708300 -1.86487900 H 5.64091000 -2.66534900 -3.94244600 H 5.09104400 -0.54581900 -2.79370900 H 1.89803000 -2.51305700 -0.69667000 C 3.33534900 3.51437800 -3.33596800 C 3.89509800 3.50274600 -2.05385600 C 3.87882800 2.34822500 -1.27101600 C 3.30295900 1.16748900 -1.75212200 C 2.73608400 1.17787000 -3.03460100 C 2.75161700 2.33340600 -3.81188700 H 4.35303900 4.41137000 -1.66536000 H 4.31978000 2.36145600 -0.27691000 H 2.29242100 0.26742700 -3.43364100 H 2.30764300 2.32221700 -4.80636900 C -3.37177300 -1.31672500 1.69497700 C -2.62472800 -2.48416200 1.50318900 C -2.92529400 -3.64658800 2.21326900 C -3.98221000 -3.68063500 3.12917900 C -4.72983700 -2.51102400 3.31812400 C -4.43165500 -1.34742900 2.61298500 H -1.80138400 -2.48195600 0.79264900 H -2.32941300 -4.54445800 2.05502300 H -5.55633900 -2.51646200 4.02752100 H -5.02160900 -0.44849200 2.78283200 C -2.68137100 1.30557600 2.95458800 C -3.23781600 1.23148200 1.66981800 C -3.81281000 2.38587200 1.12735100 C -3.83765200 3.57725800 1.85241900 C -3.28385300 3.65394200 3.13489800 C -2.70498800 2.49801300 3.67404000 H -2.23623000 0.41769700 3.39994100 H -4.24239000 2.34962100 0.12882100 H -4.29448800 4.46465500 1.41637800 H -2.26857800 2.53689400 4.67117300 C -11.34935900 -1.27720700 -0.29205500 C -10.07883700 -1.21963400 -0.88056500 C -9.54847900 -2.39794900 -1.42442600 C -10.26885600 -3.58968400 -1.38182700 C -11.54406500 -3.62739800 -0.81807100 C -12.08435900 -2.46036800 -0.27935400 C -11.25476400 1.47563200 -0.45304300 C -9.99366200 1.26250600 -1.02609700 C -9.38758600 2.32979400 -1.70377200 C -10.02527200 3.56417500 -1.80517100 C -11.29225300 3.75503300 -1.25393700 C -11.90766400 2.69927200 -0.58258700 H -8.56026600 -2.37388700 -1.87218900 H -9.82950800 -4.49002800 -1.80085800 H -12.11199000 -4.55204300 -0.79266400 H -13.07293400 -2.46512500 0.17233700 H -8.40559500 2.18681900 -2.14260600 H -9.52808400 4.37643900 -2.32698000 H -11.79609100 4.71258200 -1.34019000 H -12.89162300 2.82419000 -0.13812300 C 11.44420300 -1.16816300 0.31375600 C 10.17778800 -1.09668800 0.90939400 C 9.67358000 -2.24758700 1.53103600 C 10.41500100 -3.42688600 1.55564500 C 11.68555500 -3.47735100 0.98243200 C 12.20012700 -2.33693700 0.36698600 C 11.30558500 1.58717100 0.31514900 C 10.05217600 1.38730100 0.90940700 C 9.43299800 2.48154800 1.52963700 C 10.05099000 3.72971300 1.55557300 C 11.31101400 3.90876000 0.98470300 C 11.93929200 2.82641100 0.36990800 H 8.68924200 -2.21256600 1.98647500 H 9.99606400 -4.30674700 2.03475000 H 12.26976400 -4.39177400 1.00883000 H 13.18486800 -2.35252800 -0.09272800 H 8.45646500 2.34800700 1.98344900 H 9.54415400 4.56250900 2.03392500 H 11.79975900 4.87755500 1.01238300 H 12.91800500 2.94159600 -0.08852100 N -9.33808200 -0.00162400 -0.93579400 N 9.41656400 0.10971700 0.89621100 S 6.96986500 -0.00056600 -0.47503400 S 4.41198200 -0.05062200 3.00782000 S 0.44187700 -0.01946200 2.13117800 S -0.36176500 -0.11733700 -2.15046400 S -4.32830400 -0.21609200 -3.02889200 S -6.89300600 -0.01787900 0.44344800 H 7.71195300 0.03383200 3.17338100 H -7.62855400 -0.16985400 -3.20308400 C 2.02362700 5.58345600 -3.89353300 C 3.30171400 4.77742800 -4.15645600 H 1.99956000 6.50157200 -4.49197600 H 1.13524800 4.98815000 -4.14011100 H 1.95505900 5.86076100 -2.83395500 H 3.36347200 4.52832500 -5.22506100 H 4.17936300 5.39589000 -3.92234400 C 3.59380900 -5.13555500 -5.05701100 C 4.37275400 -5.07146700 -3.73750200 H 3.85844900 -4.28766100 -5.70174800 H 3.80666900 -6.06191500 -5.60301700 H 2.51367900 -5.08729300 -4.86849800 H 4.11120800 -5.93894800 -3.11580700 H 5.44972800 -5.14115600 -3.94475000 C -4.26733400 -4.91823600 3.93933300 C -3.49825400 -4.91182700 5.26614400 H -5.34514600 -4.98919700 4.14179000 H -3.99227500 -5.81130800 3.36123900 H -2.41718600 -4.86240900 5.08351500 H -3.77575100 -4.03656600 5.86745500 H -3.70693300 -5.81294300 5.85438100 C -4.64685000 4.97063100 4.78516900 C -3.36747100 4.92395000 3.94068400 H -4.70615700 5.89499700 5.37136600 H -5.53438900 4.91308500 4.14209300 H -4.68150300 4.12053700 5.47862600 H -3.34114300 5.79251700 3.26811300 H -2.49125700 5.00421800 4.59900100 S -12.02452300 0.17985800 0.58236500 S 12.08698000 0.24599700 -0.65149800 |
| (ppt)2TDH | C -8.04867900 0.07357500 -0.95861400 C -5.53766600 -0.01966600 -0.52951900 C -7.30008000 0.16804700 -2.10703600 C -5.90975900 0.11484000 -1.86430700 C -3.43326200 0.08417300 -1.49160000 C -4.14786500 -0.03228400 -0.31100500 C -3.20511800 -0.15466900 0.88410800 C -1.85783900 -0.08850400 0.16589000 C -2.03540800 0.05519500 -1.20091200 C -0.49946500 -0.11093500 0.52361200 C 0.38416500 0.00982100 -0.55548500 C 1.91939700 -0.23463800 1.16047300 C 1.74243100 -0.06144300 -0.20303900 C 3.09004500 0.03383600 -0.91691000 C 4.03238600 -0.11871100 0.27551000 C 3.31686000 -0.27520800 1.45086300 C 5.79314100 -0.32916700 1.82360500 C 5.42195600 -0.15503400 0.49316800 C 7.18343100 -0.33085500 2.07349100 C 7.93276600 -0.15752800 0.93485200 C -3.04534100 -3.87979700 1.79191700 C -4.08076200 -4.00487000 2.72314800 C -4.80033900 -2.85517300 3.06994600 C -4.49586800 -1.62119300 2.50295700 C -3.45823900 -1.50124600 1.56876700 C -2.73839900 -2.64733000 1.21750800 H -2.47217600 -4.76243000 1.51223900 H -5.60980900 -2.93220500 3.79420700 H -5.05884000 -0.73776000 2.79817100 H -1.93528200 -2.57799200 0.48765400 C -3.31100000 3.25251800 3.59770900 C -3.89622900 3.33311300 2.33064400 C -3.89125700 2.24120800 1.46394700 C -3.30028900 1.03334800 1.84695900 C -2.70923300 0.94880400 3.11490500 C -2.71447900 2.04322400 3.97445100 H -4.36542100 4.26524200 2.01967600 H -4.35173300 2.33064800 0.48302900 H -2.25725300 0.01249300 3.43753700 H -2.25167700 1.96109700 4.95667600 C 3.34468100 -1.12225900 -1.88864400 C 2.59242000 -2.29968200 -1.84627300 C 2.89859500 -3.36580500 -2.69134200 C 3.96201500 -3.28885700 -3.59550900 C 4.71663800 -2.10996600 -3.62973200 C 4.41304400 -1.04121500 -2.79219200 H 1.76148500 -2.38514300 -1.15021000 H 2.29935700 -4.27413400 -2.65125500 H 5.55016400 -2.03133400 -4.32593100 H 5.00039700 -0.12660500 -2.85058700 C 2.61704900 1.60572900 -2.85229300 C 3.18823000 1.40771400 -1.58815500 C 3.75937000 2.50272200 -0.93265200 C 3.76366200 3.76191000 -1.53047300 C 3.19376900 3.96502300 -2.79093700 C 2.62125000 2.86609600 -3.44256800 H 2.17816500 0.76267900 -3.38298600 H 4.20073400 2.37294700 0.05259400 H 4.21637800 4.60406300 -1.00937300 H 2.17312900 3.00406900 -4.42534200 C 15.59132500 -0.98929000 -0.59707100 C 14.28443000 -1.08545100 -0.09536500 C 13.66501700 -2.34465700 -0.11522000 C 14.33537200 -3.46246800 -0.60789000 C 15.64590300 -3.35889400 -1.06849800 C 16.27235600 -2.11346400 -1.05267100 C 15.61227000 1.45991100 0.65763400 C 14.30356100 1.12655100 1.03879200 C 13.70230800 1.88730300 2.05350900 C 14.39152800 2.93125200 2.66722900 C 15.70327300 3.22689500 2.30379300 C 16.31195400 2.47748300 1.29782300 H 12.64802600 -2.44799200 0.24837700 H 13.82538200 -4.42138400 -0.62044700 H 16.17433100 -4.23080500 -1.44097600 H 17.29101300 -2.00012200 -1.41422500 H 12.68441400 1.66695000 2.35731500 H 13.89525700 3.50893300 3.44168300 H 16.24624900 4.03179100 2.78909800 H 17.33115800 2.69086300 0.98652600 C -15.70913300 -1.13552500 0.29127600 C -14.39804600 -1.09832200 -0.20736700 C -13.76981300 -2.32070800 -0.49209300 C -14.43532800 -3.52893700 -0.29513800 C -15.74955700 -3.54887200 0.16566800 C -16.38488000 -2.34100500 0.45104700 C -15.73721300 1.54863500 -0.31896600 C -14.42334100 1.32607900 -0.75848800 C -13.81822300 2.31814700 -1.54560100 C -14.50845000 3.47974100 -1.88610400 C -15.82497600 3.67031000 -1.47333200 C -16.43751900 2.69124900 -0.69220400 H -12.74942800 -2.32665500 -0.86052100 H -13.91823200 -4.45868500 -0.51406200 H -16.27420600 -4.48834600 0.30824800 H -17.40681900 -2.32545100 0.82067300 H -12.79660100 2.18422300 -1.88522500 H -14.00903000 4.23421600 -2.48704800 H -16.36886200 4.56868300 -1.74777200 H -17.46064600 2.81637400 -0.34758900 N 13.61079600 0.05330300 0.41941000 N -13.72836500 0.13531400 -0.42050500 S -6.98544100 -0.09675100 0.51811200 S -4.46485800 0.21903800 -2.95225600 S -0.49983600 0.17780800 -2.12201800 S 0.38400400 -0.31298100 2.08617400 S 4.34699300 -0.47823600 2.90475000 S 6.87047800 0.01350900 -0.54236400 H -7.74196200 0.29923000 -3.08851700 H 7.62488000 -0.42722400 3.05924400 C -1.99811100 5.28466600 4.26781400 C -3.26383500 4.45236300 4.50677300 H -1.96150100 6.15788200 4.92931200 H -1.10018500 4.67943500 4.44515300 H -1.95977100 5.63652300 3.22922100 H -3.29623800 4.12596600 5.55566300 H -4.15194800 5.07835400 4.34249000 C -3.56052500 -5.49302200 4.67893600 C -4.36984300 -5.32530800 3.38723600 H -3.79873800 -4.69124700 5.38933600 H -3.77056200 -6.45416200 5.16211600 H -2.48484400 -5.44064600 4.46845200 H -4.13439300 -6.14714800 2.69680800 H -5.44265000 -5.39977600 3.61363000 C 4.32772700 -4.46438200 -4.46311100 C 5.34301000 -5.37880600 -3.76678600 H 3.42432000 -5.03910800 -4.71033900 H 4.74650000 -4.10828800 -5.41472500 H 6.25967600 -4.82495100 -3.52804700 H 4.93244900 -5.76127200 -2.82381500 H 5.61148800 -6.23383500 -4.39783400 C 4.52293400 5.46189800 -4.30860600 C 3.25441700 5.31293900 -3.45991200 H 4.56734100 6.44297900 -4.79529700 H 5.41854100 5.34556100 -3.68530200 H 4.55819900 4.68936700 -5.08720400 H 3.22584100 6.10589200 -2.69971100 H 2.36873400 5.45195600 -4.09546300 C 11.37477500 0.50251300 -0.45582000 C 9.98984000 0.45552100 -0.33832800 C 9.37928000 -0.10901900 0.79490300 C 10.20785800 -0.63210900 1.80679800 C 11.59105200 -0.57503200 1.69344800 C 12.18300400 -0.00732400 0.55958700 H 11.84727700 0.94075000 -1.33004600 H 9.37335000 0.87943100 -1.12716700 H 9.76006000 -1.10574000 2.67609600 H 12.22972500 -0.98128800 2.47499800 C -10.32064500 -0.18551400 -1.92238700 C -11.70406000 -0.16150500 -1.80226800 C -12.30000000 0.11657000 -0.56703600 C -11.49540000 0.37363900 0.54227700 C -10.10995900 0.36118100 0.42035400 C -9.49544600 0.08406000 -0.81301000 H -9.87004900 -0.43662600 -2.87860800 H -12.34002400 -0.37114100 -2.65980600 H -11.97087500 0.58904400 1.49469400 H -9.49655000 0.58675700 1.28918700 S 16.37913800 0.64706100 -0.78664000 S -16.51125400 0.39929400 0.87035600 |
| (px)2TDH | C 8.00891100 0.04461800 1.07016300 C 5.51277400 0.00018100 0.57980400 C 7.24777600 0.02770600 2.20446900 C 5.85977100 0.00552800 1.92865700 C 3.39199300 0.00873200 1.51552900 C 4.12371900 0.00592600 0.34101400 C 3.19874800 -0.01576400 -0.87471400 C 1.84135200 -0.00591900 -0.17357400 C 1.99751200 0.00770600 1.20240700 C 0.48821100 0.00630900 -0.55306500 C -0.41105000 0.02315400 0.51897900 C -1.92013500 -0.04957900 -1.23523200 C -1.76400800 -0.01173800 0.14025800 C -3.12120600 -0.00765800 0.84160500 C -4.04646500 -0.03292600 -0.37400000 C -3.31451800 -0.06965000 -1.54789400 C -5.78201100 -0.10951500 -1.96052200 C -5.43540500 -0.05783500 -0.61256000 C -7.17005700 -0.11370700 -2.23700200 C -7.93189200 -0.05884800 -1.10438600 C 3.03032900 -3.65955100 -2.06932200 C 4.08514300 -3.72313800 -2.98469600 C 4.82190500 -2.55740200 -3.22638300 C 4.51558000 -1.36750300 -2.57268400 C 3.45788000 -1.30896700 -1.65517600 C 2.72075800 -2.47156500 -1.40907500 H 2.44364500 -4.55521200 -1.87075700 H 5.64739100 -2.58667800 -3.93583700 H 5.09503200 -0.47093900 -2.78436000 H 1.90150800 -2.45067200 -0.69437600 C 3.34208300 3.59218300 -3.31119700 C 3.87846100 3.58207900 -2.02002700 C 3.86216800 2.42535700 -1.24253900 C 3.30918800 1.24198800 -1.74150400 C 2.76595200 1.24838000 -3.03308300 C 2.78228900 2.40744400 -3.80359200 H 4.31851400 4.49423500 -1.61997100 H 4.28406900 2.44333200 -0.24045700 H 2.34519100 0.33313900 -3.44532100 H 2.35815400 2.39562000 -4.80642000 C -3.37075700 -1.27797000 1.66234900 C -2.61959100 -2.43973800 1.45859600 C -2.91915100 -3.60855300 2.15671400 C -3.97762200 -3.65354200 3.06883800 C -4.72875300 -2.48881800 3.26785000 C -4.43249200 -1.31802800 2.57626200 H -1.79686500 -2.43345600 0.74762900 H -2.32143500 -4.50355200 1.99084500 H -5.55770800 -2.50384900 3.97372600 H -5.02357500 -0.42185900 2.75488700 C -2.69907900 1.32408000 2.96048700 C -3.24083700 1.27499600 1.66928200 C -3.79695400 2.44009900 1.13220500 C -3.81657900 3.62128400 1.87195900 C -3.27686100 3.67544900 3.16062900 C -2.71856400 2.50742400 3.69311700 H -2.27214100 0.42470500 3.40038900 H -4.21391900 2.42529200 0.12798300 H -4.25758600 4.51933500 1.44210900 H -2.29390000 2.52951100 4.69555800 C -11.41755300 -1.23903500 -0.64877300 C -10.02668500 -1.27236600 -0.82099000 C -9.38475700 -2.51128600 -0.81671300 C -10.11871100 -3.68686500 -0.64674800 C -11.50061300 -3.63753200 -0.47971300 C -12.14998300 -2.40230200 -0.48106500 C -11.41837400 1.15668600 -0.75913500 C -10.02760600 1.17490900 -0.93452700 C -9.38726900 2.40965000 -1.04638400 C -10.12195500 3.59545900 -0.98530700 C -11.50346400 3.56073100 -0.81236500 C -12.15154600 2.33003900 -0.69881600 H -8.30729900 -2.55052900 -0.94686400 H -9.59984100 -4.64043300 -0.64589000 H -12.07400600 -4.54948000 -0.34791600 H -13.22390600 -2.31388000 -0.35341100 H -8.31017900 2.43684200 -1.18238300 H -9.60435800 4.54563500 -1.07414300 H -12.07759000 4.48045300 -0.76496300 H -13.22527400 2.25285700 -0.56253100 C 11.50701700 -1.12241600 0.67969000 C 10.11643400 -1.16087300 0.85277200 C 9.48734700 -2.40488900 0.91420100 C 10.23359500 -3.58022800 0.80809300 C 11.61512400 -3.52560000 0.63985400 C 12.25164700 -2.28536800 0.57527800 C 11.48279200 1.27563600 0.65966700 C 10.09172700 1.28884600 0.83341900 C 9.43851500 2.52105200 0.87844900 C 10.16083400 3.70937900 0.75309200 C 11.54274500 3.67971000 0.58223700 C 12.20374100 2.45153100 0.53582800 H 8.41016100 -2.44849500 1.04514100 H 9.72457300 -4.53781400 0.85771100 H 12.19812500 -4.43729000 0.55777000 H 13.32473800 -2.19273800 0.44365900 H 8.36113600 2.54417200 1.01290100 H 9.63329900 4.65749900 0.79006800 H 12.10726500 4.60143900 0.48471600 H 13.27831600 2.37831200 0.40411200 N -9.31713100 -0.05377600 -0.99651100 N 9.39407600 0.05802700 0.96187600 S 6.96808800 0.02729200 -0.45931500 S 4.39813600 0.00180300 2.99772400 S 0.44807500 0.04118600 2.10767400 S -0.37080200 -0.03927000 -2.14128100 S -4.32012700 -0.14311200 -3.02859900 S -6.89143100 -0.00050200 0.42438400 H 7.69448700 0.03143100 3.19225300 H -7.61621900 -0.15596400 -3.22413600 C 2.01847900 5.65000300 -3.87425500 C 3.30783600 4.85864300 -4.12552200 H 1.99165700 6.57167900 -4.46687800 H 1.13963000 5.04674100 -4.13449300 H 1.93267600 5.91875600 -2.81386800 H 3.38747900 4.61585100 -5.19437200 H 4.17712100 5.48348600 -3.87755600 C 3.59336200 -5.05530700 -5.05698300 C 4.37843100 -4.99190000 -3.74120300 H 3.85071900 -4.20427900 -5.70019300 H 3.80636400 -5.97899800 -5.60723100 H 2.51415000 -5.01024300 -4.86353500 H 4.12407200 -5.86166100 -3.11954700 H 5.45492500 -5.05756500 -3.95224500 C -4.26096600 -4.89927200 3.86625500 C -3.48967200 -4.90510200 5.19168900 H -5.33867300 -4.97333500 4.06823700 H -3.98734400 -5.78637800 3.27822700 H -2.40913000 -4.85143600 5.00815600 H -3.76593600 -4.03569400 5.80162500 H -3.69588400 -5.81175800 5.77203500 C -4.64386300 4.98767300 4.80967900 C -3.35516400 4.93656400 3.98000200 H -4.70113000 5.90570400 5.40576500 H -5.52429700 4.94541400 4.15611700 H -4.69665000 4.13004000 5.49223300 H -3.30950800 5.81241900 3.31789400 H -2.48507600 4.99945500 4.64835200 O -12.12991100 -0.03849500 -0.64418500 O 12.20686200 0.08342700 0.61027200 |
| (ppx)2TDH | C -8.05112500 -0.43746300 -0.86834800 C -5.53964300 -0.27848100 -0.46501500 C -7.30456400 -0.95116000 -1.90115800 C -5.91343100 -0.85713700 -1.67468200 C -3.43635500 -0.69667500 -1.33984700 C -4.14975600 -0.17977100 -0.27116400 C -3.20594500 0.33187400 0.81488700 C -1.85968400 0.01354300 0.16616300 C -2.03813500 -0.57256800 -1.07678400 C -0.50129500 0.17893100 0.48350100 C 0.38196200 -0.27762500 -0.50199400 C 1.91725300 0.40272400 1.09194800 C 1.74025100 -0.15612000 -0.16357000 C 3.08791800 -0.44974900 -0.82156300 C 4.03069600 0.04162200 0.27584200 C 3.31457100 0.51685000 1.36188600 C 5.78943100 0.66146100 1.71206600 C 5.42038300 0.12379600 0.48205000 C 7.17912100 0.78842500 1.93050200 C 7.93042700 0.34975400 0.86726700 C -3.04144900 -2.37335000 3.53264300 C -4.08866200 -2.00526100 4.38266000 C -4.81784700 -0.85104800 4.07220900 C -4.51131500 -0.09120700 2.94740900 C -3.46217300 -0.46566600 2.09710100 C -2.73212200 -1.61833600 2.40224200 H -2.46063300 -3.26588500 3.76013800 H -5.63581100 -0.54721000 4.72366000 H -5.08212400 0.81028800 2.73223400 H -1.91862900 -1.93013400 1.75148700 C -3.29391600 4.65057400 1.38050800 C -3.86709600 4.06946000 0.24539500 C -3.86850200 2.68692600 0.06655800 C -3.29617700 1.84666300 1.02628800 C -2.71697700 2.42458800 2.16397400 C -2.71578300 3.80564000 2.33537600 H -4.32211800 4.71039300 -0.50814900 H -4.31936900 2.25953000 -0.82585800 H -2.28069400 1.78583100 2.92985200 H -2.26289200 4.23936200 3.22559700 C 3.33780600 -1.94489700 -1.04144300 C 2.57931300 -2.92074100 -0.38816300 C 2.87743100 -4.27348100 -0.54719500 C 3.93890100 -4.68899600 -1.35628800 C 4.70051400 -3.70791100 -2.00282700 C 4.40544100 -2.35662600 -1.85087800 H 1.74905500 -2.62379200 0.24795600 H 2.27289600 -5.02181000 -0.03705700 H 5.53271000 -4.01151000 -2.63603400 H 4.99823800 -1.61238600 -2.37967600 C 2.63405100 -0.12663700 -3.29905200 C 3.18754600 0.37038000 -2.11173200 C 3.73859100 1.65555800 -2.11653000 C 3.74098600 2.42040900 -3.28166500 C 3.18877000 1.92958300 -4.46880100 C 2.63650800 0.64329800 -4.45872400 H 2.21061900 -1.12916900 -3.31832500 H 4.16457600 2.06366800 -1.20304800 H 4.17745300 3.41795400 -3.27054700 H 2.20230500 0.24331100 -5.37373300 C 15.68253300 -0.95515900 0.05518600 C 14.28209700 -0.95738200 0.16157700 C 13.61542100 -2.17946300 0.04438200 C 14.32871000 -3.35904200 -0.18469800 C 15.71570200 -3.33594700 -0.29637100 C 16.39272700 -2.12035700 -0.17219600 C 15.74044500 1.41959500 0.41103800 C 14.34055000 1.45810300 0.51596500 C 13.73046700 2.69722200 0.72650100 C 14.49985700 3.85804100 0.84103000 C 15.88682400 3.79903800 0.74324700 C 16.50621500 2.56621400 0.52391600 H 12.53395200 -2.20669400 0.13594300 H 13.78721600 -4.29614800 -0.27263900 H 16.27246000 -4.25016300 -0.47507800 H 17.47323700 -2.05135000 -0.24553200 H 12.64852000 2.75228800 0.79750700 H 14.00189600 4.80893400 1.00521100 H 16.48737500 4.69855100 0.83240200 H 17.58337600 2.46932700 0.43453200 C -15.88923900 -1.20655400 -0.24276200 C -14.49159600 -1.30462100 -0.33983900 C -13.91673700 -2.57768500 -0.32879500 C -14.71830700 -3.71769700 -0.22812900 C -16.10206100 -3.60198100 -0.13610300 C -16.68652500 -2.33262900 -0.14321200 C -15.75999000 1.19136400 -0.34008700 C -14.36041200 1.13055200 -0.44098900 C -13.65338000 2.33076700 -0.54499300 C -14.32791700 3.55439400 -0.54346400 C -15.71502800 3.59599700 -0.43953800 C -16.43169500 2.40064200 -0.33800500 H -12.83744100 -2.67425800 -0.39761800 H -14.24842900 -4.69662300 -0.22142500 H -16.72777900 -4.48522400 -0.05792000 H -17.76015100 -2.19160600 -0.07154500 H -12.57109500 2.30496700 -0.62816300 H -13.75649500 4.47414200 -0.62505700 H -16.24214500 4.54462600 -0.43774300 H -17.51372200 2.38187500 -0.25699900 N 13.60534200 0.25940200 0.39385600 N -13.72204900 -0.12706800 -0.43934900 S -6.98552900 0.19967700 0.47281700 S -4.46955800 -1.34194200 -2.65586900 S -0.50267300 -0.94599800 -1.92836400 S 0.38212600 0.81650000 1.92435400 S 4.34275500 1.09424100 2.71242900 S 6.87180700 -0.26451200 -0.48972100 H -7.75010200 -1.40467800 -2.77964100 H 7.61986200 1.21495700 2.82480100 C -1.96246400 6.73055800 0.92771700 C -3.24101100 6.14709100 1.54151600 H -1.92203900 7.81959100 1.04516600 H -1.07413300 6.29872900 1.40565600 H -1.90847900 6.49664200 -0.14295300 H -3.28879600 6.40837200 2.60793200 H -4.11937000 6.60350200 1.06424400 C -3.58672600 -2.25083100 6.83188900 C -4.38086600 -2.78860600 5.63530100 H -3.83596700 -1.19841500 7.01781800 H -3.79946600 -2.82089400 7.74353000 H -2.50875900 -2.30628000 6.63433800 H -4.13404100 -3.84756400 5.47658300 H -5.45607400 -2.74440000 5.85832800 C 4.29505400 -6.14720000 -1.47905400 C 5.31274000 -6.56642500 -0.41114700 H 3.38818500 -6.76038900 -1.38350100 H 4.70786700 -6.34646300 -2.47790500 H 6.23307400 -5.97604900 -0.50342900 H 4.90841500 -6.39370000 0.59418400 H 5.57346000 -7.62731400 -0.50024200 C 4.52500400 2.43867700 -6.53431300 C 3.24673300 2.73430600 -5.74043700 H 4.56736800 3.02469800 -7.45958300 H 5.41329100 2.67572400 -5.93520800 H 4.57705300 1.37467200 -6.79790500 H 3.20118900 3.80631500 -5.50329200 H 2.36838500 2.51017800 -6.36171400 C 11.38503500 0.25404900 -0.63986100 C 9.99936600 0.27116400 -0.52878400 C 9.37772400 0.31604400 0.73184300 C 10.19411000 0.33098200 1.87893200 C 11.57863900 0.31544400 1.76752300 C 12.18165300 0.27800000 0.50699400 H 11.86607400 0.22620500 -1.61403200 H 9.39036000 0.27576100 -1.42951200 H 9.73417700 0.32554000 2.86330200 H 12.20988200 0.32199500 2.65228300 C -10.30973600 -0.42437500 -1.89405600 C -11.69370700 -0.35777300 -1.79218800 C -12.29919900 -0.20708900 -0.54177600 C -11.50744700 -0.12664000 0.60533900 C -10.12284100 -0.20103300 0.50472000 C -9.49772500 -0.35422000 -0.74573900 H -9.84707400 -0.50632200 -2.87369300 H -12.32201300 -0.40834400 -2.67759300 H -11.99144000 -0.01059900 1.57145400 H -9.51817500 -0.16073400 1.40736000 O 16.42403600 0.22269700 0.18134500 O -16.53634700 0.03283400 -0.23982400 |