Supporting Information

Crystal anisotropy implications on the intrinsic magnetism in van der Waals FePS3

Ellenor Geraffy*1, Shahar Zuri1, Milosz Marcin Rybak2, Faris Horani1, Adam K. Budniak1, Yaron Amouyal3, Magdalena Birowska*2 and Efrat Lifshitz*1

1Schulich Faculty of Chemistry, Solid State Institute, Russell Berrie Nanotechnology Institute, and the Helen Diller Quantum Information Center, Technion – Israel Institute of Technology, Haifa, Israel

2Institute of Theoretical Physics, Faculty of Physics, University of Warsaw, Pasteura 5, Warsaw 02-093, Poland.

3Department of Materials Science and Engineering, Technion – Israel Institute of Technology, 3200003 Haifa, Israel

*Corresponding authors

1. Characterization of single crystal FePS3

(b)

(a)

Figure S1: EDX measurements of bulk FePS3 synthesised via CVT. (a) Percentage breakdown of each element in FePS3 bulk sample, (b) SEM image of FePS3 sample using the secondary electron (SE) detector.

EDX measurements

  - XRD measurements

Table S 1 Bond lengths of bulk FePS3 at 140K

| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- | --- |
| Fe1 | S1 | 2.5361(16) |  | S1 | P1 | 2.0244(17) |
| Fe1 | S11 | 2.5442(14) |  | S2 | Fe14 | 2.5464(17) |
| Fe1 | S12 | 2.5442(14) |  | S2 | Fe16 | 2.5464(17) |
| Fe1 | S13 | 2.5361(16) |  | S2 | P1 | 2.031(3) |
| Fe1 | S24 | 2.5464(17) |  | P1 | S17 | 2.0244(17) |
| Fe1 | S25 | 2.5464(17) |  | P1 | P18 | 2.182(4) |
| S1 | Fe11 | 2.5442(14) |  |  |  |  |

Table S 2 Bond angles of bulk FePS3 at 140K

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S1 | Fe1 | S11 | 94.91(7) |  | S24 | Fe1 | S25 | 94.85(7) |
| S11 | Fe1 | S12 | 95.51(5) |  | Fe1 | S1 | Fe13 | 84.49(5) |
| S1 | Fe1 | S12 | 85.13(5) |  | P1 | S1 | Fe1 | 103.14(8) |
| S11 | Fe1 | S13 | 85.13(5) |  | P1 | S1 | Fe13 | 103.23(8) |
| S1 | Fe1 | S13 | 95.51(5) |  | Fe14 | S2 | Fe16 | 85.15(7) |
| S12 | Fe1 | S13 | 179.05(8) |  | P1 | S2 | Fe16 | 103.24(8) |
| S1 | Fe1 | S24 | 179.57(5) |  | P1 | S2 | Fe14 | 103.24(8) |
| S11 | Fe1 | S25 | 179.57(5) |  | S17 | P1 | S1 | 114.41(12) |
| S11 | Fe1 | S24 | 85.12(5) |  | S1 | P1 | S2 | 114.05(7) |
| S1 | Fe1 | S25 | 85.12(5) |  | S17 | P1 | S2 | 114.05(7) |
| S12 | Fe1 | S24 | 94.44(6) |  | S17 | P1 | P18 | 104.39(8) |
| S13 | Fe1 | S24 | 84.91(6) |  | S1 | P1 | P18 | 104.39(8) |
| S12 | Fe1 | S25 | 84.91(6) |  | S2 | P1 | P18 | 103.88(14) |
| S13 | Fe1 | S25 | 94.44(6) |  |  |  |  |  |

Table S 3 Bond lengths of bulk FePS3 at RT

| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- | --- |
| Fe1 | S1 | 2.539(3) |  | S1 | P1 | 2.030(3) |
| Fe1 | S11 | 2.547(3) |  | S2 | Fe14 | 2.549(3) |
| Fe1 | S12 | 2.547(3) |  | S2 | Fe16 | 2.549(3) |
| Fe1 | S13 | 2.539(3) |  | S2 | P1 | 2.027(4) |
| Fe1 | S24 | 2.550(3) |  | P1 | S17 | 2.030(3) |
| Fe1 | S25 | 2.549(3) |  | P1 | P18 | 2.191(6) |
| S1 | Fe11 | 2.547(3) |  |  |  |  |

Table S 4: Bond angles of bulk FePS3 at RT

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S1 | Fe1 | S11 | 94.84(13) |  | S24 | Fe1 | S25 | 94.61(14) |
| S11 | Fe1 | S12 | 95.57(11) |  | Fe1 | S1 | Fe13 | 84.43(11) |
| S1 | Fe1 | S12 | 85.09(11) |  | P1 | S1 | Fe1 | 103.25(14) |
| S11 | Fe1 | S13 | 85.09(11) |  | P1 | S1 | Fe13 | 103.34(11) |
| S1 | Fe1 | S13 | 95.57(11) |  | Fe14 | S2 | Fe16 | 85.39(14) |
| S12 | Fe1 | S13 | 179.03(10) |  | P1 | S2 | Fe16 | 103.29(13) |
| S1 | Fe1 | S24 | 179.53(7) |  | P1 | S2 | Fe14 | 103.29(13) |
| S11 | Fe1 | S25 | 179.53(7) |  | S17 | P1 | S1 | 114.46(18) |
| S11 | Fe1 | S24 | 85.28(12) |  | S1 | P1 | P18 | 104.15(10) |
| S1 | Fe1 | S25 | 85.28(12) |  | S17 | P1 | P18 | 104.15(10) |
| S12 | Fe1 | S24 | 94.44(11) |  | S2 | P1 | S17 | 114.15(11) |
| S13 | Fe1 | S24 | 84.90(11) |  | S2 | P1 | S1 | 114.16(11) |
| S12 | Fe1 | S25 | 84.90(11) |  | S2 | P1 | P18 | 104.04(18) |
| S13 | Fe1 | S25 | 94.44(11) |  |  |  |  |  |

2. DFT+U calculations

Table S 5:DFT +U calculated energies for FePS3 , assuming the lattice parameters and positions of the atoms taken from XRD measurements

| Thermal energy [K] | dE [meV/atom] |  | Energy [eV/atom] | Energy [eV/cell] | Energy [Ry/cell] |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1033.89 |  | 89.09 | -899.867 | -17997.34637 | -1322.780079 | FM |
| 0.96 |  | 0.08 | -899.956 | -17999.12653 | -1322.910919 | Neél |
| 1025.89 |  | 88.40 | -899.868 | -17997.36017 | -1322.781094 | Zigzag |
| 612.70 |  | 52.79 | -899.903 | -17998.07225 | -1322.833431 | Stripe |
| 0 |  | 0 | -899.956 | -17999.12819 | -1322.911041 | a/b Zigzag |
| 29.01 |  | 2.50 | -899.953 | -17999.07817 | -1322.907365 | Striped Zigzag |
| 31.05 |  | 2.67 | -899.953 | -17999.07466 | -1322.907107 | a/b Stripe |

Table S 6: DFT+U calculated energies for MnPS3

| Thermal energy [K] | dE [meV/atom] | Energy [eV/atom] | Energy [eV/cell] | Energy [Ry/cell] |  |
| --- | --- | --- | --- | --- | --- |
| 420.66 | 36.24 | -899.9203607 | -17998.40721 | -1322.85805 | FM |
| 0 | 0 | -899.9566093 | -17999.13219 | -1322.911335 | Neél |
| 69.653 | 6.00 | -899.9506073 | -17999.01215 | -1322.902512 | Zigzag |
| -0.56 | -0.04 | -899.9566583 | -17999.13317 | -1322.911407 | Stripe |

Figure S 2: Band structures in vicinity of Fermi level: using DFT+U+SOI (U=5.3eV for FePS3, U=5eV for MnPS3

3. Optical Measurements

Intensity

1       2

Figure S 3: Optical measurements of ME transition. (a) Polar plot of linear polarization measurements of ME transition at 4K. (b) Temperature dependent measurements of ME transition, where T = 4-130K

(a)

ME transition measurements

  - Gaussian fits of PL spectra

Figure S 4: Gaussian fits of LE transition at (a) 4K and (b) 70K.

Figure S 5: Gaussian fits of HE transition at (a) 4K and (b) 70K