Supporting Information

Disrupted cellulose aggregation leads to the reduced mechanical performance of wood-adhesive interphase during freeze-thaw cycles

Yizhong Caoa, b*, Chuhang Xua, b, Shuwei Xua, b, Haili Chena, b, Yutao, Yana, b, Yifan Chena, b, Qiang Wua, b*, Siqun Wangc

a. College of Chemistry and Materials Engineering, Zhejiang A&F University, Hangzhou, 311300, China

b. National Engineering and Technology Research Center of Wood-based Resources Comprehensive Utilization, Hangzhou, 311300, China

c. Center for Renewable Carbon, University of Tennessee, Knoxville, TN 37996, USA

*Corresponding author: Y. Cao (20210024@zafu.edu.cn) and Q. Wu (wuqiang@zafu.edu.cn)

This Supporting information contains two figures that describe the cooling rate of the FTCs and the sample preparation for SAXS analysis. Calculating radius of gyration (Rg) and the grain size (L) of the nanocellulose crystal, fractal dimension and distance between cellulose macromolecules (d) using the data of SAXS was also listed here.

Fig.S1 The cooling rate of wood-adhesive bonds at different freezing temperatures.

Fig.S2 The sample preparation procedures for SAXS analysis.

Calculating radius of gyration (Rg) and the grain size (L) of the nanocellulose crystal, fractal dimension and distance between cellulose macromolecules (d) using the data of SAXS

The relationship between the radius of gyration (Rg) and the grain size (L) of the nanocellulose crystal can be described using following equations (Zhu 2008, Ba et al. 2021):

|  | Rg=L23 | (1) |
| --- | --- | --- |

Where Rg can be obtained from Guinier formula (Eq.2)(Guinier et al. 1964, Glatter and Kratky 1982, Roe 2000):

|  | I(q)=IeMn2exp⁡(-q2Rg23) | (2) |
| --- | --- | --- |

In Eq.2, the I(q) represent the SAXS intensity and the q is the value of scattering vector. M is the number of incoherent particles, n is the total number of electrons, and Ie is the scattering intensity of one electron. Rg can be calculated by obtaining the slope (α) of lnI(q)-q2 curves (Eq.3)(Zhu 2008).

|  | Rg=-3α | (3) |
| --- | --- | --- |

Combination of Eq.1 and Eq.3 yields the L as:

|  | L=12-α | (4) |
| --- | --- | --- |

It should be noted that the slope fitting reveals well in the range of 0<q2<0.003 Å−2, thus the same fitting range was used in this work.

The Porod law meets the formula of I(q)=aq-4+b, and a Power law with a formula of I(q)=q-α fits well in the smaller q ranges (less than 0.035 Å−1). The fractal dimension can be obtained according to following rules (Penttila et al. 2010, Penttila et al. 2013):

(1) α<3, fractal dimension D=α, mass fractal

(2) 3<α<4, fractal dimension D=6-α, surface fractal

The distance between cellulose macromolecules (d) can be obtained from Eq.5, and the qmax represents the peak location in the Kratky plot using a parabola fit on the top of the peak (Virtanen et al. 2015).

|  | d=2π/qmax | (5) |
| --- | --- | --- |

Reference

Ba, Z., Chen G., Luo H. and Luo J. (2021) In situ SAXS analysis of the water effects on the thickness evolution of nanocellulose within bamboo fiber. Wood Sci. Technol., 55 (2): 351-360.

Glatter, O. and Kratky O. (1982) In small angle X-ray scattering, London, Oxford Press.

Guinier, A., Lorrain P., Sainte-Marie Lorrain D. and Gillis J. (1964) X-Ray Diffraction in Crystals, Imperfect Crystals, and Amorphous Bodies. Physics Today, 17 (4): 70-72.

Penttila, A., Varnai A., Leppanen K., Peura M., Kallonen A., Jaaskelainen P., Lucenius J., Ruokolainen J., Siika-aho M., Viikari L. and Serimaa R. (2010) Changes in submicrometer structure of enzymatically hydrolyzed microcrystalline cellulose. Biomacromolecules, 11: 1111-1117.

Penttila, P., Kilpelainen P., Tolonen L., Suuronen P., Sixta H., Willfor S. and Serimaa R. (2013) Effects of pressurized hot water extraction on the nanoscale structure of birch sawdust. Cellulose, 20 (5): 2335-2347.

Roe, J. (2000) Methods of X-ray and neutron scattering in polymer science, New York, Oxford University Press.

Virtanen, T., Penttila P., Maloney T., Gronqvist S., Kamppuri T., Vehvilainen M., Serimaa R. and Maunu S. (2015) Impact of mechanical and enzymatic pretreatments on softwood pulp fiber wall structure studied with NMR spectroscopy and X-ray scattering. Cellulose, 22 (3): 1565-1576.

Zhu, Y. (2008) Small angle X-ray scattering-theory, testing, calculation and application, Beijing, Chemical Industry Press.