Appendix

Table S 1. Zeta Potentials of blank-NS formulations

| Blanks | Zeta Potential (24 h) | Zeta Potential (30 Days) | Zeta Potential (90 Days) |
| --- | --- | --- | --- |
| Q-S154 | -17.7 ± 0.06 | -11.20 ± 0.35 | -6.45 ± 0.28 |
| Q-C888 | -8.90 ± 1.09 | -11.4 ± 0.65 | -4.62 ± 0.66 |
| Q-CHD 5 | -12.9 ± 0.20 | -8.75 ± 0.59 | -6.56 ± 0.35 |

Key: QHCl = Quinine hydrochloride, S154 = Softisan® 154, C888 = Compritol® 888 ATO, CHD 5 = Compritol® HD 5 ATO. Q-S154 = blank formulation of QHCl made with S154; Q-C888 = blank formulation of QHCl made with C888; Q-CHD 5 = blank formulation of QHCl made with CHD 5.

Q9            	        			20000x

Quinine Hydrochloride       	       2000 X

Phospholipon® 90H        				1200 X

Softisan®154		        		500 X

Q7                            			 20000x

Q12			     	 		 20000x

Figure S1. SEM micrographs of drug and some excipients

Key: QHCl = Quinine hydrochloride, S154 = Softisan® 154, C888 = Compritol® 888 ATO, CHD 5 = Compritol® HD 5 ATO. Selected  formulations of QHCl-NS = Q7, Q9 and Q12, made with S154, CHD 5 and C888 respectively.

FTIR spectra of Compritol® HD5 ATO	  		   (F)

FTIR spectra of Compritol® HD5 ATO     		(E)

FTIR spectra of Compritol® 888 ATO              (D)

FTIR spectra of Lipid matrix made with Softisan® 154 and Phospholipon® 90H					(C)

FTIR spectra of S154				(B)

FTIR spectra of Phospholipon® 90H    (A)

Figure S2. FTIR Spectra of Excipients and QHCL-NS formulation (A-L)

FTIR spectra of Lipid matrix made with Compritol® HD5 ATO and Phospholipon® 90H		   (H)

FTIR spectra of Q7 (containing 1.5 % w/v QHCl, 3 % w/v CHD 5, 2 % w/v T80 and sonicated for 90 min)	(J)

FTIR spectra of Q12 (containing 1.5 %w/v QHCl, 3 %w/v C888, 5 %w/v T80 and sonicated for 60 min)		(L)

FTIR spectra of Q9 (containing 1.5 %w/v  QHCl, 3 % w/v S154, 2 %w/v  T80 and sonicated for 60 min)      (K)

FTIR spectra of Quinine Hydrochloride	       (I)

FTIR spectra of Lipid matrix made with Compritol® 888 ATO and Phospholipon® 90H		(G)

Table S2.  DSC analysis results of plain drugs and, lipids and lipid matrices

| Materials | Melting peak (°C) | Enthalpy (J/g) | Type of peak |
| --- | --- | --- | --- |
| Quinine hydrochloride | 115.67 | 75.066 | Endothermic |
| S154 | 57.68 | 94.675 | Endothermic |
| S154 + P90H | 57.55 | 56.923 | Endothermic |
| S154 in S154 + P90H + THP | 55.67 | 44.533 |  |
| S154 in S154 + P90H + THP+MCT | 47.99 |  |  |
| C888 | 72.53 | 116.25 | Endothermic |
| C888 in C888 + P90H | 67.03 | 95.464 | Endothermic |
| C888 in C888 + P90H + THP | 64.17 | 93.656 |  |
| C888 in C888 + P90H + THP+MCT | 57.35 |  |  |
| CHD5 | 59.56 | 117.83 | Endothermic |
| CHD5 in CHD5 + P90H | 53.93 | 41.709 | Endothermic |
| CHD5 in CHD5 + P90H + THP | 44.87 | 11.189 |  |
| CHD5 in CHD5 + P90H + THP+MCT | 24.46 |  |  |

Figure S3: DSC thermogram of lipid matrix made with C888 and P90H.