Supporting Information

Experimental section

General remarks

Dried glassware’s were used for the reactions and maintained the reaction conditions. A Perkin-Elmer Spectrometer (Model no.783USA) was used to get FTIR spectra of compounds in the range of 400-4000 cm -1 using KBr pellets to confirm the material and surface functionalization. The weight loss curves were obtained by heating the sample using instrument TA SDT Q600 V20.9 Build 20 from 25 o C to 1000 o C. The elemental composition was analyzed by Perkin-Elmer 2400, Series II, CHNS/O analyser. Phase identification and structural analysis of synthesized compounds were studied using X-Ray diffractometer RIGAKU Mini flex 600 (XRD) in the 2θ range from 20° to 80°. The morphology of samples was examined using a Philips CM 200 model TEM, with an operating voltage of 20-200 kV. Magnetization measurements were performed on Lakeshore magnetometer, USA, Model 7410 (VSM). Inductions heating of all samples were performed in a plastic microcentrifuge tube (1.5 mL) with a 6 cm diameter coil (4 turns). Nano-magnetite (1), silica coated nano-magnetite (2) and 3-chlopropyl modified silica coated nano-magnetite (4) were prepared following literature procedure. [1-3] All other chemicals were obtained from local suppliers and used without further purification.

[Nano-magnetite-[FemTriaz]Cl] (6)

A mixture of 4 (1 g), 1-N-ferrocenylmethyl triazole (5) (0.94 g, 3 mmol) in DMF (25 mL) was heated at 80 °C in an oil bath. After 72 h, the product was separated by external magnet, washed with DMF (3×50 mL), methanol (3×50 mL), CH 2 Cl 2 (3×50 mL) and dried under vacuum at 50 °C for 24 h to yield [Nano-magnetite-[FemTriaz]Cl] (6). FT-IR (KBr, Thin Film, υ, cm −1 ): 3936, 3844, 3409, 1881, 1662, 1546, 1111, 804, 643, 558, 474, 396 cm −1 .

Nano-magnetite-FemTriaz-NHC-Au complex (7)

A mixtrure of 6 (1g), tiphenylphosphonium gold chloride (0.0247 g, 0.5 mmol), K 2 CO 3 (0.138 g, 1 mmol) in DCM (25 ml) was external magnet and subsequent washed with diethyl ether to afford Nano-magnetite-FemTriaz-NHC-Au complex (7). FT-IR (KBr, Thin Film, υ, cm −1 ): 3442, 2962, 2925, 2853, 2387, 2288, 1645, 1555, 1402, 1034, 629, 562, 465, 396 cm −1 . ( N: 1.8 %)Loading: 0.075 mmol of Au units g −1 of 7.

General method for MTT assay

The Nano-magnetite (1), [Nano-magnetite-FemTriaz]Cl (6) and nano-magnetite-FemTriaz-NHC-Au complex (7) were screened for in vitro anticancer activity against human breast cancer MCF-7 cells at three different concentrations using MTT assay. The cell lines were incubated with nanoparticles of 1, 6 and 7 for 48h with concentration of 10, 30 and 100 µg/mL in the 5% CO2 atmosphere. The results of MTT assay are summarized in (Table 1). The results revealed that 1, 6 and 7 displayed moderate to significant anticancer activity against human breast cancer cell line MCF-7 with % inhibition ranging from 38.04 to 46.08 as compared to standard drug used 5-fluoro uracil (52.60 %). It is noteworthy that 7 exhibited significant anticancer activity with 46.08 % inhibition compared to 5-fluoro uracil. The significantly higher anticancer activity of 7 is attributed to synergistic effect of NHC ligand and architecture and gold metal.

General method for CAM assay

Angiogenesis is a vital step in cancer metastasis and tumor development and therefore its inhibition is regarded as one of the assured strategies in anticancer therapy. The nanotechnology-based approaches help in the management of angiogenesis by specific delivery of angiogenesis inhibitors to the cancerous cells. In view of this Nano-magnetite-FemTriaz-NHC-Au complex (7) was evaluate for antiangiogenic properties using in ovo CAM assay on fertilized chick eggs. The eggs were treated with 7 and assessed for antiangiogenic activities on the 3rd, 6th and 8th day post incubation and antiangiogenic effect was observed (Table 2). There is a significant decrease in density of secondary blood vessels at concentration 0.01g/50ul

Table no 1: Anticancer activity of nano-magnetite (1), [Nano-magnetite-FemTriaz]Cl (6) and of nano-magnetite-FemTriaz-NHC-Au complex (7) against human breast cancer MCF-7 cells

| Compound | Human breast cancer cell line MCF-7 |  |  |
| --- | --- | --- | --- |
|  | % Inhibitiona | % Inhibitionb | %Inhibitionc |
| Nano-magnetite (1) | 38.04 | 42.66 | 45.26 |
| [Nano-magnetite-FemTriaz]Cl (6) | 39.81 | 40.45 | 43.18 |
| Nano-magnetite-FemTriaz-NHC-Au complex (7) | 43.33 | 45.77 | 46.08 |
| 5-Fluorouracil (5-FU) | 49.06 | 51.63 | 52.60 |

Table 3: Hyperthermia setup for compounds at fixed magnetic field 335.2 Oe with 400 kHz frequency using AC current

| Sr. no. | Time in Sec | Minutes | Temperature for nanomagnetite (1) | Temperature for [Nano-magnetite-[FemTriaz]Cl](6) | Temperature for nano-magnetite-FemTriaz-NHC-Au complex (7) |
| --- | --- | --- | --- | --- | --- |
| 1 | 600 | 0 | 27.5 | 27.3 | 29.1 |
| 2 | 540 | 1 | 35.6 | 31.1 | 32.2 |
| 3 | 480 | 2 | 41.8 | 35.0 | 35.1 |
| 4 | 420 | 3 | 47.0 | 38.5 | 37.0 |
| 5 | 360 | 4 | 52.1 | 41.1 | 38.6 |
| 6 | 300 | 5 | 57.0 | 43.2 | 39.1 |
| 7 | 240 | 6 | 60.5 | 45.5 | 40.7 |
| 8 | 180 | 7 | 63.9 | 47.5 | 42.7 |
| 9 | 120 | 8 | 67.0 | 48.6 | 43.9 |
| 10 | 60 | 9 | 70.0 | 50.2 | 45.5 |
| 11 | 0 | 10 | 72.2 | 51.4 | 46.8 |

Table 5: Hyperthermia setup for nano-magnetite-FemTriaz-NHC-Au complex (7) complex at variable magnetic field 251.4 Oe and 335.2 Oe with 276 kHz frequency using AC current.

| Sr. no. | Time in Sec | Minutes | Temperature for complex (7) at 300Oe | Temperature for complex (7) at 400Oe |
| --- | --- | --- | --- | --- |
| 1 | 600 | 0 | 28.1 | 29.1 |
| 2 | 540 | 1 | 31.2 | 32.2 |
| 3 | 480 | 2 | 32.3 | 35.1 |
| 4 | 420 | 3 | 34.1 | 37.0 |
| 5 | 360 | 4 | 35.2 | 38.6 |
| 6 | 300 | 5 | 36.6 | 39.1 |
| 7 | 240 | 6 | 37.1 | 40.7 |
| 8 | 180 | 7 | 38.3 | 42.7 |
| 9 | 120 | 8 | 39.6 | 43.9 |
| 10 | 60 | 9 | 40.5 | 45.5 |
| 11 | 0 | 10 | 42.2 | 46.8 |

Reference:

- X. Zhao, Y. Shi, T. Wang, Y. Cai, G. Jiang, Journal of Chromatography A 1188, 140-147 (2008).

- Q. Liu, Z. Xu, J. A. Finch, R. Egerton, Chem Mater 10, 3936-3940 (1998).

- A. Naikwade, M. Jagadale, D. Kale, S. Gajare, G. Rashinkar, Catalysis Letters 148, 3178-3192 (2018).