Tables

Table 1 EDS results of the marked spots 1-5 in Fig 4(b).

| Marked zone | Compositions (atomic %) |  |  |  |  | Corresponding phase |
| --- | --- | --- | --- | --- | --- | --- |
|  | Ti | Si | Al | C | O |  |
| 1 | 6.81 | 2.36 | 0.40 | 90.42 | - | Csf |
| 2 | 50.93 | 3.84 | 1.10 | 44.13 | - | TiC (rich in Ti) |
| 3 | 5.23 | 57.71 | 0.79 | 36.27 | - | SiC |
| 4 | 45.56 | 15.34 | 0.59 | 38.51 | - | Ti3SiC2 |
| 5 | 2.67 | 1.36 | 26.21 | 23.68 | 46.09 | Al2O3 |

Table 2 The determined and calculated densities of the as-prepared Ti3SiC2 and Csf/Ti3SiC2 composites.

| Nominal compositions (vol %) | Apparent density (g cm−3) | Theoretical density (g cm−3) | Relative density (%) |
| --- | --- | --- | --- |
| Ti3SiC2 | 4.45 | 4.53 | 98.23 |
| 2 Csf/Ti3SiC2 | 4.41 | 4.47 | 98.65 |
| 5 Csf/Ti3SiC2 | 4.35 | 4.39 | 99.09 |
| 10 Csf/Ti3SiC2 | 4.24 | 4.25 | 99.76 |