Supplementary Information

Balanced coexistence of reversible and irreversible covalent bonds in a conductive triple polymeric network enables stretchable hydrogel with high toughness and adhesiveness

Kyuha Park1,2†, Kyumin Kang1,2†, Jungwoo Kim3, Subin Jin3, Mikyung Shin2,3,4*, and Donghee Son1,2,5*

1Department of Electrical and Computer Engineering, Sungkyunkwan University, Suwon 16419, Republic of Korea

2Center for Neuroscience Imaging Research, Institute for Basic Science (IBS), Suwon 16419, Republic of Korea

3Department of Intelligent Precision Healthcare Convergence, Sungkyunkwan University, Suwon 16419, Republic of Korea

4Department of Biomedical Engineering, Sungkyunkwan University, Suwon 16419, Republic of Korea

5Department of Superintelligence Engineering, Sungkyunkwan University, Suwon 16419, Republic of Korea

†These  authors  contributed  equally  to  this  work.

This Supplementary Information includes:

Fig. S1 to S7

Table S1

Captions for Supplementary Video 1 to 4

Supplementary Figures

Fig. S1 a) Photographs for gelation of each formulation, ET-2, ET-3, ET-4, and ET-5, as a function of time. Scale bar = 20 mm. b) Time to complete gelation of the formulations.

Fig. S2. Cross-sectional SEM images of ET-2 (top) and ET-5 (bottom) and their elemental analysis of oxygen (O; red), nitrogen (N; blue), and sulfur (S; cyan).

Fig. S3 a) Comparison of chemical structures of Alg with cis-diol groups to that of CMC without cis-diol groups. b) and c) Rheological properties of CMC-containing ET-6 hydrogels b) or Alg-containing ones c). G’ for black symbol and G” for red one. d) Tensile stress-strain curves of CMC- (blue) or Alg- (purple) based ET-4.

Fig. S4 Strain–stress curves of 50% notched ET-2 (black), ET-3 (red), ET-4 (blue), and ET-5 (pink). The inset graph for clarifying the curves of ET-2 and ET-3.

Fig. S5 Changes in electrical resistance of ET-2, ET-3, and ET-5 during one-hundred cyclic stretching test (at a speed of 0.3 mm/s, strain of 100%). The 1st scheme includes experimental setting and variables for the stretching test.

Fig. S6. Electrochemical impedance of TSC-TAH at the frequency ranging from 50 to 100,000 Hz when immersed in phosphate buffered saline (PBS).

Fig. S7. a) In vitro cytotoxicity (%) of TSC-TAH as a function of concentration, 25, 50, and 100 mg/mL. b) Fluorescent images of the live cells (green dots) and dead cells (red dots) after 24-hour treatment of the releasates from the TSC-TAH.

Supplementary Table

Table S1. Quantity of precursors to fabricate TSC-TAH.

| Precursor | a)Alg | b)CMC | c)EDOT: d)TBA | e)AAm | f)MBAA | g)TEMED | h)APS |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Weight (mg) | 300 | 364 | 134:0 (‘ET-1’) 120.6:10 (‘ET-2’) 84.4:37 (‘ET-3’) 49.6:63 (‘ET-4’) 13.4:90 (‘ET-5’) 0:100 (‘ET-6’) 0:0 ('Alg/PAAm' or 'CMC/PAAm') | 2400 | 10 | 7.76 | 800 |
| Mol (mmol) | 1.388 | 1.388 | 0 to 0.7034 | 33.765 | 0.130 | 0.172 | 3.506 |
| Molar ratio to Alg | 1 | 1 | 0 to 0.5067 | 24.325 | 0.093 | 0.124 | 2.526 |

a)Alg = sodium alginate, b)CMC = sodium carboxymethylcellulose, c)EDOT = 3,4-ethylenedioxythiophene, d)TBA = 3-thienylboronic acid, e)AAm = acrylamide, f)MBAA = N,N'-methylenebisacrylamide, g)TEMED = N,N,N',N'-tetramethyl ethylenediamine, and g)APS = ammonium persulfate

Captions for the Supplementary Videos

The Videos (from 1 to 4) are available online.

Video 1. Robust adhesiveness of TSC-TAH onto skin tissues.

Video 2. Stretching the TSC-TAH about 200% strain.

Video 3. Demonstration of the TSC-TAH-based IS-HMI for paper and rock motions.

Video 4. Demonstration of the TSC-TAH-based IS-HMI for handshaking motions.