Synthesis, structure,Hirshfeld surface analysisand computational studies of 2-amino-5-nitropyridine-2,4-dinitrophenol cocrystal

Shanmugam Sivaraman1,2•Chellakarungu Balakrishnan1,3•Palusamy Suppuraj3•
Subbiah Meenakshisundaram1*

1Department of Chemistry, Annamalai University, Annamalainagar-608002, Tamil Nadu, India.

2Department of Chemistry, IndraGanesan College of Engineering, Manikandam, Tiruchirapalli -620012, TamilNadu, India.

3 Department of Chemistry, Erode Sengunthar Engineering College, Erode - 638057, Tamil Nadu, India.

*Corresponding author:

Dr. SP. Meenakshisundaram

CSIR Emeritus Scientist

Department of Chemistry

Annamalai University

Annamalainagar - 608 002

Tamil Nadu, India

Tel: +91 94430 91274

E-mail: aumats2009@gmail.com

Supporting information

Supplementary Table

Table S1 Selected bond lengths, angles and torsion angles [Å, °]

| Bond Lengths [Å] |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C(1)-C(2) | 1.369(2) | C(5)-C(6) |  | 1.360(2) | N(1)-O(2) |  | 1.2136(17) |
| C(1)-C(6) | 1.393(2) | C(7)-N(4) |  | 1.350(2) | N(1)-O(1) |  | 1.2214(17) |
| C(1)-N(1) | 1.455(2) | C(7)-C(11) |  | 1.403(2) | N(2)-O(3) |  | 1.2111(17) |
| C(2)-C(3) | 1.380(2) | C(8)-N(4) |  | 1.3211(19) | N(2)-O(4) |  | 1.2306(17) |
| C(3)-C(4) | 1.401(2) | C(8)-C(9) |  | 1.373(2) | N(5)-O(7) |  | 1.2153(19) |
| C(3)-N(2) | 1.448(2) | C(9)-C(10) |  | 1.392(2) | N(5)-O(6) |  | 1.222(2) |
| C(4)-O(5) | 1.3322(19) | C(9)-N(5) |  | 1.434(2) | - |  | - |
| C(4)-C(5) | 1.398(2) | C(10)-C(11) |  | 1.357(2) | - |  | - |
| Bond Angles [°] |  |  |  |  |  |  |  |
| C(2)-C(1)-C(6) | 121.22(14) | C(5)-C(6)-C(1) |  | 119.42(14) | O(2)-N(1)-C(1) |  | 118.13(13) |
| C(2)-C(1)-N(1) | 118.79(14) | N(3)-C(7)-N(4) |  | 115.89(16) | O(1)-N(1)-C(1) |  | 118.21(13) |
| C(6)-C(1)-N(1) | 119.98(13) | N(3)-C(7)-C(11) |  | 122.34(16) | O(3)-N(2)-O(4) |  | 122.37(13) |
| C(1)-C(2)-C(3) | 118.70(14) | N(4)-C(7)-C(11) |  | 121.76(14) | O(3)-N(2)-C(3) |  | 119.06(13) |
| C(2)-C(3)-C(4) | 121.76(14) | N(4)-C(8)-C(9) |  | 123.16(14) | O(4)-N(2)-C(3) |  | 118.56(13) |
| C(2)-C(3)-N(2) | 117.22(13) | C(8)-C(9)-C(10) |  | 119.64(14) | C(8)-N(4)-C(7) |  | 117.85(14) |
| C(4)-C(3)-N(2) | 120.99(13) | C(8)-C(9)-N(5) |  | 119.75(14) | O(7)-N(5)-O(6) |  | 122.11(15) |
| O(5)-C(4)-C(5) | 116.95(14) | C(10)-C(9)-N(5) |  | 120.61(14) | O(7)-N(5)-C(9) |  | 118.90(16) |
| O(5)-C(4)-C(3) | 125.69(14) | C(11)-C(10)-C(9) |  | 117.86(15) | O(6)-N(5)-C(9) |  | 119.00(14) |
| C(5)-C(4)-C(3) | 117.36(14) | C(10)-C(11)-C(7) |  | 119.72(14) | - |  | - |
| C(6)-C(5)-C(4) | 121.53(14) | O(2)-N(1)-O(1) |  | 123.66(14) | - |  | - |
| Torsion Angles [°] |  |  |  |  |  |  |  |
| C(6)-C(1)-C(2)-C(3) |  |  | -0.6(2) | N(3)-C(7)-C(11)-C(10) |  | 178.13(17) |  |
| N(1)-C(1)-C(2)-C(3) |  |  | -179.17(13) | N(4)-C(7)-C(11)-C(10) |  | -0.9(3) |  |
| C(1)-C(2)-C(3)-C(4) |  |  | 0.6(2) | C(2)-C(1)-N(1)-O(2) |  | 3.1(2) |  |
| C(1)-C(2)-C(3)-N(2) |  |  | 178.86(13) | C(6)-C(1)-N(1)-O(2) |  | -175.49(15) |  |
| C(2)-C(3)-C(4)-O(5) |  |  | 179.75(14) | C(2)-C(1)-N(1)-O(1) |  | -176.99(14) |  |
| N(2)-C(3)-C(4)-O(5) |  |  | 1.6(2) | C(6)-C(1)-N(1)-O(1) |  | 4.5(2) |  |
| C(2)-C(3)-C(4)-C(5) |  |  | -0.3(2) | C(2)-C(3)-N(2)-O(3) |  | 2.3(2) |  |
| N(2)-C(3)-C(4)-C(5) |  |  | -178.42(14) | C(4)-C(3)-N(2)-O(3) |  | -179.44(15) |  |
| O(5)-C(4)-C(5)-C(6) |  |  | 179.86(15) | C(2)-C(3)-N(2)-O(4) |  | -176.54(14) |  |
| C(3)-C(4)-C(5)-C(6) |  |  | -0.1(2) | C(4)-C(3)-N(2)-O(4) |  | 1.7(2) |  |
| C(4)-C(5)-C(6)-C(1) |  |  | 0.1(3) | C(9)-C(8)-N(4)-C(7) |  | 1.0(2) |  |
| C(2)-C(1)-C(6)-C(5) |  |  | 0.3(2) | N(3)-C(7)-N(4)-C(8) |  | -179.01(15) |  |
| N(1)-C(1)-C(6)-C(5) |  |  | 178.78(14) | C(11)-C(7)-N(4)-C(8) |  | 0.1(2) |  |
| N(4)-C(8)-C(9)-C(10) |  |  | -1.2(3) | C(8)-C(9)-N(5)-O(7) |  | 178.46(16) |  |
| N(4)-C(8)-C(9)-N(5) |  |  | 179.86(15) | C(10)-C(9)-N(5)-O(7) |  | -0.4(3) |  |
| C(8)-C(9)-C(10)-C(11) |  |  | 0.4(2) | C(8)-C(9)-N(5)-O(6) |  | -1.9(3) |  |
| N(5)-C(9)-C(10)-C(11) |  |  | 179.25(16) | C(10)-C(9)-N(5)-O(6) |  | 179.25(17) |  |
| C(9)-C(10)-C(11)-C(7) |  |  | 0.6(2) | - |  | - |  |

Symmetry transformations used to generate equivalent atoms:

Table S2 Mulliken atomic charges

| Atoms | Charges (e) | Atoms | Charges (e) | Atoms | Charges (e) | Atoms | Charges (e) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C1 | 0.1138 | H9 | 0.1583 | H17 | 0.2665 | H25 | 0.1181 |
| C2 | -0.0011 | N10 | 0.1777 | C18 | 0.2878 | N26 | -0.4302 |
| H3 | 0.2097 | N11 | 0.1214 | C19 | 0.1302 | N27 | -0.3478 |
| C4 | 0.1525 | O12 | -0.2616 | H20 | 0.1580 | N28 | 0.1831 |
| C5 | 0.1722 | O13 | -0.2688 | C21 | 0.0152 | O29 | -0.2639 |
| C6 | -0.0815 | O14 | -0.1526 | C22 | 0.0144 | O30 | -0.2848 |
| H7 | 0.1466 | O15 | -0.3411 | H23 | 0.1695 | H31 | 0.2130 |
| C8 | -0.0301 | O16 | -0.3878 | C24 | -0.1771 | H32 | 0.2202 |