Real-time observation of the large polaron buildup in α-FAPbI3

Xingyu Yue,1,2,3,6 Chunwei Wang,1,3,4,6 Bo Zhang,5,6 Zeyu Zhang,1,2,3*, Zhuang Xiong,5, Xinzhi Zu,1,2,3 Zhengzheng Liu1,2,3, Zhiping Hu,2 George Omololu Odunmbaku5, Kuan Sun*5, Juan Du*1,2,3

1 State Key Laboratory of High Field Laser Physics and CAS Center for Excellence in Ultra-intense Laser Science, Shanghai Institute of Optics and Fine Mechanics (SIOM), Chinese Academy of Sciences (CAS), Shanghai 201800, China

2 School of Physics and Optoelectronic Engineering, Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences, Hangzhou, 310024, China

3 Center of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, China

4 School of Physical Science and Technology, ShanghaiTech University, 100 Haike Road, Shanghai 201210, China

5 MOE Key Laboratory of Low-grade Energy Utilization Technologies and Systems, CQU-NUS Renewable Energy Materials & Devices Joint Laboratory, School of Energy & Power Engineering, Chongqing University, Chongqing 400044, China

6 These authors contribute equally to this work.

*E-mail: zhangzeyu@ucas.ac.cn, kuan.sun@cqu.edu.cn, dujuan@siom.ac.cn

Supporting Information

Supplementary Figure S1

Figure S1 XRD data for 0.85FA and 0.95FA. Based on Bragg’s law, since I- is larger than Br-, the diffraction angle of XRD peak increases with the increase of Br content

Supplementary Figure S2

Figure S2 Absorption spectrum of 0.85FA and 0.95FA perovskites respectively

Supplementary Figure S3

Figure S3 THz time-domain emission spectra of 0.85FA measured with different excitation fluence at incident angle of 45°; The inset shows pump fluence dependent peak-to-valley value of THz signals with 480nm laser excitation.

Supplementary Figure S4

Figure S4 Incident angle θ dependent peak-to-valley value of THz signals with 480nm laser excitation, solid line is the theoretical curve calculated Eq. (1) in the text.

Supplementary Figure S5

Figure S5 Polarization dependence of the emitted THz fields.

Supplementary Figure S6

Figure S6 THz transients from 0.95FA (a-b) and 0.85FA (c-d) thin-films with different sample orientations. The emitted THz amplitude does not change upon changing the sample orientation shown for different φ angles.

Supplementary Figure S7

Figure S7 (a) Schematic diagram of the experimental setup for changing the polarization state of the pump beam with half-wave plate (HWP) and quarter-wave plate (QWP); Terahertz (THz) emission with half-wave plate in 0.95FA (b) and 0.85FA (c), inset in (b-c) are the fitting parameters C1, C2, L2, and D fitted from formula 2; (d) Schematic diagram of the continuum bands (VB and CB) having Rashba spin splitting, and related optical transitions with circular polarized light. The imbalance in momentum space causes the carriers to have a net velocity in a certain direction, which generates electric current; THz emission due to ultrafast photogalvanic (PGE) currents in 0.95FA (e) and 0.85FA (f), inset in (e-f) are the fitting parameters C1, C2, L2, and D fitted from formula 2.

Supplementary note S1

Figure S7(a) shows the experimental setup for changing the polarization state of the pump light with quarter-wave plate and half-wave plate. From Figure a and Figure b, it can be seen that there are four equal peaks in the THz electric field intensity with the linear polarization direction of the pump light, which can be fitted by the following formula:

J(β)=Esin(4β)+Fcos(4β)+G                  ⑴

Here, β is the angle between the fast axis of the half-wave plate and the pump light polarization, E, F and G are constants. Since the half-wave plate can change the polarization direction of the linearly polarized light, this may be caused by the different absorption coefficients of s-light and p-light on the sample surface.

In HOIPs, the conduction band (CB) bottom consists of J=12states, whereas the valence band (VB) top has S=12 states1. Heavy atoms contribute to a giant spin−orbit coupling (SOC), leading to the splitting of the conduction band and valence band, which is called Rashba band splitting. Figure S7(d) depicts the splitting of the conduction band and valence band when the reverse pair forming is broken. According to the selection rule, the electron transition must be satisfied ∆mJ=±1. When absorbing left (right) circular polarized light, the electron will be unbalanced in the momentum space, resulting in a certain direction of photocurrent, and different polarized light will lead to different directions of photocurrent. A quarter-wave plate is used to change the polarization of the pump light by rotating the angle, α between the fast axis of the QWP and the pump light polarization. Figure. S7(e) are THz emission signal peak-to-valley value of 0.95FA under 480nm optical excitation. The photocurrent can usually be expressed as2:

Jα=C1sin2α+C2sin2α+L1sin4α+L2sin4α+D         ⑵

Here, C1 is the CPGE current, C2 is mainly due to misalignment between the fast axis of the λ/4 waveplate and the incident light polarization，and L1 andL2 are the photocurrent induced by linearly polarized light, which may be induced by linear photogalvanic effect (LPGE) or photon drag effect，D is the photocurrent generated by the photo-dember effect. Inset in figure 7(f) shows the fitting parameters C1, L2, and D fitted from formula 3, the parameter D is much larger than the other parameters. Overall, the main mechanism of THz emission in HOIPs is the photo-dember effect.

Supplementary Figure S8

Figure S8 Amplitude spectrum of the emitted THz field for 0.95FA (a) and 0.85FA (b).

References

1.	Li, J. & Haney, P.M. Circular photogalvanic effect in organometal halide perovskite CH3NH3PbI3. Applied physics letters 109, 193903 (2016).

2.	Liu, X. et al. Circular photogalvanic spectroscopy of Rashba splitting in 2D hybrid organic–inorganic perovskite multiple quantum wells. Nature communications 11, 1-8 (2020).