Supplementary information

Optimization of moist and oven-dried bacterial cellulose production for functional properties

Ioana M. Bodea1, Florin I. Beteg1, Carmen R. Pop2, Adriana P. David3, Mircea Cristian Dudescu4, Cristian Vilău4, Andreea Stănilă2, Ancuța M. Rotar2, Giorgiana M. Cătunescu*3

1 Department of Preclinics and Clinical Sciences, Faculty of Veterinary Medicine, University of Agricultural Sciences and Veterinary Medicine Cluj-Napoca, Romania.

2 Department of Food Science, Faculty of Food Science and Technology, University of Agricultural Sciences and Veterinary Medicine Cluj-Napoca, Romania.

3 Department of Technical and Soil Sciences, Faculty of Agriculture, University of Agricultural Science and Veterinary Medicine Cluj-Napoca, Romania.

4 Department of Mechanical Engineering, Technical University of Cluj-Napoca, Romania.

*corresponding author: giorgiana.catunescu@usamvcluj.ro

# PRELIMINARY STUDY

## Principal component analysis of the effect of harvest day and inoculum volume on film thickness, uniformity, weight, and yield

The principal component analysis (PCA) biplots (Figure 1) shows the distribution of samples and the influence of inoculum volume and harvest period on BC properties (thickness, uniformity, dry weight, water content and yield). The first 3 principal factors were selected: F1 consisting of dry weigh, water content, and thickness and accounted for 53.48% of the variability in the samples; F2 consisting of yield with 22.15% of the variability; and F3 consisting of uniformity with 14.45% of the variability (Table 1).

Figure 1. Principal component analysis (PCA) biplots of the samples and analyzed parameters of bacterial cellulose (axes F1 and F2: 75.63%; F1 and F3: 67.93%)

where: 1 - dry weigh; 2 - water content; 3 - thickness; 4 - uniformity; 5 - yield; i – inoculum, d – harvest day; the number following “i” stands for inoculum volume 1, 3, 5 mL and the number following “d” represents the harvest day 6, 12, 18 days.

This grouping showed the positive correlation among dry weigh, water content, and thickness (r > 0.53; p < 0.006), and the among water content, thickness, and uniformity (r > 0.42; p < 0.037). The samples are grouped mainly by the harvest day on both biplots, showing once again the strong influence of this parameter upon the selected properties of BC.

Table 1. Correlations between variables and Principal component analysis (PCA) factors, contribution of the variables and squared cosines of the variables

| PCA variable | Correlations between variables and PCA factors |  |  | Contribution of the variables (%) |  |  | Correlations between variables and PCA factors |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | F1 | F2 | F3 | F1 | F2 | F3 | F1 | F2 | F3 |
| dry weigh | 0.77 | 0.34 | -0.33 | 22.39 | 10.33 | 15.24 | 0.60 | 0.11 | 0.11 |
| water content | 0.91 | -0.19 | -0.23 | 30.75 | 3.10 | 7.51 | 0.82 | 0.03 | 0.05 |
| thickness | 0.90 | -0.19 | -0.03 | 30.42 | 3.10 | 0.12 | 0.81 | 0.03 | 0.00 |
| uniformity | 0.65 | -0.08 | 0.74 | 15.82 | 0.55 | 74.93 | 0.42 | 0.01 | 0.54 |
| yield | 0.13 | 0.96 | 0.13 | 0.63 | 82.92 | 2.20 | 0.02 | 0.92 | 0.02 |
| inoculum | 0.00 | 0.58 | 0.40 |  |  |  | 0.00 | 0.33 | 0.16 |
| day | 0.78 | -0.03 | -0.15 |  |  |  | 0.62 | 0.00 | 0.02 |

Note: Values in bold correspond for each variable to the factor for which the squared cosine is the largest.

Table 2. Characteristics of the bacterial cellulose pellicle dependent on the incubation and inoculum volume, mean±SD

| Harvest day (d) | Inoculum volume (mL) | Thickness (mm) | Uniformity (mm) | Dry weigh (mg) | Water Content (mg) | Yield g/L |
| --- | --- | --- | --- | --- | --- | --- |
| 6 | 1 | 1.68±0.16fgh | 0.281±0.165bcd | 5.80±3.83bcd | 790.73±58.36bcdefg | 0.23±0.15bcd |
|  | 2 | 1.41±0.32h | 0.189±0.115cd | 4.03±2.94bcde | 702.07±139.44defg | 0.16±0.12bcde |
|  | 3 | 1.45±0.08h | 0.168±0.015d | 3.60±0.80cde | 531.53±42.39fg | 0.14±0.03cde |
|  | 4 | 1.57±0.08gh | 0.175±0.009d | 3.53±0.32de | 491.50±141.30g | 0.14±0.01de |
|  | 5 | 1.34±0.20h | 0.224±0.089cd | 4.03±2.40bcde | 633.57±198.20efg | 0.216±0.01bcde |
| 9 | 1 | 2.31±0.53abc | 0.283±0.083bcd | 4.93±3.07bcde | 1138.53±266.20a | 0.12±0.12bcde |
|  | 2 | 1.82±0.48cdefgh | 0.341±0.048bcd | 4.53±2.58bcde | 929.20±92.30abcde | 0.18±0.10bcde |
|  | 3 | 1.70±0.39efgh | 0.234±0.052cd | 5.23±1.33bcde | 937.30±77.19abcde | 0.21±0.05bcde |
|  | 4 | 1.95±0.25bcdefg | 0.327±0.102bcd | 4.83±0.67bcde | 752.20±119.14cdefg | 0.19±0.03bcde |
|  | 5 | 1.81±0.12defgh | 0.350±0.175bcd | 5.33±2.10bcde | 881.13±193.43abcde | 0.21±0.08bcde |
| 12 | 1 | 2.13±0.61bcdef | 0.300±0.032bcd | 2.63±1.10e | 823.33±166.60abcdefg | 0.11±0.04e |
|  | 2 | 1.68±0.15fgh | 0.239±0.022cd | 6.10±1.31bcd | 753.77±344.19cdefg | 0.24±0.05bcd |
|  | 3 | 2.09±0.15bcdef | 0.254±0.071bcd | 5.00±2.15bcde | 937.43±195.11abcde | 0.20±0.09bcde |
|  | 4 | 2.16±0.13bcdef | 0.343±0.100bcd | 5.17±1.37bcde | 885.20±175.17abcde | 0.21±0.05bcde |
|  | 5 | 1.95±0.10bcdefg | 0.336±0.196bcd | 4.80±1.31bcde | 740.57±134.98cdefg | 0.19±0.01bcde |
| 15 | 1 | 2.17±0.20abcdef | 0.251±0.175cd | 6.53±0.93bcd | 1072.00±31.29abc | 0.26±0.04bcd |
|  | 2 | 1.95±0.25bcdefg | 0.240±0.174cd | 5.50±0.36bcde | 837.40±318.44abcdef | 0.22±0.01bcde |
|  | 3 | 2.06±0.25bcdefg | 0.232±0.116cd | 6.60±0.36bc | 973.03±135.72abcd | 0.26±0.01bc |
|  | 4 | 2.33±0.18ab | 0.597±0.164a | 5.53±1.72bcde | 990.93±188.85abcd | 0.22±0.07bcde |
|  | 5 | 2.39±0.36ab | 0.378±0.173bc | 9.83±1.46a | 1094.17±93.67ab | 0.39±0.06a |
| 18 | 1 | 2.67±0.67a | 0.285±0.072bcd | 6.33±0.32bcd | 1133.33±439.23a | 0.25±0.01bcd |
|  | 2 | 2.19±0.03abcde | 0.262±0.121bcd | 6.23±0.65bcd | 1107.03±107.63ab | 0.25±0.03bcd |
|  | 3 | 2.30±0.22abcd | 0.444±0.115ab | 6.83±0.32ab | 1009.30±90.95abcd | 0.27±0.01ab |
|  | 4 | 2.27±0.31abcd | 0.229±0.089cd | 6.63±3.87bc | 964.77±484.63abcde | 0.27±0.15bc |
|  | 5 | 2.28±0.23abcd | 0.304±0.099bcd | 4.83±0.40bcde | 967.70±11.07abcde | 0.19±0.02bcde |

Note: The data are presented as mean ± SD. Different letters (a-h) within the same column show significant differences among the samples (Fisher (LSD), p < 0.05)

# OPTIMIZATION STUDY

## Water uptake ability: swelling ratio and moisture content

Table 3. Swelling ratio over time of the bacterial cellulose membranes dependent on the incubation and inoculum volume.

| Harvest day (d) | Inoculum volume (mL) | BC type | 10 min | 20 min | 30 min | 1 h | 6 h | 24 h |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6 | 1 | dry | 879.4±83.9abc | 1182.7±442.5a | 1402.4±360.0a | 1486.3±376.0a | 1681.2±569.4a | 1931.4±759.9a |
| 18 | 1 | dry | 794.6±140.0bc | 1008.9±130.2a | 1189.4±274.6a | 1310.2±287.4a | 1500.0±420.4a | 1924.0±530.5a |
| 12 | 3 | dry | 694.8±66.5c | 882.3±29.9a | 1089.4±136.1a | 1333.4±332.8a | 1387.2±350.8a | 1578.9±443.1a |
| 6 | 5 | dry | 958.6±232.3ab | 1290.0±587.6a | 1374.5±665.7a | 1653.8±951.3a | 1814.0±953.4a | 1900.4±900.4a |
| 18 | 5 | dry | 1079.4±81.6a | 1253.0±169.6a | 1460.3±162.2a | 1545.3±52.8a | 1765.3±309.8a | 2343.0±572.0a |
| 6 | 1 | moist | 624.7±174.6a | 809.6±98.2a | 1187.7±476.5a | 1321.3±536.8a | 1428.4±585.9a | 1481.8±567.4a |
| 18 | 1 | moist | 887.7±1000.6a | 1113.1±1121.9a | 1282.3±1213.3a | 1367.3±1439.9a | 1435.2±1391.8a | 1519.8±1421.4a |
| 12 | 3 | moist | 628.9±105.6a | 889.4±215.8a | 1163.6±311.8a | 1333.7±391.3a | 1500.8±442.6a | 1636.9±504.4a |
| 6 | 5 | moist | 758.7±75.8a | 1040.8±84.9a | 1189.4±138.4a | 1284.8±212.1a | 1308.6±214.4a | 1408.9±150.4a |
| 18 | 5 | moist | 649.9±169.3a | 1048.2±258.9a | 1334.1±346.6a | 1566.4±393.8a | 1702.3±340.2a | 1791.8±376.9a |

Note: The data are presented as mean ± SD. Different letters (a-c) within the same column show significant differences among dry or moist BC samples (Fisher (LSD), p < 0.05)

Table 4. Moisture content over time of the bacterial cellulose membranes dependent on the incubation period and inoculum volume.

| Harvest day (d) | Inoculum volume (mL) | BC type | 10 min | 20 min | 30 min | 1 h | 6 h | 24 h |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6 | 1 | dry | 89.7±0.9abc | 91.6±2.4a | 93.1±1.5a | 93.5±1.4a | 94.0±1.6a | 97.6±3.3a |
| 18 | 1 | dry | 88.6±1.9bc | 90.9±1.0a | 92.0±1.5a | 92.7±1.5a | 93.5±1.5a | 94.8±1.3a |
| 12 | 3 | dry | 87.4±1.0c | 89.8±0.3a | 91.5±1.0a | 92.7±1.8a | 93.0±1.9a | 93.7±1.9a |
| 6 | 5 | dry | 90.2±2.3ab | 92.0±2.9a | 92.3±3.0a | 93.1±3.3a | 93.7±3.5a | 94.2±2.7a |
| 18 | 5 | dry | 91.5±0.6a | 92.5±0.9a | 93.5±0.7a | 93.9±0.2a | 94.5±0.9a | 95.8±0.9a |
| 6 | 1 | moist | 85.7±3.1a | 88.9±98.2a | 91.5±2.9a | 92.2±3.0a | 92.7±2.9a | 93.0±2.8a |
| 18 | 1 | moist | 82.1±11.7a | 86.9±8.0a | 89.0±6.4a | 88.4±7.5a | 89.8±6.1a | 90.6±5.6a |
| 12 | 3 | moist | 86.1±1.9a | 89.6±2.0a | 91.8±1.8a | 92.7±1.8a | 93.5±1.6a | 93.9±1.7a |
| 6 | 5 | moist | 88.3±1.1a | 91.2±0.7a | 92.2±0.9a | 92.7±1.1a | 92.8±1.1a | 93.3±0.7a |
| 18 | 5 | moist | 86.1±3.5a | 91.0±2.2a | 92.7±2.1a | 93.7±1.7a | 94.3±1.2a | 94.6±1.2a |

Note: The data are presented as mean ± SD. Different letters (a-c) within the same column show significant differences among dry or moist BC samples (Fisher (LSD), p < 0.05

## Drug release

Table 5. Drug release over time of the bacterial cellulose membranes dependent on the incubation period and inoculum volume.

| Harvest day (d) | Inoculum volume (mL) | BC type | 30 min | 1 h | 2 h | 3 h | 6 h | 24 h | 48 h | 72 h |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6 | 1 | dry | 0.317±0.01a | 0.295±0.01ab | 0.237±0.01c | 0.262±0.01abc | 0.258±0.01bc | 0.256±0.01bc | 0.240±0.02bc | 0.217±0.02c |
| 18 | 1 | dry | 0.284±0.03a | 0.268±0.02ab | 0.218±0.03bc | 0.224±0.03bc | 0.233±0.03abc | 0.224±0.03bc | 0.218±0.02bc | 0.194±0.02c |
| 12 | 3 | dry | 0.248±0.05a | 0.244±0.04a | 0.211±0.04ab | 0.221±0.05ab | 0.211±0.05ab | 0.180±0.03bc | 0.152±0.03cd | 0.116±0.00d |
| 6 | 5 | dry | 0.489±0.07a | 0.484±0.08a | 0.438±0.06ab | 0.413±0.07abc | 0.371±0.05bc | 0.347±0.06bcd | 0.315±0.05cd | 0.251±0.04d |
| 18 | 5 | dry | 0.525±0.14a | 0.493±0.13a | 0.468±0.12a | 0.431±0.12ab | 0.394±0.08ab | 0.377±0.10ab | 0.343±0.08ab | 0.276±0.09b |
| 6 | 1 | moist | 1.385±0.04a | 1.293±0.06ab | 1.209±0.05bc | 1.164±0.04c | 1.102±0.04cd | 0.996±0.03d | 0.877±0.10e | 0.829±0.10e |
| 18 | 1 | moist | 1.445±0.31a | 1.343±0.28a | 1.242±0.26a | 1.182±0.26a | 1.099±0.24a | 1.042±0.23a | 1.016±0.28a | 0.985±0.31a |
| 12 | 3 | moist | 1.678±0.33a | 1.625±0.32a | 1.538±0.28ab | 1.454±0.26abc | 1.336±0.23abc | 1.099±0.29bc | 1.000±0.26c | 1.002±0.19c |
| 6 | 5 | moist | 1.043±0.20a | 0.936±0.15ab | 0.896±0.14ab | 0.825±0.15abc | 0.743±0.10bc | 0.745±0.15bc | 0.643±0.10c | 0.587±0.11c |
| 18 | 5 | moist | 1.330±0.18a | 1.290±0.16ab | 1.220±0.19ab | 1.100±0.18abc | 0.998±0.17abc | 0.957±0.20bc | 0.949±0.33bc | 0.759±0.17c |

Note: The data are presented as mean ± SD. Different letters (a-d) within the same column show significant differences among the samples (Fisher (LSD), p < 0.05)

## Scanning electron microscopy (SEM)

Figure 2. SEM images of moist BC. a-i1d6; b - i5d6; c- i1d18; d- i5d18; e- i3d12; i – inoculum, d – harvest day; the number following “i” stands for inoculum volume 1, 3, 5 mL and the number following “d” represents the harvest day 6, 12, 18 days (electron high tension (EHT) = 10.00 kV; magnitude (Mag) = 10.00 KX; working distance (WD) = 7.0 mm; Signal A = SE1)

Figure 3. SEM images of dry BC. a-i1d6; b - i5d6; c- i1d18; d- i5d18; e- i3d12; i – inoculum, d – harvest day; the number following “i” stands for inoculum volume 1, 3, 5 mL and the number following “d” represents the harvest day 6, 12, 18 days. (electron high tension (EHT) = 10.00 kV; magnitude (Mag) = 10.00 KX; working distance (WD) = 7.0 mm; Signal A = SE1)