Supplementary Information

Schiff base-functionalized Metal-Organic Frameworks for Selective Sensing of Chromate and Dichromate in Water

Manpreet Kaur a, Mohamad Yusuf a, Ashok Kumar Malik a,*

a Department of Chemistry, Punjabi University, Patiala-147002, Punjab, India

*Corresponding author: malik_chem2002@yahoo.co.uk (A.K.M.)

Figure S1. FTIR spectrum of Schiff base ligand L.

Figure S2. PL Spectra of ZnMOF-1 and CdMOF-1 (3 mg) dispersed in aqueous solution of different anions (3 mL; 10 mM).

Figure S3. Stern–Volmer (SV) plots for CrO42−/Cr2O72− (0-2.0 mM) in presence of water suspension of ZnMOF-1 & CdMOF-1 (3.0 mg/ 3 mL); Quenching of fluorescence intensity of ZnMOF-1 & CdMOF-1 (3.0 mg/ 3 mL) in water suspension upon addition of CrO42−/Cr2O72− solution (0-2.0 mM).

Figure S4. The fluorescence quenching percentage of water suspension of ZnMOF-1 & CdMOF-1 (3.0 mg/ 3 mL) for CrO42−/Cr2O72−.

Section S1: Calculation of Detection Limit for CrO42-/Cr2O72-

To prepare 50 ml of 10 mM aqueous CrO42-/Cr2O72- solution, 97.1 mg K2CrO4/147.1 K2Cr2O7 was dissolved in distilled water. The fluorescence quenching experiments was carried out by using above prepared solution. To achieve a concentration of 100 μM, i.e., 0.97 mg K2CrO4/1.47 mg K2Cr2O7 in 50 ml solution, 0.5 ml of 10 mM aqueous CrO42-/Cr2O72- solution was diluted with water. Another set of fluorescence quenching titration experiment for the determination of limit of detection was performed by using above prepared diluted 100 μM aqueous CrO42-/Cr2O72- solution.

Figure S5. Linear region of fluorescence intensity (λex = 282 nm and λem = 427 (ZnMOF-1); 418 nm (CdMOF-1)) for ZnMOF-1 and CdMOF-1 suspensions in water upon incremental addition of CrO42- and Cr2O72- solutions.

To the water suspension (3 mg LMOF dispersed in 3 ml water) of ZnMOF-1 and CdMOF-1, incremental amount of 100 μM aqueous CrO42-/Cr2O72- solution in the volume ranging 0.0 μL to 200 μL was added to determine the limit of detection. For each incremental addition of aqueous CrO42-/Cr2O72- solution, the fluorescence intensity thus observed was plotted against the respective increasing concentration of CrO42-/Cr2O72-. Slop of the curve thus drawn was found to be CrO42- = 5.5571 (R2 = 0.9958); Cr2O72- = 4.9714 (R2 = 0.9981) for ZnMOF-1 and CrO42-= 5.6143 (R2 = 0.9998); Cr2O72- = 10.186 (R2 = 0.9972) for CdMOF-1. Standard deviation (σ) in the LOD determination for ZnMOF-1 and CdMOF-1 were calculated from five blank measurements for each LMOF. Detection limit (LOD = 3σ/m) is calculated according to earlier report S1, S2, while 
the findings are tabulated ahead:

| Blank Readings |  | ZnMOF-1 |  | CdMOF-1 |  |
| --- | --- | --- | --- | --- | --- |
|  |  | CrO42- | Cr2O72- | CrO42- | Cr2O72- |
| #1 | Fluorescence Intensity (a.u.) | 615 | 615 | 856 | 856 |
| #2 | Fluorescence Intensity (a.u.) | 567 | 567 | 862 | 837 |
| #3 | Fluorescence Intensity (a.u.) | 589 | 589 | 851 | 835 |
| #4 | Fluorescence Intensity (a.u.) | 594 | 594 | 849 | 846 |
| #5 | Fluorescence Intensity (a.u.) | 605 | 605 | 854 | 843 |
| Standard deviation (σ) |  | 18.13836 | 18.13836 | 5.029911 | 5.029911 |
| Slope (m) |  | -5.5571 µM | -4.9714 µM | -5.6143 µM | -10.186 µM |
| Detection limit (3σ/m) |  | 9.792167 µM or 1.90 ppm | 10.94562 µM or 3.2 ppm | 2.687732µM or 0.52 ppm | 1.481419µM or 0.43 ppm |

Figure S6. UV-vis absorption spectra of CrO42− and Cr2O72− in their aqueous solutions.

Figure S7. UV-vis absorption spectra of ZnMOF-1, CdMOF-1, L, and H2bdc in their aqueous solutions.

Figure S8. Spectral overlap between normalized absorbance spectra of different anion solutions and normalized emission spectra of ZnMOF-1 and CdMOF-1 in water.

| Table S1. Comparison among Various LCP/LMOF Sensors for Aqueous-Phase Cr(VI) Detection. |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Sr. No. | Material (LCP/LMOF) | Analyte (CrO42-/Cr2O72-) | Quenching constant (Ksv, M-1) | LOD (µM) | Reference |
| 1. | Ln3+@MIL-121 | Cr2O72- | 4.34×103 | 0.054 | S3 |
| 2. | {[Zn2(tpeb)2(2,3-ndc)2]·H2O}n | CrO42-/Cr2O72- | 3.46×103 /4.20×103 | 0.008/0.008 | S4 |
| 3. | [Zn(btz)]n [Zn(ttz)H2O]n | CrO42-/Cr2O72- CrO42-/Cr2O72- | 3.19×103/4.23×103 2.35×103/2.19×103 | 10/2 20/2 | S5 |
| 4. | [Zn(IPA)(L)]n [Cd(IPA)(L)]n | CrO42-/Cr2O72- CrO42-/Cr2O72- | 1.00×103/1.37×103 1.30×103/2.91×103 | 18.33/12.02 2.52/2.26 | S1 |
| 5. | [Zn(2-NH2bdc)(bibp)]n | Cr2O72- | 6555070 | - | S6 |
| 6. | {[Cd(L)(BPDC)]·2H2O}n {[Cd(L)(SDBA)(H2O)]·0.5H2O}n | Cr2O72- Cr2O72- | 6.4×103 4.97×103 | 37.6 48.6 | S7 |
| 7. | [Y(BTC)(H2O)6]n:0.1Eu | CrO42-/Cr2O72- | 1.18×103 /4.52×103 | 0.03/0.04 | S8 |
| 8. | {[Zn(ATA)(L)]⋅2H2O}n {[Cd(ATA)(L)]⋅2H2O}n | CrO42-/Cr2O72- CrO42-/Cr2O72- | 1.48×103/2.62×103 0.97×103/3.11×103 | 0.25/0.43 0.18/0.19 | S2 |
| 9. | ZnMOF-1 | CrO42-/Cr2O72- | 1.19 × 103/ 1.48 × 103 | 9.79 /10.94 | This work |
| 10. | CdMOF-1 | CrO42-/Cr2O72- | 1.38 × 103/ 3.63 × 103 | 2.68/1.48 | This work |

References

S1. B. Parmar, Y. Rachuri, K.K. Bisht, R. Laiya, E. Suresh, Mechanochemical and conventional synthesis of Zn (II)/Cd (II) luminescent coordination polymers: dual sensing probe for selective detection of chromate anions and TNP in aqueous phase, Inorganic chemistry 56(5) (2017) 2627-2638.

S2. B. Parmar, Y. Rachuri, K.K. Bisht, E. Suresh, Mixed-ligand LMOF fluorosensors for detection of Cr (VI) oxyanions and Fe3+/Pd2+ cations in aqueous media, Inorganic chemistry 56(18) (2017) 10939-10949.

S3. J.-N. Hao, B. Yan, Ln 3+ post-functionalized metal–organic frameworks for color tunable emission and highly sensitive sensing of toxic anions and small molecules, New Journal of Chemistry 40(5) (2016) 4654-4661.

S4. T.-Y. Gu, M. Dai, D.J. Young, Z.-G. Ren, J.-P. Lang, Luminescent Zn (II) coordination polymers for highly selective sensing of Cr (III) and Cr (VI) in water, Inorganic chemistry 56(8) (2017) 4668-4678.

S5. C.-S. Cao, H.-C. Hu, H. Xu, W.-Z. Qiao, B. Zhao, Two solvent-stable MOFs as a recyclable luminescent probe for detecting dichromate or chromate anions, CrystEngComm 18(23) (2016) 4445-4451.

S6. L. Wen, X. Zheng, K. Lv, C. Wang, X. Xu, Two amino-decorated metal–organic frameworks for highly selective and quantitatively sensing of HgII and CrVI in aqueous solution, Inorganic chemistry 54(15) (2015) 7133-7135.

S7. S. Chen, Z. Shi, L. Qin, H. Jia, H. Zheng, Two new luminescent Cd (II)-metal–organic frameworks as bifunctional chemosensors for detection of cations Fe3+, anions CrO42–, and Cr2O72– in aqueous solution, Crystal Growth & Design 17(1) (2017) 67-72.

S8. T.-W. Duan, B. Yan, H. Weng, Europium activated yttrium hybrid microporous system for luminescent sensing toxic anion of Cr (VI) species, Microporous and Mesoporous Materials 217 (2015) 196-202.