Supplementary Material

Novel grafted hydrogel for Iron and ammonia removal from ground water, synthesis and computational chemistry study

H. M. Abd El-Salam 1, Ali M El Shafey 1, and Mahmoud K. Abdel-Latif 2,3 *

1 Department of Chemistry, Faculty of Science, Polymer Research Laboratory, Beni-Suef University, 62514 Beni-Suef City, Egypt,

2 Chemistry Department, Faculty of Science, Beni-Suef University, Beni-Suef City, Egypt

3 Chemistry Department, Collage of Science, United Arab Emirates University, Al-Ain, UAE

* Corresponding author.   E-mail address: mahmoud.abdellatif@science.bsu.edu.eg

Figure S1: Effect Temperature on the removal iron(A) and ammonia(b) efficiency at different dose of grafted hydrogel. Van’t Hoff plot for the adsorption of iron (c) and ammonia (d) on grafted hydrogel

Figure S2: Temkin isotherm for iron (a) and ammonia (b) removal by grafted hydrogel

Figure S3: Pseudo-first-order kinetic model of iron (a) and ammonia (b) removal. Pseudo-second-order kinetic model of iron (c) and ammonia (d) removal.

Figure S4: The optimized structure of complexed grafted hydrogel different positions with NH4+ ion at B3LYP/6-311G(d,p) level of theory

Table S1: IR bands and their assignments for hydrogel and grafted hydrogel.

| Wave number cm-1 | Wave number cm-1 | Assignments | Ref. |
| --- | --- | --- | --- |
| Hydrogel | Grafted hydrogel |  |  |
| 612vw | 608m | Stretching vibration of substituted benzene ring | a* |
| 777vw | 783s |  |  |
| 1115w | 1110w | C-O and C-N stretching | b* |
| 1176w | 1180w |  | c* |
| 1334w | 1330w | CH2 bending | d* |
| 1449m | 1447m |  |  |
| - | 1590w | C=O, C=C and/or adsorbed H2O molecules and –COONa | e* |
| 1656s | 1657s |  |  |
| - | 2069m | Overtone and combination bands |  |
| 2376w | 2382w |  |  |
| 2516w | - | Aliphatic CH | f* |
| 2859w | - |  |  |
| 2926m | 2931s |  |  |
| 3422b | 3410b | Stretching vibration of OH and/or NH2 free or bonded | g* |
| w=weak, b=broad, s=strong, m=medium |  |  |  |

a*: (Abd El-Mageed, Abd El-Salam, Abdel- Latif, & Mustafa, 2018)

b*: (Monteiro & Neves, 2014)

c*: (Paiva, 2007)

d*: (Silverstein, Bassler,  & Morill, 1974)

e*: (Reddy & Lee, 2007)

f*: (Asabe & Bashar, 2016)

g*: (Rojas & Carlos 2019)

Table S2: TGA data of the fabricated samples (hydrogel and grafted hydrogel).

| TGA parameters for polymeric samples |  |  |  | Comments |
| --- | --- | --- | --- | --- |
| Hydrogel |  | grafted hydrogel |  |  |
| Midpiont 0C | Approx. Wt. loss % | Midpiont 0C | Approx. Wt. loss % |  |
| 73 | 4 | 95 | 2 | Moisture losing |
| 140 | 12 | 116 | 8 | Bonded water loss |
| 233 | 21 | 220 | 13 |  |
| 335 | 38 | 367 | 17 | Series of fragmentation of the polymer backbone depend on the bond strength between atoms |
| 371 | 50 | - | - |  |
| 403 | 52 | - | - |  |
| 422 | 63 | 441 | 55 |  |
| 466 | 72 | 460 | 60 |  |
| 703 | 90 | 725 | 60 | Complete degradation with carbonic residue is about 10% for hydrogel but for graft the residue is about 40%. |
| - |  | 821 | 60 |  |
| - |  | 918 | 60 |  |
| - |  | 952 | 60 |  |

Table S3: Thermodynamic parameters

| G (kJ mol-1)∆ |  | Thermodynamic parameters |  |
| --- | --- | --- | --- |
| Removal of iron | Removal of ammonia |  |  |
| -6332.12 | -1076.26 | 283 | Temperature K |
| -3795.64 | -1051.82 | 293 |  |
| -2042.85 | -1021.42 | 303 |  |
| -280.085 | -912.508 | 313 |  |
| -62.687 | -55.005 | ∆H (kJ mol-1) |  |
| -244.9 | -203.219 | S (J mol-1 K -1)∆ |  |

Table S4: Kinetic models parameters data.

| Parameter value |  |  | Parameter | Model |
| --- | --- | --- | --- | --- |
| Iron removal | Ammonia removal |  |  |  |
| 0.0283 |  | 0.0554 | k1(min-1) | Pseudo-first order |
| 128 |  | 254.6 | qe (mg g-1) |  |
| 0.98 |  | 0.8988 | R2 |  |
| 7.71 |  | 0.023 | k2(min-1) | Pseudo-second order |
| 0.295 |  | 1.06 | qe(exp) (mg g-1) |  |
| 0.36 |  | 1.469 | qe(cal) (mg/g) |  |
| 0.9979 |  | 0.9788 | R2 |  |