Suppl. Table 2. Chemical composition of the beet sugar raw filter cake.

| Constituents | Values (%) |
| --- | --- |
| SiO2 | 1.11 |
| Al2O3 | 0.29 |
| Fe2O3 | 0.24 |
| CaO | 47.73 |
| MgO | 3.21 |
| Na2O | 0.02 |
| K2O | 0.07 |
| SO3 | 0.94 |
| TiO2 | 0.02 |
| P2O5 | 0.62 |
| Organic matter | 12 |
| pH value | 9.02 |

This analysis was performed at the Delta Sugar Company, Egypt.