Suppl. Table 2. Chemical composition of the beet sugar raw filter cake.
	Constituents
	Values (%)

	SiO2
	1.11

	Al2O3
	0.29

	Fe2O3
	0.24

	CaO
	47.73

	MgO
	3.21

	Na2O
	0.02

	K2O
	0.07

	SO3
	0.94

	TiO2
	0.02

	P2O5
	0.62

	Organic matter
	12

	pH value
	9.02


This analysis was performed at the Delta Sugar Company, Egypt.


