Supplementary Information

Synthesis of core/shell nanocrystals with ordered intermetallic single-atom alloy layers for nitrate electroreduction to ammonia

Qiang Gao1,†, Bingqing Yao2,†, Hemanth Somarajan Pillai1,†, Wenjie Zang2, Xue Han1, Yuanqi Liu1, Shen-Wei Yu3, Zihao Yan1, Bokki Min1, Sen Zhang3, Hua Zhou4, Lu Ma5, Hongliang Xin1, , Qian He2,, & Huiyuan Zhu1,

1Department of Chemical Engineering, Virginia Polytechnic Institute and State University, 635 Prices Fork Rd., Blacksburg, Virginia 24061, USA.

2Department of Materials Science and Engineering, National University of Singapore, 9 Engineering Drive 1, 117575, Singapore.

3Department of Chemistry, University of Virginia, Charlottesville, Virginia 22904, USA.

4X-ray Science Division, Advanced Photon Source, Argonne National Laboratory, Lemont, Illinois 60439, USA

5National Synchrotron Light Source II (NSLS-II), Brookhaven National Laboratory, Upton, NY 11973, USA

Supplementary Figure 1 | Characterizations of Cu nanocubes. a, b, TEM images of Cu nanocubes.

Supplementary Figure 2 | Characterizations of the core/shell Cu/CuAu ordered SAA nanocubes.  a, an atomic-resolution HAADF image. b, and c, are the corresponding line profiles of line 1 and line 2 in (a), respectively.

As shown in the corresponding line profile, the intensity profiles show d-spacings of ~2.0 Å and ~3.69 Å from line 1 and line 2, which can be assigned to (-110) and (001) plane of the ordered intermetallic CuAu structure along [110] direction.

Supplementary Figure 3 | Characterizations of the core/shell Cu/CuAu ordered SAA nanocubes. a, an atomic-resolution HAADF image, and b, the corresponding FFT image of the o Cu/CuAu ordered SAA nanocubes. c-e, the corresponding FFT images of regions 1-3 in (a), showing the crystal structure along the Cu[001], CuAu [001] and CuAu[110] directions, respectively.

The corresponding FFT patterns in different regions display the crystal structure along Cu [001], CuAu [001], and CuAu [110] directions, respectively, indicating the epitaxial growth of ordered intermetallic CuAu over the Cu cube.

Supplementary Figure 4 | Illustration of the ordered intermetallic structure of CuAu. Illustration of a tetragonal P4/mmm ordered intermetallic structure of CuAu. Brown and yellow balls correspond to Cu and Au atoms, respectively.

Supplementary Figure 5 | Characterizations of the core/shell Cu/CuAu SAA nanocubes. a, an atomic-resolution HAADF-STEM image, and b, c, the corresponding unit cell mapping of Cu/CuAu SAA nanocubes.

Supplementary Figure 6 | XRD characterization. XRD patterns of as-synthesized Cu/CuAu SAA, Cu/CuAu ordered SAA nanocubes, and Cu nanocubes.

Supplementary Figure 7 | EDX characterization. EDX spectrum of the Cu/CuAu ordered SAA nanocubes.

Supplementary Figure 8 | EXAFS spectra. a, R space and b, inverse FT fitting curves of the Au L-edge for Cu/CuAu SAA nanocubes.

Supplementary Figure 9 | EXAFS spectra. a, R space and b, inverse FT fitting curves of the Au L-edge for Cu/CuAu ordered SAA nanocubes.

Supplementary Figure 10 | Characterizations of the core/shell ordered SAA. HAADF-STEM images of a, Cu/CuPd ordered SAA and b, Cu/Cu3Pt ordered SAA. Blue, yellow, and grey balls represent Cu, Pd, and Pt atoms, respectively.

Supplementary Figure 11 | TEM image of carbon-supported catalysts. TEM image of carbon-supported Cu/CuAu ordered SAA nanocubes.

Supplementary Figure 12 | Characterizations of Au nanocubes. a, b, TEM images of pure Au nanocubes.

Supplementary Figure 13 | Electrocatalytic HER performance. LSV curves of Cu/CuAu SAA nanocubes, Cu/CuAu ordered SAA nanocubes, Cu nanocubes, and Au nanocubes normalized to the geometric area. The polarization curves were obtained by sweeping the potential from -0.6 to -1.8 V vs. Ag/AgCl with a sweep rate of 20 mV s-1 in 1 M KOH.

Supplementary Figure 14 | Capacitance measurement. Cyclic voltammograms in the region of -0.1-0 V vs. Ag/AgCl for different studied samples: a, Cu/CuAu ordered SAA nanocubes, b, Cu/CuAu SAA nanocubes, c, Cu nanocubes, and d, Au nanocubes.

Supplementary Figure 15 | Capacitance measurement. Plots showing the extraction of the Cdl for different catalysts.

Supplementary Figure 16 | Electrocatalytic NO3RR performance. a, linear scan voltammetry curves of Cu/CuAu ordered SAA nanocubes, Cu/CuAu SAA nanocubes, Cu nanocubes, and Au nanocubes normalized to ECSA. b, partial NH3 current densities normalized to ECSA.

Supplementary Figure 17 | Electrocatalytic NO3RR performance. CA measurements of catalysts at different potentials for 1 h in 1 M KOH + 1 M KNO3 solution normalized to the geometric area. a, Cu/CuAu SAA nanocubes, b, Cu/CuAu ordered SAA nanocubes, c, Cu nanocubes, and d, Au nanocubes.

Supplementary Figure 18 | Ion chromatography measurements of the concentrations of NO2-. Calibration curve of NO2- with different concentrations. Electrolytes after catalysis were diluted to ensure the NO2- concentrations in the test solutions were in the linear range of the calibration curve.

Supplementary Figure 19 | UV-vis measurements of the concentrations of ammonium with Nessler’s reagents. a, the ultraviolet-visible absorption spectra of different solutions with different ammonium concentrations. b, calibration curve colorimetric NH3 assay using Nessler reagent. Electrolytes after catalysis were diluted to ensure the ammonia concentrations in the test solutions were in the linear range of the calibration curve.

Supplementary Figure 20 | Electrocatalytic NO3RR performance. FE of NH3 and NO2- for NO3RR on Cu/CuAu ordered SAA nanocubes at different potentials.

Supplementary Table 1 | Comparison of the catalytic parameter of different NO3RR electrocatalysts.

| Catalyst | Electrolyte | NH3 FE(%) | NH3 yield rate (mol/gcat*h) | Ref. |
| --- | --- | --- | --- | --- |
| Cu/CuAu ordered SAA | 1 M KOH + 1 M KNO3 | 85.5 | 8.47 | This work |
| Cu/CuAu SAA | 1 M KOH + 1 M KNO3 | 84.8 | 6.24 | This work |
| CuPd nanocubes | 1 M KOH + 1 M KNO3 | 92.5 | 6.25 | Ref. 1 |
| Fe single atom/C | 0.5 M KNO3 + 0.1 M K2SO4 | 75 | 1.18 | Ref. 2 |
| Oxygen-doped-Ru | 1 M KOH + 1 M KNO3 | 96 | 5.56 | Ref. 3 |
| Cu50Ni50 alloys | 1 M KOH + 0.1 M KNO3 | 99 | N/A | Ref. 4 |
| Pd4Cu4@N-pC | N/A | <20 | N/A | Ref. 5 |
| Cu/Cu2O | 200 ppm NO3--N + 0.5 M Na2SO4 | 95.8 | 0.2449 mmol h-1 cm-2 | Ref. 6 |
| TiO2-x nanotubes | 50 ppm NO3--N + 0.5 M Na2SO4 | 85 | N/A | Ref. 7 |
| Co3O4-TiO2/Ti | 50 ppm NO3--N + 0.1 M Na2SO4 | 89 | N/A | Ref. 8 |

Supplementary Figure 21 | Electrocatalytic NO3RR performance of Cu/CuAu ordered SAA nanocubes. The yield rate of NH3 with or without nitrate at -0.6 V vs. RHE.

Supplementary Figure 22 | ATR-SEIRAS results. ATR-SEIRAS spectra of Cu/CuAu ordered SAA nanocubes during CV cycling between 0 V and -1.8 V vs. Ag/AgCl at 5 mV/s in 0.1 M KOH + 1 M KNO3.

Supplementary Figure 23 | Electrocatalytic NO3RR performance. a, LSV curves of Cu/CuAu ordered SAA nanocubes in 1 M KOH + 1 M KNO3 solution and 1 M KOH + 0.1 M KNO3 solution. b, CA measurements of Cu/CuAu ordered SAA nanocubes at different potentials in 1 M KOH + 0.1 M KNO3 solution normalized to the geometric area. c, FE of NH3 and d, NH3 yield rate at different potentials in 1 M KOH + 1 M KNO3 solution and 1 M KOH + 0.1 M KNO3 solution.

Supplementary Figure 24 | Stability test. Stability test by running the CA measurement on Cu/CuAu ordered SAA nanocubes at -0.5 V vs. RHE for 12 h.

Supplementary Table 2 | Free formation energies of reaction intermediates at 0 V vs. RHE for strained Cu/CuAu(100), Cu/CuAu SAA and Cu(100). The free formation energies (in eV) are calculated using a grand canonical DFT scheme at U = 0 V and with respect to NO3 -(aq), OH- (aq) and H2O(l) at standard conditions.

| Catalyst | (-2.5 %) Cu/CuAu(100) Ordered SAA | Cu/CuAu SAA | Cu(100) |
| --- | --- | --- | --- |
| *NO3 | 0.10 | 0.43 | 0.32 |
| *NO2 | -1.56 | -1.21 | -1.32 |
| *NO | -2.27 | -2.14 | -2.19 |
| *NHO | -2.73 | -2.11 | -2.20 |
| *NH2O | -2.68 | -2.18 | -2.28 |
| *NH2OH | -2.42 | -2.21 | -2.25 |
| *NH2 | -4.76 | -4.27 | -4.37 |

References

1	Gao, Q. et al. Breaking adsorption-energy scaling limitations of electrocatalytic nitrate reduction on intermetallic CuPd nanocubes by machine-learned insights. Nat. Commun. 13, 2338, (2022).

2	Wu, Z.-Y. et al. Electrochemical ammonia synthesis via nitrate reduction on Fe single atom catalyst. Nat. Commun. 12, 2870, (2021).

3	Li, J. et al. Efficient Ammonia Electrosynthesis from Nitrate on Strained Ruthenium Nanoclusters. J. Am. Chem. Soc. 142, 7036-7046, (2020).

4	Wang, Y. et al. Enhanced nitrate-to-ammonia activity on copper-nickel alloys via tuning of intermediate adsorption. J. Am. Chem. Soc. 142, 5702-5708, (2020).

5	Chen, M. et al. Achieving high-performance nitrate electrocatalysis with PdCu nanoparticles confined in nitrogen-doped carbon coralline. Nanoscale 10, 19023-19030, (2018).

6	Wang, Y., Zhou, W., Jia, R., Yu, Y. & Zhang, B. Unveiling the Activity Origin of a Copper-based Electrocatalyst for Selective Nitrate Reduction to Ammonia. Angew. Chem., Int. Ed. 59, 5350-5354, (2020).

7	Jia, R. et al. Boosting Selective Nitrate Electroreduction to Ammonium by Constructing Oxygen Vacancies in TiO2. Acs Catal. 10, 3533-3540, (2020).

8	Gao, J. et al. Non-precious Co3O4-TiO2/Ti cathode based electrocatalytic nitrate reduction: Preparation, performance and mechanism. Appl. Catal. B: Environ. 254, 391-402, (2019).