Table 1 Summary of synthesise of different nanomaterials by A. scholaris plant extract reported in recent paper till date
	Synthesized 
nanomaterial
	
	Particle Size (nm)
	       Application
	
	Reference (year)
	
	
	

	Ag nanoparticles 
	
	    5-50
	       Catalytic 

    
	
	Rajasekar et al. (2021)


	
	
	

	
	
	
	
	
	
	
	
	

	Ag nanoparticles
	
	   16.57
	   Photocatalytic           
	
	Sherin et al. (2021)
	
	
	

	
	
	
	
	
	
	
	
	

	Ag nanoparticles
	
	     1-99
	 Antimicrobial        coatings
	
	Supraja et al. (2016)


	
	
	

	Ag nanoparticles
Ag nanoparticles

Ag nanoparticles

MgO nanoparticles 

Poly (Lactic-co-Glycolic) Acid nanoparticles

ZnO nanoparticles 

RGO nanosheet

Au-RGO nano composite
	
	14-20

Not Shown

15-38

20
199.5

20

Not applicable

5-10
	Antivenom agents and anti-microbial activity

Antimicrobial activity

Not shown

Anti-inflammatory 
and anti-oxidant activity

Antimicrobial activity

Antimicrobial             activity

Photocatalytic

Photocatalytic, Catalytic, Antibacterial and antiprotozoal activity
	
	Ghosh et al. (2021)

Bandyopadhyay and SI (2018)

Shimpi et al. (2015)

  Shahid et al. (2022)

  Tripathi et al. (2019)

   Supraja et al. (2018)

   Ghosh et al. (2021)

    (our previous work)

   Present work
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