Supporting information

Supercapacitive Performance of Sustainable/Eco-friendly Oxygen rich Activated-carbons derived using Hazardous Soot Particles

Deepak Kumar,b Vikrant Sahu,b Raj Kishore Sharmab and Ram Bhagat Marichia,*

aChaudhary Ranbir Singh University, Jind-126102, (Haryana)INDIA

bDepartment of Chemistry, University of Delhi, Delhi-110 007, INDIA

*Dr. Ram Bhagat Marichi, Assistant Professor 
 Department of Chemistry, 
C.R.S. University, Jind-126102

Email id: rammarichi@gmail.com

: rambhagat@crsu.ac.in

- Calculations

From GCD curves, specific capacitance (Cm, F g-1), energy density (E, Wh kg-1), power density (W kg-1) and coulombic efficiency (η) for symmetric cells was calculated from GCD curves as given by equations;

cm=I×Δtm×Δv                                                        S1

E=Cm×Δv22×3.6                                                      S2

P=E×3600Δt                                                         S3

η=ΔtdΔtc                                                             S4

here, Cm is specific capacitance (F g-1), I is current (A) applied, Δt is discharging time (s), m is total mass deposited on both the electrodes (g), Δv is working voltage window (V) excluding IR-drop, Δtc and Δtd are charging and discharging time (s) respectively [1, 2].

- Structural & Electrochemical Characterization

Fig. S1. BET surface area bar diagram for ADS, AWS and ACS.

Table S1: Weight Percentage of Carbon, Hydrogen, Nitrogen, Sulfur and Oxygen in ACS, 	    ADS and AWS.

| Name of Sample | Carbon | Hydrogen | Nitrogen | Oxygen | Sulfur |
| --- | --- | --- | --- | --- | --- |
| ACS | 15.43 | 0.12 | 0.32 | 80.89 | 3.24 |
| ADS | 56.56 | 0.54 | 1.00 | 41.17 | 0.77 |
| AWS | 83.73 | N. D. | 0.30 | 15.97 | N. D. |

Table S2. Comparative specific capacitance values of all three activated carbon samples at different scan rate.

| Scan Rate (mV s-1) | 5 | 10 | 25 | 50 | 75 | 100 |
| --- | --- | --- | --- | --- | --- | --- |
| AWS | 409 | 295 | 218 | 185 | 171 | 160.5 |
| ADS | 361 | 246 | 170 | 156 | 121 | 112 |
| ACS | 440 | 294 | 175 | 122 | 98 | 85 |

Table S3. Maximum Energy density and Power density observed for ACS, ADS, and AWS carbon samples.

| Name of Sample | Energy Density (Wh kg-1) | Power Density (kW kg-1) |
| --- | --- | --- |
| ACS | 12.5 | 2.2 |
| ADS | 14.5 | 1.6 |
| AWS | 5.97 | 2.3 |

References

[1] Tomar AK, Singh G, Sharma RK (2018) Fabrication of a Mo‐Doped Strontium Cobaltite Perovskite Hybrid Supercapacitor Cell with High Energy Density and Excellent Cycling Life. Chem Sus Chem 11:4123−4130.

[2] Joshi A, Sahu V, Singh G, Sharma RK (2019) Performance enhancement of a supercapacitor negative electrode based on loofah sponge derived oxygen rich carbon through encapsulation of MoO3 nanoflowers. Sustain Energy Fuels 2019:1248-1257.