List of Figures:

Fig. 1:  Energy dispersive X-ray (EDX) spectrum of the As30Te64Ga6 bulk alloy.

Fig. 2: X-ray diffraction patterns of the as-prepared As30Te64Ga6 glassy alloy and annealed samples at 450, 475, and 575 K for 1 h under vacuum.

Fig. 3: DSC thermo-grams for bulk the As30Te64Ga6 glass at the different heating rates (β).

Fig. 4: DSC trace for bulk As30Te64Ga6 glass at a heating rate β = 5 K min−1; (the first exothermic peak), the lined area AT shown between Ti and Tf of the peak, Ti, Tf, and T are according to the text.

Fig. 5: The typical sigmoid curve of the volume fraction crystallized (χ) as a function of temperature (T) for bulk As30Te64Ga6 glass alloy at the different heating rates (β).

Fig. 6: Crystallization rate (dχdt) versus temperature (T) of the exothermal peaks for bulk As30Te64Ga6 glass alloy at different heating rates (β).

Fig. 7: The test of the validity of relation’s Lasocka for bulk As30Te64Ga6 glass alloy at different heating rates (β).

Fig. 8: The plot of lnβTg2 versus 1000/ Tg and also the plot of lnβ versus 1000/ Tg for bulk As30Te64Ga6 glass alloy at different heating rates (β).

Fig. 9: The plot of the liquid fragility (F) versus 1000/ Tg and plot of the cooling rate (Qc) as a function of the glass transition temperature (Tg) for bulk As30Te64Ga6 glass alloy at different heating rates (β).

Fig. 10: The plot of lnβTp2 versus (1000Tp) for bulk As30Te64Ga6 glass alloy at different heating rates (β).

Fig. 11: The plot of lnβ versus (1000Tp) for bulk As30Te64Ga6 glass alloy at different heating rates (β).

Fig. 12: The plot of lnβTp versus (1000Tp) for bulk As30Te64Ga6 glass alloy at different heating rates (β).

Fig.13: The plot of (dχ/dt)p versus (1000/TP) for bulk As30Te64Ga6 glass alloy at different heating rates (β).

Fig. 14: The plot of ln(-ln(1-χ) versus (1000/T) at different heating rates (β) for bulk As30Te64Ga6 glass alloy for (a) first, and (b) second crystallization peak.

Fig. 15: The plot of (a) K(Tg), and (b) K(Tp) as a function of Tg and Tp for the As30Te64Ga6 sample.

Fig. 16: The plot of (a) Kr(Tg), and (b) Kr(Tp) as a function of Tg and Tp for the As30Te64Ga6 sample.