Supporting informations

Arsenic adsorption by functionalized polystyrene microplastics: kinetics and mechanisms

Xiringvl Mamtimin a，Wei Songb, Yun Wanga, Nuzahat Habibul a*

a College of Chemistry and Chemical Engineering, Xinjiang Normal University, Urumqi, 830054, China

b Technical Center for Hefei Customs, Hefei 230022, China

* Corresponding author

Nuzahat Habibuil,  E-mail address: nuzahat@mail.ustc.edu.cn

This Supporting Information contains 5-page document, including 4 figures, 1 table and this cover page.

Fig.S1 The Pseudo-first-order adsorption kinetics of As(III) and As(V) on different particle size of PS-COOH and PS-NH2

Fig. S2 The Freundlich adsorption isotherm models of As(III) and As(V) on the PS-COOH and PS-NH2

Fig.S3 XPS C1s and O1s spectra of the PS-COOH before and after the adsorption of As(V)

Fig.S4 XPS C1s, O1s and N1s spectra of the PS-NH2 before and after the adsorption of As(V)

Table S1 Zeta potential of PS-COOH and PS-NH2 MPs

| NPs | 82 nm PS-COOH | 200 nm PS-COOH | 500 nm PS-COOH | 80 nm PS-NH2 |
| --- | --- | --- | --- | --- |
| pH=7 | -24.2 | -32.5 | -38.4 | -8.87 |

表S1 82，200，500 nmPS-COOH，80 nm PS-NH2 zeta电位。