Pyrolysis characteristics, kinetics and biochar of fermented pine-sawdust-based waste

Yiteng Zhanga,b, Jun Hua,b, Xingxing Chenga,b,*, Mudassir Hussain Tahirc

aSchool of Energy and Power Engineering, Shandong University, Jinan, 250061, China

bNational Engineering Laboratory for Reducing Emissions from Coal Combustion, Jinan, 250061, China

cDepartment of Chemistry, Division of Science and Technology, University of Education, Lahore, 54000, Pakistan

Corresponding author: 17923 Jingshi Road, Jinan, 250061, China.

E-mail address: xcheng@sdu.edu.cn (X. Cheng).

| Samples | Time/min | Absorbance/mg/L |
| --- | --- | --- |
| PD-500 | 180 | 4.97 |
| PD-600 | 180 | 4.95 |
| PD-700 | 180 | 4.87 |
| PD-800 | 180 | 4.25 |
| FPD-500 | 180 | 4.48 |
| FPD-600 | 180 | 3.72 |
| FPD-700 | 180 | 3.65 |
| FPD-800 | 180 | 3.40 |

Table S1 The balanced concentration of MB solution

The morphological features of pine sawdust-derived biochar (PD-800) and biochar of fermented pine sawdust (FPD-800) were examined using SEM imaging (Fig.S1). The PD-800 presented a fat and rugged surface with no clear porous and massive collapse structure. In contrast to PD (Fig.S1), the roughness degree of surface of FPD-800 increased, and the apparent porous structure could be observed after fermentation and carbonization at 800 ℃. Microbial fermentation contributed to the cracking and melting of pine sawdust. Then, a feature that can have a positive impact on the adsorption efficiency were found with a complex robust structure and stereoscopic pore network.

(a)                                      (b)

Fig. S1 SEM patterns of (a) PD and (b) FPD.