Supplementary Information

Self-healing passive cooling utilizing endothermic reaction of NH4NO3/H2O driven by moisture sorption for photovoltaic cell

Seonggon Kim1,2, Jong Ha Park2, Jae Won Lee2, Yongchan Kim1,2, Yong Tae Kang1,2*

1School of Mechanical Engineering, Korea University, 145 Anam-ro, Seongbuk-gu, Seoul 02841, Republic of Korea

2Research Center for Plus Energy Building Innovative Technology, 145 Anam-ro, Seongbuk-gu, Seoul 02841, Republic of Korea

*Corresponding author

E-mail: ytkang@korea.ac.kr, Tel: +82-2-3290-5952, Fax: +82-2-922-3260

Table S1. Components analysis using energy dispersive X-ray spectrometer

|  | Element (wt%) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Materials | O | Na | Mg | Al | Si | Ca | K | Fe | P |
| Zeolite 13X | 40.7 | 15.1 | 1.5 | 17.9 | 24.3 | 0.5 | - | - | - |
| Zeolite 5A | 41.9 | 2.6 | 0.9 | 18.9 | 22.1 | 13.6 | - | - | - |
| Zeolite 3A | 38.8 | 9.3 | 2.6 | 17.1 | 25.1 | - | 6.3 | 0.8 | - |
| Zeolite Y | 49.5 | 0.8 | - | 14.2 | 35.5 | - | - | - | - |
| SAPO-34 | 39.0 | 19.0 | 0 | 20.8 | 20.0 | - | - | - | 1.2 |
| SSZ-13 | 51.42 | - | - | 7.27 | 41.31 | - | - | - | - |

Figure S1. Visualization analysis during heat dissipation process; a) Schematic of thermal imaging experiment; b) Latent cooling using zeolite 13X/H2O; c) Endothermic reaction cooling using NH4NO3/H2O

Figure S2. Experimental device for evaluation of heat dissipation performances

Figure S3. FE-SEM images for mesoporous materials; a) Zeolite 13X; b) Zeolite 5A; c) Zeolite 3A; d) Zeolite Y; e) SAPO-34; f) SSZ-13

Table S2. Theoretical solubility difference in the range of 20-70 oC and endothermic reaction heat

| Materials |  | Reaction heat (kJ/mol) | Solubility difference (g/g) |
| --- | --- | --- | --- |
| Solute | Solvent |  |  |
| NH4Cl | H2O | 14.76 | 0.92 |
| NH4NO3 | H2O | 28.05 | 3.96 |
| KCl | H2O | 17.21 | 0.47 |
| Na2CO3 | CH3COOH | 26.48 | 0.022 |
| CoSo4∙7H2O | SOCl2 | 90.82 | 0.87 |

Table S3. Materials cost of MS-ER cooling unit (A exchange rate was applied: 1 $ = 1,000 KRW)

| Materials | Manufacturer | Package | Price (KRW) | Price ($) | Price ($/g) |
| --- | --- | --- | --- | --- | --- |
| Ammonium nitrate | Daejung Chemicals | 25 kg | 57,500 | 57.5 | 0.0023 |
| Water | Daejung Chemicals | 20 kg | 16,300 | 16.3 | 0.000815 |
| Zeolite 13X | IVENG | 1 kg | - | 1.98 | 0.00198 |

Table S4. Cost analysis of PV cell in terms of cooling unit (The cost of monocrystalline silicone is calculated based on the PV cell of LG Electronics. The operating expense is considered for building integrated PV data.)

|  | Material cost |  | Maintenance ($/W) |
| --- | --- | --- | --- |
|  | Monocrystalline Si ($/W) | Cooling unit ($/W) |  |
| PV cell with natural air cooling | 0.767 | - | 0.25 |
| PV cell with MS-ER | 0.767 | 0.261 | 0.25 |