Steric Confinement Modulation and High-Tc Realization of Lead-Free Halide Hybrid Ferroelectrics via Halogen Substitution

Qin Chen, 1,2,3, Haidong Jiang4, Yipeng Fan,2,3, Zhou Li2,3, Huang Ye2,5, Yunpeng Yao2,5, Shuang Chen4,*, Chengmin Ji1,2,5,*, Shuhua Zhang1,2,3,*, and Junhua Luo1,2,3, 5,*

1 Fujian Science & Technology Innovation Laboratory for Optoelectronic Information of China, Fuzhou, Fujian, 350108, P. R. China
2 State Key Laboratory of Structural Chemistry, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences Fuzhou, Fujian, 350002, P. R. China.

Fuzhou, Fujian, 350108, P. R. China.

3 College of Chemistry and Bioengineering, Guilin University of Technology,

Guilin, Guangxi,541004, P. R. China

4 Kuang Yaming Honors School, Nanjing University, Nanjing, Jiangsu 210023, China

5 University of Chinese Academy of Sciences, Beijing 100049, China

Beijing 100049, P. R. China

Experimental Section

Synthesis and Crystal Growth

[H2mdap]BiI5: 4.66 g Bi2O3 (10 mmol) and 0.88 g H2mdap were added to 50 ml of concentrated aqueous HI solution. The dark red precipitate dissolved after heating and stirring at heating platform for 30 minutes. Bulk single crystals were obtained through the temperature lowing control process from its saturated solution at a speed of 0.5 K/day.

[H2mdap]BiBr5: 4.66 g Bi2O3 (10 mmol) and 0.88 g H2mdap were added to 50 ml of concentrated aqueous HBr solution. Clear solution was obtained by continuously heating and stirring at heating platform. Bulk single crystals were obtained through the temperature lowing control process from its saturated solution at a speed of 0.5 K/day.

[H2mdap]BiCl5: 4.66 g Bi2O3 (10 mmol) and 0.88 g H2mdap were added to 50 ml of concentrated aqueous HCl solution. The white precipitate dissolved after heating and stirring at heating platform. Bulk single crystals were obtained through the temperature lowing control process from its saturated solution at a speed of 0.5 K/day.

Variable temperature single crystal structure determination: Single-crystal X-ray diffraction was conducted via Bruker D8 Quesr/Venture diffractometer with Mo Kα radiation (λ = 0.77 Å). Crystal structures of H2mdapBiX5 (X = I, Br, Cl) were solved through direct method and was refined via the full-matrix least squares refinements on F2 using SHELXLTL software package. Crystal data and structure information are published in Tables S1−S4, Supporting Information.

Differential scanning calorimetry (DSC), thermogravimetric (TG), Second harmonic generation (SHG) measurement: Differential scanning calorimetry (DSC) measurement was conducted on a TA DSC Q20 DSC instrument with a heating and cooling rate of 10 K/min under nitrogen atmosphere. Thermogravimetric analysis (TGA) was performed on STA449C Thermal Analyser ranging from the room temperature to 1000 K. Variable-temperature second harmonic generation measurement was performed on polycrystals using a Nd:YAG laser (λ = 1064 nm, 5 ns pulse duration, ~1.6 MW peak power, 10 Hz repetition rate).

Ferroelectric measurements: The temperature-dependent P-E hysteresis loops were measured on a ferroelectric analyzer (Radiant Precision Premier II) through the double-wave method. For avoiding electric discharge at a high electric field, single crystals of three compounds were immersed in silicone oil to measure the P-E hysteresis loops. The temperature was carefully controlled by an oil bath. Two pairs of electrodes were formed orthogonally with each other on a single crystal with silver conductive adhesive.

In order to explain that the Curie temperature of ferroelectric compounds increases with the change of halogen in perovskite from chlorine to bromine and then to iodine, the first-principles calculations are employed to demonstrate the phase transition mechanism of each perovskite. All the first-principles calculations are performed in the Vienna Ab initio Simulation Package (VASP, Version 5.4.4) based on the PBE-D3 functional. The projector augmented wave (PAW) potentials are employed to describe the interactions between electrons and ions with an energy cutoff of 520 eV. The Gaussian smearing with the width of 0.05 eV is used for all calculations.

The ferroelectric/paraelectric phases of [H2mdap]BiX5 are derived from the experimentally single-crystal XRD structures. For their geometry optimization, the total energy change is set to be less than 10−6 eV, the magnitude of the largest force acting on the atoms is set to be less than 0.01 eV/Å, and the k-point mesh of 2×4×5 is used to achieve good convergence. In order to locate the phase transition pathway, the climbing-image nudged elastic band (CI-NEB) calculations are employed here for each perovskite. Then, the total energy is set to be less than 10−6 eV, the magnitude of the largest force acting on the atoms is set to be less than 0.03 eV/Å, and a k-point grid of 2×4×5 is used. Furthermore, the spontaneous polarization of each structure along the phase transition pathway can be calculated by using the Berry phase method. For high-accuracy single-point calculations to estimate spontaneous polarizations, a high energy convergence of 10−7 eV and a denser 4×8×10 k-point mesh is used.

In order to well demonstrate the energy/polarization change during the phase transition, we define an order parameter, λ, to express the phase transition from the initial structure (λ = 0) to the final structure (λ = 1). Then, the variation of energy/polarization with this order parameter for both studied perovskites are present in Figure X and Figure X respectively.

Figure S1. Experimental and calculated PXRD patterns for: (a) [H2mdap]BiI5, (b) [H2mdap]BiBr5, and (c) [H2mdap]BiCl5.

Figure S2. Thermogravimetric analysis for: (a) [H2mdap]BiI5, (b) [H2mdap]BiBr5 and (c) [H2mdap]BiCl5.

Figure S3. Crystal structures of [H2mdap]BiI5 at LTP and HTP

Figure S4. Crystal structures of [H2mdap]BiBr5 at LTP and HTP

Figure S5. Crystal structures of [H2mdap]BiCl5 at LTP and HTP

Figure S6. The space of cupped-caves for: (a) [H2mdap]BiI5, (b) [H2mdap]BiBr5 and (c) [H2mdap]BiCl5 (Center atom represents H2mdap).

Figure S7. The NH···halogen hydrogen bond of (a) [H2mdap]BiI5, (b) [H2mdap]BiBr5 and (c) [H2mdap]BiCl5.

Figure S8. Plot of 1/ε´ vs. temperature in the vicinity of Tc: (a) [H2mdap]BiI5 (b) [H2mdap]BiBr5 and (c) [H2mdap]BiBr5.

Figure S9. The second-order NLO signals for [H2mdap]BiBr5, [H2mdap]BiCl5. and the KDP standard collected at room temperature.

Figure S10. Spontaneous polarization values of [H2mdap]BiX5 compounds.

Table S1. Crystal Data and Structure Refinement for [H2mdap]BiX5 (X = I, Br, Cl) in LTP

| Empirical formula | C4H14BiI5N2 | C4H14BiBr5N2 | C4H14BiCl5N2 |
| --- | --- | --- | --- |
| Formula weight | 933.65 | 698.70 | 476.40 |
| Temperature/K | 150.0 | 293(2) | 299.03 |
| Space group | Pna21 | Pna21 | Pna21 |
| a/Å | 18.3142(6) | 18.4385(5) | 18.2117(8) |
| b/Å | 10.8946(3) | 10.1518(3) | 9.8564(4) |
| c/Å | 8.4520(3) | 7.7634(2) | 7.4475(3) |
| α/° | 90 | 90 | 90 |
| β/° | 90 | 90 | 90 |
| γ/° | 90 | 90 | 90 |
| Volume/ Å3 | 1686.39(9) | 1454.74(7) | 1336.84(10) |
| Z | 4 | 4 | 4 |
| ρcalcg/cm3 | 3.677 | 3.190 | 2.367 |
| μ/mm-1 | 19.579 | 25.817 | 14.148 |
| F(000) | 1600.0 | 1240.0 | 880.0 |
| Radiation | MoKα (λ = 0.71073) | MoKα (λ = 0.71073) | MoKα (λ = 0.71073) |
| 2θ range for data collection/° | 4.35 to 54.952 | 4.012 to 52.742 | 7.068 to 55.076 |
| Reflections collected | 11786 | 22410 | 31555 |
| Independent reflections | 3811 [Rint= 0.0508, Rsigma = 0.0538] | 2965 [Rint= 0.0907, Rsigma = 0.0601] | 2905 [Rint= 0.0948, Rsigma = 0.0448] |
| Data/restraints/parameters | 3811/42/111 | 2965/1/112 | 2905/1/112 |
| Goodness-of-fit on F2 | 1.083 | 1.059 | 1.209 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0687, wR2 = 0.1834 | R1 = 0.0360, wR2 = 0.0661 | R1 = 0.0735, wR2 = 0.1732 |
| Largest diff. peak/hole/e Å-3 | 3.98/-3.11 | 0.87/-1.16 | 2.23/-10.70 |

Table S2. Crystal Data and Structure Refinement for [H2mdap]BiX5 (X = I, Br, Cl) in HTP

| Empirical formula | C4H14BiI5N2 | C4H14BiBr5N2 | C4H14BiCl5N2 |
| --- | --- | --- | --- |
| Formula weight | 933.65 | 698.70 | 476.40 |
| Temperature/K | 298.0 | 342.92 | 430.0 |
| Space group | Pnma | Pnma | Pnma |
| a/Å | 18.236(2) | 17.959(3) | 17.6727(16) |
| b/Å | 8.5104(8) | 7.9205(13) | 7.6092(6) |
| c/Å | 11.0066(12) | 10.3822(18) | 10.0736(9) |
| α/° | 90 | 90 | 90 |
| β/° | 90 | 90 | 90 |
| γ/° | 90 | 90 | 90 |
| Volume/ Å3 | 1708.2(3) | 1476.8(4) | 1354.6(2) |
| Z | 4 | 4 | 4 |
| ρcalcg/cm3 | 3.630 | 3.142 | 2.336 |
| μ/mm-1 | 19.329 | 25.431 | 13.962 |
| F(000) | 1600.0 | 1240.0 | 880.0 |
| Radiation | MoKα (λ = 0.71073) | MoKα (λ = 0.71073) | MoKα (λ = 0.71073) |
| 2θ range for data collection/° | 5802 to 55.172 | 4.532 to 49.988 | 6.134 to 55.074 |
| Reflections collected | 22274 | 21499 | 21115 |
| Independent reflections | 2108 [Rint= 0.0817, Rsigma = 0.0372] | 1413 [Rint= 0.1319, Rsigma = 0.0502] | 1675 [Rint= 0.0595, Rsigma = 0.0245] |
| Data/restraints/parameters | 2108/58/90 | 1413/36/78 | 1675/54/75 |
| Goodness-of-fit on F2 | 1.106 | 1.063 | 1.205 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0510, wR2 = 0.1514 | R1 = 0.0482, wR2 = 0.1216 | R1 = 0.0525, wR2 = 0.1204 |
| Largest diff. peak/hole/e Å-3 | 2.59/-1.81 | 1.34/-1.84 | 0.69/-3.07 |

Table S3. Bond lengths for [H2mdap]BiX5 (X = I, Br, Cl) in LTP

| Bond | (Å) | Bond | (Å) |
| --- | --- | --- | --- |
| Bi(01) - I(002) | 3.083(2) | Bi(01) - I(004) | 2.941(2) |
| Bi(01) - I(003) | 3.184(2) | Bi(01) - I(005) | 2.961(3) |
| Bi(01) - I(003)1 Bi(1) - Br(3) Bi(1) - Br(5) Bi(1) - Br(4) Bi(1) - Cl(4) Bi(1) - Cl(1) Bi(1) - Cl(5)1 | 3.219(2) 2.7298(16) 2.7537(16) 2.8573(15) 2.675(4) 2.699(5) 2.917(4) | Bi(01) - I(006) Bi(1) - Br(1) Bi(1) - Br(1)1 Bi(1) - Br(2) Bi(1) - Cl(5) Bi(1) - Cl(2) Bi(1) - Cl(10)A | 3.047(2) 2.9672(16) 3.0205(17) 2.8301(16) 2.808(5) 2.575(5) 2.609(5) |

Table S4. Bond lengths for [[H2mdap]BiX5 (X = I, Br, Cl) in HTP

| Bond | (Å) | Bond | (Å) |
| --- | --- | --- | --- |
| Bi(01) - I(002) | 3.0762(7) | Bi(01) - I(004) | 3.0434(8) |
| Bi(01) - I(003)1 | 2.9503(5) | Bi(01) - I(005) | 3.1493(3) |
| Bi(01) - I(003) Bi(1) - Br(4) Bi(1) - Br(1)1 Bi(1) - Br(1) Bi(01) - Cl(02) Bi(01) - Cl(02)1 Bi(01) - Cl(03) | 2.9503(5) 2.828(2) 2.7488(12) 2.7488(12) 2.592(2) 2.592(2) 2.649(4) | Bi(01) - I(005)2 Bi(1) - Br(2) Bi(1) - Br(3) Bi(1) - Br(3)2 Bi(01) - Cl(04) Bi(01) - Cl(05) Bi(01) - Cl(05)2 | 3.1493(3) 2.865(2) 2.9759(5) 2.9758(5) 2.702(4) 2.8268(3) 2.8268(3) |

Table S5. Computational analyses of [[H2mdap]BiX5 (X = I, Br, Cl)

|  | Tc (K) | Volume (Å3) | Bi-Br (Å) | Bi-Bi (Å) | Hydrogen bond (Å) | Volume Vf (Å3) |
| --- | --- | --- | --- | --- | --- | --- |
| H2mdapBiCl5 | 377 | 1323.9 | 2.74 | 5.52 | 2.17 | 817.4 |
| H2mdapBiBr5 | 318 | 1468.7 | 2.93 | 6.06 | 2.35 | 877.1 |
| H2mdapBiI5 | 264 | 1744.7 | 3.11 | 6.39 | 2.58 | 991.8 |