Fabrication of graphene and graphene derivatives based thermoplastic nanocomposite films for high barrier antibacterial packaging, EMI shielding and thermal management applications

Suman Kumar Ghosh1, Krishnendu Nath1, Soumya Sarathi Ganguly2, Tushar Kanti Das3, Sangit Paul1, Trisita Ghosh1, Amit Kumar Das2, Narayan Ch. Das1*

1 Rubber Technology Centre, Indian Institute of Technology, Kharagpur, 721302, India

2Department of Biotechnology, Indian Institute of Technology, Kharagpur, 721302, India

3Institute of Physics – Center for Science and Education, Silesian University of Technology, Krasińskiego 8, 40-019 Katowice, Poland

*Corresponding Author: Narayan Ch. Das

Email address: ncdas@rtc.iitkgp.ac.in

Section 1. Thermal stability and Zeta potential of graphene nanomaterials

Fig. S1 TGA plots of graphene nanostructured materials

Table S1. Zeta potential of graphene oxide (GO) and its derivatives

| Graphene nanomaterial | Zeta potential value (mV) |
| --- | --- |
| GO | -31.5 |
| G-Ag | -37.4 |
| RGO | -42.2 |
| GNP | -47.9 |

Section 2. Micromechanical assessment of thermoplastic nanocomposites by nanoindentation

In the nanoindentation tests, the Berkovich indentor monitors and records load vs. displacement of the indentor. Nanoindentation experiment composed of four steps. At first, the indentor comes near to the sample surface and thereafter loading up to the maximum load. Here, the maximum load applied was 8000 µN. Before unloading, the load was held for 10 s to avoid the influence of creep on the unloading feature. From the hysteresis curves, hardness (H) was calculated using Eq. S1, the projected indentation area for the Berkovich indenter was given by Eq. S2.

Hardness, H=PmaxA                                                                                                                                            (S1)

Projected indentation area,  A=24.5 hP2                 	                                                                                       (S2)

Where Pmax, A and hP are the maximum indentation load, indentation area, and contact indentation depth respectively [1].

The plasticity index (ψ) which indicates the relative elastic or plastic behavior under external stresses has been measured using Eq. S3 for all blend nanocomposites. Here, Ap and Ae are the areas under the loading and unloading curve of the hysteresis loop.

Plasticity index, ψ=Ap-AeAe                                                                                                                                 (S3)

Section 3. Nanocomposite film surface analysis by AFM

The surface texture and film roughness of a pure LLDPE and graphene-containing nanocomposite were examined using the AFM methodology. Roughness values derived from micro-graphs are also displayed in the corresponding figures, whereas Fig. S2 shows the AFM micrographs of pure LLDPE and graphene reinforced nanocomposite films. The roughness value of the nanocomposite film is always less than that of the neat LLDPE film [2]. Uniform dispersion of GNP in LLDPE matrix leads in a more reduced roughness value of the corresponding nanocomposite film compared to that for LRGO and LG-Ag nanocomposites.

Fig. S2 Surface topographical images of (a) pure LLDPE, (b) LGNP3, (c) LG-Ag3 and (d) LRGO nanocomposite films

Section 4. Mathematical expressions related to EMI shielding effectiveness of LLDPE/graphene nanocomposites

The total shielding effectiveness (SET) of the electrically conductive composite material can be expressed by the following mathematical expression:

SET (dB)=10log10PTPI=10log10ETEI=10log10HTHI                                                                           (S4)

Where PT (ET or HT) and PI (EI or HI) depict the transmitted power and incident power respectively of electric or magnetic field intensity [3]. The attenuation of incoming EM radiation occurs through three mechanisms namely absorption, reflection and multiple reflection which are denoted by SEA, SER and SEMR respectively.  Therefore total shielding effectiveness (SET) can be expressed as:

SET=SEA+SER+SEMR                                                                                                                                  (S5)

When SET > -15 dB or the skin depth (δ) of the material is less than the sample thickness, the parameter of multiple reflection (SEMR) can be neglected [4]. So, SET can be represented as the mathematical sum of SEA and SER parameters by the following equation:

SET=SEA+SER                                                                                                                                                (S6)

The scattering parameters obtained from the VNA vector analyzer in the X-band frequency region (8.2-12.4 GHz) are generally utilized to evaluate total shielding efficiency and reflection, transmission and absorption coefficients. The following equations are employed to calculate the reflection coefficient (R), absorption coefficient (A) and transmission coefficient (T) of electromagnetic radiation.

T=ETEI2=S122=S212                                                                                                                                (S7)

R=EREI2=S112=S222                                                                                                                                (S8)

A=1-R-T                                                                                                                                                    (S9)

Here, scattering parameters S12, S21 and S11 represent the reverse transmission coefficient, forward transmission coefficient and forward reflection coefficient, respectively. The total EMI attenuation can be calculated from Eq. S10.

SET dB=10log⁡1S122=10log⁡1S212                                                                                                            (S10)

SER (reflection) and SEA (absorption) parameters can be evaluated by employing the following equations:

SER dB=10log1011-S112                                                                                                                            (S11)

SEA dB=10log101-S112S112                                                                                                                            (S12)

References

1. 	Katti P, Kundan K V., Kumar S, Bose S (2017) Improved mechanical properties through engineering the interface by poly (ether ether ketone) grafted graphene oxide in epoxy based nanocomposites. Polymer (Guildf) 122:184–193. https://doi.org/10.1016/j.polymer.2017.06.059

2. 	Ghosh SK, Das TK, Ganguly S, et al (2022) Silane functionalization of sodium montmorillonite and halloysite (HNT) nanoclays by ‘grafting to’ method to improve physico-mechanical and barrier properties of LLDPE/clay nanocomposites. Polym Bull. https://doi.org/10.1007/s00289-022-04281-4

3. 	Ghosh SK, Das TK, Ghosh S, et al (2021) Selective distribution of conductive carbonaceous inclusion in thermoplastic elastomer: A wet chemical approach of promoting dual percolation and inhibiting radiation pollution in X-band. Compos Sci Technol 210:. https://doi.org/10.1016/j.compscitech.2021.108800

4. 	Bhawal P, Ganguly S, Das TK, et al (2018) Mechanically robust conductive carbon clusters confined ethylene methyl acrylate–based flexible composites for superior shielding effectiveness. Polym Adv Technol 29:95–110. https://doi.org/10.1002/pat.4092