Supporting Information

Self-healing, Solvent-free Anti-corrosion Coating based on Skin-like polyurethane/carbon nanotubes Composite with Real-time Damage Monitoring

Hui Kong a b, Xiaomin Luo a b*, Peng Zhang a b*, Jianyan Feng a b, Pengni Li c,d, Wenjie Hu a b, Xuechuan Wang a b, Xinhua Liu a b

a College of Bioresources Chemical and Materials Engineering, Shaanxi University of Science & Technology, WeiYang District, Xi’an 710021, Shaanxi, China

b National Demonstration Center for Experimental Light Chemistry Engineering Education, Shaanxi University of Science&Technology, WeiYang District, Xi’an 710021, Shaanxi, China

c Tongxiang Affairs Center of Quality and Technical Supervision, Tongxiang 314599, Zhejiang, China

d National Wool Knitwear Quality Supervision  Inspection Center（Zhe Jiang）, Tongxiang 314599, Zhejiang, China

*Corresponding authors: Xiaomin Luo and Peng Zhang

E-mails: luoxiaomin@sust.edu.cn; peter_zhang@sust.edu.cn

Figure S1 Tafel polarization curves of self-repaired coated SFPUHE-HTF-CNTs-3 steel sheets immersed in 3.5 wt% NaCl solution

As depicted in Fig. S1，compared with the original SFPUHE-HTF-CNTs-3, the damaged and self-repaired SFPUHE-HTF-CNTs-3 exhibited an increased corrosion current density of 9.12 × 10-9 A·cm-2 and a decreased corrosion potential of -0.49 V. Corrosion current density only increased by 2.01% and corrosion potential only decreased by 28.95%. Compared with the bare steel sheet (Icorr = 1.47 × 10-6 A·cm-2, Ecorr = -0.68 V), it still has a lower corrosion current density and a relatively positive corrosion potential, indicating that the self-repaired SFPUHE-HTF-CNTs coating still has good corrosion protection performance.

Table S1 Corrosion current density and corrosion potential of SFPUHE-HTF-CNTs

| Samples | Ecorr (V vs. SCE) | Icorr (A·cm-2) |
| --- | --- | --- |
| Uncoated | -0.68 | 1.47×10-6 |
| SFPU-HTF-CNTs-0 | -0.54 | 5.24×10-7 |
| SFPU-HTF-CNTs-1 | -0.50 | 5.50×10-7 |
| SFPU-HTF-CNTs-2 | -0.50 | 5.41×10-7 |
| SFPU-HTF-CNTs-3 | -0.38 | 8.94×10-9 |
| SFPU-HTF-CNTs-4 | -0.48 | 9.78×10-8 |

From Table S1, the Icorr and Ecorr of the uncoated bare steel sheet are 1.47 × 10-6 A·cm-2 and -0.68 V, respectively. When coated with PU/CNTs composites, Icorr showed a trend of decreasing then increasing and Ecorr presents the opposite. SFPUHE-HTF-CNTs-3 has the highest corrosion resistance, with corrosion current density up to 8.94×10-9 A·cm-2 and corrosion potential up to -0.38 V.

Table S2 Conductivity of SFPUHE-HTF-CNTs before and after self-healing

| Samples | Conductivity (S·m-1) |  |
| --- | --- | --- |
|  | original | healed |
| SFPUHE-HTF-CNTs-0 | － | － |
| SFPUHE-HTF-CNTs-1 | 1.46 | 1.34 |
| SFPUHE-HTF-CNTs-2 | 43.51 | 11.20 |
| SFPUHE-HTF-CNTs-3 | 180.74 | 112.92 |
| SFPUHE-HTF-CNTs-4 | 270.27 | 106.38 |

The conductivity of SFPUHE-HTF-CNTs coating before and after self-healing is shown in Table S2. The conductivity of the coatings gradually increases with the increase of CNTs spraying amount, and has the highest conductivity up to 270.27 S·m-1 when the spraying amount is 4%. It is worth noting that the composite coating still has a high electrical conductivity after damage and self-healing. Taking the composite coating with 3% spraying content as an example, the conductivity after self-healing can still reach 112.92 S·m-1, which will be beneficial for the further application of the composite coating in damage detection.