Highly stable visible-light photocatalytic properties of black rutile TiO2 hydrogenated in ultrafast flow

Junzheng Gaoa, Jing Zhangb, Wanxia Huanga*, Shuping Zhengc, and Qiwu Shia*

aCollege of Materials Science and Engineering, Sichuan University, Chengdu 610065, China

bCollege of Architecture & Environment, Sichuan University, Chengdu 610065, China

cAnalytic and Testing Centre, Sichuan University, Chengdu 610065, China

E-mail: huangwanxia@scu.edu.cn, shiqiwu@scu.edu.cn

50mL K2Cr2O7 aqueous solution (20mg/L, was adjusted by dilute H2SO4 to pH=2) with 20mg black TiO2 were used for a photocatalytic experiment, and other parameters were the same as the RhB experiment. Our black TiO2 could degrade 45.2% Cr6+ within 2h under visible light, which further demonstrated its improved visible-light photocatalytic activity.

Fig. S1 Cr6+ residual in visible-light photocatalytic reactions of 800℃-H-TiO2

Normally, hydrogenation should have brought much more surface hydroxyls, but fast hydrogen flowing in our experiments gave limited help to increase the contents of surface hydroxyls. The peaks of surface hydroxyl exhibited were almost all caused by absorbing water in the air rather than hydrogenating, which explained why black TiO2 and white TiO2 had similar low amounts of surface hydroxyls. This result further indicated that black TiO2 prepared by annealing in ultrafast hydrogen flow could have good visible-light photocatalytic performance without dependence on surface defects.

Fig. S2 XPS spectra (O1s) of white TiO2 and 800℃-H-TiO2

TiO2 surface would experience a reconstruction process induced by titanium suboxides during reduction processes, and (110) planes were preferentially affected in the formation of suboxides as shown in Fig. S3. The sharply reduced diffraction intensity of (110) in 850℃-H-TiO2 and 900℃-H-TiO2 reflected decreased proportions of these crystal planes, while many other crystal planes such as (101) (36.1°) were not affected. Different crystal planes exhibited various activity to be photoexcited, while (111) and (110) planes were so important for rutile TiO2. Given the small percentage of (111) planes in our samples, (110) planes played a dominant role in these photocatalysis processes. Therefore, the weakening in (110) planes brought great negative effects to forming photogenerated electrons and holes.

Tab. S1 Diffraction intensity of different crystal plane in TiO2

Fig. S3 The magnified figures of the peaks around 27.38°, 36.04°, 41.20°, and 54.26°

The conclusion as above was further revealed by two experiments whose results were exhibited in Fig. S4. The intensity of PL spectra in Fig. S4a was inversely proportional to the recombination of carriers, so 850℃-H-TiO2 and 900℃-H-TiO2 had weaker recombination of electron-hole pairs than that of 800℃-H-TiO2, due to the higher content of VO which could increase carries density. The commonly used theory that the photocatalytic activity of black TiO2 was damaged by easy recombination of carriers did not tally with our experiments. Final results were obtained by combining PL spectra with photocurrent experiments shown in Fig. S4b. Partial electron-hole pairs would recombine during the diffusion process to the surface of TiO2 nanoparticles after photoexcitation, and the remnant carrier concentration reflected in photocurrent intensity. The photocurrent of 800℃-H-TiO2 was 3.2 µA, while 850℃-H-TiO2 and 900℃-H-TiO2 had extremely weak photocurrent intensity. Although the recombination in these samples was slow, the final carrier concentration showed low levels, indicating reduced generation of electrons and holes, so 850℃-H-TiO2 and 900℃-H-TiO2 had significantly decreased photocatalytic activities.

Fig. S4 a PL spectra of X℃-H-TiO2 (X=800, 850, and 900), b Photocurrent intensity of X℃-H-TiO2 (X=800, 850, and 900)