Table 2. Demographic data and main results of studies.

| Study | Country of study | Study design | Objective | Application | Biomaterial | Type of propolis | Propolis origin | Characterization of propolis | Drug release | Toxicity | Controls | Simple size | Main findings |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bruschi et al., 2007 | Brazil | in vitro study | Development and characterization of semisolid systems containing propolis prepared from carbomer 934P and poloxamer 407 (P407) | Periodontal pocket for the treatment of periodontitis | Semisolid Systems | Ethanolic extract | Propolis was collected from an experimental apiary in the farm of the State University of Maringa (Parana State, Brazil) | Not available | 80% in 168h | Not available | Formulations without propolis microparticles | n=5 | The release profile studies showed that propolis could be released from the systems for an extended period (more than 7 days). The properties of the candidate formulations indicate a potential advantageous role in the treatment of periodontal diseases. |
| Fabri et al., 2011 | Brazil | in vitro study | Development and characterization of semisolid systems containing propolis or sildenafil prepared from Carbopol 934P and poloxamer 407 | Endodontics in pulp protection | Binary polymeric systems containing poloxamer 407 (P407) and Carbopol 934P (C934P) were designed to deliver propolis extract (PE) | Ethanolic extract | Propolis was collected from an experimental apiary in the farm of the State University of Maringa (Parana State, Brazil). | Rheological analysis by ViscoStar− Plus R controlled shear rate rotating viscometer | 50% in 500min | Not available | Sildenafil citrate was purchased from Pfizer (Dongcheng District, Beijing, China) | n=3 for all tests, except bioadhesive strength (n=5) | The data obtained in these formulations indicated a potentially useful role in pulp protection, however, clinical evaluation is necessary. |
| Ferreira et al., 2013 | Brazil | in vitro study | The antimicrobial activity of microparticles was evaluated against some microorganisms of periodontal importance. | Periodontal pockets | Ethylcellulose microparticles | Ethanolic extract | Three samples of propolis from Apis mellifera L. beehives were collected at apiaries in the Northeast of Paraná state, Brazil. | Determination of total flavonoid content and, determination of total phenol content by Folin-Ciocalteu method | 20% in 32h | Not available | Metronidazole | n=3 for all tests, except the determination of total flavonoid content and total phenol content (n=6) | The strains of Enterococcus faecalis, Streptococcus pyogenes, and Streptococcus mutans were more susceptible to the propolis and E. faecalis to the metronidazole. |
| Franca et al., 2014 | Brazil | in vitro study | Antimicrobial activity of sustained-release propolis-based chitosan varnish useful on dental cariogenic biofilm prevention | Anti-cariogenic agent | Propolis - based chitosan varnish | Ethanolic extract | Green propolis was collected from commercial beekeeping named Pharmanéctar® in Minas Gerais State, Brazil. | Provided by fabricant *PharmaNectar, Brazil, 2007, not described the techniques was used | 20% in 24h | Not available | Chlorhexidine 0.12%, chitosan-based varnish and nystatin | n=5 | Sustained-release chitosan-based propolis varnishes (5%, 10%, and 15%) inhibited all tested microorganisms, deserving clinical studies to confirm it is in vivo activity. |
| Asawahame et al., 2014 | Thailand | in vitro study | Antibacterial activity against Streptococcus mutans and the inhibition of adhesion on a smooth glass surface during the biofilm formation was tested. | Mouth-dissolving dosage form and as an anti-cariogenic agent | Propolis-PVP electrospun fibers | Ethanolic extract 5% (w/v) | Propolis was obtained from Chiangmai Healthy Product Co., Ltd. (Chiangmai, Thailand). | Not available | Not available | Not available | Chlorhexidine mouthwash solution (0.12%) 1 mg/mL | n=8 (SEM); n=3 (antimicrobial assays) | The results indicated the potential of electrospun fibers to be used as mouth-dissolving fibers for effective antibacterial activity in the oral cavity. |
| Borges et al., 2015 | Brazil | in vitro study | Production and characterization of orally disintegrating films from gelatin and hydrolyzed collagen containing the ethanol extract of propolis. | Control oral infection | Films of gelatin and hydrolyzed collagen | Ethanolic extract | 12-type resin (Star Rigel Raf- ˜ fard, Sao Paulo, Brazil) | Folin–Ciocalteau method, Fourier transform infrared spectroscopy (FTIR) and, scanning electron microscopy | 80% in 15min | Not available | Films without the ethanol extract of propolis | n=10 for all tests, except SEM (n=16); in vitro release and antimicrobial assay (n=3) | The ethanol extract of propolis produced the antimicrobial activity in the film as well as provided a better resistance matrix and increased mucoadhesiveness. |
| Al-Bayaty et al., 2017 | Malaysia | in vitro study | Formulated periodontal chips from Malaysian propolis in chitosan base and to evaluate the physical, biological and antibacterial properties. | Treatment of chronic periodontitis | Biodegradable periodontal chips | Ethanolic extract | Raw propolis purchased from Ayer Keroh, Malacca, Malaysia | Not available | 80% in 6 days | Not available | Chlorhexidine (0.2%, w/v) and ethanol (20%, w/v) | n=15 for all tests, except surface morphology and thickness (n=35) | Malaysian propolis can be evaluated into a chip and be used in treating patients with periodontal disease. It was found to be biodegradable have a high release rate, and have antimicrobial activity against gram-positive and gram-negative bacteria. |
| Balata et al., 2018 | Egypt | in vitro study and animal model | The formulation of commercial Saudi propolis into biodegradable chitosan chips and evaluation of its effectiveness as a pulpotomy agent. | Treatment of vital pulpotomy | Saudi Propolis into biodegradable chitosan chips | Ethanolic extract | Propolis (El Akbr)® was obtained from a honey bee market located in Jeddah, Saudi Arabia (El Maher shop, Wadi El Nahil Co., Taeif, Saudi Arabia). | Determination of total phenolic content, determination of total flavonoid content, determination of the antioxidant activity of the extract, quantification of polyphenolic constituents | 35% in 7 days | Histopathological evaluation | Formocresol | n=6 (in vitro); n=18 (animal model) | Formulation of propolis extract as chitosan biodegradable chips can be used effectively for local sustained propolis delivery into the infected periodontal pockets, as it results in the production of higher quality secondary dentin with the less inflammatory response of the pulp. |
| de Toledo et al., 2018 | Brazil | in vitro study | Development of a novel liquid crystalline system containing MNPs and propolis | Periodontal pockets | A liquid crystalline system containing iron oxide magnetic nanoparticles (MNPs) | Ethanolic extract | Propolis was acquired from the Iguatemi Experimental Farm of the State University of Maringa, Parana state, Brazil. | Folin-Ciocalteu method | 36% in 120h | Cytotoxicity by micro-crustacean Artemia salina and fibroblasts cell line. | A system without propolis | n=6 | The system containing propolis and magnetic nanoparticles displays important in vitro fungicide activity, which was increased when an alternating external magnetic field was applied, indicating a potential alternative therapy for the treatment of periodontal disease. |
| Simu et al., 2018 | Romania | in vitro study | Designed a composite biomaterial based on a high viscosity soft propolis extract (70% propolis) and shell clam, with antiseptic and osteoinductive qualifies for hard tissue regeneration. | Mineralized tissue engineering that can be used in dentistry | Bioactive cement with antiseptic and osteoinductive qualities | Aqueous extract 70% | Commercial 70% soft propolis extract, Bioremed, Romania. | Scanning electronic microscopy (SEM), reversed-phase liquid chromatography (HPLC) with diode array detection, proliferation assay, and differentiation assay | Not available | Cell viability and adhesion level with human dental papilla cell line and differentiation assay by Alizarin Red staining. | The cells cultured in normal culture condition (DMEM-F12 (Sigma-Aldrich) supplemented with 10% FCS (Hyclone), 1% Antibiotic-antimycotic (Sigma-Aldrich) | n=3 | The shell-propolis-based biomaterial promoted and sustained human stem cells attachment, proliferation, and differentiation, presenting an important osteoinductive effect essential for the mineralized tissue reparation process. |
| Ahi et al., 2019 | Turkey | in vitro study | Produce barrier membranes from biodegradable polymers, namely, PLLA and PCL, with an antibacterial feature promoted by propolis. | Guided tissue regeneration in periodontology | Biodegradable polymer films | Ethyl alcoholic extract | Not informed | Not available | Not available | Not available | Antibiotic disk including 30 μgr chloramphenicol (C30) (HIMEDIA) | n=5 | Propolis has a positive influence on the thermal, mechanical, and degradation properties of the blend films to achieve the required values for GTR. Also, films with propolis showed antibacterial activity against Gram (+) bacteria. |
| Bonadies et al., 2019 | Italy | in vitro study | The optimization of the electrospinning process to fabricate zein electrospun nanofibres (ZN) loaded with propolis (PZN). | Tissue inflammation in the presence of oral lesions | Electrospun fibers | Hydroalcoholic solution | Informed only the location Erbaflor, Italy | Not available | 70% in 24h | Not available | Pure propolis | n=20 | The zein nanofibers can guarantee a sustained release of propolis directly to the target, providing a more efficient solution for treatments based on the administration of 'one shot' of the active ingredient, minimizing side effects. |
| Son et al., 2021 | Korea | in vitro study | The potential of propolis-embedded zeolite nanocomposites for dental implant application. | Dental implants | Propolis-embedded zeolite nanocomposites | Aqueous extract | Propolis extracts were purchased from Rapha Propolis Co., (Jeonju, Korea). | Fourier transform-infrared spectra (FT-IR) | 90% in 30 days | MTT cell cytotoxicity assay | PLA/PCL pellets containing propolis‐embedded zeolite nanocomposites | Not informed | Eluted propolis solution from PLA/PCL pellets showed significant antibacterial efficacy against C. albicans, S. mutans, and S. sobrinus. |