Appendix A. Supplementary Information

| Samples | Ia | Ib | crystallinity index (%) |
| --- | --- | --- | --- |
| MCC | 70 | 90 | 0.78 |
| CNCs | 120 | 139 | 0.86 |

Table S1.  Calculated values crystallinity index percentage of (MCC) and (CNCs)

Table S2.  Calculated values of crystallinity (I002) percentage of (MCC) and (CNCs)

| Samples | Icr | Iam | Crystallinity (I222) (%) |
| --- | --- | --- | --- |
| MCC | 93.80 | 23.54 | 74.90 |
| CNCs | 76.66 | 12.39 | 83.84 |