Table S1 Main survey data of NSP kilns and shaft kilns

| Item |  | NSP kilns |  |  |  | Shaft kilns |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Mean | Min | Max | Standard Deviation | Mean | Min | Max | Standard Deviation |
| Plants |  | 177 |  |  |  | 61 |  |  |  |
| Production lines |  | 185 |  |  |  | 69 |  |  |  |
| Clinker production/Mt |  | 194.68 |  |  |  | 10.29 |  |  |  |
| Fuel intensity/kgce/t |  | 110.04 | 96.23 | 132.00 | 10.69 | 121.09 | 84.33 | 152.90 | 14.89 |
| Power intensity/kWh/t |  | 62.46 | 45.07 | 87.64 | 11.65 | 59.18 | 34.55 | 166.00 | 23.10 |
| Chemical composition of raw meal/% | LOSS | 35.51 | 32.91 | 36.77 | 0.87 | 39.03 | 34.60 | 41.15 | 1.26 |
|  | SiO2 | 13.24 | 11.93 | 14.24 | 0.56 | 12.66 | 11.41 | 14.48 | 0.59 |
|  | Al2O3 | 2.93 | 2.26 | 3.44 | 0.27 | 3.55 | 2.22 | 4.61 | 0.44 |
|  | Fe2O3 | 2.12 | 1.67 | 2.95 | 0.26 | 2.44 | 1.78 | 3.72 | 0.34 |
|  | CaO | 43.39 | 41.48 | 45.45 | 0.91 | 40.67 | 37.98 | 44.02 | 1.13 |
|  | MgO | 1.42 | 0.43 | 2.79 | 0.59 | 1.48 | 0.33 | 2.62 | 0.53 |
| Raw meal intensity/kg/t |  | 1504.47 | 1447.25 | 1536.20 | 20.87 | 1572.49 | 1483.18 | 1648.26 | 31.96 |
| Chemical composition of clinker/% | SiO2 | 21.79 | 20.74 | 22.51 | 0.42 | 20.20 | 18.47 | 22.70 | 0.69 |
|  | Al2O3 | 5.14 | 4.46 | 5.93 | 0.34 | 5.71 | 3.79 | 7.62 | 0.70 |
|  | Fe2O3 | 3.42 | 2.91 | 4.53 | 0.28 | 3.90 | 2.76 | 5.50 | 0.49 |
|  | CaO | 65.26 | 63.26 | 66.71 | 0.75 | 64.44 | 61.21 | 66.83 | 1.06 |
|  | MgO | 2.20 | 0.77 | 4.31 | 0.91 | 2.30 | 0.55 | 4.27 | 0.89 |
| Waste heat power generation/kWh/t |  | 23.39 | 0.00 | 39.02 | 13.86 | - | - | - | - |
| Raw material substitution/% |  | 2.88 | 0.00 | 11.85 | 3.48 | 2.43 | 0.00 | 19.50 | 4.34 |

Table S2 Comparison of emissions from different scale production processes

| Item | NSP kilns |  |  |  |  |  | Shaft kilns |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Scale | Average | ＜2000 | 2000~ 2500 | 3000~ 4000 | 4000~ 5000 | ＞5000 | Average | ≤300 | 500~900 | 1000 | ＞1000 |
| Sample number | 177 | 28 | 57 | 27 | 51 | 14 | 61 | 26 | 19 | 9 | 7 |
| Production lines | 185 | 33 | 59 | 27 | 52 | 14 | 69 | 31 | 19 | 11 | 8 |
| Clinker production/Mt | 194.68 | 8.41 | 46.03 | 29.22 | 78.31 | 32.71 | 10.29 | 3.41 | 2.08 | 2.34 | 2.45 |
| Fuel intensity/kgce/t | 110.04 | 119.96 | 115.03 | 110.36 | 108.10 | 104.79 | 121.09 | 129.65 | 120.52 | 116.96 | 113.59 |
| Power intensity/kWh/t | 62.46 | 74.30 | 68.12 | 61.53 | 59.99 | 58.20 | 59.18 | 72.26 | 66.27 | 48.31 | 45.33 |
| Waste heat power generation/kWh/t | 23.39 | 5.67 | 20.08 | 24.11 | 26.57 | 24.32 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| Raw material substitution/% | 2.88 | 2.95 | 3.81 | 2.70 | 2.54 | 2.54 | 2.43 | 2.77 | 4.41 | 2.53 | 0.16 |
| CaO in clinker/% | 65.26 | 65.55 | 65.35 | 65.33 | 65.08 | 65.42 | 64.44 | 64.40 | 64.05 | 64.86 | 64.43 |
| MgO in clinker/% | 2.20 | 1.94 | 2.10 | 2.09 | 2.40 | 2.00 | 2.30 | 2.25 | 2.43 | 2.13 | 2.40 |
| Process-related emissions/kg/t | 529.33 | 528.24 | 524.02 | 528.07 | 532.95 | 529.54 | 521.00 | 515.63 | 514.09 | 523.79 | 531.67 |
| Fuel-related emissions/kg/t | 291.74 | 316.70 | 303.69 | 299.62 | 285.39 | 276.65 | 319.67 | 342.28 | 318.17 | 308.76 | 299.89 |
| Power-related emissions/kg/t | 37.52 | 69.40 | 45.58 | 36.52 | 32.36 | 31.23 | 57.56 | 70.74 | 64.35 | 46.69 | 43.84 |
| Emission reduction from waste heat power generation/kg/t | 22.40 | 5.73 | 19.05 | 23.53 | 25.73 | 22.42 |  |  |  |  |  |
| Emission reduction from raw material substitution/kg/t | 7.58 | 8.16 | 12.59 | 8.25 | 4.81 | 6.43 | 10.59 | 15.16 | 15.91 | 9.26 | 0.97 |
| Clinker emission factor/kg/t | 858.59 | 914.34 | 873.29 | 864.21 | 850.71 | 837.42 | 898.24 | 928.65 | 896.60 | 879.25 | 875.40 |

# Table S3 Application rate of various energy savings and low carbon technologies in China's cement industry in 2030

| Stage | ID | Measures | Hebei | Shan xi | Inner Mongolia | Liao ning | Jiang su | Zhe jiang | Anhui | Fu jian | Jiang xi | Shan dong | Henan | Hubei | Hunan | Guang dong | Guang xi | Chong qing | Si chuan | Gui zhou | Yun nan | Tibet | Shaan xi | Xin jiang |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Raw meal preparation | R1 | Efficient transport system | 69.35 | 59.79 | 88.31 | 64.89 | 98.87 | 99.34 | 77.47 | 98.54 | 90.43 | 76.84 | 79.09 | 78.34 | 87.64 | 90.22 | 90.08 | 69.54 | 77.05 | 77.05 | 69.54 | 18.29 | 69.84 | 71.59 |
|  | R2 | Use of gravity system instead of pneumatic system | 72.28 | 63.37 | 77.11 | 63.37 | 85.94 | 96.63 | 77.83 | 97.86 | 82.57 | 74.11 | 58.30 | 73.00 | 77.05 | 74.55 | 69.98 | 52.75 | 66.61 | 75.01 | 59.97 | 18.29 | 64.14 | 51.60 |
|  | R3 | Raw meal process control | 70.89 | 71.59 | 78.52 | 72.28 | 97.03 | 94.69 | 80.60 | 99.40 | 95.32 | 83.27 | 72.28 | 83.27 | 85.74 | 76.84 | 74.06 | 57.17 | 65.79 | 65.79 | 62.48 | 26.26 | 58.45 | 46.14 |
|  | R4 | Use of roller mills | 82.21 | 74.91 | 89.97 | 55.81 | 94.25 | 91.72 | 83.56 | 76.84 | 78.95 | 59.79 | 53.64 | 62.38 | 82.07 | 68.18 | 72.47 | 64.14 | 87.77 | 78.34 | 79.59 | 26.26 | 73.36 | 85.46 |
|  | R5 | High-efficiency classifiers/separators | 83.41 | 52.26 | 76.43 | 64.52 | 94.69 | 95.50 | 79.81 | 81.26 | 72.47 | 69.04 | 73.66 | 82.65 | 82.65 | 87.44 | 84.62 | 83.15 | 68.18 | 68.18 | 70.62 | 14.52 | 68.23 | 61.83 |
|  | R6 | Variable frequency drive in raw mill vent fan | 86.91 | 70.81 | 73.57 | 82.07 | 96.07 | 99.63 | 99.63 | 96.35 | 93.22 | 81.29 | 81.29 | 81.29 | 97.48 | 99.23 | 99.23 | 77.78 | 90.91 | 90.91 | 90.91 | 37.36 | 48.43 | 37.36 |
|  | R7 | High-efficiency fan for raw mill vent fan with inverter | 71.85 | 69.88 | 84.65 | 88.36 | 97.52 | 98.87 | 98.87 | 94.16 | 94.16 | 83.37 | 94.45 | 83.37 | 98.39 | 98.39 | 98.39 | 67.48 | 86.37 | 86.37 | 86.37 | 50.72 | 64.81 | 50.72 |
|  | R8 | Efficient vertical roller mill for coal grinding | 61.65 | 57.48 | 87.35 | 59.79 | 72.44 | 85.90 | 78.80 | 99.78 | 93.62 | 74.85 | 89.55 | 77.78 | 84.17 | 68.18 | 91.21 | 49.35 | 58.45 | 69.04 | 60.81 | 26.26 | 82.76 | 82.96 |
|  | R9 | Variable frequency drive in coal mill vent fan | 76.35 | 67.88 | 94.85 | 68.37 | 65.79 | 98.31 | 98.31 | 90.43 | 90.43 | 90.43 | 98.54 | 90.43 | 90.43 | 90.43 | 90.43 | 68.37 | 68.37 | 68.37 | 68.37 | 22.50 | 68.37 | 22.50 |
|  | R10 | High-efficient grit separator in coal mill | 80.86 | 62.17 | 92.48 | 72.98 | 98.68 | 92.48 | 92.48 | 92.68 | 92.68 | 92.68 | 98.54 | 92.68 | 92.68 | 92.68 | 92.68 | 75.06 | 75.06 | 75.06 | 75.06 | 14.52 | 68.76 | 14.52 |
|  | R11 | Efficient optimization of grinding energy saving technology | 72.28 | 76.39 | 94.19 | 49.18 | 87.80 | 97.46 | 79.36 | 76.45 | 76.45 | 76.45 | 83.27 | 91.21 | 94.11 | 93.03 | 89.13 | 76.43 | 81.29 | 81.29 | 66.40 | 26.26 | 67.98 | 88.37 |
|  | R12 | Other | 87.80 | 72.28 | 99.87 | 84.25 | 95.57 | 99.99 | 85.94 | 87.77 | 87.77 | 87.77 | 96.15 | 85.36 | 94.25 | 88.19 | 94.78 | 94.78 | 94.78 | 94.78 | 94.78 | 46.14 | 82.36 | 88.17 |
| Clinker making | A1 | calcareous material substitution | 11.13 | 6.31 | 3.25 | 7.81 | 6.21 | 4.69 | 2.47 | 1.69 | 3.15 | 4.79 | 4.03 | 7.71 | 3.15 | 3.25 | 3.15 | 2.37 | 6.21 | 5.46 | 6.21 | 1.59 | 2.37 | 1.59 |
|  | A2 | Siliceous materials substitution | 9.68 | 10.93 | 7.81 | 6.41 | 9.48 | 7.91 | 7.81 | 4.79 | 6.21 | 10.73 | 7.81 | 7.71 | 6.96 | 9.28 | 7.71 | 6.21 | 7.71 | 6.21 | 4.69 | 3.15 | 7.81 | 6.21 |
|  | A3 | Fuel substitution | 18.89 | 14.85 | 13.47 | 17.57 | 28.79 | 29.95 | 14.85 | 17.57 | 18.89 | 23.99 | 21.58 | 17.57 | 18.89 | 28.89 | 23.99 | 18.89 | 20.19 | 14.85 | 18.89 | 4.69 | 17.57 | 9.18 |
|  | C1 | Energy management and process control systems | 77.47 | 81.21 | 90.69 | 97.75 | 86.73 | 86.73 | 92.66 | 79.81 | 96.35 | 65.79 | 77.47 | 74.87 | 95.71 | 93.19 | 94.61 | 84.17 | 51.08 | 65.79 | 52.10 | 33.52 | 54.83 | 33.52 |
|  | C2 | Kiln combustion system improvements | 82.26 | 65.56 | 70.64 | 96.96 | 88.83 | 88.83 | 88.83 | 65.79 | 87.50 | 74.99 | 83.04 | 78.80 | 99.11 | 97.95 | 98.63 | 71.43 | 47.31 | 59.79 | 49.20 | 26.26 | 64.97 | 34.46 |
|  | C3 | Kiln shell heat loss reduction | 80.69 | 72.47 | 82.52 | 93.07 | 83.80 | 83.80 | 83.80 | 75.82 | 98.71 | 77.24 | 88.22 | 95.11 | 97.39 | 92.51 | 94.19 | 76.09 | 54.83 | 54.83 | 54.83 | 34.46 | 68.76 | 41.04 |
|  | C4 | Low temperature waste heat recovery for power generation | 98.83 | 92.51 | 91.41 | 99.99 | 99.84 | 99.99 | 93.43 | 99.59 | 94.19 | 98.61 | 99.74 | 97.75 | 100.00 | 99.43 | 99.98 | 94.46 | 92.39 | 95.83 | 84.76 | 68.37 | 90.63 | 63.31 |
|  | C5 | Low pressure drop cyclones for NSP kilns | 94.09 | 54.22 | 94.09 | 94.09 | 89.82 | 89.82 | 89.82 | 93.32 | 93.32 | 93.32 | 97.67 | 93.32 | 96.04 | 96.04 | 96.87 | 83.56 | 61.52 | 80.58 | 69.88 | 34.46 | 56.29 | 34.46 |
|  | C6 | Upgrading of a preheater to a preheater/precalciner kiln | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
|  | C7 | Conversion of long dry kilns to NSP kilns | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
|  | C8 | Adjustable speed drive for kiln fan | 98.83 | 83.80 | 99.87 | 99.95 | 84.06 | 85.02 | 99.11 | 99.63 | 99.99 | 73.26 | 99.98 | 99.01 | 92.79 | 81.29 | 99.46 | 98.62 | 95.57 | 89.85 | 56.57 | 93.25 | 64.81 | 56.56 |
|  | C9 | Upgrading the preheater from 5 stages to 6 stages | 26.15 | 26.15 | 72.28 | 72.28 | 72.11 | 72.11 | 72.11 | 78.95 | 83.84 | 82.02 | 69.04 | 84.89 | 87.40 | 87.40 | 74.29 | 53.64 | 42.56 | 55.41 | 37.79 | 27.22 | 53.64 | 18.29 |
|  | C10 | Conversion to reciprocating grate cooler | 74.15 | 79.11 | 86.85 | 87.28 | 84.92 | 84.92 | 79.89 | 71.62 | 99.15 | 59.35 | 88.83 | 81.29 | 94.16 | 89.48 | 97.76 | 50.52 | 44.46 | 44.46 | 37.89 | 29.15 | 44.46 | 37.28 |
|  | C11 | Optimize heat recovery/Upgrade clinker cooler for clinker making in rotary kilns | 87.51 | 87.51 | 87.51 | 96.78 | 96.96 | 93.62 | 93.62 | 74.99 | 99.68 | 90.73 | 97.17 | 86.78 | 99.78 | 99.09 | 99.39 | 74.11 | 56.29 | 66.40 | 56.29 | 47.90 | 53.01 | 47.90 |
|  | C12 | Modification of clinker cooler | 73.00 | 73.00 | 69.15 | 91.34 | 93.69 | 91.34 | 94.61 | 73.00 | 98.65 | 90.11 | 93.22 | 89.24 | 92.73 | 88.01 | 90.63 | 68.76 | 55.41 | 65.61 | 57.17 | 52.45 | 51.19 | 57.37 |
|  | C13 | Efficient kiln drives | 88.35 | 88.35 | 99.70 | 99.70 | 92.66 | 92.66 | 92.66 | 95.10 | 92.66 | 92.66 | 99.96 | 92.66 | 92.66 | 92.66 | 95.71 | 98.31 | 79.20 | 70.31 | 66.40 | 52.45 | 63.31 | 53.29 |
|  | C14 | Variable frequency drive in cooler fan of grate cooler | 73.26 | 73.26 | 93.45 | 99.11 | 99.11 | 99.11 | 99.11 | 99.11 | 99.11 | 99.11 | 92.73 | 99.11 | 99.11 | 99.11 | 95.56 | 84.06 | 84.06 | 84.06 | 68.76 | 47.02 | 60.81 | 47.02 |
|  | C15 | Replacing vertical shaft kilns with NSP kilns | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
|  | C16 | Replacement of preheater fan with high-efficiency fan | 92.23 | 97.22 | 95.35 | 98.31 | 96.23 | 96.23 | 96.23 | 87.08 | 98.82 | 98.82 | 92.23 | 98.82 | 98.82 | 98.82 | 98.34 | 98.34 | 98.34 | 92.23 | 73.66 | 19.28 | 50.27 | 19.28 |
|  | C17 | Seal replacement in rotary kilns | 59.35 | 59.35 | 59.35 | 99.10 | 98.43 | 96.39 | 96.39 | 78.34 | 96.39 | 89.48 | 89.48 | 94.66 | 96.24 | 92.51 | 89.60 | 74.85 | 52.10 | 67.98 | 53.01 | 41.95 | 63.31 | 47.90 |
|  | C18 | Low nitrogen decomposing furnace system | 18.29 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 26.26 | 9.56 | 26.26 | 18.29 | 18.29 | 9.56 | 14.03 | 9.56 | 9.56 | 2.96 | 9.56 | 1.98 |
|  | C19 | Two stage supporting short kiln | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 9.56 | 18.29 | 9.56 | 18.29 | 14.03 | 14.03 | 14.03 | 9.56 | 11.37 | 9.56 | 4.89 | 11.37 | 2.96 |
|  | C20 | Other | 97.52 | 75.59 | 99.46 | 99.67 | 88.19 | 88.19 | 88.19 | 99.88 | 99.80 | 91.13 | 99.38 | 94.64 | 98.75 | 88.85 | 99.98 | 98.99 | 85.66 | 75.01 | 71.53 | 58.18 | 67.61 | 58.18 |