Table 1 Optimization of conditions in the model reaction of benzoin (3), 4-chlorobenzaldehyde (4a), ammonium acetate (5) under different conditions in the presence of the Fe3O4/SiO2-TMA-Me (1).

| Entry | Catalyst | Catalyst Loading (mg) | Condition | Time (min) | Yield (%)a |
| --- | --- | --- | --- | --- | --- |
| 1 | - | -- | Solvent-free/ 100 ˚C | 300 | 34 |
| 2 | - | -- | H2O/ r.t. | 300 | Trace |
| 3 | - | -- | EtOH / r.t. | 300 | Trace |
| 4 | - | -- | EtOH / reflux | 300 | 40 |
| 5 | Fe3O4/SiO2-TMA-Mel (1) | 20 | EtOH / r.t. | 120 | 60 |
| 6 | Fe3O4/SiO2-TMA-Mel (1) | 20 | EtOH / 60˚C | 120 | 72 |
| 7 | Fe3O4/SiO2-TMA-Mel (1) | 20 | EtOH / reflux | 30 | 96 |
| 8 | Fe3O4/SiO2-TMA-Mel (1) | 15 | EtOH / reflux | 30 | 95 |
| 9 | Fe3O4/SiO2-TMA-Mel (1) | 10 | EtOH / reflux | 35 | 95 |
| 10 | Fe3O4/SiO2-TMA-Mel (1) | 5 | EtOH / reflux | 45 | 92 |
| 11 | Fe3O4/SiO2-TMA-Mel (1) | 2 | EtOH / reflux | 60 | 87 |
| 12 | Melamine | 10 | EtOH / reflux | 35 | 75 |
| 13 | Trimesic acid | 10 | EtOH / reflux | 35 | 79 |
| 14 | Fe3O4/SiO2 | 10 | EtOH / reflux | 35 | 73 |
| aReaction conditions: benzoin (3, 1 mmol), 4-chlorobenzaldehyde (4a, 1 mmol) and NH4OAc (5, 2.5 mmol), Fe3O4/SiO2-TMA-Me (1) and solvent (2 ml). |  |  |  |  |  |

Table 2 Scope of the three-component synthesis of imidazole derivatives catalyzed by Fe3O4/SiO2-TMA-Me (1)a

| Entry | Aldehyde (4) | Product (6) | Time (min) “Benzoin” | Time (min) “Benzil” | Yield (%) “Benzoin” | Yield (%) “Benzil” | Observed Melting Point (˚C) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 4-Chlorobenzaldehyde (4a) | 2-(4-chlorophenyl)-4,5-diphenyl-1H-imidazole (6a) | 35 | 30 | 95 | 98 | 258-25928 |
| 2 | Benzaldehyde (4b) | 2,4,5-triphenyl-1H-imidazole (6b) | 65 | 63 | 82 | 86 | 270-27229 |
| 3 | 2-Chlorobenzaldehyde (4c) | 2-(2-chlorophenyl)-4,5-diphenyl-1H-imidazole (6c) | 45 | 35 | 89 | 93 | 197-19930 |
| 4 | 4-Methylbenzaldehyde (4d) | 4,5-diphenyl-2-(p-tolyl)-1H-imidazole (6d) | 75 | 73 | 80 | 84 | 188-19031 |
| 5 | 4-Methoxybenzaldehyde (4e) | 2-(4-Methoxyphenyl)-4,5-diphenyl-1H-imidazole (6e) | 65 | 55 | 89 | 92 | 228-22932 |
| 6 | 2,4-Dichlorobenzaldehyde (4f) | 2-(2,4-dichlorophenyl)-4,5-diphenyl-1H-imidazole (6f) | 55 | 45 | 80 | 84 | 17833 |
| 7 | 4-Nitrobenzaldehyde (4g) | 2-(4-nitrophenyl)-4,5-diphenyl-1H-imidazole (6g) | 45 | 38 | 88 | 92 | 236-23834 |
| 8 | 4-(Dimethylamino)benzaldehyde (4h) | 4-(4,5-diphenyl-1H-imidazol-2-yl)-N,N-dimethylaniline (6h) | 100 | 90 | 70 | 83 | 228-22935 |
| 9 | 2-Thiophenecarboxaldehyde (4i) | 4,5-diphenyl-2-(thiophen-2-yl)-1H-imidazole (6i) | 90 | 83 | 70 | 79 | 263-26532 |
| 10 | Furan-2-carbaldehyde (4j) | 2-(furan-2-yl)-4,5-diphenyl-1H-imidazole (6j) | 85 | 80 | 80 | 85 | 200-20232 |
| a Reaction conditions: benzil or benzoin (2 or 3, 1 mmol), aldehyde derivatives (4a–j, 1 mmol) and ammonium acetate (5, 2.5 mmol) in the presence of 10 mg Fe3O4/SiO2-TMA-Me (1) in EtOH under reflux conditions |  |  |  |  |  |  |  |