Supplementary information for

Prediction of phosphoric acid plus hydrogen peroxide (PHP) pretreatment efficiency using artificial neural network modeling

Qing Wang a, b, c, Jinguang Hu c, Li Zhao b, Mei Huang b, Dong Tian b, Yongmei Zeng b, Shihuai Deng b, Fei Shen b*, and Xinquan Zhang a*

a College of Grassland Science and Technology, Sichuan Agricultural University, Chengdu, Sichuan 611130, P. R. China.

b Institute of Ecological and Environmental Sciences, Sichuan Agricultural University, Chengdu, Sichuan 611130, P. R. China.

c Department of Chemical and Petroleum Engineering, Schulich School of Engineering, the University of Calgary, Calgary T2N 4H9, Canada.

To whom correspondence should be addressed:

*Fei Shen         Email: fishen@sicau.edu.cn

*Xinquan Zhang    Email: zhangxq@sicau.edu.cn

Content:

Table S1 Experimental setups of PHP pretreatment and the obtained results for ANN modeling

Table S2 Experimental setups of PHP pretreatment and the obtained results for ANN testing

Table S3 Optimized key parameters of the ANN models

Fig. S1 Architecture of an artificial neuron

Table S1 Experimental setups of PHP pretreatment and the obtained results for ANN modeling

| NO. | Pretreatment conditions |  |  |  | Cellulose content (C-C, %) | Cellulose recovery (C-Ry, %) | Hemicellulose content (H-C, %) | Hemicellulose removal (H-Rl, %) | Lignin content (L-C, %) | Lignin removal (L-Rl, %) | Solid recovery (S-Ry, %) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Time (t, h) | Temperature (T, °C) | H3PO4 (Cp, %) | H2O2 (Ch, %) |  |  |  |  |  |  |  |
| 1 | 2 | 30 | 65 | 7.06 | 34.86 | 67.60 | 19.66 | 30.46 | 20.53 | 42.96 | 68.06 |
| 2 | 2 | 30 | 70 | 5.29 | 42.23 | 75.90 | 20.31 | 33.40 | 17.93 | 53.83 | 63.08 |
| 3 | 2 | 30 | 80 | 1.76 | 45.63 | 100.00 | 18.33 | 16.17 | 19.91 | 28.50 | 88.00 |
| 4 | 2 | 30 | 85 | 0.00 | 66.40 | 100.00 | 0.00 | 100.00 | 26.32 | 8.61 | 85.06 |
| 5 | 3 | 30 | 65 | 7.06 | 54.25 | 96.32 | 0.00 | 100.00 | 14.80 | 62.36 | 62.31 |
| 6 | 3 | 30 | 70 | 5.29 | 44.15 | 66.93 | 0.00 | 100.00 | 12.97 | 71.84 | 53.21 |
| 7 | 3 | 30 | 80 | 1.76 | 56.43 | 80.39 | 14.23 | 63.02 | 17.01 | 65.29 | 49.99 |
| 8 | 3 | 30 | 85 | 0.00 | 70.70 | 100.00 | 0.00 | 100.00 | 28.01 | 21.88 | 68.32 |
| 9 | 4 | 30 | 65 | 7.06 | 43.99 | 79.68 | 10.08 | 66.69 | 12.23 | 68.27 | 63.58 |
| 10 | 4 | 30 | 70 | 5.29 | 51.05 | 80.42 | 17.63 | 49.33 | 9.98 | 77.48 | 55.28 |
| 11 | 4 | 30 | 80 | 1.76 | 71.83 | 100.00 | 0.00 | 100.00 | 14.91 | 68.51 | 51.72 |
| 12 | 4 | 30 | 85 | 0.00 | 67.92 | 100.00 | 0.00 | 100.00 | 26.35 | 22.48 | 72.07 |
| 13 | 2 | 40 | 65 | 7.06 | 54.15 | 75.91 | 0.00 | 100.00 | 14.86 | 70.17 | 49.20 |
| 14 | 2 | 40 | 70 | 5.29 | 70.27 | 87.49 | 0.00 | 100.00 | 12.08 | 78.46 | 43.69 |
| 15 | 2 | 40 | 80 | 1.76 | 84.19 | 100.00 | 0.00 | 100.00 | 17.99 | 66.38 | 45.78 |
| 16 | 2 | 40 | 85 | 0.00 | 63.14 | 100.00 | 0.00 | 100.00 | 25.92 | 14.17 | 81.13 |
| 17 | 3 | 40 | 65 | 7.06 | 52.52 | 65.58 | 0.00 | 100.00 | 11.12 | 80.12 | 43.82 |
| 18 | 3 | 40 | 70 | 5.29 | 76.54 | 87.26 | 0.00 | 100.00 | 10.86 | 82.26 | 40.01 |
| 19 | 3 | 40 | 80 | 1.76 | 100.00 | 100.00 | 0.00 | 100.00 | 17.21 | 71.55 | 40.52 |
| 20 | 3 | 40 | 85 | 0.00 | 71.31 | 100.00 | 0.00 | 100.00 | 31.78 | 24.40 | 58.29 |
| 21 | 4 | 40 | 65 | 7.06 | 54.35 | 61.75 | 0.00 | 100.00 | 12.50 | 79.66 | 39.87 |
| 22 | 4 | 40 | 70 | 5.29 | 75.93 | 87.28 | 0.00 | 100.00 | 10.46 | 82.78 | 40.34 |
| 23 | 4 | 40 | 80 | 1.76 | 80.30 | 95.53 | 0.00 | 100.00 | 16.21 | 72.38 | 41.75 |
| 24 | 4 | 40 | 85 | 0.00 | 71.50 | 100.00 | 0.00 | 100.00 | 23.58 | 16.60 | 86.67 |
| 25 | 2 | 50 | 65 | 7.06 | 47.14 | 52.23 | 0.00 | 100.00 | 11.87 | 81.16 | 38.89 |
| 26 | 2 | 50 | 70 | 5.29 | 80.68 | 85.67 | 0.00 | 100.00 | 13.78 | 79.04 | 37.26 |
| 27 | 2 | 50 | 80 | 1.76 | 78.83 | 100.00 | 0.00 | 100.00 | 22.56 | 57.54 | 46.10 |
| 28 | 2 | 50 | 85 | 0.00 | 64.98 | 79.62 | 0.00 | 100.00 | 28.84 | 49.39 | 43.00 |
| 29 | 3 | 50 | 65 | 7.06 | 54.50 | 57.67 | 0.00 | 100.00 | 12.09 | 81.67 | 37.14 |
| 30 | 3 | 50 | 70 | 5.29 | 81.14 | 84.22 | 0.00 | 100.00 | 12.33 | 81.66 | 36.43 |
| 31 | 3 | 50 | 80 | 1.76 | 72.39 | 78.62 | 0.00 | 100.00 | 26.34 | 59.02 | 38.11 |
| 32 | 3 | 50 | 85 | 0.00 | 79.40 | 100.00 | 0.00 | 100.00 | 33.28 | 32.17 | 49.94 |
| 33 | 4 | 50 | 65 | 7.06 | 51.05 | 55.36 | 0.00 | 100.00 | 11.44 | 82.23 | 38.06 |
| 34 | 4 | 50 | 70 | 5.29 | 84.71 | 86.33 | 0.00 | 100.00 | 12.70 | 81.46 | 35.77 |
| 35 | 4 | 50 | 80 | 1.76 | 79.03 | 83.40 | 0.00 | 100.00 | 25.57 | 61.35 | 37.03 |
| 36 | 4 | 50 | 85 | 0.00 | 58.27 | 79.94 | 0.00 | 100.00 | 19.44 | 61.80 | 48.14 |

Note: Some of the cellulose recoveries are calculated higher than 100%, and they are regarded as 100% in the table.

Table S2 Experimental setups of PHP pretreatment and the obtained results for ANN testing

| NO. | Pretreatment parameters |  |  |  | Cellulose content (C-C, %) | Cellulose recovery (C-Ry, %) | Hemicellulose content (H-C, %) | Hemicellulose removal (H-Rl, %) | Lignin content (L-C, %) | Lignin removal (L-Rl, %) | Solid recovery (S-Ry, %) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Time (t, h) | Temperature (T, °C) | H3PO4 (Cp, %) | H2O2 (Ch, %) |  |  |  |  |  |  |  |
| 1 | 2 | 45 | 65 | 7.06 | 34.86 | 67.60 | 19.66 | 30.46 | 20.53 | 42.96 | 68.06 |
| 2 | 2 | 45 | 70 | 5.29 | 42.23 | 75.90 | 20.31 | 33.40 | 17.93 | 53.83 | 63.08 |
| 3 | 2 | 45 | 80 | 1.76 | 45.63 | 100.00 | 18.33 | 16.17 | 19.91 | 28.50 | 88.00 |
| 4 | 2 | 45 | 85 | 0.00 | 58.27 | 79.94 | 0.00 | 100.00 | 19.44 | 61.80 | 48.14 |

Note: Some of the cellulose recoveries are calculated higher than 100%, and they are regarded as 100% in the table.

Table S3 Optimized key parameters of the ANN models

| Output variables | Parameters for ANN modeling |  |  |  |
| --- | --- | --- | --- | --- |
|  | Hidden layers | Activation functions | Iterations | Neurons |
| C-C | 1 | Tanh | 900 | 9 |
| C-Ry | 1 | Tanh | 900 | 10 |
| H-Rl | 1 | Tanh | 900 | 10 |
| L-Rl | 1 | Tanh | 900 | 12 |

Fig. S1 Architecture of an artificial neuron (Kartal et al., 2021).

References

Kartal, F., Özveren, U., 2021. An improved machine learning approach to estimate hemicellulose, cellulose, and lignin in biomass. Carbohydr. Polym. Technol. Appl. 2, 100148. https://doi.org/10.1016/j.carpta.2021.100148.