Strong nanostructured films and effective Pb (II) removal capacity based on nitro oxidized cellulose nanofibrils prepared from banana rachis

Edward Rwegasila1, Ngesa Ezekiel Mushi 1, 2*, Lars A Berglund2

1University of Dar es Salaam, College of Engineering and Technology, Department of Mechanical

and Industrial Engineering, P.O.BOX 35131, Dar es Salaam, Tanzania

2Wallenberg Wood Science Center, KTH Royal Institute of Technology, School of Engineering

Sciences in Chemistry, Biotechnology and Health, SE-100 44 Stockholm, Sweden

* Corresponding author e-mail: ngesaaone@gmail.com

Supporting Information

Figure S1: Conductivity data used for determination of the degree of oxidation of NOCNF by NaOH conductometric titrations.

Figure S2: Regular light transmittance curve of the 0.1 wt. % NOCNF hydrocolloidal suspension.

Figure S3: FTIR spectra of NOCNF before and after purification of Pb (II) (NOCNF-Pb(II)).

Table S1: The parameters for pseudo-order kinetic model

| Model | Parameter |  |  |
| --- | --- | --- | --- |
|  | Qe, mg g-1 | K, g mg-1 min-1 | R2 |
| Pseudo-second order | 769 | 0.0169 | 0.9999 |

Freundlich model

Freundlich model is given in Eq. (S1) based on the assumption of multilayer adsorption on the active sites of the adsorbent.

log Qe=log Kf+ 1nlog Ce                                                                                                            (S1)

Where Kf and n are Freundlich constants calculated from the slope and intercept of log Qe versus log Ce plot. Kf is an indicative of the relative capacity and n is a measure of the nature and strength of the adsorption process and the distribution of the active sites1-3.

Figure S4: Freundlich equilibrium adsorption isotherm plot for experimental data.

Table S2: Parameters of adsorption isotherms

|  | Langmuir model |  | Freundlich model |  |
| --- | --- | --- | --- | --- |
| Equation | y=0.0006x+0.8731 |  | y=0.9581x +0.0021 |  |
| R2 | 0.9869 |  | 0.9984 |  |
| Parameters | KL (Lmg-1) | Qm (mg/g) | n | Kf (mg1-1/n L1/n g-1) |
| Value | 0.00068 | 1667 | 1.044 | 1.005 |

Table S3: Density and porosity data of the NOCNF films

| # of films | Mass (g) | Thickness (cm) | Diameter (cm) | Volume (cm3) | Density (g/cm3) | Porosity (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.272 | 0.006 | 7 | 0.2309 | 1.1787 | 21.42 |
| 2 | 0.272 | 0.006 | 7 | 0.2309 | 1.1795 | 21.37 |
| 3 | 0.275 | 0.006 | 7 | 0.2309 | 1.1940 | 20.4 |
| 4 | 0.246 | 0.006 | 6.8 | 0.2179 | 1.1933 | 20.45 |
| 5 | 0.271 | 0.006 | 7 | 0.2309 | 1.1771 | 21.53 |

Note: Data was determined using five specimen

References

1.	Gadd, G. M., Biosorption: critical review of scientific rationale, environmental importance and significance for pollution treatment. J. Chem. Technol. Biotechnol 2009, 84, (1), 13-28.

2.	Hubbe, M. A.; Hasan, S. H.; Ducoste, J. J., Cellulosic substrates for removal of pollutants from aqueous systems: A review. 1. Metals. BioResources 2011, 6, (2), 2161-2287.

3.	Freundlich, H., Über die adsorption in lösungen. Z Phys Chem 1907, 57, (1), 385-470.