Extended Data Fig. 1 | Probe-wavelength-resolved resonant-IVS data of APDC-DTPA and TTM-3PCz: a (APDC-DTPA), c (TTM-3PCz), Differential transmission map following excitation with a 10-fs pulse centred at 575 nm, at room temperature. b (APDC-DTPA), d (TTM-3PCz), Wavelength-resolved impulsive Raman map of following impulsive photo-excitation into lowest excited CT state

Extended Data Fig. 2 | Probe-wavelength-resolved resonant-IVS studies on non-fullerene acceptor (NFA) molecules in chloroform solution: The chemical structures of the NFA molecules studied and the corresponding absorption spectra in chloroform are shown in the top panel (dashed box). Wavelength-resolved impulsive Raman map of a ITIC, b IO-4Cl, c o-IDTBR, d Y5, e Y6, f Y7. Transient absorption spectra at 1-2 picosecond are plotted in the right inset of every panel.

Extended Data Fig. 3 | Analysis of the exciton-vibration coupling constant of TTM-3PCz and assignment of strongly coupled mode to the excited state: a, Excited-state Raman map of TTM-3PCz in CHCl3, b Calculated Hung-Rhys factor associated with the lowest energy transition (D0 → D1) of TTM-3PCz, c vector displacement diagram of the normal modes with calculated frequency 156, 202, 204 cm-1 which correspond to experimentally obtained 150, 232 cm-1 mode.

The description of this figure is discussed in further detail in Supplementary Information (Section 9).

Extended Data Fig. 4 | Probe-wavelength-resolved IVS studies on a, TTM-3NCz (CHCl3) and b, 4CzIPN (toluene): (I) Chemical structure, (II) probe wavelength-resolved impulsive Raman map, (III) excited-state Raman spectra shown for representative probe wavelength (625-635 nm for TTM-3NCz and 870-880 nm for 4CzIPN). Black asterisk (*) corresponds to the solvent modes.

Extended Data Fig. 5 | Electronic and Vibrational dynamics of internal conversion from D2 to D1 state of TTM-TPA: a) transient absorption signal in the form of differential transmission (ΔT/T) upon photo-excitation with P1 and P2 pump pulse at different time delays (the purple shaded area: P2 excitation; and magenta line: P1 excitation). b) electronic population dynamics of the D2 exciton for a representative wavelength (790-800 nm) which turns out to be 670±125 fs. (The method is described in SI section 8). c, d, the spectra obtained from the vibrational coherence at early time (150-1500 fs) and later time (650-2000 fs) in band selective excitation experiment with c) P2 excitation and d) P1 excitation at representative probe wavelength (710-750 nm). It is important to note that a very close resemblance of the later time spectra of P2 excitation and early time spectra of the P1 excitation is consistent with this barrierless and coherent internal conversion process from D2 to D1 state which was predicted from excitation wavelength dependent photoluminescence measurement41.

Extended Data Fig. 6 | Band selective Impulsive vibrational spectroscopy of TTM-TPA: a Temporal profile of the pulse P1 and P2 used in band selective experiment to excite charge transfer and local exciton-rich excited state respectively. b, Vibrational coherence generated after photo-excitation with P1 and P2 pulse for a representative probe window (680-700 nm). c, d, Wavelength-resolved impulsive Raman map (time-resolution corrected) of TTM-TPA following impulsive photo-excitation by c) the P2 pulse to the D2 rich state and d) the P1 pulse to the D1 state; The diagonal strips in the d, arise due to the interference scattering with the P1 pump.

The fact that, the dominance of the high-frequency oscillations (time-period = 20-30 fs) is highly pronounced in the D2 state even after photo-excited with the slower pump pulse, strongly support the data and calculation presented in the Fig. 3.

Extended Data Fig. 7 | Perturbational effect on the exciton wavefunction (transition density) of the D2 and D1 state along the coordinate of all experimentally obtained high-frequency vibrational modes (full mode resolved picture of the data represented in Fig. 3g-h): on the top left panel, experimentally obtained D1 and D2 state rich Raman spectra are reproduced. In the table, ωk(cm-1) corresponds to the frequency of the kth vibrational mode. Inside parenthesis, the theoretically obtained frequencies are provided. q(k) corresponds to the vector displacement diagram of the kth mode. {Δρ(D2)}k and {Δρ(D1)}k are the differential exciton wavefunction (transition density) upon displacement along the kth mode for D2 and D1 exciton respectively.

Extended Data Fig. 8 | Mode-resolved reorganization energy (λv) and contribution of the high-frequency modes to the vibrational reorganization energy: a, Mode-resolved picture of reorganisation energy for D2 state of TTM-TPA obtained from TDDFT calculation displacing the ground state optimised geometry along the coordinate of each normal modes. b, Mode-resolved picture of reorganisation energy for D1 state of TTM-TPA. c, φlfhf calculated for lowest excited state of Pentacene (S1, non-CT exciton), TTM radical (D1, non-CT exciton), TTM-3PCz (D1, CT exciton), APDC-DTPA (S1, CT exciton), TTM-TPA (D1, CT exciton)

The reduced vibrational coupling to the high frequency regime in TTM-TPA and TTM-3PCz with respect to the TTM presented in c, is in agreement with previous non-adiabatic coupling calculations41. Kimura et al48 have shown strong high-frequency vibrational coupling in the PyBTM and bisPyTM which are similar LE exciton like TTM.

Extended Data Table 1 | Experimentally obtained non-radiative rates of the studied molecules

|  | System | λem (nm) | τ (ns) | Ф (%) | kr (106 s-1) | knr (106 s-1) | krknr |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Deep-red emission | TTM-3PCz17 | 695 | 22.2 | 65 a / 46 b | 21 | 24 | 0.85 |
|  | TTM-3NCz17 | 707 | 17.2 | 86 a /49 b | 28 | 29 | 0.96 |
|  | APDC-DTPA14 | 687 | 11.2 | 63 | 57 | 32 | 1.78 |
|  | IO-4Cl | 678 | 1.8 | 36 | 200 | 356 | 0.56 |
|  | o-IDTBR | 750 | 1.6 | 19 | 119 | 506 | 0.23 |
|  | ITIC | 740 | 0.4 | 2 | 50 | 2450 | 0.02 |
| NIR emission | TTM-TPA | 800 | 8.4 | 24 | 29 | 90 | 0.32 |
|  | Y5 | 789 | 0.7 | 5 | 71 | 1357 | 0.05 |
|  | Y6 | 797 | 1.1 | 8 | 73 | 836 | 0.08 |

λem : PL maxima; τ: PL lifetime; Ф: PLQE; kr: radiative rate; knr: non-radiative rate. (a: 3 wt% in CBP blend, b: Toluene solution). The ratio of kr/knr gives an estimate of how efficient radiative decay pathways are in comparisons to non-radiative decay pathways.

Extended Data Fig. 9 | Experimentally obtained non-radiative rates of the studied low energy-gap molecules (based on Extended Data Table 1)

Extended Data Table 2 | Experimental and calculated (TDDFT) values of the three lowest energy transition of TTM-TPA

| Experimental Absorption (nm) | Calculated transition energy (nm) | Orbital excitation contribution (%) |
| --- | --- | --- |
| 670 | 718 (D0 → D1) | 192 beta (HOMO)→ 193 beta (SOMO): 97% |
| 495 | 463 (D0 → D2) | 190 beta (HOMO-2) → 193 beta (SOMO): 80% 189 beta (HOMO-3) → 193 beta (SOMO): 10% |
| 433 | 441 | 189 beta (HOMO-3) → 193 beta (SOMO): 69% 190 beta (HOMO-2) → 193 beta (SOMO): 15% 192 alpha (HOMO) →195 alpha (LUMO+1): 4% |

The experiment performed on 4CzIPN, is a 3-optical pulse IVS experiment46 due to the spectral bandwidth limitation of direct impulsive excitation high-energy transitions (>2.4 eV, see methods). 4CzIPN (toluene) is excited to 1CT state24 with 450 nm (200 fs) pulse followed by inducing vibrational coherence (VC) with 850 nm-centred broadband (8.5 fs) impulsive pulse, 500fs after initial photo-excitation. The impulsive pulse spectrally overlaps with the excited state absorption of 4CzIPN observed >550 nm49. The result shown for 4CzIPN, was recorded in 1mm pathlength cuvette.

This experiment is analysed in further detail in Supplementary information (Section 7  ).