Supporting Information

Interfacial Chemical Bond and Internal Electric Field Modulated Z-Scheme Vs-ZnIn2S4/MoSe2 Photocatalyst for Efficient Hydrogen Evolution

Xuehua Wang1, Xianghu Wang2, Jianfeng Huang4, Shaoxiang Li5, Alan Meng2,*, Zhenjiang Li1,3,5*

1 College of Materials Science and Engineering, Qingdao University of Science and Technology, Qingdao 266042, Shandong, P. R. China

2 Key Laboratory of Optic-electric Sensing and Analytical Chemistry for Life Science, MOE. College of Chemistry and Molecular Engineering, Qingdao University of Science and Technology, Qingdao 266042, Shandong, P. R. China.

3  College of Sino-German Science and Technology, Qingdao University of Science and Technology, Qingdao 266061, Shandong, P. R. China.

4 School of Material Science and Engineering, International S&T Cooperation Foundation of Shaanxi Province, Xi’an Key Laboratory of Green Manufacture of Ceramic Materials, Shaanxi University of Science and Technology, Xi’an 710021, China

5 Shandong Engineering Technology Research Center for Advanced Coating, Qingdao University of Science and Technology, Qingdao, 266042, P. R. China

* Corresponding author.

E-mail address:

zhenjiangli@qust.edu.cn (Z. J. Li); alanmengqust@163.com (A. L. Meng)

Fig. S1. Morphology characterizations of ZIS. a SEM, b-d the corresponding element mapping images of b Zn, c In and d S in ZIS

Fig. S2. EDS spectrum of ZIS.

Table S1. Elemental analyses of the ZIS photocatalyst by EDS.

| Element | Atomic (%) |
| --- | --- |
| Zn | 14.33 |
| In | 26.49 |
| S | 59.18 |
| Zn1.00In1.85S4.13 |  |

Fig.S3. Morphology characterizations of Vs-ZIS. a, b SEM, c, d TEM and HRTEM, e-g the corresponding element mapping images of c Zn, d In and e S.

Fig. S4. EDS spectrum of Vs-ZIS.

Table S2. Elemental analyses of the Vs-ZIS photocatalyst by EDS.

| Element | Atomic (%) |
| --- | --- |
| Zn | 15.95 |
| In | 30.62 |
| S | 53.43 |
| Zn1.00In1.92S3.35 |  |

Table S3. Elemental analyses of the Vs-ZIS/MoSe2 photocatalyst by EDS.

| Element | Weight (%) | Atomic (%) |
| --- | --- | --- |
| Mo | 2.08 | 1.37 |
| Se | 2.54 | 2.04 |
| Zn | 16.43 | 15.89 |
| In | 52.81 | 29.06 |
| S | 26.14 | 51.64 |
| Zn1.00In1.83S3.25 |  |  |

Table S4. Elemental analyses of the Vs-ZIS/MoSe2 photocatalyst by XPS.

| Theoretical chemical formula | ZIS |  |  | Vs-ZIS |  |  | Vs-ZIS/MoSe2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Element | Zn | In | S | Zn | In | S | Zn | In | S |
| Peak area ratio | 0.235 | 0.656 | 0.109 | 0.235 | 0.673 | 0.092 | 0.235 | 0.668 | 0.097 |
| Atomic ratio | 0.042 | 0.090 | 0.163 | 0.042 | 0.093 | 0.138 | 0.042 | 0.090 | 0.141 |
| Actual chemical formula | Zn1.00In2.15S3.87 |  |  | Zn1.00In2.20S3.29 |  |  | Zn1.00In2.14S3.36 |  |  |

Fig. S5. Wavelength-dependent H2 production rate in the presence of Vs-ZIS/5.0MoSe2.

Table S5. The calculated AQE of Vs-ZIS/MoSe2 photocatalyst at different wavelengths.

| Wavelength | The mean H2 production in 1 hour | Light power (Xe lamp) | AQE |
| --- | --- | --- | --- |
| 380 nm | 90.46 μmol | 0.034 W | 93.08% |
| 420 nm | 258.53 μmol | 0.107 W | 76.48% |
| 500 nm | 156.66 μmol | 0.140 W | 29.70% |
| 600 nm | 0.88 μmol | 0.134 W | 0.15% |

The apparent quantum yield (AQY) was measured following the same reaction conditions as photocatalytic test except that the incident light was supplied by a 300W Xe lamp equipped with specific band-pass filters to get the desired monochromatic incident wavelength (λ＝380, 420, 500 and 600 nm). AQY was roughly calculated based on the following equation:

AQY=the number of reacted electronsthe number of incident photons×100%=4×the number of H2 moleculesthe number of incident photons×100%=4×the  number of H2 moleculesN×100%

λ=380 nm:

N=Eλhc=0.034×3600×380×10-96.626×10-34×3×108=2.34×1020

AQY=4×90.46×10-6×6.02×10232.34×1020×100%=93.08%

λ=420 nm:

N=Eλhc=0.107×3600×420×10-96.626×10-34×3×108=8.14×1020

AQY=4×258.53×10-6×6.02×10238.14×1020×100%=76.48%

λ=500 nm:

N=Eλhc=0.140×3600×500×10-96.626×10-34×3×108=1.46×1021

AQY=4×156.66×10-6×6.02×10231.27×1021×100%=29.70%

λ=600 nm:

N=Eλhc=0.134×3600×600×10-96.626×10-34×3×108=1.46×1021

AQY=4×0.88×10-6×6.02×10231.46×1021×100%=0.15%

Fig. S6. UV–vis absorption spectra of Vs-ZIS/MoSe2 with different mass ratio of MoSe2 to ZIS.

Fig. S7. Photoluminescence spectra (PL, excited at 375 nm) of Vs-ZIS/MoSe2 with different mass ratio of MoSe2 to ZIS.

Fig. S8. Photocurrent response of Vs-ZIS/MoSe2 with different mass ratio of MoSe2 to ZIS.

Table S6. Comparison of representative ZnIn2S4-based photocatalysts for their H2 evolution behavior recently.

| Photocatalysts | Light source | H2 evolution rate (mmol·g-1·h-1) | AQE | Refs |
| --- | --- | --- | --- | --- |
| Co9S8/ZnIn2S4 | 300 W Xe lamp (λ>400 nm) | 9.039 | 4.49% at 420 nm | 1 |
| Co9S8@ZnIn2S4 | 300 W Xe lamp, λ>400 nm | 6.250 | / | 2 |
| ZnIn2S4-Ti3C2TX (3 wt% Pt co-catalyst) | 300 W Xe lamp, λ>420 nm | 3.475 | 11.14 at 420 nm | 3 |
| Zn2In2S5/Ti3C2(O, OH) x (2 wt% Pt co-catalyst) | 300 W Xe lamp, λ>420 nm | 2.596 | 8.96% at 420 nm | 4 |
| g-C3N4/Aminated-ZnIn2S4 (1 wt% Pt co-catalyst) | 300 W Xe lamp | 4.851 | / | 5 |
| N-doped ZnIn2S4 | 300 W Xe lamp, λ>400 nm | 11.086 | 16.6% at 420 nm | 6 |
| UiO-66-(COOH)2/ZnIn2S4/MoS2 | 300 W Xe lamp | 18.794 | / | 7 |
| AgxAu1-x/ZnIn2S4 | 300 W Xe lamp, λ>420 nm | 5.401 | 8.06% at 420 nm | 8 |
| Zn3In2S6/FCN (2 wt% Pt co-catalyst) | 300 W Xe lamp, λ>420 nm | 0.510 | / | 9 |
| ZnIn2S4/1%MoSe2 | 300 W Xe lamp, λ>400 nm | 6.454 | / | 10 |
| Co/NGC@ZnIn2S4 | 300 W Xe lamp, λ>400 nm | 11.270 | 5.07% at 420 nm | 11 |
| NiS/Vs-ZnIn2S4/WO3 | 300 W Xe lamp, λ>400 nm | 11.090 | 72% at 420 nm | 12 |
| ultra-thin ZnIn2S4/protonated g-C3N4 | 300 W Xe lamp, λ>400 nm | 8.601 | 0.92% at 400 nm | 13 |
| Ni2P/ZnIn2S4 | 300 W Xe lamp, λ>420 nm | 2.066 | 7.7% at 420 nm | 14 |
| ZnIn2S4@NH2-MIL-125(Ti) | 300 W Xe lamp, λ>420 nm | 2.204 | 4.3% at 420 nm | 15 |
| Cubic/hexagonal ZnIn2S4 heterophase junctions | 300 W Xe lamp, λ>420 nm | 3.806 | 18.67% at 420 nm | 16 |
| ZnIn2S4/MoSe2 | 300 W Xe lamp, λ>420 nm | 2.228 | 21.39% at 420 nm | 17 |
| 2D/2D g-C3N4 nanosheet@ZnIn2S4 | 300 W Xe lamp, λ>420 nm | 2.780 | / | 18 |
| Hydrogenated ZnIn2S4 | 300 W Xe lamp, λ>320 nm | 0.215 | 13.2% at 420 nm | 19 |
| MoS2/ZnIn2S4 | 300 W Xe lamp, λ>400 nm | 8.898 | / | 20 |
| Half-unit-cell ZnIn2S4 | 300 W Xe lamp, λ>400 nm | 13.478 | 53.68% at 365 nm | 21 |
| ZnmIn2Sm+3@In2S3 | 300 W Xe lamp, λ>420 nm | 3.300 | / | 22 |
| Vs-ZnIn2S4/MoSe2 | 300 W Xe lamp, λ>420 nm | 63.21 | 76.48% at 420 nm | This work |

References

1. Zhang, G. et al. Construction of Hierarchical Hollow Co9S8/ZnIn2S4 Tubular Heterostructures for Highly Efficient Solar Energy Conversion and Environmental Remediation. Angew. Chem. Int. Ed. 59, 8255-8261 (2020).

2. Wang, S. Guan, B. Wang, X. & Lou, X. Formation of Hierarchical Co9S8@ZnIn2S4 Heterostructured Cages as an Efficient Photocatalyst for Hydrogen Evolution.  J. Am. Chem. Soc. 140, 15145-15148 (2018).

3. Zuo, G. et al. Ultrathin ZnIn2S4 Nanosheets Anchored on Ti3C2TX MXene for Photocatalytic H2 Evolution.  Angew. Chem. Int. Ed. 59, 11287-11292 (2020).

4. Wang, H. et al. Electrical promotion of spatially photoinduced charge separation via interfacial-built-in quasi-alloying effect in hierarchical Zn2In2S5/Ti3C2(O,OH)x hybrids toward efficient photocatalytic hydrogen evolution and environmental remediation. Appl. Catal. B: Environ. 245, 290-301 (2019).

5. Gao, Z. et al. Aminated flower-like ZnIn2S4 coupled with benzoic acid modified g-C3N4 nanosheets via covalent bonds for ameliorated photocatalytic hydrogen generation. Appl. Catal. B: Environ. 268, 118462 (2020).

6. Du, C. Yan, B. Lin, Z. & Yang, G. Enhanced carrier separation and increased electron density in 2D heavily N-doped ZnIn2S4 for photocatalytic hydrogen production. J. Mater. Chem. A. 8, 207-217 (2020).

7. Mu, F. et al. Construction of 3D hierarchical microarchitectures of Z-scheme UiO-66-(COOH)2/ZnIn2S4 hybrid decorated with non-noble MoS2 cocatalyst: A highly efficient photocatalyst for hydrogen evolution and Cr(VI) reduction. Chem. Eng. J. 384, 123352 (2020).

8. An, H.  Li, M.  Liu, R. Gao, Z. & Yin, Z. Design of AgxAu1−x alloy/ZnIn2S4 system with tunable spectral response and Schottky barrier height for visible-light-driven hydrogen evolution. Chem. Eng. J. 382, 122953 (2020).

9. Wu, Y. et al. Construction of hierarchical 2D-2D Zn3In2S6/fluorinated polymeric carbon nitride nanosheets photocatalyst for boosting photocatalytic degradation and hydrogen production performance. Appl. Catal. B: Environ. 233, 58-69 (2018).

10. Yang, M. et al. Self-surface charge exfoliation and electrostatically coordinated 2D hetero-layered hybrids. Nat. Commun. 8, 14224 (2017).

11. Wang, S. et al . Supporting Ultrathin ZnIn2S4 Nanosheets on Co/N‐Doped Graphitic Carbon Nanocages for Efficient Photocatalytic H2 Generation. Adv. Mater. 31, 1903404 (2019).

12. Li, Z. et al. Two-dimensional Janus heterostructures for superior Z-scheme photocatalytic water splitting. Nano Energy. 59, 537-544 (2019).

13. Yang, H. et al. Constructing electrostatic self-assembled 2D/2D ultra-thin ZnIn2S4/protonated g-C3N4 heterojunctions for excellent photocatalytic performance under visible light. Appl. Catal. B: Environ. 256, 117862 (2019).

14. Li, X.  et al.  Fabrication of two-dimensional Ni2P/ZnIn2S4 heterostructures for enhanced photocatalytic hydrogen evolution. Chem. Eng. J. 353, 15-24 (2018).

15. Liu, H. Zhang, J. & Ao, D. Construction of heterostructured ZnIn2S4@NH2-MIL-125(Ti) nanocomposites for visible-light-driven H2 production. Appl. Catal. B: Environ. 221, 433-442 (2018).

16. Wang, J. et al.  Cubic quantum dot/hexagonal microsphere ZnIn2S4 heterophase junctions for exceptional visible-light-driven photocatalytic H2 evolution. J. Mater. Chem. A. 5, 8451-8460 (2017).

17. Zeng, D. et al. Hierarchical ZnIn2S4 /MoSe2 Nanoarchitectures for Efficient Noble-Metal-Free Photocatalytic Hydrogen Evolution under Visible Light. ChemSusChem, 10, 4624-4631 (2017).

18. Lin, B. et al. Preparation of 2D/2D g-C3N4 nanosheet@ZnIn2S4 nanoleaf heterojunctions with well-designed high-speed charge transfer nanochannels towards high-efficiency photocatalytic hydrogen evolution.  Appl. Catal. B: Environ. 220, 542-552 (2018).

19. Zhu, Y.  Wang, L.  Liu, Y. Shao, L. & Xia, X. In-situ hydrogenation engineering of ZnIn2S4 for promoted visible-light water splitting. Appl. Catal. B: Environ. 241, 483-490 (2019).

20. Li, W. Lin, Z. & Yang, G. A 2D self-assembled MoS2/ZnIn2S4 heterostructure for efficient photocatalytic hydrogen evolution. Nanoscale.  9, 18290-18298 (2017).

21. Du, C.  et al. Half-unit-cell ZnIn2S4 monolayer with sulfur vacancies for photocatalytic hydrogen evolution. Appl. Catal. B: Environ. 48, 193-201 (2019).

22. Li, Y. Han, P. Hou, Y. Peng, S. & Kuang, X. Oriented ZnmIn2Sm+3@In2S3 heterojunction with hierarchical structure for efficient photocatalytic hydrogen evolution. Appl. Catal. B: Environ. 244, 604-611 (2019).