Article type: Original Article

Amine-Functionalized Lignin as an Eco-Friendly Antioxidant for Rubber Compounds

June-Young Chung1, Uiseok Hwang1, Junyoung Kim2, Na-Yeon Kim2, Jeonghyeon Nam1, Jinho Jung1, Sung-Hoon Kim1, Jung Keun Cho1, Bumhee Lee2, In-Kyung Park1, Jonghwan Suhr1,3, and Jae-Do Nam1,2, *

1Department of Polymer Science and Engineering, Sungkyunkwan University Suwon 16419, Republic of Korea

2Department of Energy Science, Sungkyunkwan University, Suwon 16419, Republic of Korea

3School of Mechanical Engineering, Sungkyunkwan University, Suwon 16419, Republic of

Korea

*Corresponding author: jdnam@skku.edu (Prof. J.-D. Nam)

Scheme S1. Amination reaction between the KL and DETA, leading to the formation of phenolic C5 substituted lignin units.

Fig. S1. (a) FE-SEM image and the corresponding EDS C and O elemental mapping images of KL particles. (b) EDS profile and elemental composition of KL.

Fig. S2. (a) FE-SEM image and the corresponding EDS C and O elemental mapping images of AL particles. (b) EDS profile and elemental composition of AL.

Fig. S3. Digital image of broken specimen of rubber compounds incorporated with KL particles after ozone aging under 20% stretching.

Table S1. Curing characteristics of NB compounds in terms of the antioxidant content.

| Sample | Minimum torque (ML, dNm) | Maximum torque (MH, dNm) | Torque difference (ΔMH, dNm) | ts2 (min) | tc90 (min) | CRI (min-1) |
| --- | --- | --- | --- | --- | --- | --- |
| NB/6P-2 | 1.51 | 19.06 | 17.55 | 3.37 | 5.93 | 39.06 |
| NB/KL-2 | 1.83 | 20.84 | 19.01 | 4.30 | 6.98 | 37.31 |
| NB/AL-1 | 1.70 | 23.35 | 21.65 | 2.87 | 4.81 | 51.55 |
| NB/AL-2 | 1.76 | 24.40 | 22.64 | 2.02 | 3.65 | 61.35 |
| NB/AL-4 | 1.81 | 25.58 | 23.77 | 1.25 | 2.80 | 64.52 |
| ts2: scorch time; tc90: optimum cure time; Torque difference (ΔMH), MH−ML; Cure rate index (CRI), 100/(tc90-ts2) |  |  |  |  |  |  |

Table S2. Mechanical properties of NB compounds in terms of the antioxidant content and thermal aging at 120 °C for 24 h.

| Sample |  | No aging |  |  |  |  | Aging at 120 °C /24 h |  |  |  |  | Degradation |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Shore A hardness (SA, HA) | Tensile strength (σ, MPa) | Elongation at break (ε, %) | 50 Modulus (MPa) |  | Shore A hardness (SA, HA) | Tensile strength (σ, MPa) | Elongation at break (ε, %) | 50 Modulus (MPa) |  | Shore A hardness (△SA, %) | Tensile strength (△σ, %) | Elongation at break (△ε, %) | 50 Modulus (%) |
| NB/6P-2 |  | 50 | 20.1 ± 0.2 | 562.7 ± 5.3 | 1.06 ± 0.001 |  | 57 | 11.5 ± 0.3 | 282.8 ± 10.1 | 1.66 ± 0.001 |  | 13.0 | - 43.0 | - 49.7 | 57.5 |
| NB/KL-2 |  | 51 | 20.2 ± 0.4 | 561.3 ± 10.0 | 1.14 ± 0.005 |  | 58 | 11.8 ± 0.4 | 294.1 ± 8.0 | 1.64 ± 0.003 |  | 12.8 | - 40.8 | - 47.6 | 43.9 |
| NB/AL-1 |  | 54 | 18.6 ± 0.3 | 497.4 ± 3.4 | 1.25 ± 0.002 |  | 62 | 11.3 ± 0.2 | 257.6 ± 9.3 | 1.93 ± 0.001 |  | 13.9 | - 39.4 | - 48.2 | 54.4 |
| NB/AL-2 |  | 55 | 19.0 ± 0.1 | 499.5 ± 2.1 | 1.36 ± 0.002 |  | 62 | 13.0 ± 0.4 | 268.4 ± 14.2 | 2.09 ± 0.010 |  | 11.8 | - 36.2 | - 46.9 | 51.5 |
| NB/AL-4 |  | 57 | 19.9 ± 0.3 | 502.3 ± 4.2 | 1.53 ± 0.001 |  | 64 | 13.9 ± 0.4 | 267.3 ± 8.1 | 2.33 ± 0.003 |  | 11.8 | - 29.3 | - 43.7 | 54.2 |

Table S3. Swelling properties of NB compounds with different types and content of antioxidants.

| Sample | Swelling index (Q%, %) | Crosslink density (v, × 10−4 mol/cm3) | Dissolution fraction (s, %) |
| --- | --- | --- | --- |
| NB/6P-2 | 197.9 | 3.795 | 10.46 |
| NB/KL-2 | 208.3 | 3.220 | 9.53 |
| NB/AL-1 | 189.3 | 3.964 | 9.50 |
| NB/AL-2 | 185.7 | 4.107 | 9.51 |
| NB/AL-4 | 183.4 | 4.185 | 9.47 |

Table S4. Surface roughness parameter of NB compounds after ozone aging at 50 pphm/40 °C/72 h.

| Sample | Crack size (μm) |  |  | Arithmetical mean height (Sa, μm) | Root mean square height (Sq, μm) | Maximum height (Sz, μm) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Depth | Width |  |  |  |  |
| NB/6P-2 | 162.05 | 56.90 |  | 4,737 | 13.199 | 213.217 |
| NB/AL-2 | 67.76 | 22.26 |  | 2.077 | 4.047 | 115.138 |