Supporting Information

White Light Emissive Vitrimers for Phosphor-free Light Emitting Diode Encapsulations

Hong Gao*1, Miaomiao Wang1, Yifan Mao1, Zhen Wang1, Cheng Zhang1, Ling Jin1, Youyi Xia1, Weijin Li2, Kui Zhang*1, and Haibo Zeng*2

1School of Chemistry and Chemical Engineering, Anhui University of Technology, Ma’anshan Anhui 243032, China.

2Institute of Optoelectronics and Nanomaterials, MIIT Key Laboratory of Advanced Display Materials and Devices, College of Materials Science and Engineering, Nanjing University of Science and Technology, Nanjing 210094, China.

Email：pshgao@ahut.edu.cn; zhangkui@mail.ustc.edu.cn; zeng.haibo@njust.edu.cn

Contents

1 Materials	S3

2 Preparation	S3

2.1 Synthesis of vitrimer DC-TEPA and reference vitrimers	S3

2.2 Recycling and application of DC-TEPA	S4

2.3 Synthesis of DC-xPD	S4

2.4 Synthesis of DC-xPD-TEPA	S4

3 Instrumentation and characterization	S6

4 Supporting figures	S8

4.1 The synthesis and properties of DC-TEPA and reference vitrimers	S8

4.2 The reprocessing and recycles of DC-TEPA	S13

4.3 The PL emissions of DC-TEPA and reference vitrimers	S15

4.4 The PL emissions of DC-xPD	S18

4.5 The routes of DC-xPD-TEPA	S20

4.6 The thermal and mechanical properties of DC-xPD-TEPA	S21

4.7 The reprocessing evaluation of DC-xPD-TEPA	S23

4.8 The white emissions of DC-xPD-TEPA	S25

4.9 The applications of DC-xPD-TEPA for LED encapsulations without phosphors	S26

4.10 The reliability of LED encapsulated by DC-xPD-TEPA	S27

1 Materials

Diglycidyl 1,2-cyclohexanedicarboxylate (DC, ≥98%), tetraethylenepentamine (TEPA, 99%),  4,4'-diamino diphenyl methane (DDM, 98%), glycerol (GL, ≥99%), 1,5,7-triazabicyclo[4.4.0]dec-5-ene (TBD, >98%), methanol(AR), isopropanol(AR), triethylamine (AR), toluene (AR) and petroleum ether (AR) were purchased from Shanghai Titan Scientific Co., Ltd. Perylene-3,4,9,10-tetracarboxylic dianhydride(PD), 1,4,5,8-naphthalene tetracarboxylic anhydride(NT) and pyromellitic dianhydride (PM) were purchased from Aladdin Co., Ltd. 2-Ethyl-4-methyl-1H-imidazole (2E4MI) was supplied by Shenzhen Jiadida New Material Technology Co., Ltd.

2 Preparation

2.1 Synthesis of vitrimer DC-TEPA and reference vitrimers

The vitrimer DC-TEPA was prepared by the reaction of DC with TEPA at the molar ratio of 3.5:1. DC and TEPA were vigorously mixed and degassed at room temperature in a TMV-200T high-speed mixer at 2000 rpm for 2 min under a reduced-pressure environment. The bubble-free mixture was poured into a polytetrafluoroethylene (PTFE) mold and cured at 25°C for at least 16 h and at 60°C for another 3 h.

The reference vitrimers, DC-DDM or DC-DDM-TBD, were prepared by the reaction of DC with DDM at a molar ratio of 2:1. For the DC-DDM-TBD, 5-mol% TBD on the basis of the epoxy groups was used as the catalyst. All the raw materials (DC, DDM, and catalysts if needed) were ground three times on a three-roller machine (Longxin Chemical Machinery Co., Ltd.) and then degassed in a TMV-200T high-speed mixer at 2000 rpm for 2 min under a reduced-pressure environment at room temperature. The bubble-free mixture was poured into a PTFE mold and cured at 80°C for 3 h, 150°C for 3 h, and 180°C for 2 h in an oven.

The reference vitrimers, DC-GL-TBD or DC-GL-2E4MI, were prepared by the reaction of DC with GL at a molar ratio of 1.5:1. For the DC-GL-2E4MI, 5% 2E4MI based on the total mass of GL and DC was used as the curing accelerant. For the DC-GL-TBD, 5-mol% TBD on the basis of the epoxy groups was used as the catalyst. The mixing and degassing procedures of the DC-GL-TBD or DC-GL-2E4MI were the same as before. The bubble-free mixture was poured onto the PTFE mold and cured at 120°C for 3 h, 150°C for 3 h, and 180°C for 6 h in an oven.

2.2 Recycling and application of DC-TEPA

Recycling: The cured DC-TEPA was ground into fine powder (denoted as “GR”) and then different ratios of GR were mixed with the fresh DC-TEPA resin system (denoted as DC-TEPA-yGR), where y represents the weight percentage of GR in the DC-TEPA-yGR.

Applications: The mixed DC-TEPA was poured into cartoon mold and cured at room temperature for 24 h. The mixed DC-TEPA resin was screen-printed with the “AHUT” pattern on glass or filter paper, and then the patterns were cured at room temperature for 24 h.

2.3 Synthesis of DC-xPD

In a typical reaction, the mixture of PD and DC was ground three times on a three-roller mill at room temperature, where the color of the mixture changed to a uniform red color, indicating that PD and DC were fully mixed. The mixture in a 50 mL three-necked flask was refluxed at 180°C for 100 min in an oil bath, where the color of the mixture DC-xPD changed progressively from red to yellow with high transparency. Here, x indicates that in 1 mole of epoxy group, x × 10−4 moles of epoxy groups reacted with PD. The other reaction conditions (150°C–200°C and 40 min–140 min) were also tested.

As a comparison system, PM or NT was used to react with DC. The reaction formulae and operation methods were the same as those for the DC-2PD (180°C for 100 min), which were denoted as DC-2PM or DC-2NT, respectively. Since the reaction between the anhydride and epoxy resin required high-temperature conditions, the reference DC was refluxed under the same conditions.

2.4 Synthesis of DC-xPD-TEPA

The mixtures of DC and PD with different contents based on the formulations in Table S1 were ground three times in a three-roller mill at room temperature and then refluxed with magnetic stirring at 180°C for 100 min. The mixture changed from red to yellow. After cooling to room temperature, the required TEPA based on the formula in Table S1 was added under vacuum stirring. The bubble-free mixtures were cured at 25°C for 16 h and 60°C for another 3 h to prepare the vitrimers DC-xPD-TEPA. Here, x indicates that in 1 mole of epoxy group, x × 10−4 moles of epoxy groups reacted with PD. The remaining epoxy groups were cured by TEPA.

Table S1 The molar ratio of raw materials in DC-xPD-TEPA.

| Samples codes | DC(mol) | PD(×10-4 mol) | x(×10-4 mol) | TEPA(mol) |
| --- | --- | --- | --- | --- |
| DC-1PD -TEPA | 1 | 0.5 | 1 | (1-1×10-4)/3.5 |
| DC-1.5PD -TEPA | 1 | 0.75 | 1.5 | (1-1.5×10-4)/3.5 |
| DC-2PD -TEPA | 1 | 1 | 2 | (1-2×10-4)/3.5 |
| DC-2.5PD -TEPA | 1 | 1.25 | 2.5 | (1-2.5×10-4)/3.5 |
| DC-3PD -TEPA | 1 | 1.5 | 3 | (1-3×10-4)/3.5 |

3 Instrumentation and characterization

The stress relaxation experiments of the vitrimers were conducted using a DMA TA Q800 instrument in tension mode. After 20 min of temperature equilibration, the stress was monitored over time at a 1% strain, and the relaxation stress Gt was recorded over time at a stationary temperature. The time-dependent stress Gt was normalized by the initial stress G0. The activation energy Ea was calculated from the equation S1.

lnτ=EaRT-lnA,              (S1)

where Ea represents the activation energy of the transesterification reaction, τ represents the time for the stress to reach to 1/e of its initial relaxation stress.

Swelling experiments were performed as follows. Typically, the samples (10 mm × 10 mm × 1 mm) were immersed in solvents at 25°C for several days until the swelling equilibrium was reached. Then, the samples were removed, and the extra solvent on the surface was removed carefully with filter paper. The swollen samples were then weighed on a balance.

The gel point of DC-TEPA was calculated from Flory-Stockmayer equation S2.   pc=1[r+rρ(f-2)]12           (S2)

where pc is the fraction of the functional groups which have undergone reaction at gelation. r is the ratio of all A to all B groups. f is branching units of functionality. ρ is the ratio of A’s belonging to branch units to the total number of A’s. As for DC-TEPA, r =1due to complete reaction between epoxy groups and amine groups, ρ = 1 because all amine groups in TEPA are branch units. f = 7 for TEPA. So the calculate pc = 0.408 from equation S2 for DC-TEPA.

Rheological experiments of uncured DC-TEPA were performed using a TA Discovery HR2 rheometer with 40-mm parallel plate geometry. The applied strain during the measurement was in the range of the linear viscoelasticity region. The storage modulus G' and loss modulus G'' of the uncured DC-TEPA were measured at 50°C for 60 min. The cross-over point of the two modulus curves provided an estimation of the time at which the resin started to gel.

The PL spectra (excitation and emission) were investigated on a Hitachi F-7100 fluorescence spectrometer. The excitation and emission were measured in quartz cell under a xenon discharge lamp (150 W) excitation, and the scan rate was 1200 nm min−1. The in situ PL spectra were measured as follows. The sample cell was raised to 50°C, the cell with uncured DC-TEPA was excited at 365 nm, and the PL spectra were measured at intervals.

The process of LED encapsulation was as follows. The uncured DC-xPD-TEPA resin as an encapsulating material was applied to a 365-nm LED chip, and then the encapsulated LED was placed at 25°C for 16 h and then baked at 50°C for 3 h. The encapsulated LED was placed on the lamp holder of an integrating sphere photoelectric test system (Hangzhou Yuanfang) to measure the CIE, CCT, CRI, and spectra of the LED device. The test currents were in the range of 60–100 mA at a voltage 3.4 V.

4 Supporting figures

4.1 The synthesis and properties of DC-TEPA and reference vitrimers

Scheme S1. Synthesis strategy of the reference vitrimers. a The synthesis of DC-DDM and DC-DDM-TBD. b The synthesis of DC-GL-TBD and DC-GL-2E4MI. The aromatic epoxy vitrimers as one of the reference vitrimers were synthesized via the reaction of DC with the aromatic amine DDM in the absence or presence of TBD, which were denoted as “DC-DDM” or “DC-DDM-TBD”, respectively. In addition, another type of reference vitrimers based on transesterification without tertiary amines was prepared by replacing TEPA with GL in the presence of “2E4MI” or “TBD,” which was denoted as the “DC-GL-TBD” or “DC-GL-2E4MI”, respectively.

Figure S1. Non-isothermal exothermic curves of DC-TEPA and the reference vitrimers. The DC-TEPA showed a lower curing temperature because TEPA was a typical room-temperature curing agent. The peak temperature of the DC-DDM was at 149.3°C, which shifted to a lower temperature of 139.6°C after the loading of TBD, suggesting that TBD significantly catalyzed the curing reaction of epoxy resin in addition to being a known catalyst for transesterification. The DC-GL with TBD or 2E4MI showed a broad curing temperature from 125°C to 240°C, the main curing peak temperatures of which were higher than those of the DC-TEPA and DC-DDM, indicating that the reactions of hydroxyl groups with the epoxy were difficult compared with those of the amino groups.

Figure S2. FTIR spectra of DC-TEPA and the reference vitrimers. The peaks at 907 cm−1 disappeared completely, and the broad peaks at 3445 cm−1 belonging to hydroxyl groups appeared simultaneously, indicating that all epoxy groups had been opened.

Figure S3. DSC curves of the cured DC-TEPA and the reference vitrimers. Both DC-TEPA and DC-DDM with/without TBD exhibited higher Tg values than the DC-GL system, which was attributed to the imperfect network integrity of the DC-GL system due to the lower curing activity of GL. The Tg value of the DC-DDM was higher than that of the DC-DDM-TBD, confirming again that the TBD directly catalyzed the ring-opening polymerization of epoxy resins.

Figure S4. TGA curves of DC-TEPA and the reference vitrimers. The decomposition temperatures (Td5%) of all the vitrimers reached 300°C, which was much greater than the network topology rearrangement temperature of 180°C, indicating that the thermal performance of the polymerization network remained stable during the hot pressing process and that thermal degradation would not occur in this process.

Figure S5. The mechanical and dynamic properties of the vitrimers. a The stress-strain curves of DC-TEPA and the reference vitrimers. b The average tensile strengths of DC-TEPA and the reference vitrimers. The tensile strength of the DC-TEPA (68.1 MPa) was much higher than those of the DC-GL-2E4MI (36.5 MPa) and DC-GL-TBD (59.1 MPa), although their network structures were similar. The DC-DDM exhibited the highest tensile strength of 72.4 MPa. After the addition of TBD, the strength of the DC-DDM-TBD decreased significantly to 55.2 MPa, which may be ascribed to the direct catalytic DC self-polymerization by TBD, resulting in aromatic amines not entering the vitrimer network. The DC-GL system also had a similar phenomenon of decreasing strength.

Figure S6. Normalized stress relaxation curves of DC-TEPA and the reference vitrimers at 180℃. The relaxation rate is often gauged by the relaxation time (τ), which is defined as the time for the stress to reach 1/e of its initial relaxation stress. The reference vitrimers DC-GL-2E4MI and DC-GL-TBD exhibited similar relaxation times of 42.6 and 47.6 min, respectively. Unlike the DC-TEPA, the DC-DDM in the absence of extra catalysts hardly produced stress relaxation. After the TBD loading, the DC-DDM-TBD exhibited partial relaxation, which decreased to ∼72% in 100 min. Here, tertiary amines obtained from the reacted DDM in the DC-DDM had no catalytic activity for transesterification because the basicity of the tertiary amine formed by aromatic DDM was weaker than that formed by aliphatic TEPA due to p-π conjugation effect in aromatic system.

Figure S7. Storage modulus of DC-TEPA and the reference vitrimers. The E' values of DC-GL-2E4MI, DC-GL-TBD, DC-TEPA, DC-DDM-TBD, and DC-DDM increased successively, and that of DC-DDM was as high as 4560 MPa.

Figure S8. Solvent resistance measurement of DC-TEPA and the reference vitrimers. a Solvent immersion of DC-TEPA and the reference vitrimers before and after 7days in toluene, ethyl acetate, triethylamine, isopropanol and methanol (from left to right) at 25°C. b The swelling results of DC-TEPA and the reference vitrimers before and after 7 days immersing. The colors of the organic solvents before and after swelling were still colorless and transparent, indicating that the polymerization networks of the vitrimers were insoluble, and thus, they were typical thermosetting polymers. The swelling of the DC-TEPA after immersion was very low in the solvents, implying that the chemical resistance of the DC-TEPA was excellent.

4.2 The reprocessing and recycles of DC-TEPA

Figure S9. The images of DC-TEPA during 3 times reprocessing at 180oC and 1000psi for 1h. P1, P2 and P3 represent the first reprocessing, the second reprocessing and the third reprocessing of vitrimers, respectively.

Figure S10. The structure changes of DC-TEPA during 3 time reprocessing. a FTIR of DC-TEPA before and after reprocessing. FTIR revealed no major variations between the recycled and original samples. b DSC curves of DC-TEPA after hot pressing. The Tg value of P1 increased from 69.5oC to 85.3oC due to post-curing and then the value tended to stabilize as increasing reprocessing times. c TGA curves of DC-TEPA before and after reprocessing. d Normalized stress relaxation curves of DC-TEPA after reprocessing at 180℃. Thermostability and stress relaxation after reprocessing were almost the same to the original ones.

Figure S11. Physical recycling process of the cured DC-TEPA via mixing with fresh resin DC-TEPA.

Figure S12. Thermal and dynamic properties of DC-TEPA-yGR before (a-c) and after (d-f) heat treatment at 180℃. a DSC curves of DC-TEPA-yGR before heat treatment. b TGA curves of DC-TEPA-yGR before heat treatment. c Normalized stress relaxation curves of DC-TEPA-yGR before heat treatment. d DSC curves of DC-TEPA-yGR after heat treatment. e TGA curves of DC-TEPA-yGR after heat treatment. f Normalized stress relaxation curves of DC-TEPA-yGR after heat treatment.

4.3 The PL emissions of DC-TEPA and reference vitrimers

Figure S13. Photos of DC-TEPA and the reference vitrimers under UV light of 365 nm. DC-TEPA exhibited a stronger blue light than the reference vitrimers

Figure S14. The excitation and emission spectra of DC-TEPA. a The excitation spectrum of DC-TEPA. b The emission spectra of DC-TEPA under different excitation lights. A clear excitation-dependent emission (EDE) effect with the transformation from dominant short wavelength emission (~450 nm) to weak long-wavelength emission (∼500 nm) was observed. At excitation of λex=365 nm, the highest intensity of emission (λem= ~450 nm) was obtained.

Figure S15. The factors affecting fluorescence of DC-TEPA. a The emission spectra of DC-TEPA treatment at 25-200℃ for 10min. When the temperature rose, the strength of the emission peak fell, especially, this decline was more pronounced above Tg (~70oC). b The emission spectra of DC-TEPA after treatment at 180℃ for 0-20min. The intensity of emission peak decreased as time. c The emission spectra of DC-TEPA after immersion in ethanol, acetone, tetrahydrofuran, ethyl acetate and ether for one week. The PL intensities of DC-TEPA samples soaked in the solvents dropped the most, which were due to an increase in the gap between luminous clusters in the cross-linked network caused by the immersion of solvent molecules, suppressing through-space interactions between clusters and clusters. d DSC curves of DC-rTEPA. The higher the Tg value that is related to crosslink density, the stronger the PL intensity.

Figure S16. The PL spectra of DC-TEPA during curing process. a In situ PL spectra of DC-TEPA resin at 50℃ during 180 min. b The emission wavelength variation of DC-TEPA resin with time at 50oC. At the initial stage, the peak at ~415 nm belonged to TEPA emission. As the reaction proceeded, the peak shifted to 450-455 nm, indicating a large amount of TEPA had reacted with DC to form oligomers.

4.4 The PL emissions of DC-xPD

Figure S17. The color images of PD and DC-PD under UV lamp. a Color images of PD with different concentrations in alkali solution. b The images of PD powder in petroleum ether under UV lamp. c-d The images of the reflux product DC-PD in petroleum ether and toluene under UV lamp. The single PD at powder state could not emit any light via 365 nm excitation, which showed yellow emission in alkali solution under UV excitation, indicating that PD obeyed ACQ mechanism.

Figure S18. The PL spectra of DC-2PD after reflux at 150℃-200℃ for 100 min. The amounts of PD reacting with DC were very rare at 150oC-170oC. When the reflux temperature was 180oC, the solution was yellow with high transparency and the PL intensity was the largest at 530 nm.

Figure S19. Exothermic curves of DC-xPD reaction. The reaction active periods of DC-xPD were from ~170oC to ~200oC.

Figure S20. The PL spectra of DC-2PD after reflux at 180oC for 40-140min. The intensity of DC-2PD reached the highest at 100 min, indicating PD had been grafted to DC forming macromolecular photoluminescence.

4.5 The routes of DC-xPD-TEPA

Scheme S2. Synthesis strategy of DC-xPD-TEPA. The mixtures of DC and PD with different contents were refluxed at 180°C to produce DC-xPD, and then the remaining DC in DC-xPD was cured by TEPA, producing DC-xPD-TEPA.

4.6 The thermal and mechanical properties of DC-xPD-TEPA

Figure S21. Curing exothermic curves of the reaction of DC-xPD with TEPA. The curing actions of DC-xPD-TEPA were the same due to the lower PD levels.

Figure S22. FTIR of the (a) raw materials and (b) DC-xPD-TEPA. The results indicated epoxy groups had reacted completely.

Figure S23. Thermal and mechanical properties of DC-xPD-TEPA. a DSC curves of DC-xPD-TEPA. b TGA curves of DC-xPD-TEPA. c The stress-strain curves of DC-xPD-TEPA. d The average tensile strength of DC-xPD-TEPA (A-E represent DC-1PD-TEPA, DC-1.5PD -TEPA, DC-2PD-TEPA, DC-2.5PD-TEPA and DC-3PD-TEPA, respectively). These results indicated a small amount of PD had little effect on thermal and mechanical properties of DC-xPD-TEPA.

4.7 The reprocessing evaluation of DC-xPD-TEPA

Figure S24. The images of DC-2PD-TEPA during 3 times reprocessing at 180oC and 1000psi for 1h. Good reprocessing performances of DC-2PD-TEPA were achieved without extra catalyst.

Figure S25. The characterization of DC-2PD-TEPA after reprocessing. a FTIR of DC-2PD -TEPA during 3 time reprocessing. b DSC curves of DC-2PD-TEPA during 3 times reprocessing. c The stress-strain curves of DC-2PD-TEPA during 3 times reprocessing. d TGA curves of DC-2PD -TEPA during 3 times reprocessing.

4.8 The white emissions of DC-xPD-TEPA

Figure S26. The PL spectra of DC- xPD-TEPA. DC-xPD-TEPA fluoresced with a white-light emission due to the overlapping of short- and long-wavelength peaks.

4.9 The applications of DC-xPD-TEPA for LED encapsulations without phosphors

Figure S27. DC-xPD-TEPA as encapsulating materials for 365nm LED chips. a-c Lighting photographs, color coordinate diagram and spectra of LED encapsulated by DC-1PD -TEPA. d-f Lighting photographs, color coordinate diagram and spectra of LED encapsulated by DC-1.5PD-TEPA. g-i Lighting photographs, color coordinate diagram and spectra of LED  encapsulated by DC-2.5PD-TEPA. j-l Lighting photographs, color coordinate diagram and spectra of LED encapsulated by DC-3PD-TEPA. The LED encapsulated by the DC-2PD-TEPA exhibited a broad white-light spectrum, with dual emission peaks at around 430 and 550 nm.

4.10 The reliability of LED encapsulated by DC-xPD-TEPA

Figure S28. Normalized curves of color coordinates, CCT and CRI of LED encapsulated by DC-2PD-TEPA at different currents (a 60mA; b 80 mA; c 100 mA) for 15min. When the currents were 60–100 mA, the CIE, CCT, and CRI changed very little, nearly on a horizontal line.