2.1 Powder synthesis

SmAlO3 powders were synthesized according to a synthetic procedure, as shown in Fig. 1. In the experiments, analytical grade reagents samarium oxide (Sm2O3), aluminum nitrate hexahydrate [Al(NO3)3·9H2O], and stearic acid(C17H35COOH) were chosen as raw materials. In light of its hygroscopic nature, Sm2O3 powder must be prefired at 900 ℃ for 4 h before weighing procedure. First of all, 0.005 mol Sm2O3 was dissolved in diluted nitric acid to form a transparent solution under magnetic stirring at 80 ℃. In addition, 30 g stearic acid was weighed and then heated slowly to melt completely at 75 ℃ in a beaker, then 0.01 mol Al(NO3)3·9H2O was slowly added and dissolved in the molten stearic acid until a clear solution was obtained with continuous stirring. Next, the Sm(NO3)3 solution was added dropwise into the molten stearic acid in the same manner. By increasing the heating temperature to 100 ℃ for a sufficient period of time, the unnecessary water in the mixture was removed. After that, the mixture was continuously magnetic stirred and maintained at 130 ℃ until a uniform sol-like solution was produced, accompanied by the release of a large volume of reddish brown gases. By naturally cooling down to room temperature and drying for 12 h in an oven, a dried gel was formed. Subsequently, the dried gel was reheated to 230 ℃ for 2 h until it transformed into a black resinous precursor. Finally, the SmAlO3  powder was obtained after the precursor was calcined in air at various temperatures.

The suggested chemical reactions are as follows:

6CH3CH216COOH+2Sm(NO3)3→2[CH3CH216COO]3Sm+3H2O↑+6NO2↑+3O↑

6CH3CH216COOH+2Al(NO3)3→2[CH3CH216COO]3Al+3H2O↑+6NO2↑+3O↑

[CH3CH216COO]3Sm+[CH3CH216COO]3Al+39O2→SmAlO3+15H2O↑+36CO2↑

2.2Samples preparation

The as-synthesized SmAlO3 powders, along with a small amount of PVA binder, were granulated and then pressed into cylindrical green samples with a size of about Φ10 mm×5 mm. Finally, these as-pressed cylinders were pressurelessly sintered for densification at 1350–1550 ℃ for 4 h.

2.3Characterization and measurements

XRD patterns were collected using a powder X-ray diffraction analyzer (Bruker D8, Germany) with CuKα radiation at 2 = 20- 80 °. Thermal analysis of dried gel was employed on a Shimadzu DTG-60H instrument in a temperature range of 30–900 ℃, in air with a heating rate of 10 ℃/min. FT–IR spectra were obtained on a Nicolet 6700 FT-IR device by the KBr pellet method, ranging from 400 to 4000 cm-1. FE–SEM was used to evaluate the morphology and microstructure by depositing a gold coating on the surface of samples. The particulate properties of synthesized powders were examined using transmission electron microscopy (JEOL–200). In accordance with the Archimedes method, the bulk densities of sintered ceramics were measured. Relative dielectric constant and dielectric loss of sintered microwave ceramics were evaluated using the Hakki–Coleman DR method by a vector network analyzer (Agilent 8722ET) [20, 21]. τf was determined through the equation (1):

τf=f80-f25f2580-25                          (1)

Where f25 and f80 denote the resonant frequencies at 25 and 80 ℃, respectively.